The Fifth International Ural Seminar

RADIATION DAMAGE

PHYSICS OF METALS AND

ALLOYS

Abstracts

February 23– March 1

Snezhinsk							Russia

2003

Contents

- General Problems of Radiation Damage Physics

Molecular Dynamics Simulation of a Swift Ion Track in NiAl

C. Abromeit, A.R. Kuznetsov							3

Physical Principles of Radiation Resistance of Alloys

Structural Self-Organization

# V.V  Bryk, I.M. Neklyudov	3

Radiation Defects Annealing in Austenitic Stainless Steels with

Different Microstructures

S.E. Danilov, V.L. Arbuzov, K.V. Shal’nov, V.A. Pavlov 	4

Correlation Effects in Cascades of Atomic Collisions

Yu.N. Devyatko, S.V. Rogozhkin and V.M. Chernov	5

Effect of Intermetallic Precipitates on Evolution of

Radiation-Induced Defects in Austenitic Alloys

A.P. Druzhkov, V.L. Arbuzov, D.A. Perminov, K.V. Shal’nov, V.A. Pavlov	5

Theory of Damage Accumulation under Cascade Damage Conditions

S.I. Golubov, B.N. Singh and H. Trinkaus						6

Calculation of Track Transverse Sizes in a YBa2Cu3O7-x Single

Crystal Taking into Account Energy Transfer Velocity

Dependence on Temperature of Excited Electrons

I.N. Goncharov, B.F. Kostenko, J. Pribiš	7

# Long-Range Effect. The  Theory and Experiments

## V.S. Khmelevskaya, V.G. Malynkin	7

Theory of Irradiation Hardening of Metals and Alloys 
Based on the Energy Concept of Ductility

Yu.V. Konobeev, V.A. Pechenkin, F.А. Garner 	8

Effect of Initial Dislocation Structure on Accumulation and

Annealing of Radiation Defects in Austenitic Alloys

D.A. Perminov, A.P. Druzhkov, V.L. Arbuzov, V.A. Pavlov 	9

Cascades of Atomic Collisions and Point Defect Accumulation

S.V. Rogozhkin, Yu.N. Devyatko and V.M. Chernov	10

Modeling Complexes of Defects in Solid Solution

Using Neutron Spectroscopy

V.V. Sumin	10

Sputtering of Sub-atom Carbon Films on Surfaces of Metals

by Low-Energy Gas Ions

# A.L. Suvorov, A.G. Zaluzhnyi, V.P. Babaev,   N.E. Lazarev,

# Yu.N. Devyatko, A.A. Zaluzhnyi	11

Theory and Computer Simulation of Radiation Processes in

Multicomponent Materials

Yu.V. Trushin, D.V. Kulikov, V.S. Kharlamov, P.V. Rybin	11

Effect of Irradiation on Electronic Properties of Pure

Compensated Metal Single Crystals  at High Magnetic Fields

V.V. Marchenkov, V.E. Arkhipov, A.L. Suvorov and H.W. Weber			12

Quantitative Measurement of Electron Diffuse Scattering by Single

Manometer-Sized Defects in Au and Mo
M. A. Kirk, M. L. Jenkins, R. D. Twesten						13

- Effect of Irradiation on Changes in Microstructure and

Properties of Metals and Alloys

NDT Measurements of Irradiation Induced Void Swelling in

EBR-II Materials

I. I. Balachov, F.A. Garner, I. Isobe, H. T. Tang					17

Peculiarities of Martensitic Transformation Kinetics
in a Monocrystal of Cu-Al-Ni Alloy Being Irradiated
by Reactor Neutrons in Low-Temperature Helium Loop

S.P. Belyaev, R.F. Konopleva, I.V. Nazarkin, V.A. Chekanov			18

Dose Dependences of Mechanical Properties and Composition of

Titanium Alloy Surface During Si+ and Ar+ Ion Irradiation

P.V. Bykov, F.Z. Gil’mutdinov, A.A. Kolotov, V.Ya. Bayankin			19

Atomic Mechanisms of the Microcrack Propagation in Titanium

During Ion Irradiation

A.Yu. Drozdov, M.A. Baranov, V.Ya. Bayankin					20

Disordering of LaMnO3-Based  Compounds by  Fast Neutrons

S. F. Dubinin, V. E. Arkhipov, V. D. Parkhomenko, S. G. Teploukhov,

Yu. G. Chukalkin, Ya. M. Mukovskii						21

The influence of displacement rate on void swelling in model

Fe-Cr-Ni alloys irradiated with either neutrons or nickel ions

F. A. Garner, T. Okita, T. Sato and N. Sekimura					21

Radiation-Enhanced Amorphism: Comparison of Materials and

Influence Techniques

N.N. Gerasimenko								22

- Phase Transformations in Ion Irradiated NiTi Thin Films

T. LaGrange, R. Schäublin, D.S. Grummon, C. Abromeit and

R. Gotthardt									23

# Radiation-Induced Enhancement of Critical Current Density

in YBa2Cu3O7-x Superconductors

E.M. Ibragimova, M.A. Kirk							24

Monitoring an Insulator-Metal Transition in Icosahedral AlPdRe

by Neutron Irradiation

A.E. Karkin, B.N. Goshchitskii, V.I. Voronin, S.J. Poon, V. Srinivas,

and O. Rapp									25

Martensitic Transformations and Shape Memory Effect in TiNi

Alloys in the Process of Neutron Irradiation in Low-Temperature

Helium Loop

R.F. Konopleva, S.P. Belyaev, A.E. Volkov, I.V. Nazarkin,

V.A. Chekanov									26

The  Percolation Model of  Radiation Porosity Influence on

Austenitic Steel Strength

A. V. Kozlov, I. A. Portnykh, S. V. Bryushkova, E. A. Kinev			27

Temperature Dependence of Radiation Swelling of

ChS-68 Steel Analyzed by Different Models

A.V. Kozlov, Yu. V. Konobeev, I. A. Portnykh, E. A. Kinev			28

About the Surface Erosion Mechanisms under the Pulsed Ion

Beams Irradiation

G.A. Bleikher, V.P. Krivobokov, O.V. Paschenko					29

Formation of Nanoscale Intermetallic Phases at High-Intensity

Ion Implantation

E.V. Kozlov, A.I. Raybchikov, Yu.P. Sharkeev, I.A. Kurzina,

I.B. Stepanov, S.V. Fortuna, D.O. Sivin, T.S. Prokopova, I. A. Mel’nik		30

# Vacancy Clusters in Titanium Nickelide Irradiated with Fast

# Neutrons

V.D. Parkhomenko, S.F. Dubinin, S.G. Teploukhov, E.Z. Valiev			30

Swelling and Microstructure of EP-753 and Nimonic PE-16

High Nickel Alloys after Neutron Irradiation to High Doses

S. I. Porollo, Yu. V. Konobeev and F. A. Garner					32

Long-Range Effect in Ion Implantation-Ordered Alloys

N.N. Syutkin, V.V. Alehin	32

A Short Range Order In The Amorphous Ribbon of

Ti0,5Ni025Cu0,25 Irradiated by Fast Neutrons

V. D. Parkhomenko, S. F. Dubinin, S. G. Teploukhov				33

Structural Phase Transitions in Intermetallic Compounds Y2Fe17

and Ce2Fe17 after Irradiation with Fast Neutrons

V.I. Voronin, E.F. Berger, A.E. Karkin, A.G. Kuchin,

Yu.G. Chukalkin, B.N. Goshchitskii 						34

Comparison of the Effects of Radiation- and Strain-Induced

Defects on the Phase  Transformation in Iron Alloys

V.V. Sagaradze, A.R. Kuznetsov 							35

Long-Range Effect in Metal Foils under Ion and Photon Irradiation

D.I. Tetelbaum, A.Yu. Azov, E.V. Kuril’chik, Yu.A. Mendeleva,

V.Ya. Bayankin, F.Z. Gil’mutdinov, A.V. Nikitin					36

- Implanted and Transmutational Gaseous Impurities Behavior in

Irradiated Metals and Alloys

Determination of Hydrogen Permeation Reduction Factor (PRF)

for Different Protective Coats on Vanadium

S.E. Afanasev, T.V. Kulsartov, V.P. Shestakov, E.V. Chikhray, D. Smith		39

Gas Bubble Evolution peculiarities in Ferritic and Austenitic

Steels and Alloys under Helium Irradiation

S.Yu. Binyukova, I.I. Chernov, A.N. Kalashnikov, B.A. Kalin,

Mitkhal Abu Kharroub								39

Hydrogen Accumulation and Retention in Materials of

Reactor VVER-1000 Vessel Components

I.M. Neklyudov, B.A. Shilyaev, A.N. Morozov,

A.A. Parkhomenko, V.V. Bryk							40

Investigation of Concentration and Temperature Dependences of

Processes of Hydrogen and Helium Accumulation and Desorption

in Steel 08Cr18Ni10Ti

V.V. Bryk, O.V. Borodin, V.N. Voyevodin,, I.M. Neklyudov,

V.V. Ruzhitsky, G.D. Tolstolutskaya						40

### Hydrogen Thermodesorption from Helium Ions-Implanted

### Steel 08Cr18Ni10Ti

A.N. Morozov, I.M. Neklyudov, V.V. Bryk, V.G. Kulish, V.I. Zhurba		40

Influence of Interstitial and Substitution Elements on

Helium and Hydrogen Behavior in FCC and BCC Metals

I.I. Chernov, B.A. Kalin								41

Investigation of Tritium Permeation Process Produced in

Lead-Lithium Eutectic Pb83Li17 Through Tube Steel Sample

F82H- in Reactor Irradiation Conditions

T.V. Kulsartov, V.P. Shestakov, E.V. Chikhray, E.A. Kenzhin,

A.N. Kolbaenkov, Hiroshi Kawamura and Masaru Nakamichi			42

Investigation of Helium-3 Buildup Operation in Structural Materials

by “Tritium Trick” Method

I.L. Malkov, V.G. Klevtsov, A.A. Yukhimchuk, S.V. Zlatoustovski 	42

Hydrogen Permeation Through Thin Coatings

A.A. Kurdyumov									43

Development of Helium Bubbles near Grain Boundaries in

Nickel-Carbon Alloys

I.V. Reutov and V.F. Reutov							44

Radiation Microstructure, Helium, Hydrogen in Reactor

VVER-1000 Vessel Structure Elements

V.N. Voyevodin, V.V. Bryk, O.V. Borodin, B.A. Shilyaev,

I.M. Neklyudov 									45

Formation and Growth of Hydrides in Irradiated Zirconium

Alloys

A.A. Shmakov,  A.G. Ioltukhovsky,  B.A. Kalin,  E.A. Smirnov			45

Structural Factors Influence on Hydrogen Extraction from

Irradiated Construction Materials

A.G. Zaluzhnyi, V.P. Kopytin, A.L. Suvorov, D.M. Uspenskyi			46

Specific Features of Interaction of Heavy Hydrogen Isotopes and

Radiation-Resistant Cr16Ni15M03Ti1 and SS316L Steels

Yu.N. Dolinsky, Yu.N. Zouev, I.A. Lyasota, I.V. Podgornova,

I.V. Saprykina, V.V. Sagaradze							47

Mechanism by Which Titanium Influences Formation of Radiation-

Induced Segregation of Deuterium in Cr16Ni15Mo3(Ti1) Steel

G.A. Raspopova, V.L. Arbuzov, V.V. Sagaradze, N.L. Pecherkina,

V.A. Pavlov, K.V. Shal’nov, A.P. Druzhkov					47

### The In-Pile Experiments on the Reactor IVG.1M

V.P. Shestakov, T.V. Kulsartov, E.V. Chikhray, U.L. Zheldak

A.N. Kolbaenkov, E.A. Kenzhin, V.V. Zverev, I. V. Prozorova,

U.N. Gordienko, A.F. Incov							48

- Radiation-Enhanced and Radiation-Stimulated Phenomena

Segregative Manifestation of the “Long-Range Action Effect” During

Irradiation of Permalloy Foil with Boron and Phosphorus Ions

A.V. Nikitin, F.Z. Gil’mutdinov, D.I. Tetelbaum, V.Ya. Bayankin			51

The Radiation-Enhanced and Radiation-Induced Phenomena in

Fe-16Cr Based Alloys

A.L. Nikolaev 									52

Theory of Solute Segregation in the Boundary of Finite Size

Grains in Polycrystals

V.V. Slezov, L.N. Davydov, O.A. Osmayev					53

Acceleration of the Rate of Short-Range Layering in Alloy

Fe+15at%Cr under Irradiation with Gaseous and

Metallic Ions

V.V. Ovchinnikov, B.Yu. Goloborodsky, N.V. Gushchina,

L.S. Chemerinskaya, V.A. Semyonkin, E. Wieser, W. Möller	54

# The Laws Governing Radiation-Dynamic Effects in Alloy

# Fe+8.25at%Mn under Combined Electromagnetic and

# Ion Irradiation

V.V. Ovchinnikov, B.Yu. Goloborodsky, N.V. Gushchina,

L.S. Chemerinskaya, V.A. Semyonkin, A.V. Luzgin	55

Effect of Ion Irradiation on Oversaturated Solid Solution

Decomposition in Alloy Al-4%Cu

V.V. Ovchinnikov, N.V. Gushchina, B.Yu. Goloborodsky,

L.S. Chemerinskaya	56

On the Laws and Nature of Long-Range Dynamic Effects under

Corpuscular Irradiation

V.V. Ovchinnikov	56

Mössbauer Effect Observation on 57Fe Isotope in α-Iron under

Ion Bombardment (in situ)

V.V. Ovchinnikov, B.A. Semyonkin, B.Yu. Goloborodsky	57

Modeling of Accelerated Embrittlement in Reactor 
Pressure Vessel Steels at High Neutron Fluences

V.A. Pechenkin, Yu.V. Konobeev, I.A. Stepanov, Yu.A. Nikolaev	58

### Significance of Radiation-Induced Segregation in Alloy

### Properties Alteration under Irradiation

V.A. Pechenkin, Yu.V. Konobeev	58

Grain Shape Effect on the Solute Segregation

in Elastic Stressed Polycrystal

R.V. Shapovalov, V.V.  Slezov, O.A. Osmayev					59

The Effect of Impurities and Grain Boundaries on

Radiation-Enhanced Diffusion in Zirconium

E.A. Smirnov,  A.A. Shmakov							60

Kinetics of Intragranular and Intergranular Radiation-Induced

Phosphorus Segregation in Reactor Pressure Vessel Steels

I. A. Stepanov, V. A. Pechenkin and Yu. V. Konobeev				60

Modeling of Radiation-Induced Segregation in Fe-Cr-Ni alloys

I. A. Stepanov and V. A. Pechenkin						61

# Redistribution of Phosphorus in Reactor Pressure Vessel

# Materials During Operation

O.O. Zabusov									62

Radiation-Induced Crystallization of Amorphous Materials

I.A. Antoshina, V.S. Khmelevskaya						63

- Materials for Nuclear and Thermonuclear Power Engineering

Uranium Containing Active Layers Behavior under

Irradiation at RFNC-VNIITF Pulse Fission Reactors

# S.I. Abramenko, I.L. Svyatov, A.E. Shestakov, L.N. Lokhtin			67

Atomic Vibrations and Polymorphism of Actinides

M.S. Blanter, V.P. Glazkov, L.N. Konovalov, A.V. Laushkin,

V.K. Orlov, D.D. Petrov, V.M. Sergeev, V.A. Somenkov				67

Basic Results of Forced Tests of Core Structural Materials in

Fast BN-600 Reactor

V. V. Chuev, A. N. Ogorodov, V.V. Maltsev					68

Commercial Fast Reactor MOX Irradiation Validation

V. V. Chuev, A. N. Ogorodov, V. V. Maltsev, F. G. Reshetnikov,

N. B. Sokolov, O. S. Korostin							68

Studies on Modification of Some First Wall Materials

Using 3-6.8 MeV He Ions

B. Constantinescu								70

Recent developments concerning void swelling in PWR austenitic

internals at relatively low irradiation temperatures

F. A. Garner									71

Corrosion and Electrochemical Properties of EP - 450 Steel

Exposed to High-Dose Irradiation in  BN - 600 Reactor

O.A. Golosov, V.B. Semerikov, T.L. Kuzina, A.N. Ogorodov, 
E.A. Kozmanov, E.A. Medvedeva							71

Irradiation-Assisted Intergranular Stress Corrosion Cracking

of Austenitic Stainless Steel in Steam-Water Mixture

A.L. Evseev, Yu.D. Goncharenko, V.A. Kazakov, V.K. Shamardin,

A.M. Pechyorin, G.V. Filyakin, Z.E. Ostrovsky 					72

X –ray Investigation of Fine Structure of  Alloy Zr –2.5% Nb

after In –pile Irradiation at ~ 80 °C

V. E. Kalachikov, V. A. Tsygvintsev, N. V. Gloushkova				73

Changing of Physical and Chemical States of Iron Atoms in

Zirconium Alloys Oxide Films During Neutron Irradiation

V.P. Filippov, A.B. Bateev, R.N. Pugachev,  G.P. Kobyljansky 			74

Variation of Isothermal Kinetics of -Transformation of

Unalloyed Plutonium over Different Times of Samples

Self-Irradiation

# A.M. Lyasota, A.V. Troshev, S.I. Abramenko, V.N. Kordyukov,

# Yu.N. Zouev, B.V.. Litvinov, E.P. Magda						75

Radiation Phenomena in Austenitic Steels Irradiated in

SM, BOR-60, VVER-1000 Reactors at 280-400 oC

V.S. Neustroev, Z.E. Ostrovsky, V.K. Shamardin	75

Peculiar Features of Structure and Behavior Changes in

Some Zirconium Materials at Damage Doses up to 50 dpa

G.P. Kobylyansky, A.E. Novoselov, Z.E. Ostrovsky,

V.K. Shamardin, A.V. Obukhov, V.N. Shishov and M.M. Peregud			76

Microstructure Changes in EI-847 Steel Exposed to Long-Term

Irradiation at 300 -390 °C in Fast Neutron Reactor

I.A. Portnykh V. L. Panchenko, E. N. Shcherbakov , A. V. Kozlov			77

Influence of Radiation Swelling on Thermal Expansion

Coefficient of Steel ChS-68

E.N.  Shcherbakov, A. V. Kozlov, I. A. Portnykh, O. I. Asiptsov,

V. L. Panchenko, L. A. Skryabin 							77

# Influence of Structure-Phase State Zr-Nb- Containing Alloys

on Irradiation-Induced Growth

V.N. Shishov, M.M. Peregud,  A.V. Nikulina,  G.P. Kobyliansky,

A.E. Novoselov, Z.E. Ostrovsky	78

# Damage of Beryllium under High-Dose Neutron Irradiation

V.P. Chakin, V.A. Kazakov, R.R. Melder, G.A. Shimansky,

S.V. Belozerov, D.N. Suslov, R.N. Latypov, Z.Ye. Ostrovsky,

Yu.D. Goncharenko, D.V. Pevtsov, I.B. Kupriyanov				79

The Mechanisms of Uranium Metal Fuel Radiation Creep  and

Its Temperature Nonlinearity

V.D. Rusov, V.A. Tarasov 							79

Modification of Plutonium Dioxide Properties under

Exposure to Radiation

A.V. Troshev, S.I. Abramenko, V.N. Kordyukov, A.M. Lyasota			80

The Investigation of Distribution of Erbium in Uranium-Erbium

Oxide Fuel of RBMK by X–ray Analysis

V. A. Tsygvintsev, A. N. Timokhin, V. R. Kuznetsov, V. Ivanov			80

Comparison of Irradiation Conditions for Fusion Materials in

IFMIF and ESS

P.V. Vladimirov, A. Möslang							81

New Structural Material for Fusion Reactor Based on

Ferritic Stainless Steel-Clad V-Ti-Cr Alloy

А.V. Vatulin, G.P. Vedernikov, А.V. Vertkov, S.N. Votinov, I.N. Gubkin,

V.A. Evtikhin, I.Е. Lyublinskiy, D.V. Sokolovskiy, А.K. Shikov			82

Study of the Effect of Tritium and Reactor Irradiation on Properties

of Materials in the First Wall of Fusion Reactors

Yu.N. Zouev, B.N. Goshchitskii, V.V. Sagaradze 					82

Effects of Actual Aging (Self-Irradiation) of Delta-Stabilized

Pu Alloy with Gallium on Microstructure, Mechanical Properties,

Phase Transformation Macrokinetics in Weak Shock-Waves

Е.А. Коzlov, L. F. Тimofeyeva, V.I. Таrzhanov, I.V. Теlichko,

D.М. Gorbachev, D.G. Pankratov, А.N. Grachev, А.V. Vorobyev,

V.G. Shmygin, V.S. Sakov, V.I. Cherkasov, Yu.N. Zouev, N.N. Маrkelov,

А.V. Zimin, I.L .Svyatov, N.А. Tsepilov, D.V. Таskin, I.V. Podgornova		84

### Effects of Prolonged Self-Irradiation on Shear Strength of

### Unalloyed Pu under Explosive Loading

Е.А. Коzlov, V.I. Таrzhanov, I.V. Теlichko, D.М. Gorbachev,

D.G. Pankratov,  А.N. Grachev, А.V. Vorobyev, V.G. Shmygin,

V.S. Sakov, V.I. Cherkasov, Yu.N. Zouev, N.N. Маrkelov, А.V. Zimin,

I.L. Svyatov, N.А. Tsepilov, D.V. Таskin, I.V. Podgornova			85

Features of Microstructural Changes in Unalloyed Coarse-Grained

Anisotropic Depleted Uranium after Shock-Wave Loading in

the Range of 20-50 GPa at Loading Impulse Duration of 0.5-1.3 s

E.A. Kozlov, V.G. Vil'danov, A.O. Borshevsky, Yu.N. Zouev,

I.V. Podgornova									86

Structural Changes in Reactor Alloy of the Hastalloy Type

during Long-Time High-Temperature Exposure

I.I. Kositsyna, V.V. Sagaradze, V.G. Subbotin, Yu.N. Zouev			86

- Facilities and Techniques of Experiment

Neutron Diffraction Studies of Internal Stresses in

Structural Materials for Nuclear Reactors

A.M. Balagurov									89

Investigations of Thermomechanical Effect in Metals on

Impulse Electron Accelerators EMIR-М and IGUR-3

V. Afanas’ev, V. Bychkov							89

Research Center of Simulation and Modeling of Irradiation

Phenomena in State Scientific Center of Russian Federation

“Institute of Physics and Power Engineering”

A.V. Gulevich, Yu.V. Konobeev, V.A. Pechenkin, V.A. Romanov			90

Scanning Probe Microscopy of Radiation Damages of

Proton Absorbers

M. Kozodaev, A. Drozdovskyi, O. Makeev					91

Investigation of Behavior of Model Heat Producing Rods for

Ignition Pulse Reactor under Pulse Neutron Heating at

YAGUAR Reactor

Yu.N. Zouev, Yu.G. Garas’, V.V. Kosarev, Yu.A. Kulinich,

G.Yu. Lysitsin, B.G. Levakov, E.P. Magda, V.G. Svidlov,

M.T. Chineykin, et al.	92

Miniature Scanning Tunnelling Microscope

for Intrareactor Investigations

A.L. Suvorov, B.A. Loginov, M.A. Kozodaev, O.N. Makeev			92

Monte Carlo Simulation of Neutron Yield from Be, B, Li and

C Targets Irradiated with 10-MeV Proton Beam

V.V.  Plokhoi, Ya.Z. Kandiev, S.I. Samarin, G.V. Lukin,

D.G. Modestov, G.N. Malyshkin, A.A. Malakhov, S.G. Spirina			93

Ion Track Nanotechnology

V.F. Reutov, S.N. Dmitriev							94

Neutrino Method of Fuel Burning-Out and

Radiation Creep Rate Monitoring

V.D. Rusov, V.A. Tarasov, I.Yu. Shaaban, D.A. Litvinov 	94

Mass-Spectrometric Facilities for Isotope and Chemical

Analysis of Multi-component Mixtures

A.V. Kozlovsky, S. N. Markovsky, G.L. Saksagansky, I. L. Fedichkin		95

Automated Hydrogen Measuring System at IVG.1M reactor

E. Chikhray, V. Shestakov, T. Kulsartov, E. Kenzhin				96

Calorimeter for Intense Electron Beams Dosimetry

A.P. Stepovik, D.V. Khmelnitsky, V.N. Afanas’ev					97

Implanter for Ions of Hydrogen Isotopes Based on

Accelerator of NG-12 Device

A.P. Stepovik, G.V. Mokichev,  E.P. Magda, S.V. Kiryushkin,

A.N. Kozikov, A.L. Semkov, A.V. Kurochkin, A.V. Lukin,

D.V. Khmelnitsky, V.P. Popov, A.A. Frantsuzov					98

Proton Accelerator-Based Intense Source of Radioactive Ions

M.S. Avilov, K.V. Gubin, N.Kh. Kot, P.V. Logatchev,

P.V. Martyshkin, S.N. Morozov, S.V. Shiyankov, A.A. Starostenko,

Ya.Z. Kandiev, V.V. Plokhoi, S.I. Samarin, L. Tecchio				99

Source of High-Energy Resonance -Rays Based on

Proton Storage Ring with Electron Cooling

V.A. Vostrikov, K.V. Gubin, V.A. Mashinin, V.V. Parkhomchuk,

V.G. Shamovsky									99

Elastic-Plastic Crack Propagation under Irradiation and

Cyclic Loads Caused by Thermoacoustic Instability of

Heat-Carrier in Active Zone

V.D. Rusov, V.I. Skalozubov, V.A. Tarasov	99

### Reactor Antineutrino Cross-Correlation Spectrometry

V.D. Rusov, V.A. Tarasov, D.A. Litvinov	101

Development of Measurement and Governing Systems

Meant for Study with Hydrogen Isotope Mixtures

Yu.I. Vinogradov, A.V. Kuryakin, V.S. Aryutkin, S.V. Fil’chagin	101

Synthesis, Study and Application of Aza- and Diazabicyclononanes

as Complexing Agents and Preparations for Radiation

Hygiene and Medicine

V. A. Dokichev, R. I. Yusupov, E.P. Magda, Y.A. Kulinich,

A.G. Tsvetokhin, Y.V. Tomilov	102

- Some Aspects of Physics of Radiation Phenomena in

Semiconductors and Insulators

Effect of the Nanoparticle Size and Structural Defects on Magnetic

Properties of Antiferromagnetic and Ferromagnetic Oxides

T.I. Arbuzova, S.V. Naumov, B.A. Gizhevskii, V.L. Arbuzov,

K.V. Shal`nov, E.A. Kozlov	105

# Quantitative Model of Irradiated Semiconductor

# V.N. Brudnyi, S.N. Grinyaev, N.G. Kolin	106

Fermi-Level Pinning in Irradiated Non-Metallic Materials

V.N. Brudnyi, S.N. Grinyaev, N.G. Kolin	107

11B and 25Mg NMR Estimates of Electron Density-of-States

in Superconducting MgB2 Disordered by n1-Irradiation

### A.P. Gerashenko, K.N. Mikhalev, S.V. Verkhovskii,

### A.E. Karkin and B.N. Goshchitskii	108

Long-Lived Radiation Defects on Implanted Silicon

N.N. Gerasimenko (junior), N.N. Gerasimenko, V.Yu. Troitskii	109

Investigation of Defectiveness of Nanocrystal Ceramics

CuO  by Positron Annihilation Method

A.P. Druzhkov, B.A. Gizhevskii, V.L. Arbuzov, E.A. Kozlov,

S.V. Naumov, K.V. Shal’nov, D.A. Perminov, N.V. Kostromina	110

Neutron Diffraction Studies of Structural State of Mn3O4

after Shock Wave Loading

V.I. Voronin, B.A. Gizhevskii, E.A. Kozlov, T.I. Arbuzova,

S.V. Naumov, N.V. Kostromina, L.Z. Akhtyamova	111

Development of Compacting Technology and Processing of

Non-Metal Materials Using Spherical Explosive

E.A. Kozlov, B.A.. Gizhevskii, S.V. Naumov	112

Effect of Indexed-Spectrum and 14-MeV Neutrons on

Arsenide - Gallium Schottky Field-Effect Transistors

V.T. Gromov, O.V. Tkachov, V.P. Shukaylo, S.V. Obolensky	113

Effect of Reactor Neutron Irradiation on InP Single Crystal

Structure

N.G. Kolin,  V.T. Bublik, M.I. Voronova, D.I. Merkurisov,

K.D. Scherbachev 	114

Influence n- Irradiations on Physical Properties of

SiC-Based Diodes

N.G. Orlov, V.T. Gromov, V.P. Shukaylo, A.A. Lebedev,

A.M. Strelchuk, N.S. Savkina	115

Charge Stability of Submicron Integral CMOS-Transistors

Based on Silicon-on-Insulator Structures

V.P. Shukaylo, V.Т. Gromov, I.V. Vorozhtsova, T.N. Krushinsky,

V.P. Popov, N.V. Sapozhnikov, А.А. Frantsuzov	115

Ge/Si Nanostructures with Quantum Dots

Grown by Ion-Beam Assisted Heteroepitaxy

A.V. Dvurechenskii, Z.V. Smagina, R. Groetzschel, A.K. Gutakovskii	116

Radiation Processes in Si Single Crystals

L.S. Smirnov	117

Properties of Р-Channel Transistors on Silicon Gate Oxide

Created Using BF2+ Ions for Drain/Source Areas

A.N. Tarasenkov, N.N. Gerasimenko, E.V. Kuznetsov, E.Yu. Denisenko	118

Investigation of Solid-Phase Processes in Insulator and Semiconductor

Materials under Influence of Powerful Electron Irradiation

A.P. Surgikov, A.M. Pritulov, V.V. Peshev, T.S. Frangulian,

A.V. Chernyavski, R.U. Usmanov, B.B. Moyzes, S.A. Gyngazov	118

# Defect Detection in Binary Zinc-Blende Compounds –

# Experimental (part-2)

A. Kisiel, B.V. Robouch, E. Burattini, A. Marcelli, M. Cestelli Guidi,

P. Calvani, A. Nucara, E.M. Sheregii,  J. Polit,  J. Cebulski		119

Authors Index	121

        - General Problems of Radiation Damage Physics

Molecular Dynamics Simulation of Swift Ion Track in NiAl

C. Abromeit1, A.R. Kuznetsov1,2

1 Hahn-Meitner-Institute Berlin, Germany

2 Institute of Metal Physics UB RAS, Yekaterinburg, Russia

(Abromeit@hmi.de)

The aim of the work is to simulate the formation of a track in a metallic alloy and phase transformations induced by irradiation with swift ions. The extremely strong electronic excitations inside a track due to the electronic energy loss during the slowing down process can result in a significant modification of the solid-state structure, e.g., martensitic, and order-disorder phase transformations (in ordered alloys and intermetallics) are possible. Examples for such transformation are Ni-Al alloys where martensitic transformations are well documented. In this study we chose stoichiometric and non-stoichiometric NiAl (which can undergo B2-L10 martensitic transition, order-disorder transition and also amorphization under irradiation). We used the molecular dynamics method (with many-body interatomic potentials). The method is very suitable for study of such fast processes, as track formation, to directly simulate at the atomic level the process of track formation and possible transitions in it.

We showed that swift ions form tracks in NiAl and induce the following microstructural modifications: melting and crystallization, order-disorder and martensitic transformations. Disordering induced in the track is kept after crystallization of the track. Equilibrium (martensitic L10) phase cannot be reached in ion tracks in the first stage, when diffusion in a solid does not play a role. Martensitic transition commonly begins from the development of lattice instability. The sine-like lattice oscillations are transformed into a sequence of kink-like excitations – “soliton lattice”. The character of the formed domain structure and the kinetics of the transition can depend on the presence of a track. A track can change the scheme of the martensitic transition, i.e., it can be started near the track without freezing of the long-wavelength phonon.

Physical Principles of Radiation Resistance of Alloys

Structural Self-Organization

# V.V  Bryk, I.M. Neklyudov

# National Research Center Institute of Physics and Technology, Kharkov, Ukraine (bryk@kipt.kharkov.ua)

Radiation Defects Annealing in Austenitic Stainless Steels with

Different Microstructures

###### S.E. Danilov, V.L. Arbuzov, K.V. Shal’nov, V.A. Pavlov

Institute of Metal Physics, UB RAS, Ekaterinburg, Russia (danilov@imp.uran.ru)

Point defect interactions and radiation-induced structural and phase transformations in the Fe-16%Cr-15%Ni-3%Mo steels has been investigated by residual resistivity and scanning tunneling microscopy (STM).

Stainless steels non-doped and doped by titanium at the level of 0.6% and 1.0%  have been smelted from high purity components.  After cutting the samples of this steels has been  quenched from 1373 K  in cold water. The existence of the only one austenitic phase has been suggested by X-ray analysis. The part of the investigated samples were annealed at 773 K for short range ordering (SRO) and other part were annealed at 923 K for the formation of -phase precipitates. The steels were irradiated by 5 MeV electrons at 80 K , 320 К and 573 K.

The isochronous annealing after low temperature irradiation (80K) of Ti doped steel  indicate the annealing peaks at 110 and 220 K. The migration energy of self interstitials estimated as 0.65 eV. It is not observed the influence of Ti content and the microstructures to the annealing of interstitials.

The migration of vacancies begin near 300 K with migration energy over 1.0 eV. The decomposition of vacancy complexes occurs in the range 400-550 K with decomposition energy over  1.4-1.5 eV.

The ordering processes characteristic of these alloys take place at temperatures more than 300K owing to the migration of vacancies during irradiation and at the annealing. The titanium doping suppresses the ordering. The resistivity of irradiated and nonirradiated steels higher than 750 K settles to the equilibrium dependencies of resistivity via temperature. This dependencies is altered in according with the concentration of titanium.

The radiation-induced formation of -phase precipitates with size of 2 – 3 nm with the concentration over 1018 cm-3 has been detected at 573 K electron irradiation by means STM investigation.  The thermal formation of such precipitates occurs at temperatures higher than 800 K. The influence of microstructures on the radiation-induced processes is considered.

This work was carried out with the financial support of the Russian Foundation for Fundamental Research (Project 01-02-16877) and the State Program of Support to Leading Scientific Schools of Russia (Project 00-15-96581).

Correlation Effects in Cascades of Atomic Collisions

Yu.N. Devyatko*, S.V. Rogozhkin* and V.M. Chernov**

*Moscow Engineering and Physics Institute (the State University), Russia (devyatko@veshn.mephi.msk.su).

**A.A. Bochvar Institute of Inorganic Materials, Moscow, Russia

The defect formation in metallic materials under reactor irradiation takes place due to cascades of atomic collisions. Only long-term effects of these microscopic processes can be investigated by an experimental way. That is why the main methods of the research of the initial radiation damage via cascades formations are theoretical or computational. Being irradiated in a reactor, materials is non-equilibrium medium with strong fluctuations. The average concentrations of defects in such medium are by far more than their equilibrium thermodynamic values. The fluctuations of the defect concentration resulted from the cascades are not thermodynamic. Their values vary depending on the energy of a primary knocked atom (PKA). Moreover, the PKA energy having released in the region of the cascade excites strong non-equilibrium fluctuations of temperature. All these circumstances must be taken into account to describe the process of point defect accumulation inside the medium correctly. However, the consequent procedure of averaging is not applied, and the role of fluctuations is neglected. The effective source of defect formation is much less than the value determined by the cascade function.

One of the aspects in which fluctuations play especially important role is the void size distribution. Usually (follow Lifshitz and Slezov) the void formation are considered as a phase transition in oversaturated solution of vacancies. In this approach, the Fokker-Planck equation should be used to describe the void size distribution. In fact this means that random forces presented in the void growth equation are -correlated. It is cannot be used for cascade fluctuations. The input of these fluctuations significantly modifies the void growth equation. The critical radius of a void sharply decreases while the amplitude of defect density fluctuations rises. Thus, the defect creation in atomic collision cascades needs the correlation function of random forces to be calculated very accurately, because it defines the diffusion in the space of void sizes. To sum up, the correlation function is another important characteristic of the defect formation process in cascades.

The Effect of Intermetallic Precipitates on the Evolution of

Radiation-Induced Defects in Austenitic Alloys

A.P. Druzhkov, V.L. Arbuzov, D.A. Perminov, K.V. Shal’nov, V.A. Pavlov

Institute of Metal Physics, Ural Branch RAS, Ekaterinburg, Russia (druzhkov@imp.uran.ru)

The projected degree of the atomic fuel burnout in fast-neutron atomic reactors imposes stringent requirements on the radiation resistance of constructional austenitic steels. In this connection, the search for efficient methods of suppressing the vacancy swelling of these steels represents one of the key problems of the radiation materials science. Some researchers proposed to reduce swelling of austenitic alloys by producing elastically distorted microscopic regions related to coherent boundaries of fine precipitates of secondary phases. In particular, it was hypothesized that point defects are recombined quickly on coherent interfaces in precipitation-hardening alloys.

To verify this hypothesis, we studied the accumulation of radiation defects under electron irradiation in controlled conditions at an early stage of radiation damage (104-103 dpa) of Fe-36%Ni-2%Ti model alloys, which were quenched and aged beforehand. The samples were quenched and aged at 923 K for 0.5 to 50 hours. The size and concentration of coherent Ni3Ti intermetallic precipitates was 2 to 15 nm and 1017 to 1015 cm3 respectively depending on the aging time. The irradiation temperature was varied between room temperature and 573 K. The accumulation of vacancy-type radiation defects in the form of three-dimensional clusters or nuclei of loops was checked by the positron annihilation spectroscopy.

It was found that the precipitates affected the accumulation of vacancy-type defects at an irradiation temperature of 573 K. The density of vacancy loops in aged Fe-36%Ni-2%Ti alloys decreased several times as compared to the density in the Fe-36%Ni alloy irrespectively of the size of the precipitates. Radiation-accelerated precipitates, which also inhibited the accumulation of loops, appeared in the quenched titanium-loaded alloy with increasing radiation fluence.

Vacancies interacted with titanium atoms in the solid solution at lower temperatures. This interaction made it difficult to determine the role of the precipitates.

This study was performed with the financial support from the Russian Fund for Fundamental Research (Projects Nos. 01-02-16877 and 00-15-96581).

Theory of Damage Accumulation under Cascade Damage Conditions

S.I. Golubov1), B.N. Singh2) and H. Trinkaus3)

1) State Scientific Center of Russian Federation, Institute of Physics and Power Engineering,

Obninsk, Russian Federation

2)Materials Research Department, Risø National Laboratory, DK-4000 Roskilde, Denmark

3)Institut Für Festkörperforschung, Forschungszentrum Jülich, D-2425 Jülich, Germany

In recent years, a considerable amount of effort has been spent on establishing a new model called the Production Bias Model (PBM) originally proposed by Woo and Singh (1990, 1992). The model takes into account the consequences of intracascade recombination, spontaneous formation of clusters of vacancies and self-interstitial atoms (SIAs) and one-dimensional diffusion of the SIA clusters. While diffusing, these clusters are likely to interact with all other sinks present in the crystal. Over the years, these features of the primary damage production and the ensuing consequences have been incorporated in the production bias model (PBM). During the last ten years or so, various aspects of defect accumulation and microstructural evolution under cascade damage conditions have been treated both analytically and numerically within the framework of the PBM. It has been shown that the PBM explains many features of damage accumulation under cascade damage conditions, which could not be explained in terms of the SRT and BEK types of models. Thus the model allows rationalizing high swelling rate at low dislocation density, the grain boundary/size effects, the decoration of dislocations with SIA loops, void lattice formation and saturation of void growth. The present talk will, first of all, briefly review the progress and the main results. Recently, the dose and temperature dependences of microstructural evolution including SIA loops, stacking fault tetrahedra (SFTs) and voids have been evaluated. The main results of these calculations will be presented and compared with experimental results. Implications of these results to further calculations, for example, of microstructural evolution in alloys will be discussed.

Calculation of Track Transverse Sizes in a YBa2Cu3O7-x Single Crystal Taking into Account Energy Transfer Velocity Dependence on Temperature of Excited Electrons

I.N. Goncharov, B.F. Kostenko, J. Pribiš

Joint Institute for Nuclear Research, Dubna, Russia (ingonch@sunhe.jinr.ru)

High resolution electron microscope measurements of track transverse sizes in high temperature superconductor single crystals testify to a relatively small scatter of their values (for the specific type of heavy ions) and sharp borders of the internal amorphous region. These facts point out to a dominant role of superfast melting-hardening processes in track creation (thermal spike model). The effective times of electron-atom energy relaxation (τeff) in a YBa2Cu3O7-x single crystal were calculated in our paper [1]. They are in satisfactory agreement with the experimental data, obtained using short laser pulses for the same material, and with the Allen theory which has predicted a linear τ dependence of excited electron temperature (see references in paper [1]).

Taking into account the foregoing, we have calculated the transfer sizes of heavy ions with dE/dx=20÷40 KeV/nm in YBCO in the frame of the thermal spike model.

References

1. Goncharov I.N., Kostenko B.F., Philinova V.P., Physics Letters A 288, 111 (2001)

# Long-Range Effect. The  Theory and Experiments

## V.S. Khmelevskaya, V.G. Malynkin

## Obninsk Institute of Nuclear Power Engineering, Obninsk, Russia (khmel@iate.obninsk.ru)

Long-range effect (effect of deep and superdeep penetrating of a radiation damage front into a matter) is a subject of  thorough studies and wide discussions for a long time because this is a phenomenon of a great interest for both fundamental and applied needs. Present models of irradiation-matter interaction are based on a consideration of isolated collisions of fast particles with atoms of a matter and following diffusional relaxation of damages. This  predicts a very small depth of radiation-changed layer (of 100 – 1000 A for middle energies of ions). By the way experiments give significantly larger values – microns or even tens and hundreds of microns. In the frame of present models two explanations are proposed to this disparity. It is, firstly, an appearance of considerable strains within a subsurface layer; secondly, an influence of radiation-stimulated diffusion. However, due various reason a totality of experimental facts are not explained adequately by these. It seems to be that some models based on supposition of a co-operative interaction are more perspective ones [1,2].

A straight evidence of long-range effect existence is obtained by us. We observed “radiation white layers” on cross-sections of the Fe-Cr-Ni, the Fe-Cr, the V-Ti-Cr alloy samples (the layers of changed etching capability) of 20-30 μm depth. A radiation-induced hardening and changes of other properties extend for the same depth. Similar layers were observed in various materials including hard alloy (VK8) where it with difficulty can be supposed deep spreading of strains. Additionally it was observed a disintegration of supersaturated solid solution (the alloy of the nimonic type) and an appearance of particles of other phases within a clearly limited subsurface layer of approximately the same depth.

A field of the long-range effect manifestation in metal alloys studied corresponds to the field of dissipative structures formerly found by us [3,4]. These are nonequilibrium states arising in open systems within nonlinear range. It is known that such structures are a result of a co-operative  response of a system to an external influence. So  the results of the experiments described are  the confirmation of the models of the co-operative mechanism of the long-range effect.

References

- Levinson I.B., Maslov D.L. // Poverkhnost. 1987. № 4. P.5-7 (in Russian)

- Devjatko Ju.N., Tronin V.N. // Thesis of reports I conf. “Modif. Svoistv konstr. Mat.”, Tomsk. 1988. P.II. P.86-88 (in Russian)

- Khmelevskaya V.S., Malynkin V.G. // Phase Transitions. 1997. V.60. P.59-65.

- Khmelevskaya V.S., Malynkin V.G. // Materialovedenie. 1998.№ 2. P.25-32 (in Russian)

Theory of Irradiation Hardening of Metals and Alloys 
Based on the Energy Concept of Ductility

Yu.V. Konobeev *, V.A. Pechenkin *, F.А. Garner **

* SSC RF Institute of Physics&Power Engineering, Obninsk, Russia (konobeev@ippe.ru)

** Pacific Northwest National Laboratory, Richland, USA

The irradiation induced hardening of metals and alloys is determined by their microstructure (density of dislocation network, sizes and concentrations of dislocation loops, voids, precipitates, etc.). The conventional approach in estimating irradiation hardening consists in evaluation of the critical shear stress for a dislocation segment bowing between two identical barriers. Total hardening by all microstructural components is obtained as the sum of separate contributions or as the root square of the sum of squared separate contributions.

In the present work a new method of calculating the yield strength of metals and alloys is proposed, based on energy concept of ductility. This method allows to calculate barrier hardening constants in an explicit form within the framework of isotropic elasticity theory. Expressions for hardening  by the dislocation network, voids and precipitates  are derived. In the case of dislocation hardening, the tensile yield strength depends as the root square of dislocation density, the hardening constant is close to unity. This result coincides with well known result based on the forest dislocation theory. In the case of hardening by voids a distinct from widely known result is obtained: hardening constant is determined by the void surface energy, but not by the shear modulus. In the case of hardening by spherical misfit precipitates in isotropic and homogeneous medium a general expression for the yield strength is derived. This yield strength is proportional to product of the misfit and root square of the volume occupied by precipitate particles. The last result means that the precipitate hardening should not change under irradiation beginning from the stage of coalescence or coagulation of precipitates.

Effect of Initial Dislocation Structure on Accumulation and Annealing of

Radiation Defects in Austenitic Alloys

D.A. Perminov, A.P. Druzhkov, V.L.Arbuzov, V.A. Pavlov

Institute of Metal Physics, Ural Branch RAS, Ekaterinburg, Russia (d_perm@rambler.ru)

Chromium-nickel stainless steels are among main constructional materials of active zones in fast-neutron reactors. Vacancy swelling represents a significant phenomenon limiting the use of these steels. Preliminary cold deformation may be used as one of the methods for inhibiting the vacancy swelling of the constructional materials. Dislocations, which are formed during cold deformation, serve as sinks of point defects. The accumulation of radiation defects may also be reduced by introducing alloying impurities, such as silicon or titanium, into the steels. The goal of this study was to determine the effect of the dislocation structure and impurity titanium atoms on the accumulation and annealing of vacancy-type defects in model austenitic alloys at an early stage of radiation damage (104-103 dpa).

Fe-36.5 mass % Ni and Fe-36.5 mass % Ni-2 mass % Ti alloys, which were pre-deformed (40%) at room temperature, were studied. The samples were irradiated with 5-MeV electrons at 300 K and 573 K in a linear accelerator. Isochronal annealing was performed in a vacuum of 105 Pa at an average heating rate of 1 K/min. The positron annihilation spectroscopy, which is highly sensitive to vacancy defects and dislocations, but is insensitive to interstitial atoms and their agglomerates, was used in the study.

It was found that the accumulation and annealing of point defects in the austenitic alloys depended on the initial microstructure of the samples. When the initial density of dislocations in the Fe-Ni samples was large, the accumulation of vacancy clusters decreased several times as compared to the samples subject to solid-solution hardening. Alloying of the compound with titanium caused a considerable change in the behavior of vacancy defects and dislocations during irradiation and annealing. Titanium enhanced clusterization of vacancies both in quenched and deformed samples at room temperature and retarded dissociation of vacancy clusters during annealing. Ni3Ti precipitates, which were formed on the dislocation lines in the titanium-loaded alloy, pinned the dislocations. Consequently, initial stages of recrystallization were decelerated. The same precipitates impeded the capture of positrons by dislocations.

This study was performed with the financial support from the Russian Fund for Fundamental Research (Projects Nos. 01-02-16877 and 00-15-96581).

Cascades of Atomic Collisions and Point Defect Accumulation

S.V. Rogozhkin*, Yu.N. Devyatko* and V.M. Chernov**

*Moscow Engineering and Physics Institute (the State University), Russia (h@rsv.mephi.msk.su).

**A.A. Bochvar Institute of Inorganic Materials, Moscow, Russia

Cascades of atomic collisions play an important role in the defect structure formation. However, as they last very short time (about several picoseconds), there is no detail understanding how they work. Computer simulation and some analytical approaches allow to bring to light a number of peculiarities of the cascade and to distinguish some stages in the process itself. The evolution of a defect structure in the irradiated material is usually described by models based on macroscopically averaged characteristics (for example, the concentrations of point defects). The non-linear interaction of the defects in a cascade area needs additional attention to calculating their average concentration. To note, the description using the average concentration completely misses the peculiarities of defect creation in cascades. The interaction between bombarding particles and atoms of the target is a probabilistic process. Therefore, defect creation is a random process. For the quantitative description of point defect accumulation it is necessary to use the stochastic equations and to average them.

In this work we have completed an careful sequential procedure of averaging the kinetic equations describing point defect accumulation. We have managed to take into account the fluctuations of the defect formation process in material under irradiation. An effective source of point defect creation is obtained. The calculations were carried out for the case of pure iron irradiated by fast reactor neutrons with the energy 0.6 MeV. The values Q turned out to depend upon the density of sinks in the medium.  The obtained values Q are far less than those that can be found in the literature for the source of defects under neutron irradiation  dpa/s. Thus, it should be noted that the damage calculation based on the only dpa parameter results in overestimations.

Modeling Complexes of Defects in Solid Solution

Using Neutron Spectroscopy

V.V. Sumin

Joint Institute for Nuclear Research, Frank Laboratory of Neutron Physics,

Dubna, Russia (sumin@nf.jinr.ru)

A new method for the calculation of splitting of the fundamental local modes was proposed. It takes account of the relaxation of metal atoms around the defects and the elastic interaction of the deformation fields. This approach allows one to explain the neutron spectroscopy results, which was impossible in case of the force constant approach.

This method will be useful in interpretation of neutron spectroscopy data in interaction between radiation point defects and interstitial (O, C, N, H) atoms.

Sputtering of Sub-atom Carbon Films on the Surfaces of Metals

by the Low-Energy Gas Ions

# A.L. Suvorov, A.G. Zaluzhnyi, V.P. Babaev,   N.E. Lazarev, Yu.N. Devyatko, A.A. Zaluzhnyi

SSC RF Institute for Theoretical and    Experimental Physics, Moscow, Russia (alex.suvorov@itep.ru)

An earlier developed original experimental technique for measuring and analyzing the parameters of low-frequency fluctuations of field-electron current of metal-film systems was used in the present work to measure  sputtering yield Yf of carbon films (degree of covering θfrom 1 to 5)  onFe, Nb, Ta and U. The measured values proper were amplitudes ΔIn of anomalous field-electron current fluctuations arising due to single bombarding ions hitting the film. Sputtering yield Yf evaluation was carried out with the use of an analytical expression of the developed theoretical model. Measurements were made of coefficients Yf of carbon films sputtering with ions H+ and He+ with energies  Ei ranging between 2.0 and 10.0 keV. For each type of ions, the energy dependence of Yf were obtained for fixed values of θ; besides, for certain fixed ion energy values Ei, for each type of ions, there were obtained the dependence of Yf on θ. The measured values of Yf in all cases noticeably exceed the same in case of pure carbon.

Another original technique combining field-ion microscopy and fine measurements of light characteristics of local areas of field-ion microscopy images was used to determine energy thresholds Eth of the beginning of sputtering of carbon films on metal surface. Energy distributions of Yf for different values of θ in the threshold energy range were measured.

Theory and Computer Simulation of Radiation Processes in

Multicomponent Materials

Yu.V. Trushin, D.V. Kulikov, V.S. Kharlamov, P.V. Rybin

A.F.Ioffe Physico-Technical Institute of RAS, St.Petersburg, Russia (trushin@theory.ioffe.rssi.ru)

The basis of the radiation processes in the multicomponent materials is presented briefly [1-4]. The physical features of the cascade processes in the materials with impurities are examined as well as processes taking place on the diffusion and sink evolution stages and their influence on the changes of macroscopic properties of the materials.

The problems of computer simulation of the radiation processes in the multicomponent materials are viewed [2,3]. The features of Monte-Carlo computer codes' constructing with accounting of cascade regions' overlapping when irradiating with high fluences are noted [2,3]. Several results of the ballistic simulation for specific materials are presented [2,3,5.6]. The attention is put on the describing of the physical principles of diffusion simulation in the irradiated materials. The physical results for computer simulation for the materials with different composition and structure under irradiation are presented [2,3,7,8].

References

- Trushin Yu.V. Theory of Radiation Processes in Metal Solid Solutions. USA, New York, 1996.

- Trushin Yu.V. Radiation Processes in Multicomponent Materials (Theory and Computer Simulation) (in Russian), 2002, SPb, Ioffe-PTI.

3.   Trushin Yu.V., Kulikov D.V. In: Modern Condensed Matter Physics: Experimental Methods and Devices  Related Topics. Eds. Suvorov A.L., Abov Yu.G., Firsov V.G. Akademprint, Moscow,  2001, p.84-112.

4.   Rybin V.V., Trushin Yu.V.// Tech.Phys.Lett., 1997, vol.23(4), p.326-328.

- Schmidt A.A., Trushin Yu.V., Ber B.J. Zhurkin E.E. In: Modern Condensed Matter Physics:  Experimental Methods and Devices  Related Topics. Eds. Suvorov A.L., Abov Yu.G., Firsov V.G. Akademprint, Moscow,  2001, p.287-291.

- Rybin V.V., Trushin Yu.V., Fedorov P.Yu., V.S.Kharlamov// Tech.Phys.Lett., 2000, vol.26(10),

p.876-878.

7.  Rybin P.V., Kulikov D.V., Trushin Yu.V., Pezoldt J., Yankov R.// Proc.of SPIE, 2000, vol.4046, p.301-307.

- Kulikov D.V., Safonov K.L., Trushin Yu.V., Pezoldt J.// Proc.of SPIE, 2002, vol.4627, p.299-303.

Effect of Irradiation on Electronic Properties of Pure Compensated Metal

Single Crystals  at High Magnetic Fields

V.V. Marchenkov*, V.E. Arkhipov*, A.L. Suvorov** and H.W. Weber*** 
*Institute of Metal Physics, Ekaterinburg, Russia (march@imp.uran.ru) 
** Russian State Research Center “Institute for Experimental and Theoretical Physics”, Moscow, Russia  
***Atomic Institute of the Austrian Universities, Vienna, Austria

The effect of 5 MeV electron irradiation on the crystal structure, transverse magnetoresistivity ρxx and Shubnikov – de Haas effect in pure tungsten single crystals was investigated. The structure of tungsten was studied by field-ion microscopy. The electronic properties were measured in magnetic fields up to 15 T and over the temperature range 2 – 55 K in tungsten single crystals having a residual resistivity ratio ρ293К/ρ4.2К ≈ 75000 prior and after irradiating up to fluences of 1·1018 els/cm2 and 2·1018 els/cm2 near room temperature. It was shown that the radiation-induced defects strongly affect the transverse magnetoresistivity and the amplitude of Shubnikov – de Haas oscillations. It was observed that the radiation-induced defects lead to substantial changes in the temperature dependence of the magnetoresistivity at low temperatures, i.e., the exponential dependence changes to the power one. The possible reasons of such behavior of ρxx  are discussed. The field-ion microscopy study showed the presence of the isolated vacancies and their compact complexes in irradiated crystals. Namely these types of radiation-induced defects lead to the substantial changes in the electronic properties.

Quantitative Measurement of Electron Diffuse Scattering by

Single Manometer-Sized Defects in Au and Mo

M. A. Kirk, M. L. Jenkins*, R. D. Twesten**
Materials Science Division, Argonne National Laboratory, Argonne, IL 60439
*Department of Materials, University of Oxford, Oxford, UK
**Center for Microanalysis of Materials, Seitz Materials Research Laboratory,

Urbana, USA

Elastic diffuse scattering of electrons by single nanometer-sized defects in ion irradiated Au and Mo has been measured quantitatively.  Huang scattering from isolated single defects is separated from Bragg scattering at a weakly excited diffraction peak (usually 2 g, with near 5 g excited). The asymmetry in the Huang scattering immediately reveals the interstitial or vacancy 
nature of the defect.  Results will be compared among various dislocation loop geometries and with calculations.  Comparison to similar measurements on necessarily broad distributions of defect types and sizes by diffuse x-ray scattering will be made.  Contributions of inelastic electron scattering to defect images and diffraction data are also measured and will be discussed.

Work is supported by DoE.