- Facilities and Techniques of Experiment

Neutron Diffraction Studies of Internal Stresses in Structural Materials

for Nuclear Reactors

A.M. Balagurov

Frank Laboratory of Neutron Physics, JINR, Dubna (bala@nf.jinr.ru)

For investigations of internal stresses in structural materials various techniques of non-destructive testing have been used so far: x-ray diffraction, ultrasonic scanning, measurement of magnetic induction and susceptibility, Barkhausen effect etc. Unfortunately, all these tools have serious limitations. High resolution neutron diffraction has been adopted for solution of this problem about 10 years ago and has been widely expanded due to a whole series of important advantages in comparison with traditional methods. The most important of them are: the identification of internal stress deep in the sample volume (up to 2 cm for steel), high spatial resolution (about 1 mm at any direction), simultaneous measurement of average deformation in gauge volume and microstresses in crystal grains, the determination of the deformation anisotropy and stress distribution for each component of multiphase material, the possibility of studying both magnetic and nonmagnetic compounds.

At FLNP in Dubna specialized equipment for internal stress measurements in volume materials and details has been set up and tested. These studies are performed with the high-resolution Fourier neutron diffractometer (HRFD) at the IBR-2 pulsed reactor. Multi-axes goniometer for determination of the stress tensor, loading machine with 60 kN load, mirror furnace up to 2000С are used for experiments. The minimal gauge volume is about 2´2´2 mm3, typical time needed for measurement of a diffraction pattern is around 24 hours.

At HRFD a series of experiments in main directions of this field has been carried out. For instance, the mechanical properties of austenitic steel samples at various applied load, including cyclic one, have been investigated. At different degree of low cycle fatigue the residual stresses and amount of the martensitic phase, which appeared as a result of the plastic deformation of the initial austenitic phase, were measured. Measurements of residual stresses in shape welded steel have been performed. The residual stresses, phase composition and mechanical properties of new prospective materials – Cu/W and MoSi2/SiC gradient compounds, Al/Al2O3, Ni3Al/Al2O3 composites etc. – have been investigated. The results of neutron diffraction experiments are used for optimization of manufacture processes for obtaining materials with needed mechanical properties.

Investigations of Thermomechanical Effect in Metals on Impulse Electron

Accelerators EMIR-М and IGUR-3

V. Afanas’ev, V. Bychkov

Russian Federal Nuclear Center – All-Russian Science and Research Institute
 of Technical Physics, Snezhinsk, Russia

Set-up and experimental results of the measurements of the thermomechanical effect in metals carried out on the installations IGUR-3 and EMIR-М [1] are presented. These installations operated in the regime of electron beam output in the atmosphere. The fluences of electron energy on the spot of sample displacement were 5 - 8 cal/cm2. The loading impulse profiles were measured by means of a quartz gauge, and the fluences of energy, by steel calorimeters of full absorption. Pressure amplitudes and values of mechanical impulses in the samples were calculated in accordance with the classical knowledge of generation and spreading of stress mechanical waves in metals [2-5].The experimental results for some materials with different  ρ and Z are displayed in the table.

Table

Measured shock pressure parameters of metals under electron beam irradiation on EMIR-М and IGUR-3 (fluence of energy 1 cal/cm2)

| Parameter of stress pulse | Al (AMg6) | Ti (VT-1) | Fe (St.3) | Cu (M1) | Ta | Pb | Sn |
| --- | --- | --- | --- | --- | --- | --- | --- |
| EMIR-М |  |  |  |  |  |  |  |
| Рmax10-6, Pа | 172 | 111,5 | 263 | 253 | 233 | 253 | 132 |
| t1/2, ns | 35070 | 22030 | 12030 | 20030 | 7015 | 25030 | 20020 |
| I, Pаs | 5.9 | 2.4 | 3.1 | 5.0 | 1.6 | 6.2 | 2.6 |
| IGUR-3 |  |  |  |  |  |  |  |
| Рmax10-6, Pа | 112 | 102 | 253 | 263 | 233 | - | - |
| t1/2, ns | 55070 | 30030 | 15040 | 22030 | 8515 | - | - |
| I, Pаs | 6.1 | 3.0 | 3.7 | 5.7 | 1.9 | - | - |

It is seen from the table that smaller duration of irradiation pulse and higher average energy of electrons on the accelerator IGUR-3 in comparison with the accelerator EMIR-M resulted in increase both in the stress pulse duration and the magnitude of mechanical impulses.

References

1 Diankov V.S, Kovalev V.P., Kormilitsyn A.I. Lavrent’ev B.N.  Obzor eksperimentalnykh ustanovok VNIITF dlya radiatsionnykh issledovanii.// FММ, 1996, V.81, Vip.2, P.119-123.

2. F.C. Perry. Thermoelastic Response of Polycrystalline Metals to Relativistic Electron Beam Absorption.//  J.Appl. Phys. 1970, V.41, N.12, P.5017-5022.

3. Kalmykov A.A. et al. О razlete mgnovenno nagretogo vestchestva.// PMTF, 1966, №5, P.1-14.

4. Raush. Vliyanie vremeni nagreva na volny napryazenyi, vyzvannye teplovym vozdeistviem. Prikladnaya mekhanika, 1969, №2,P.204.

5. R.A. Graham, F.W. Neilson. Piezoelectric Current from Shock Loaded  Quartz – a submicrosecond Stress Gauge.// J. Appl. Phys. 1965, V.36, N.5, P.1775-1783.

Research Center of Simulation and Modeling of Irradiation Phenomena

in State Scientific Center of Russian Federation

“Institute of Physics and Power Engineering”

A.V. Gulevich, Yu.V. Konobeev, V.A. Pechenkin, V.A. Romanov

SSC RF Institute of Physics & Power Engineering, Obninsk, Russia (gulevich@ippe.obninsk.ru)

An opportunity of foundation of the Center for investigations by simulation and modeling of irradiation phenomena in the SSC RF IPPE is considered.

The objective of the foundation is to create the experimental and theoretical basis for a substantiation of a choice of irradiation resistant advanced materials for reaching ultrahigh nuclear fuel burn-ups and for providing the technical and economical effectiveness and competitiveness of future nuclear power engineering.

The research base of the Center consists of a set of ion and electron accelerators: EGP-15, EGP-10M, ILU-100, EG-2.5, EG-1, KG-2.5, KG-0.3, pulsing reactor BARS-6, diffractometer DIN-2PI at the reactor IBR-2.

Primary tasks of the Center are the following:

- Express assessment of irradiation resistance of candidate structural materials for various nuclear power facilities including fast reactors, VVERs, fusion reactors and accelerator driven systems (ADS) at design and beyond design irradiation doses.

- Accumulation of experimental data on microstructural changes, precipitation and radiation-induced segregation in structural materials under ion and neutron irradiation that is necessary for the further development of radiation damage theory.

- Modeling of the microstructure evolution and precipitation in alloys under irradiation and calculating energy and diffusion characteristics of point defects and point defect clusters using the methods of molecular dynamics.

- Studies of radiation-induced processes in dielectric materials under conditions of powerful pulsing and continues irradiation.

The main directions of fundamental and applied investigations in the field of radiation damage physics which are planned to carry out in the Center are presented too.

It seems that the organization of the Center in IPPE will compensate the loss of the accelerators of the Kharkov Institute of Physics & Technology (Ukraine) after disintegration of the USSR, and also will lead to an essential acceleration and to reduce the price of development of radiation resistant materials by means of carrying out the simulation of radiation damage using accelerators of charged particles (ions and electrons).

For the present the SSC RF IPPE possesses the necessary experimental base and personnel potential for making such a Center.

Scanning Probe Microscopy of Radiation Damages of Proton Absorbers

M. Kozodaev, A. Drozdovskyi, O. Makeev

SSC RF Institute for Theoretical and Experimental Physics,

Moscow, Russia (M_Kozodaev@vitep1.itep.ru)

Using of carbon materials in high intensity proton linacs can decrease radioactivity level in 10-100 times. As a result, operation such equipment will become more safety. To avoid degradation and spattering of carbon material it’s useful to cover it by metallic film.

This paper presents results of the study of radiation resistance of carbon materials (small-grained and boron modified graphite) which were covered by nickel film for using in high intensity proton linacs. The testing samples were exposed by proton irradiation with fluencies up to 2х1018 p/cm2. The angle of irradiation was varied from 00 to 900 concerning surface of samples. The irradiated surfaces were investigated by scanning probe microscopy [1]. The examinations stability of carbon plates in conditions of proton beam radiation were carried out. The permissible levels of a fluency of protons for the test carbon materials were estimated. The vacuum testing has shown, that the materials are satisfactory for accelerators.

Radiation examinations showed that such structures «carbon material - nickel» have a small degradation for fluencies of particles loosed during 10 years accelerating process. As a result, the mentioned structures can be successful apply as proton absorbers.

References

- Yu. N. Cheblukov, A.S. Fedotov, M.A. Kozodaev, B.A. Loginov, M.O. Popov, A.E. Stepanov, A..L. Suvorov. Quantitative scanning tunneling microscopy of radiation-induced modification of materials surface. Materials Science and Engineering A270 (1999) 102-106

Investigation of Behavior of Model Heat Producing Rods for Ignition Pulse Reactor under Pulse Neutron Heating at YAGUAR Reactor

Yu.N. Zouev, Yu.G. Garas’, V.V. Kosarev, Yu.A. Kulinich, G.Yu. Lysitsin,

B.G. Levakov, E.P. Magda, V.G. Svidlov, M.T. Chineykin, et al.

Russian Federal Nuclear Center-VNII of Technical Physics,

Snezhinsk, Russia (btk@five.ch70.chel.su)

The report presents results of literature data analysis concerning investigation of behavior of model heat producing rods fabricated from enriched to 36% uranium. Test conditions were heating up to 1000C during 1.5 ms and cooling with water stream (stream velocity – 5m/s).

Requirements to design of model heat producing rods and experimental measurement device (MD) for reactor investigations were settled.

Elaborated designs for model heat producing rods and MD, experimental parameters checking devices are described.

Possible accidents during carrying out experiments are evaluated. Technical methods of prevention are proposed.

Reactor YAGUAR was used for experiments on heating and cooling of model heat producing rod fuel velocity in real scale of time.

Miniature Scanning Tunneling Microscope

for Intrareactor Investigations

A.L. Suvorov, B.A. Loginov, M.A. Kozodaev, O.N. Makeev

SSC RF Institute of Theoretical and Experimental Physics,

Moscow, Russia (makeev@vitep1.itep.ru)

Construction and capabilities of designed and manufactured miniature scanning tunneling microscope for carrying out wide-ranging investigations inside and thermonuclear plants are described.

A head of the microscope has been specially designed for study and monitoring of surface degradation of the elements and units of thermonuclear plants. It is equipped with a transport device and a special drive for transporting in vacuum. The drive is controlled by either computer or manually. The studies are carried out both under shutdown and working conditions i.e. while the thermonuclear fusion is running in plasma. In both cases it is possible to study surfaces of working elements of nuclear and thermonuclear plants (including difficult of access zones) as well as to study the surface degradation of specimens, which are charged with the head of the microscope beforehand.

Controlling of the head and obtaining of the data is carried out by the computer and power sources, which are installed beyond a radiation effect zone. Depending on radiation level in the zone where the designed mini-microscopes operate the microscope and the electric cables can be reusable or used once.

Thus, scanning tunneling microscopy – high-resolution non-contact technique of study of surface – is now applied to surface degradation analysis inside the nuclear and thermonuclear reactors and other similar plants. Before, for the accurate study of surface degradation of the inner components of the thermonuclear plants little pieces (templates) were cut from the components or used the test-specimens.

Monte Carlo Simulation of Neutron Yield from Be, B, Li and C Targets

Irradiated with 10-MeV Proton Beam

V.V.  Plokhoi, Ya.Z. Kandiev, S.I. Samarin, G.V. Lukin, D.G. Modestov,

G.N. Malyshkin, A.A. Malakhov, S.G. Spirina

Russian Federal Nuclear Center –  E.I. Zababakhin All-Russian Scientific Research Institute of

Technical Physics, Snezhinsk, Russia (V.V.Plokhoi@vniitf.ru)

The Monte Carlo simulation results of neutron yield from 9Be, B, 6Li, 7Li, 13C and boron carbide targets irradiated with 10-MeV proton beam are presented. The depth-distribution of energy deposition and neutron yield as well as energy-angle distributions of neutrons emitted by 13C and boron carbide targets are presented too.

Monte Carlo simulations are done using PRIZMA code developed at RFNC- All Russian Institute of Technical Physics to solve the problems of transport of photons, neutrons and charged particles in matter.

The presented results allow making the proved choice of a target design and material taking into account of thermal loading and energy-angular neutron distribution.

This research was spent in interests of the ISOL project of an intense source of radioactive ions (Isotopes Separator On Line) within the framework of SPES program (Study and Production of Exotic Species) which is being carried out in the Italian Institute of Nuclear Physics (Legnaro National Laboratories).

Ion Track Nanotechnology

V.F. Reutov, S.N. Dmitriev

Joint Institute for Nuclear Research, Flerov Laboratory of Nuclear Reaction,

Dubna, Russia (reutov@nrsun.jinr.ru)

Among the currently developed methods of synthesizing various in morphology and properties nanostructures in solids, a special place is given to the so-called nuclear technology that includes a direction of studying the processes of formation and practical application of ionic tracks generated in solids at  their irradiation by high energy ions. The particular structure of track fields allows one to prognosticate wide perspectives of their application, for example, in microtechnologies. The empty or nearly empty track fields can  be filled by atoms of practically any sort.

Particular interest has recently appeared to the use of ionic tracks for the formation from various materials of one-dimensional nano- microstructures such as nanowires and microtubes, with the help of the so-called template technology. The replicas from etched tracks by way of a galvanic deposition in them of metal atoms are the first step for the development of such a microtechnology on the basis of track membranes.

In a number of cases of practical application, it is necessary to form a nanowire structure on massive substrates (the so-called metal microbrushes). It is connected with a necessity of considerable ( tens - hundreds times) increase of the surface activity of the object, for example, magnification of radiating or immersing, absorptive or desorptive abilities.

Metal microtubes of strictly fixed sizes can find wide application for production of various sensor devices, in systems of  differential gear transmission of anionic or cationic molecules, microcanisters for medicines, toxiferous and radioactive substances, etc.

Using the metal nanowires on a massive substrate, for example, as electrodes for electric erosion treatment, allows one to form metal nanoclusters on the surface of solids (metal, semiconducting, polymeric ones, etc.)

This investigation presents the results of the developments of methods for synthesizing metal nanowires and microtubes on the basis of track membranes as well as the formation of metal nanoclusters on the surface of various solids.

neutrino Method of Fuel Burning-Out and

Radiation Creep Rate Monitoring

V.D. Rusov, V.A. Tarasov, I.Yu. Shaaban, D.A. Litvinov

Odessa National Polytechnical University, Odessa, Ukraine (siiis@te.net.ua)

In the present work the essentially new method of restoration of each nuclear density component of nuclear fuel isotope structure and accordingly dynamics of their change during work of a reactor is offered. On an example of known experimental data the return task of neutrino diagnostics of a reactor active zone is considered. This return task decision, on the one hand, allows to restore with high accuracy the current values of nuclear density of each of a component of isotope structure of nuclear fuel, and with another - opens a real opportunity of creation neutrino technologies of diagnostics of time evolution of isotope structure of nuclear fuel and the reactor power in a mode on-line.

The correlation passive location algorithm structure of inside reactor division neutrino sources is submitted. The developed signals processing algorithm structure is a basis for practical realization of neutrino sources passive location system. The description of such system and its reception aerial is submitted.

The automatic system of the remote continuous control after the degree of fuel burning out and fuel radiation creep rate is considered in view of fuel arrangement in a reactor active zone, and consequently, diagnosing of its residual resource/service life with the help of model not excess of limiting burning out, model not excess loading - durability and models a parameter - field of the admission. The radiation creep rate estimation will be carried out by a method of Monte Carlo with the help of the simulation program using as entrance parameters of an estimation of concentration of radiation point defects (vacancies and interstitials), formed by division nucleus splinters. Estimations of concentration of radiation point defects turn out by the appropriate estimations of neutrino source activities. The complex of the simulation programs is developed, allowing to check up the developed algorithms and to specify a lot of parameters, for example, such as an interval of digitisation of signals, a base time interval for construction of discrete cross-correlation function and others.

Mass-Spectrometric Facilities for Isotope and Chemical Analysis of

Multi-component Mixtures

A.V. Kozlovsky*, S. N. Markovsky*, G.L.Saksagansky**, I. L. Fedichkin*

*NPO “METTEK”, St.-Petersburg, Russia

**D.V. Efremov Scientific Research Institute of Electrophysical Apparatus,

St.-Petersburg, Russia (gruss@niiefa.spb.su)

Basic principles, technical characteristics, design philosophy, and working condition of the special-purpose mass-spectrometric facilities for multi-component mixture isotope and chemical analysis are presented.

The base of the developed devices is a time-of-flight mass-spectrometer (mass-reflectron) built at a linear scheme. Method of recording and mathematical processing of a number of the impulses of current coming from the detector operates in real time. It makes possible to identify spectra with up to 1024 partial components. Developed apparatus is intended for solving analytical problems and for the  automated optimized control of the technological processes.

One of the developed facilities is oriented to work with gas containing  tritium mixtures. Its resolution is 600; measured masses range is 1-50 a.e.m.; cycle analysis duration is 0.4 s. The second facility is proposed to be used in the experiments with transuranium elements and corresponding technologies. Its resolution is 500; measured masses range is 1-600 a.e.m.; isotopic sensitivity threshold by uranium is 5·10-6; cycle analysis duration is 0.1-0.3 s.

Developed devices combine:

- high sensitivity in a wide range of  the measured masses

- measuring rapidity,

- design simplicity,

- working flexibility,

- compactness,

- compatibility with the external nets,

- lower cost compared with foreign analogues.

Automated Hydrogen Measuring System at IVG.1M reactor

E. Chikhray*, V. Shestakov*, T. Kulsartov*, E. Kenzhin**

*SRIETP KazNU, Almaty, Kazakhstan

**IAE NNC, Kurchatov, Kazakhstan

System is dedicated for real-time registration of hydrogen (and its isotopes) concentration in two volumes of experimental device during irradiative material testing experiment at IVG1M reactor.

System allows conducting of automated simultaneous real-time sampling and registration of chemical composition of gases in operational volumes of two chambers of experimental installation (in inlet and outlet sides, for example). That is especially important for experiments on study of diffusion parameters (with method of hydrogen permeation, for example).

Measurement part is based on mass-analyzing radio-frequency gouges of omegatron type RMO-13 and MX6407-P (for light masses) with appropriate set of hardware-software tools. Original programmable oscillator of omegatron operational frequency and programmable high-voltage ramp for MX6407-P deflection system were designed with purpose to provide computer control for both mass-analyzers. CAMAC interface is used to link measurement system to IBM PC.

System provides possibility to measure wide mass-spectrum in a chamber under irradiation as well as simultaneous measurement of concentration changes of up to four masses in one chamber and registration of spectrum of light masses (2-6) in second chamber. Also it allows operation in data analysis mode when measurements are finished. Selection of operational mode, set-up of measurement duration, sampling frequency and data analysis are provided by graphic terminal of IBM PC.

System supports data acquisition and processing during four-hour reactor power session with following technical characteristics:

- Number of measure channels – 2 (one-channel operation is possible);

- Input signal – analogous, 10-5 - 10.0 V voltage;

- Channel sampling frequency  – up to 0,1 Hz

Software is functioning in environment of operational systems MS-DOS or Windows (in DOS emulation mode).  Post-measurement data processing provides visual analysis and filtration of measured arrays.

Described automated system is used for investigation of hydrogen- and tritium-permeation parameters of F82H and MANET stainless steels and vanadium alloys within the frame of international program of ITER-DEMO Thermonuclear Reactor.

Calorimeter for Intense Electron Beams Dosimetry

A.P. Stepovik, D.V. Khmelnitsky, V.N. Afanas’ev
Russian Federal Nuclear Center – All-Russian Scientific and Research Institute of Technical Physics, Snezhinsk, Russia (c5@five.ch70.chel.su)

One of the ways for loading materials with strain pulse is exposure of them with a high-power electron beam by duration 25-100 ns. To calculate the resulted thermal pressure it is required to measure the energy density value of falling electrons.

|  | Unit of total-absorption calorimeters: 1 – case protective ring, 2 - case, 3 – bracing wires, 4 –ring calorimeter (steel), 5 – central calorimeter (steel), 6 – thermocouples outlets, 7,8 – calorimeters protective shields, 9 – sample |
| --- | --- |

In [1] the construction for the unit of total-absorption calorimeters is developed (see Figure), which allows conducting measurements of the value of electrons energy density above 200 J/cm2 in the center and at the periphery of the sample without its damage.

To use the developed structure for diagnostic purposes, the thermal characteristics of calorimeters are assessed  in the given paper and the influence of electron spectrum, firms and calorimeters sizes on the measurement results is studied. Moreover, the independence of measurements of calorimeters warming-up on sample material is provided with protection against the reflected electrons with shields 7 and 8.

To determine the energy share absorbed in calorimeter material, χ, with Monte Carlo technique by MCNP4B code the calculations of electrons transport are conducted in the bodies with a form and sizes fit with the calorimeter construction. It is shown that the share of absorbed energy is mainly determined by lateral dimensions of calorimeters and average energy of electrons in a beam, and it is weakly dependent on a form of energy spectrum.

Analysis of thermal processes in the calorimeter construction after it have been heated with electronic beam and then cooled allows determining of the calorimeter average temperature <T0>, which, in its turn, is associated unambiguously with the value of electrons energy transfer in the beam by a ratio

W=h⋅dχH(<T0>)−H(Tam),

where h – calorimeter thickness, d – steel density, H(T) = C(T)dT, С(Т) – iron heat capacity, Тam – ambient temperature.

The proposed calorimeter construction is many a time applied in experiments. Its use enabled to study the spall phenomena in copper and aluminum alloys, to measure the value of Gruneisen coefficient of pyrocarbon [2] and so on. The construction seemed to be serviceable both as for hardness to electron beam and for using it as a separate single node.

References

1. Stepovik A.P. Voprosi Atomnoy Nauki i Tekhniki (Fizika Radiazionnogo Vozdeistvia na REA) Issue 3-4.,132(1999)

2. Stepovik A.P., Journ. of  Appl. Mechanics and Techn. Phys.№4, 150 (1992)

Implanter for Ions of Hydrogen Isotopes Based on Accelerator of NG-12 Device

A.P. Stepovik*, G.V. Mokichev*,  E.P. Magda*, S.V. Kiryushkin*, A.N. Kozikov*,

A.L. Semkov*, A.V. Kurochkin*, A.V. Lukin*, D.V. Khmelnitsky*, V.P.  Popov**, A.A. Frantsuzov**

*Russian Federal Nuclear Center – All-Russian Scientific and Research Institute of Technical Physics, Snezhinsk, Russia (c5@five.ch70.chel.su)

** IPP SB RAS, Novosibirsk, Russia

The results of updating of the neutron generator accelerator NG-12I are stated for its use as an implanter for ions of hydrogen isotopes (Н1+ and D2+) into silicon wafers. Ions energy is 175-210 keV, beam current is up to 10 mA [1]. For updating aims the 900 track for beam transportation is used, with the installed devices as scanning module, the ion pipe, the measurement module and the module for the wafer fastening.

For wafers exposure the system of ion beam scanning in two perpendicular-reciprocal directions is assembled and perfected. Currently the system enables to exposure the wafers of 100 mm diameter; in perspective – up to 200 mm. The uniformity of wafers exposure is perfected with using calorimeters of pyrocarbon. The recording and control system for exposure uniformity by a wafers perfected with using 21 calorimeters. The obtained non-uniformity at beam current of 0,35 mA is approximately ±10%. The approbation of exposure mode of current 1 mA is conducted, but for practical purposes the modes with current above 0,35 mA have not however been perfected yet.

Currently the device enables to exposure the wafers with protons and deuterons within wide temperature range. With that purpose the related calculations are conducted and the special constructions are developed for the silicon wafer to be fastened, that enables to change the temperature of the pad, on which the wafer is placed. Under different circumstances more than 90 silicon wafers were exposed. The trial bonding of the implanted wafers with oxidized ones for getting silicon – on – insulator-plates (SOI-plates) is performed. The obtained transport area of film is 100%.

References

1. Diyankov V.S., Mokichev G.V. et al, FMM.81, Issue 2,119( 1996)

Proton Accelerator-Based Intense Source of Radioactive Ions

(project approved by ISTC)

M.S. Avilov*, K.V. Gubin*, N.Kh. Kot*, P.V. Logatchev*, P.V. Martyshkin*, S.N. Morozov*, S.V. Shiyankov*, A.A. Starostenko*, Ya.Z. Kandiev**, V.V. Plokhoi**, S.I. Samarin**, L. Tecchio***

*INP SB RAS,Novosibirsk, Russia (gubin@inp.nsk.su)

**VNIITF, Snezhinsk, Russia

***LNL INFN, Legnaro, Italy

The proposed project is aimed the R&D study of a radioactive ion source in the framework of the SPES program at LNL. LNL has proposed a double-acceleration  design for production of ISOL-type RIB (Radioactive Ion Beam). A primary proton beam (with the energy up to 100 MeV, average power up to 300 kW, diameter 1 cm) accelerated in the superconducting linac is directed to a special neutron target and produces an intense (3·1014 cm-2s-1) flux of fast neutrons. The obtained neutron flux is directed to a hot thick target made of  235U compound. The vapor of radionuclides ionized, extracted from the target with the energy of 20-60 keV, and then separated into isotopes in the experimental zone for low energy experiments or further acceleration up to the energy 1-5 MeV/n.

The problems of source development are discussed and the way of its production is proposed.

Source of High-Energy Resonance -Rays Based on

Proton Storage Ring with Electron Cooling

V.A. Vostrikov, K.V. Gubin, V.A. Mashinin, V.V. Parkhomchuk, V.G. Shamovsky

INP SB RAS,Novosibirsk, Russia (gubin@inp.nsk.su)

Possibility of resonance -rays source with energy 9.172 MeV (nitrogen line) is discussed. -rays are produced by excited 14N nuclei obtained when nuclei of 13C captures the proton. Design of this source based on proton storage ring is proposed. The reaction takes place on thin inside 13C target. On the basis of proton beam heating compensation we propose to use electron cooling. The estimations of various source systems parameters are presented. It is shown this design is more effective than design based on direct accelerator.

Elastic-Plastic Crack Propagation under Irradiation and Cyclic Loads Caused by Thermoacoustic Instability of Heat-Carrier in Active Zone

V.D. Rusov *, V.I. Skalozubov **, V.A. Tarasov *

*Odessa National Polytechnical University, Odessa, Ukraine (vtarasov@ukr.net)

**Odessa Branch of State Scientific and Technical Centre on Nuclear and Radiating Safety

of Ecology Safety Ministry of Ukraine, Odessa, Ukraine

In [1] conditions at which occurrence thermoacoustic instability of heat-carrier (ТАI) in an active zone of some reactors is possible, in particular for water-water reactors (VVER installations of reactor) VVER-1000 they are determined. Occurrence TAI at a reactor normal exploitation (including transition periods) results to that thermal emission element’s (ТEE’s) are thus under influence of cyclic dynamic loadings which amplitude on tentative estimations makes 0,5 kg/mm2  2,0 kg/mm2, and frequency – 50 Hz  100 Hz. In metal uranium ТEE’s (both in the uranium core, and in a protective environment) thus there is an elastic - plastic development of cracks. In [2] the generalized diagram of radiation-thermal creep of the metals, showing dependence of creep mechanisms on thermodynamic parameters such, as temperature, loading and neutron flux density is submitted. In [3] it is shown, that in metal uranium at moderate temperatures and high neutron flux densities the radiation point defect concentrations considerably may exceed thermally equilibrium, also it is submitted the theoretical model of the established radiation creep within the framework of the mechanism of dislocation gliding and climbing, based on the conception of a dislocation as nonideal sink for point radiation defects. The similar phenomena it is necessary to expect and in a material of a protective environment which because of close contact to uranium also is exposed to intensive operation of division nucleus splinters of uranium. Computer modeling of radiation creep of metal uranium fuel has revealed its temperature nonlinearity [4]. These temperature nonlinearity have served the reason for search of nonlinear effects and modes (in particular, concentration waves of point defects and their influence on radiating creep) in open nonlinear stochastic system which the system metal uranium fuel under an irradiation [5] is. As mechanisms of radiation-thermal plastic deformation in top of a crack, are identical to mechanisms of radiation-thermal creep the changes of mechanisms of radiation-thermal creep received in [2-5] law on thermodynamic parameters may be the basis for development of the appropriate mechanisms of elastic - plastic development of cracks in metal uranium fuel.

In the given work for VVER installations of reactor with perspective metal uranium fuel are determined possible areas of thermodynamic parameters (temperature, loading and neutron flux densities) at which occurrence ТАI, causes elastic - plastic development of cracks with possible course of plastic deformation on mechanisms to the similar mechanisms offered for radiation-thermal creep.

References

1. Kovrizhkin L.Yu., Yemelyanenko E.Z., Skalozubov V.I. Predely bezopasnoi ekspluatatsii ustanovok v otnoshenii termoakusticheskoi neustoichivosti teplonositelya v aktivnoi zone. // Yadernaya i radiatsionnaya bezopasnost. – 1998. – V. 1, book 1. - P. 123-129.

2.  Tarasov V.A. Obobshchennaya diagramma polzuchesti otkrytoi fizicheskoi sistemy “metal (splav) + nagruzka + oblucheniye ”. // Materialovedeniye, No. 1(58), 2002, p. 12-13.

3. Tarasov V.A. Matematicheskoye modelirovaniye radiatsionnoi polzuchesti reaktornogo topliva na primere urana i yego splavov. // Materialovedeniye, No. 6(66), 2002, p. 11-17.

4. Tarasov V.A. Kompyuterne modeluvannya radiatsiinoi povzuchosti reaktornogo paliva. // UFZh, No. 10, 2000, p. 23-35.

5. Rusov V. D., Tarasov V.A., Usherenko S.M., Ovsyanko M.M. Modelirovaniye dissipativnykh struktur i voln kontsentratsii tochechnykh defektov v otkrytoi nelineinoi fizicheskoi sisteme “metal + nagruzka + oblucheniye”. // VANT, No. 4, 2001, series: FRP i RM (80), p. 3-8.

### Reactor Antineutrino Cross-Correlation Spectrometry

V.D. Rusov, V.A. Tarasov, D.A. Litvinov

Odessa National Polytechnical University, Odessa, Ukraine (siiis@te.net.ua)

In [1] importance of studying of reaction of return -disintegration on a proton is marked. It is caused by necessity of the decision of some the important problems as fundamental (structure of weak interactions, neutrino oscillations etc.), and applied value (the control of a nuclear reactor being the most powerful antineutrino source). In [2] it is shown, that for the neutrino control of reactor fuel isotope structure the measurement of reactor antineutrino power spectra is necessary. In the same place the basic opportunity of a correlation passive location antineutrino sources of division reaction with the help cross-correlation signal processing of two spatially carried antineutrino detectors (an estimation of a delay of useful signals on a maximum of cross-correlation function) for the first time is shown. In [3] it is emphasized, that as the length neutrino oscillations depends on its energy the neutrino energy measurement is necessary at their detecting, otherwise the average on energy transition probabilities are accessible to measurement only.

In the given work algorithms of a cross-correlation method of detecting and measurement of reactor antineutrino energy spectrums are submitted. The method allows to carry out measurement of antineutrino energy spectrums at their detecting. The developed method is actual, as it is necessary for the decision of some the important problems both fundamental, and applied character. In particular it may be harmoniously combined with the developed signal processing algorithms of cross-correlation system of passive location neutrino sources.

References

1. Fayans S.A. Radiatsionnye popravki i effekty otdachi v reaktsii obratnogo bega raspada antineitrino pri nizkikh energiyakh. // Yadernaya fizika. 1985.- V. 42, book 4. – P.929-940.

2. Rusov V.D., Vysotskii V.I., Zelentsova T.N. Neitrinnaya diagnostika vnutrireaktornykh protsessov i toplivosoderzhashchikh mass. // Yadernaya i radiatsionnaya bezopasnost, v.1,book 1,1998, p. 66-96.

3. Klapdor-Klaingrophaus G.V., Shtaudt A. Neuskoritelnaya fizika elementarnykh chastits. // M.: “Nauka. Fizmatlit”, 1997, 527 p.

Development of Measurement and Governing Systems Meant for Study with Hydrogen Isotope Mixtures

Yu.I. Vinogradov, A.V. Kuryakin, V.S. Aryutkin, S.V. Fil’chagin

Russian Federal Nuclear Center - All-Russian Scientific Research Institute of Experimental Physics (RFNC-VNIIEF), Sarov, Russia

This article gives a review of developments of equipment and systems of measurements and governing of facilities meant for studies conducted with hydrogen isotope mixtures. Requirements and approaches to development of such systems are analyzed.

The paper describes an automated system of control and governing of the complex of preparation of gas mixture of “TRITON” facility meant for carrying out of experimental researches of muonic catalysis of fusion nuclear reactions in the ternary mixtures of hydrogen isotopes H/D/T in the broad range of temperatures and pressures.

The automated system of control, governing and acquisition of data of “Prometey” universal stand meant to study the phenomena of accumulation and transmission of hydrogen isotopes by metals and structural materials is also described.

Synthesis, Study and Application of Aza- and Diazabicyclononanes as Complexing Agents and Preparations for Radiation Hygiene and Medicine

V. A. Dokichev*, R. I. Yusupov**, E.P. Magda**, Y.A. Kulinich**, A.G. Tsvetokhin**, Y.V. Tomilov***

*Institute of Organic Chemistry, Ufa Research Center of Russian Academy of Sciences ,

Ufa, Russia (dokichev@anrb.ru)

**Academician Zababakhin Russian Federal Nuclear Center – All-Russian Scientific-Research

Institute of Technical Physics, Snezhinsk, Russia

***N. D. Zelinslisky Institute of Organic Chemistry, Russian Academy of Sciences , Moscow, Russia

New fundamental methodological principles as well methods for the directed synthesis of skeleton aza- and diazabicyclononanes using diazo-compounds, norbornenes, 1-mono- and 1,3-dinitropropane derivatives have been developed.

The ways to create significant structural units and practically useful compounds have been proposed by means of simplifying the total chemical process owing to the unification of the stages of generating toxic and dangerous intermediate reagents and their transformation to 3-aza- and 3,7-diazabicyclo[3.3.1]nonanes. A convenient method for the one-stage synthesis of 1,5-dinitro-3,7-diazabicyclo[3.3.1]nonanes has been developed using the fourfold condensation of 1,3-dinitropropanes with formaldehyde and primary amines under Mannichs reaction conditions. It was found, that the nature of amine effects significantly on the direction of the reaction.

R1= Н, Рh, 4-BrC6H4, 2,4-Cl2C6H3; R2= H, Me, PhCH2, CH2CH2OH, cyclo-С3Н5

Chelate complexes of the given compounds with Cu, Pd and Rh chlorides and acetates have been produced. It was shown, that 3,7-diazabicyclo[3.3.1]nonane fragment of molecule behaves as bidentate ligand forming stabile complexes with transition metals.

Might selective extragents for hydrometallurgy and radiochemistry have been proposed using oligomer and polymer materials produced on the b of 3-aza- and 3,7-diazabicyclo[3.3.1]nonanes and their analogies.

In the series of 3-aza- and 3,7-diazabicyclo[3.3.1]nonanes three compounds have been revealed, which exceed antiarrhythmic drugs used at present in antiarrhythmic activity, toxicity and wide therapeutic effect.