- Materials for Nuclear

and Thermonuclear

Power Engineering

Uranium Containing Active Layers Behavior under Irradiation at

RFNC-VNIITF Pulse Fission Reactors

S.I. Abramenko, I.L. Svyatov, A.E. Shestakov, L.N. Lokhtin

Russian Federal Nuclear Center–Scientific Research Institute of Technical Physics,

Snezhinsk, Russia (btk@five.ch70.chel.su)

The report shows experimental results of study of uranium containing materials behavior under neutron irradiation at pulse fission reactors (PFR) IGRIK and YAGUAR. Subjects of study were layers of U3O8, chemically deposited on aluminum plates; uranium layers, protected by 0.5 m Al; and layers of radiation implanted uranium containing material, fabricated by ejection of material under irradiation of uranium oxide  rooks at PFR.

Techniques of scanning electronic microscopy, X-ray structural and micro X-ray spectral analysis were used to investigate specific features of layers behavior under different regimes of irradiation. Layers structure before and after irradiation was compared with the help of REM-100U scanning electronic microscope. Results of radiation stability of the layers are presented.

Atomic Vibrations and Polymorphism of Actinides

M.S. Blanter*, V.P. Glazkov*, L.N. Konovalov**, A.V. Laushkin**, V.K. Orlov**, D.D. Petrov**,

V.M. Sergeev**, V.A. Somenkov*

*RRZ «Kurchatov institute», Moscow, Russia (mike@hmngg.com)

** A.A.Bochvar Research Institute of Inorganic Materials, Moscow, Russia

Literature [1,2] and our experimental data on mean-square thermal vibration amplitudes for different actinide polymorphic modifications were analyzed. It was shown that the formation of many phases (α, β, γ, δ) as well as melting was found to be  concerned with the value and the temperature dependence in the Debye temperature. Such temperature dependence arises from the anharmonicity and/or may be non Debye phonon spectrum.

Similarly the  alloying-produced   polymorphism can be concerned with different changes of the temperature dependence in  mean-square thermal vibration amplitudes for different actinide polymorphic modifications. The proposed approach extends significantly the capabilities to investigate actinide metals and alloys by neutron diffraction methods. It  also poses the question as to the necessity of measuring of the Debye-Waller factors during polymorphic transition investigations.

References

1. Lawson A.C., Martinez B., Roberts J.A., Bennet B.I.and Richardson Jr J.W., Phil.Mag.B 80, 53 (2000)

2. Lawson A.C., Goldstone J.A., Cort B., Scheldon R.I.and Foltyn E.M., J.Alloys Comp.213-214, 426    (1994)

Basic Results of Forced Tests of

Core Structural Materials in Fast BN-600 Reactor

V. V. Chuev, A. N. Ogorodov, V.V. Maltsev

Rosenergoatom–Affiliated Beloyarskaya Nuclear Plant, Zarechny, Russia

(post@bnpp.x-atom.ru)

A review is presented of the results of regular post-reactor investigation of the laws governing change of operating working of corrosion-proof austenitic and ferritic-martensitic steels of extractable and non-extractable structures of BN-600 reactor. The most important factors limiting improvement of the working parameters of core of a high-power industrial reactor on fast neutrons are discussed.

In predicting form change of elements depending on irradiation parameters, a single methodological approach was used, and graphic and analytical dependences were developed. Analysis of form change of worked-out structures irradiated in the range of temperatures 350–700 оС to damaging dozes of about 100 dpa was carried out. The influence of the rate of damaging doze accumulation in the range of 10–7–10–6 dpa/s on radiation-induced swelling of austenitic steels with low radiation resistance was investigated.

The empirical dependence between the irradiation-induced swelling and deterioration of the mechanical properties of austenitic alloys in the absence of corrosive interaction with the coolant and uranium oxide/MOX fuel fission products was established.

The effect of the initial condition of structural materials of the fuel element jacket, as formed during metal smelting and manufacture of tubes, on their service properties has been determined. Proceeding from this, the principal lines of improving radiation resistance of structural materials able to support increased BN-600 core lifetime from the current maximum  burn-up of 10 % of h. a. to prospective burn-up of 11.2 % of h. a have been outlined. The burn-up increase to 12.2 and 18.3 % of h. a., as determined proceeding from the requirement of  optimal fuel residence time of the BN-600 commercial power unit to allow for the target load factor of about 80 %, will call for improving the available ferritic-martensitic steels and develop structural materials of a new generation.

Commercial Fast Reactor MOX Irradiation Validation

V. V. Chuev*, A. N. Ogorodov*, V. V. Maltsev*,

F. G. Reshetnikov**, N. B. Sokolov**, O. S. Korostin**

# *Rosenergoatom–Affiliated Beloyarskaya NPP, Zarechny, Russia (post@bnpp.x-atom.ru)

Tests were carried out of 28 pelletized and 9 vibropacked MOX sub-assemblies irradiated in the BN-600 reactor. All test sub-assemblies remained intact throughout all the handling operations, except for one that failed when it was dismantled in the hot cell. The test pelletized fuel sub-assemblies operated up to a peak damage dose of 79 dpa and burn-up of 11.8 % of h. a., while the vibropacked ones up to 77 dpa and 10.5 % of h. a. Peak linear rating of 48 kW/m and a fuel cladding temperature of 708°C were reached in case of the pelletized MOX sub-assemblies. The temperature parameters of the test MOX sub-assemblies were the same as those of the hottest standard uranium oxide sub-assemblies.

The post-irradiation examination of 4 test pelletized fuel sub-assemblies (~508 fuel pins) allowed the following to be found out:

- There is actually no change (below 0.4 % due to the radiation-induced swelling and creep) in the cross-sectional size of the hexagonal wrappers (originally 94.5·2.5 mm across the flats) manufactured from EP450 ferritic-martensitic steel.

- The change in diameter of the fuel pin cladding manufactured from EP172 and ChS68 cold-worked steels from the  original 6.6·0.4 mm is less than 5 or 6 %, i. e. within the limits specified by the criteria of the allowable distortion and within the limits of an increase in fuel pin diameter of the standard BN-600 sub-assemblies of the second modification core. With a damage dose of 76 dpa, the bundle averages of the actual diameter, ovalization and elongation are 3.9±0.5 %, 320±90 m and 1.4±0.2 %, respectively. With the obtained peak damage dose of 78 dpa and burn-up of 11.7 % of h. a., the operability of the cladding is not limited by the mechanical properties degradation.

- The data of the primary examination showed the operability of the pelletized MOX columns to be the same as the radiation behaviour of the standard uranium oxide fuel. The obtained spatial distribution of the fission product activity and cladding material activation is similar to the respective one with the standard fuel. The getter and the evaporable insert installed in some fuel pins did not affect the axial distribution of radioactive nuclides along the fissile part.

The examination of the test vibropacked fuel sub-assemblies showed the following:

- An increase in distance across the flats of the wrappers manufactured from steel composed of 0.05 % C, 12 % Cr, 2 % Ni and 1 % Mo is negligible (up to 0.6 to 0.8 % against the original 94.5·2.5 mm). They, as well as wrappers manufactured from EP450 steel, are able to remain serviceable at even higher operating parameters.

- The distortion parameters of the wrappers manufactured from steel composed of 0.08 % C, 16 % Cr, 11 % Ni, 3 % Mo and 1 % Ti are within the limits obtained for the same steel used in the standard BN-600 sub-assemblies of the first modification core. The lifetime of the wrapper accumulated a peak damage dose of 77 dpa and failed due to mechanical properties deterioration and brittle destruction when in the course of dismantling.

- With a peak damage dose of 77 dpa the bundle average of the distortion of the fuel pin cladding manufactured of the EP172 cold-worked steel equal to 5.2±1.0 % is higher than that obtained earlier during the commissioning of the Pervoural’sk cladding manufacturing facilities. When removing the bundle out of the wrapper the cladding of one of the pins failed in the area of maximum  swelling. The lifetime of the cladding manufactured of the initial EP172 cold-worked steel made by the VNITI prototype plant nearly ended by the criteria of the distortion and degradation of mechanical properties.

- The distribution of the slightly migrating Zr-95 and Ru-106 along the core was found out to be more non-uniform (as compared with the pelletized columns). This can be caused both by the original non-uniformity of the actual density distribution and by the specific radiation-induced restructuring of the fuel columns.

The completed in-reactor tests and post-irradiation examination of the test MOX sub-assemblies allow us to conclude that they remain serviceable at least up to 10 % of h. a., i. e. up to a standard burn-up of the second modification core. Tests continue of pelletized and vibropacked fuel of standard size and standard wrapper/cladding materials with a view to further extend the lifetime of the MOX fuel sub-assemblies.

Studies on Modification of Some First Wall Materials

Using 3-6.8 MeV He Ions

B. Constantinescu

Cyclotron Laboratory, Institute of Atomic Physics, Bucharest, Romania

A considerable effort has been directed towards the behavior of He in metals. He is known to have a low solubility in metals, much less than 1 appm; it strongly tends to participate into bubbles, causing swelling and He embrittlement. Surface damages with formation of blisters, exfoliation and sputtering are also produced. Because very few results are reported in the MeV region, we have started a systematic investigation concerning the fluence and energy dependence of blistering induced in some useful materials for the first wall (stainless steels, Ni, Cu, Mo). They have been irradiated with 3.0, 4.7 and 6.8 MeV He ions. The irradiation effects have been investigated by means of a TEMSCAN-200-CX electron microscope and two metallographic microscopes. Irradiation phenomena as sponge- and wave-like structures, submicronic cracks, multilayer flaking, micro-conglomerates, secondary blisters, microcraters were observed. Microstructural changes as helium bubbles on matrix and grain boundaries, on loops and on TiC precipitates were also observed. An interesting effect is the amorphous phase in the Ti-modified austenitic steel 12KH18N10T, phase formatted during irradiation with 6.8 MeV He+ ions up to a dose of crater occurrence (71018 ions/cm2), the temperature of specimens (100 m thick) being maintained during irradiation in the range 30-60C. The X-ray microanalysis shows the presence of the major alloy elements in the amorphous area, whereas in that embedding a microcrystallite it is to be noticed the Ni depletion and the presence of Si and Mo.

A potential explanation of the energy dependence of average blisters diameter d and blister critical dose could be stressed-induced model, because, in our cases (medium energy He ions), dtm, where t is the blister skin thickness. For our high energy data, a m=1.8 value is relatively convenient, except Mo, where m=1.5 is more suitable. Similarly, as concern the dependence of our experimental values for the critical fluence, we can assume a relationship of the form: ft2, therefore concluding that not only the resistance of the blister skin itself is important (that being proportional to t), but there are also other internal resistance factors playing an important role.

Recent Developments Concerning Void Swelling in PWR Austenitic Internals at Relatively Low Irradiation Temperatures

F. A. Garner

Pacific Northwest National Laboratory, Richland WA, USA (frank.garner@pnl.gov)

In the last 7-8 years there has been a growing awareness of the potential of void swelling in austenitic steels used as internal components to impact the operation and economics of Western pressurized water reactors. It was originally assumed that void swelling would not occur in the 300 series steels used in the baffle-former-barrel assemblies that surround the active core zone, primarily because of the lower dpa rates and lower temperatures in PWR internals compared to those of fast reactors. It is now known that lower dpa rates actually hasten the onset of swelling, which may be further accelerated by applied stresses and the higher gas (He, H) generation and retention rates characteristic of light water reactors.

Evidence is now accumulating to show that swelling is indeed occurring in PWR internals, with the potential to influence the prospects for license extension from 40 to 60 years. A summary of experimental evidence and industry/regulatory response will be presented.

Corrosion and Electrochemical Properties of EP - 450 Steel Exposed to High-Dose Irradiation in  BN - 600 Reactor

O.A. Golosov*, V. B. Semerikov*, T. L. Kuzina*, A.N. Ogorodov**, 
E. A. Kozmanov**, E. A. Medvedeva***

*Suse "SB RDIPE", Zarechny, Russia, (sfti@ uraltc.ru)

**BNPP, Zarechny, Russia

***FSUE "VNIIIM", Moscow, Russia

The ferrite martensite steel EP - 450 has been employed for many years in the cores of the fast reactors BN-600, BN-350 and BOR-60; and the items made of EP-450 have demonstrated high radiation resistance. However, when spent fuel element assemblies are extracted from the reactors and stored by the wet method, their case tubes made of EP-450 are strongly affected by corrosion in water of the decay pool. Accelerated corrosion and high percentage of corrosion products release into the water call for frequent regeneration of filters in the water chemical treatment system and cause increase in the radiation dose burden on personnel. While presenting an advanced grade of corrosion resistant steel, EP-450 may become a limiting factor for using it as a fuel cladding material in fast reactors due to its insufficient corrosion resistance, which the steel reveals in the post-operation period in decay pool water.

This paper presents the results of the investigation of  corrosion and  electrochemical properties of EP-450 case tubes in the water with pH = 7.0, after the tubes had been irradiated to a maximum damage dose of  75.6 dpa in the BN-600 reactor.

Tests  were carried out during 2000 hours with the intermediate exposures of 500 and 1000 hours. They revealed subsurface layers of lower corrosion resistance of steel to both uniform and pitting corrosion during operation in the reactor. The depth of penetration of corrosion of  both types is proportional to the damage dose  and  decreases with irradiation temperature. However, they have different kinetics, i.e. uniform corrosion depends linearly on time, and pitting corrosion depth is a parabolic function of time. Increased steel (irradiated in liquid nitrogen) liability to pitting corrosion is attributed to a dramatic decrease in the width of the area of stable passivity of steel, which is strongly dependent on neutron damage dose but is practically independent of operation temperature. At the same time, when the dose increases, the stationary potential the steel shifts towards positive values by approximately 140 mV,  and the potential of leaving the passive state deviates towards the negative values by more than 750 mV.

Irradiation-Assisted Intergranular Stress Corrosion

Cracking of Austenitic Stainless Steel in Steam-Water Mixture

A.L. Evseev, Yu.D. Goncharenko, V.A. Kazakov, V.K. Shamardin,

#### A.M. Pechyorin, G.V. Filyakin, Z.E. Ostrovsky

Federal State Unitary Enterprise «State Scientific Center of the Russian Federation

Research Institute of Atomic Reactors», Dimitrovgrad, Russia (bond@niiar.ru)

Susceptibility of austenitic stainless steels (ASS) to stress corrosion cracking (SCC), which is often of intergranular type (ISCC), is one of the important problems of their usage as in-vessel devices components of nuclear reactors in water-steam environment. The reasons of this fact arise from chromium depletion of boundaries and adjoining zones in the sensitive areas near welded joints as a result of precipitation of chromium carbides of Me23C6 and/or Me6C type. Neutron irradiation facilitates SCC propagation due to radiation-induced segregation and depletion processes at interphase surface.

The real in-vessel devices components, that have been operated for a long time, are the most informative material for SCC investigation under neutron irradiation. The external 0X18H10T ASS tube of the VK-50 reactor control assembly was chosen as the subject of examinations. The assembly was damaged in the welded joint area after 30 years of operation during scheduled replacement. In the place of fracture the tube was operated under alternative cooling with sub boiling water and water-steam mixture, and in the fracture area neutron flux was 3.01021 n/cm2 (E>0.1 MeV).

The following conclusions can be drawn according to the obtained results:

- fracture occurs mainly along the grain boundaries;

- titanium segregates on the grain boundaries, and Cr and Ni deplete them; the thickness of the segregation layer on the fracture surface is 1-1.5 µm;

- chlorine, sulfur, and copper, dangerous elements from the corrosion point of view, are available on the fracture surface. After ion etching of the examined surface the sulfur agglomerations disappear already at a depth of 3 µm.

The analysis of literature and obtained results enables us to assume the ASS IAISCC mechanism in the following way.

At the primary stage, when cracks, pores and other defects are present on the metal oxide film the rate of general corrosion process is relatively high. The generated slightly insoluble corrosion products gradually heal the defects of oxide film on the grains and decrease the area and number of anode sections. The effect of anodes gradually propagates to sensitive grain boundaries. This period is considered as incubation period. Then the process proceeds at a low rate suitable for the anode dissolution rate in passive state. The maximum rate is observed in the areas with minimum chromium concentration and as a result of it the corrosion has a nodular character. As the intergranular cracks propagate, the corrosion products obstruct the access of fresh portions of water/seam to the anode sections and removal of metal ions in the opposite direction. Moreover the access of cathode depolarizer (oxygen) is obstructed. As a result, the cathode process is transferred onto the walls of intergranular channels close to the surface [1,2]. Gradually the poisoning process of grain boundaries with sulfur and chloride released from coolant and from radioactive decay of MnS manganese sulphides becomes stronger. Copper precipitation begins on the surfaces of the generated intergranular cracks. Complex aggregations on the basis of sulfur and copper are being generated. They consist of iron, chromium, nickel, carbon and oxygen also. The effect of radiation-induced processes of grain boundaries depletion in chromium and nickel with their simultaneous enrichment in titanium, phosphorus and silicon increases. The chemical composition of boundary areas differs more and more from the matrix chemical composition. Under the effect of the residual tensile welded stresses the intergranular crack nuclei grow in width and length. At the final stage they reach the length of some tens of millimeters and form one main cross crack. The process of intergranular corrosion cracking results into the transverse fracture of the tube.

X –ray Investigation of Fine Structure of  Alloy Zr –2.5% Nb after In –pile 
Irradiation at ~ 80 °C

V. E. Kalachikov, V. A. Tsygvintsev, N. V. Gloushkova

Suse " SB RDIPE", Zarechny, Russia. (sfti@uraltc.ru).

The channel (factory # C-24) of the control and protection system made of the alloy Zr–2.5 %Nb had operated in cell # 32-25 of Unit IV at the Leningradskaya NPP for 17.4 years. After that the material of the channel was investigated by the X–ray method. A calculation neutron fluence was ~ 3×1022 th.n./cm2 (~1.2 dpa) and an irradiation temperature was ~80 °C during the alloy operation.

As a result, a shift, widening and changing intensity of X-ray lines of a-Zr matrix were observed. A value and a sign of the observed changes in the fine structure depend on the type (prismatic, basal or pyramid) of diffraction planes. A maximum increase of inter-plane distances and a half-width of the X-ray lines was noticed for the prismatic - type planes (h00) and (hk0). A decrease of the half–width and the inter- plane distance was observed in the basal - type planes (00L). The changes of the fine structure are attributed to the oriented preferential accumulation of radiation defects of interstitial type (small dislocation loops) in the prismatic planes and vacancy defects (small clusters and double or triple vacancies) in the basal planes.

Changing of Physical and Chemical States of Iron Atoms in Zirconium Alloys

Oxide Films During Neutron Irradiation

V.P. Filippov *, A.B. Bateev *, R.N. Pugachev *,  G.P. Kobyljansky **

*Moscow Engineering - Physics Institute (State University), Moscow, Russia (filippov@d108.mephi.ru)

** Research Institute of Atomic Reactors, Dimitrovgrad, Russia

The oxide films of zirconium alloys (Zr-0.76%Fe-1.6%Sn-0.95%Nb and Zr-0.76%Fe-1.6%Sn.) oxidized in autoclave and in reactor irradiation conditions were investigated by Mössbauer spectroscopy method.

The corrosion tests of flat specimens placed in tight ampoules from the stainless steel, filled by distilled water, were carried out in a reactor during 37, 80 and 112 effective days(fluency 3·1020 n/cm2, E>0,5 MeV). Similar specimens were tested in laboratory conditions during 40, 80 and 120 day in similar ampoules and identical thermodynamic conditions (350°C, 16.8 МPа).

The comparative analysis of corrosion curves has shown, that the thickness of oxide films obtained at reactor irradiation are almost three times more than thickness of films obtained at corrosion in an autoclave. It testifies that reactor irradiation essentially accelerates the corrosion process of both alloys especially 3 component alloy.

The Mössbauer researches have shown that  the spectra of both alloys oxide films, obtained in autoclave, have the lines of solid solutions of iron ions Fen+, Fen+, Fen+ in Zero and for some samples – the lines of metallic precipitates of α-Fe. The spectra of both alloy oxide films, obtained in reactor, have the lines of solid solutions of iron ions Fe2+, Fe3+, Fe4+ in ZrO2 and for some samples – the lines. of compound α-Fe2O3. The concentrations of iron atoms in different chemical states in oxide films are determined.

Comparison of kinetic curves of corrosion with results of Mössbauer researches has shown, that α-Fe metal precipitates are formed only in films of the samples subjected corrosion in autoclave but not in all oxide films. So α-Fe is formed in oxide films when alloys have good corrosion resistance. In reactor irradiation conditions when alloys show low corrosion resistance, the α-Fe is not revealed in oxide films, and formation of α-Fe2O3 compound is marked.  As to solid solution of ions Fe4+ in ZrO2, it was seen, that in oxides of alloys with good corrosion resistance the concentration of these ions is more greater. In cases with bad corrosion resistance of alloys the concentrations of ions Fe4+ in ZrO2  is decreased. Thus its possible to assert about correlation between concentration of ions Fe4+ and corrosion resistance of zirconium alloys. Obtained data  confirm the conception about positive influence of metal precipitates formed in oxide film and ions  Fe4+ on corrosion behavior of zirconium alloys.

Variation of Isothermal Kinetics of -Transformation of Unalloyed

Plutonium over Different Times of Samples Self-Irradiation

# A.M. Lyasota, A.V. Troshev, S.I. Abramenko, V.N. Kordyukov, Yu.N. Zouev, B.V.. Litvinov,

# E.P. Magda

# Russian Federal Nuclear Center – All-Russia Research Institute of Technical Physics,

# Snezhinsk, Russia (btk@five.ch70.chel.su)

The paper presents the results of investigation of the kinetics of -transformation of unalloyed plutonium under isothermal conditions over different times of samples self-irradiation. Variations in the kinetics of phase transformation vs the time of self-irradiation are discussed.

References

- Plutonii. Reference-book. Edited by O. Vik, Moscow, Atomizdat, 1973.

- Plutonium 1975 and other Actinides. Proceedings of the Conference in Baden-Baden September 10-13 1975.

- G. Christian. Teoriya prevrashchenii v metallakh i splavakh. MIR Publishers, 1978.

Radiation Phenomena in Austenitic Steels Irradiated in

SM, BOR-60, VVER-1000 Reactors at 280-400 oC

V.S. Neustroev*, Z.E. Ostrovsky, V.K. Shamardin

RIAR, Dimitrovgrad, Russia (neustroev@vinf.ru)

Recently study on microstructure evolution of austenitic steels at low irradiation temperatures has become one of the most acute issues that determines, to a greater degree, swelling and embrittlement of such steels at these temperatures. Different components of fast, pressurized and boiling reactors are made of the Fe-18Cr-10Ni-Ti steel types. Sometimes they operate at close irradiation condition parameters. Comparative study of these components allows for estimation of the effect of irradiation conditions on steel microstructure and properties.

For the last few years at SSC RF RIAR several components made of the Fe-18Cr-10Ni-Ti steel types have been chosen for the investigations. They operated in different reactors under irradiation conditions close to those of the VVER in-vessel facilities. They include: blanket assembly wrappers and tail-end adapter after their long-term operation (more than 22 years) in the BOR-60 reactor, guiding channel of the VVER-1000 peripheral fuel assembly, the SM material science assembly block. The damage dose and temperature range of the products under study changed from 1.5 up to 81 dpa and from 285 up to about 400 ºC.

The results and analysis of the performed investigations of these components allowed the comparison of microstructure, precipitated phases, radiation swelling and mechanical properties of these steels as a function of dose accumulation rate, temperature and damage dose.

The most obvious conclusions are as follows:

There are some differences in the microstructure of the investigated steel specimens irradiated in different reactors.

A long-term operation of the blanket fuel assemblies at low irradiation temperatures (about 320ºC) in BOR-60 leads to material swelling dependent on the dose accumulation rate. The investigations on radiation swelling of all above components made of the Fe-18Cr-10Ni-Ti steel types allowed the identification of the temperature threshold (300-310ºC) for voids formation.

The Fe-18Cr-10Ni-Ti steel specimens cut from the VVER-1000 components and irradiated in fast reactors showed strong hardening and reduction of relative elongation. This correlates well with the hardening values calculated on the basis of microstructure changes of irradiated steels.

Peculiar Features of Structure and Behavior Changes in Some Zirconium

Materials at Damage Doses up to 50 dpa

G.P. Kobylyansky*, A.E. Novoselov*, Z.E. Ostrovsky*, V.K. Shamardin*,

A.V. Obukhov*, V.N. Shishov** and M.M. Peregud**

*FSUE “SSC RF RIAR”, Dimitrovgrad, Russia

**FSUE VNIINM, Moscow, Russia (gpk@vinf.ru)

The irradiation-induced damage of zirconium materials subjected to neutron irradiation up to dose of 50 dpa was investigated. The dose value was caused by a change of irradiation time or fast neutron flux. The specimens of unalloyed zirconium and Zr-1%Nb, Zr-2.5%Nb and Zr-1%Nb-1.3%Sn-0.4%Fe alloys were irradiated in the BOR-60 reactor dismountable devices over the temperature range 320-420 oC. The device design allowed the removal of specimens during the reactor shut-down (2-3 times per year) and the measurement of dimensional changes in the hot cells with their subsequent return to the reactor core. The dose dependence of the irradiation growth strain increases sharply in zirconium and Zr-Nb alloy specimens irradiated at the temperature of 350 oC at doses above 10 dpa. As for Zr-1%Nb-1.3%Sn-0.4%Fe  alloy specimens it increases at doses of 37 dpa. With increasing the irradiation temperature to 420oC, a sharp accelerated irradiation growth of the Zr-1%Nb alloy begins shifting up to about 30 dpa. As for the Zr-1%Nb-1.3%Sn-0.4%Fe alloy no change of the irradiation growth rate was observed up to the dose of 55 dpa. The onset of increased irradiation growth stage in alloys correlates with the occurrence of c-component dislocation loops. This moment coincides with a loss of coherence of fine-dispersed precipitates. The post-irradiation annealing experiments demonstrated that a delay in loop formations leads to displacement of the “break-away” beginning in the dose dependence of the irradiation growth in the direction of high doses.

The high dose irradiation results in the change of the element phase composition: hcp matrix of solid solution is depleted with niobium; a gradient of element concentrations was noted along the radius of (ZrNb)2Fe particles occurring in the Zr-1%Nb-1.3%Sn-0.4%Fe alloy structure. In investigating precipitations of about 30-60 nm in size, it was established that irradiation of Zr-1%Nb and Zr-1%Nb-1,3%Sn-0,4%Fe alloys results in increase in the average size of particles and decrease in their concentration. In the irradiated samples of Zr-1%Nb alloy the contents of atoms Nb in precipitations of a phase -Nb decreases in comparison with the not irradiated material and at high dozes reaches about 50 %.

The work is executed with the support of RFFI (project # 02-02-1717b).

### Microstructure Changes in EI-847 Steel Exposed to Long-Term

Irradiation at 300 -390 °C  in Fast Neutron Reactor

I.A. Portnykh V. L. Panchenko, E. N. Shcherbakov , A. V. Kozlov

Suse "SB RDIPE", Zarechny,  Russia (sfti@uraltc.ru)

The austenite steel EI-847 was investigated after its long-term operation as a fuel element cladding in the pulse fast neutron reactor IBR -2. Test samples taken from the areas, which  had been exposed to neutron irradiation at temperatures of 300 to 390 °C. A maximum damage dose in the cladding material reached 13 dpa at an irradiation temperature of 350 °C during 16 years of operation, including 4.8 years of its performance at the reactor power of 22.5 kW/kg U.

The material was investigated by the methods of transmission electron microscopy and micro X-ray structural analysis. They revealed pores in the material irradiated at 350 °C. The diagram of pore distribution against sizes was plotted for the statistical sampling of 1000 pores. It was shown to be a unimodal distribution of the pores with a mean size of about 4 nm. The concentration of pores was ~ 2.5×1021 m-3. As a rule, they are related to those dislocations or dislocation loops, which concentration is higher than that of radiation pores.

There were no pores in the steel irradiated at the bottom of reactor core at 300 °C (damage dose was 6 dpa), though there was a large number of radiation defects of the dislocation loop type, which formed fragments of a small-cell dislocation structure.

There were also numerous dislocation loops in the microstructure of the material irradiated at the top of the core at 390 °C to the damage dose of 6 dpa, though their concentration and size were smaller as compared to those of the material irradiated at the bottom. There were no radiation pores in the material irradiated at the top of the core.

Influence of Radiation Swelling on Thermal Expansion Coefficient 
of Steel ChS-68

E.N.  Shcherbakov, A. V. Kozlov, I. A. Portnykh, O. I. Asiptsov, V. L. Panchenko, L. A. Skryabin

Suse "Sbrdipe", Zarechny, Russia (sfti@uraltc.ru)

Fuel element claddings made of the austenite stainless steel ChS-68 were exposed to long -term irradiation in the fast neutron reactor BN-600 and then a thermal expansion coefficient (TEC) of the steel was measured. The areas, where the irradiation temperature was from 430 °C to 590 °C, were investigated. A maximum damage dose in the cladding material reached 70 dpa, which corresponded to the temperature of 530 °C.

Cladding samples were tested for linear change parameters of the irradiated material within the temperatures of 200 to 700°C. The difference in TEC values was found to be very small for the material taken from different areas of the core and heated from 200 to 530 °C.

The TEC decreased substantially within 530 to 700 °C, which was, probably, due to structure transformations. In repeated heating, the run of a TEC curve in the high temperature region was changing.

The dilatometry measurements with the isothermal exposures at 420 °C and 660 °C were carried out to study the radiation-induced defect annealing. A length of samples was decreasing at the temperatures higher than the operation temperature during isothermal exposures, the decrease being from 0.01 to 0.11 % in relative units. An initial length of the samples was also decreasing during a linear heating to the temperatures higher than the operation temperature. It was found that a shrinkage value was inversely proportional to the operation temperature of the fuel element cladding material.

The methods of the transmission electron microscopy were used for a statistical processing of radiation defect assembly. It was shown that the decrease of the sample length was related to the annealing of radiation defects and vacancy pores evolution, in particular.

# Influence of Structure-Phase State Zr-Nb- Containing Alloys

on Irradiation-Induced Growth

V.N. Shishov*, M.M. Peregud*,  A.V. Nikulina*,  G.P. Kobyliansky**, A.E. Novoselov**,

Z.E. Ostrovsky**

* FSUE A.A. Bochvar Research Institute of Inorganic Materials, Moscow Russia

** FSUE RIAR, Dimitrovgrad, Russia

On account of the search of optimal composition and structure-phase state of Zr alloys much attention is paid to upgrade E 110  (Zr-1%Nb) and E 635 (Zr-1%Nb-0.35%Fe-1.2%Sn) alloys that proved well in terms of irradiation-induced creep and growth, high strength characteristics, corrosion. The difference between the alloy properties is determined by their states related to their compositions.

The structure phase state of the Zr- Nb and Zr-Nb-Fe-Sn systems has been studied after heat treatment in the α- and  α + β regions and the influence was investigated that is produced by this state on the irradiation-induced growth (IIG) during BOR-60 irradiation at T =315-350 oC. A substantial difference has been revealed in the deformation effected by IIG of those alloys, it is less for Zr-Nb-Fe-Sn  alloy in dissimilar structure-phase states. The incubation period of the accelerated growth stage is determined by the α-matrix composition, the phase state and the initial dislocation structure. Neutron irradiation leads to a redistribution of alloying elements between the matrix and the precipitates, to changes in the α-solid solution composition and affect accumulation and mobility of irradiation defects, anisotropy and formation of vacancy c-component dislocation loops. The appearance of c- loops usually correlates with an axial direction acceleration of the IIG of tubes conforming to their texture.

The basic regularities of the phase transformation have been established: a) β-Nb precipitates in Zr-Nb alloys alter their composition to reduce the Nb content from  85-90% to ~ 50%, precipitates likely enriched in Nb are formed , b) β-Zr precipitates are subject to irradiation –stimulated decomposition, c) Laves phase precipitates change the composition (the content of Fe decreases) and the crystal structure, HCP to BCC (β-Nb), d) (Zr, Nb)2Fe precipitates having the FCC lattice  retain the composition and crystal structure,   e) no amorphization of secondary phase precipitates is observable under the given conditions of irradiation (T = 315 - 350 oC).

Based  on the  dpa  the results were compared pertaining to Zr-alloy IIG deformation vs fluence in various reactors at different energies of fast neutrons. The presented  graphs enable comparison between the results of numerous experiments and prediction of Zr-material behaviour in long-term operation and at high burn-up in commercial reactors.

# Damage of Beryllium under High-Dose Neutron Irradiation

V.P. Chakina, V.A. Kazakova, R.R. Meldera, G.A. Shimanskya, S.V. Belozerova,D.N. Suslova,

R.N. Latypova, Z.Ye. Ostrovskya, Yu.D. Goncharenkoa, D.V. Pevtsova, I.B. Kupriyanovb

aState Scientific Center of Russian Federation, Research Institute of Atomic Reactors,

Dimitrovgrad, 433510, Russia

bState Unitary Enterprise, All-Russian Research Institute of Inorganic Materials,

Moscow 123060, Russia

Beryllium is supposed to be used in structural components of the future fusion reactor as plasma facing material, blanket material and neutron multiplier. Evaluation of degradation degree of beryllium properties under the influence of the neutron irradiation in the nuclear reactor is an important problem for feasibility of the fusion reactor components. The paper describes the research results of the irradiation effect in the SM and BOR-60 reactors at 70-4500C in the neutron fluence range (0.5-16)·1022 cm-2 (E>0.1 MeV) for physical-mechanical properties and microstructure of several Russian beryllium grades (TE-400, TE-56, TE-30, TIP, DIP) produced by the HE and HIP technologies.

The Mechanisms of Uranium Metal Fuel Radiation Creep  and

Its Temperature Nonlinearity

V.D. Rusov, V.A. Tarasov

Odessa National Polytechnical University, Odessa, Ukraine (vtarasov@ukr.net)

In [1] it is shown, that in uranium metal at moderate temperatures and high neutron flux densities the radiation point defect concentrations considerably may exceed thermally equilibrium, also it is submitted the theoretical model of the established radiation creep within the framework of the mechanism of dislocation gliding and climbing, based on the conception of a dislocation as a non-ideal sink for point radiation defects. Are developed the “dynamics” method of mathematical simulation of gliding and climbing of flexible dislocation interacting to obstacles of a various type (spherical centre of extension, dislocation prismatic loop and their spatially random distributions), and a computer program complex for mathematical simulation of radiation creep and radiation creep rate estimations by a method of Monte Carlo. Computer simulation of uranium metal fuel radiation creep has revealed its temperature nonlinearity [2]. These temperature nonlinearities have served the reason for search of nonlinear effects and modes in open nonlinear stochastic system which the system uranium metal fuel under an irradiation [3] is.

The generalized diagrams of radiation-thermal creep for not fissionable (constructional) metals and non-fissionable (fuel) metals are submitted. The regions of various radiation creep theoretical models are qualitatively determined. It is shown, that the nonlinearities of curve thermal dependence of the radiation creep established rate are caused by the features of used radiation creep theoretical model based on the concept conception of a dislocation as a non-ideal sink for point radiation defects and the features of point radiation defects generation in divisional metals.

References

- Tarasov V.A.. Matematicheskoye modelirovaniue radiatsionnoi polzuchesti reaktornogo topliva na primere urana i yego splavov. // VANT, No. 2, 2001, series: FRP i RM (79), p. 23-30.

- Tarasov V.A.  Kompyuternoye modeluvannya radiatsiinoi povzuchosti reaktornogo paliva. // AFZh, No. 10, 2000, p. 23-35.

- Rusov V.D., Tarasov V.A., Usherenko S.M., Ovsyanko M.M. Modelirovaniye dissipativnykh struktur i voln kontsentratsii tochechnykh defektov v otkrytoi nelineinoi fizicheskoi sisteme “metal + nagruzka + oblucheniye”. // VANT, No. 4, 2001, series: FRP i RM (80), p. 3-8.

Modification of Plutonium Dioxide Properties under Exposure to Radiation

A.V. Troshev, S.I. Abramenko, V.N. Kordyukov, A.M. Lyasota

Russian Federal Nuclear Center–Scientific Research Institute of Technical Physics,

Snezhinsk, Russia  (btk@five.ch70.chel.su)

The report shows experimental results of Pu239O2 electric resistance variations under protracted influence of radiation investigations. Obtained dependence of electric resistance on doze is compared with published results of investigations of Pu238O2 crystal lattice parameters under influence of radiation with sufficiently higher intensity. Comparison shows that despite significant difference in intensity of radiation influence notable modification of PuO2 physical properties takes place under dozes t=2010–5.

Investigation of Distribution of Erbium in Uranium – Erbium Oxide Fuel of RBMK by X–ray Analysis

V. A. Tsygvintsev*, A. N. Timokhin*, V. R. Kuznetsov*, V. Ivanov**

*Suse "SB RDIPE", Zarechny, Russia, (sfti@uraltc.ru)

**FSUE "RDIPE", Moscow, Russia.

One of the means, increasing safety and reliability of  RBMK Units operation, is adding erbium as a burn-up absorber to the RBMK fuel. A concentration and distribution of erbium in a fuel pellet is an important characteristics of the fuel element fabricated for U–Er fuel usage.

X–ray structure analysis as a ND technique allows to calculate an erbium concentration and determine a manner of erbium distribution in the pellet.

It is shown that the X-ray structure analysis is applicable for a calculation of an erbium content in the fuel. The dependence of a lattice parameter of the fuel on the erbium content is provided. The approximation function of X–ray reflections and the extrapolation function are matched in the precision method of the determination of a lattice parameter in crystalline materials with a cubic structure.

The methodology to calculate an erbium concentration, a volumetric part of areas with a different erbium content is presented. The methodology was used to investigate samples in seven lots of fuel with a different U-235 enrichment and a different mass portion of erbium.

The condition of the crystal structure of uranium–erbium oxide fuel was investigated after the fuel exposure in the IVV–2M reactor , where the calculation fuel burn up was from 0.67 to 10 MW × day/kgU.

Comparison of Irradiation Conditions for Fusion Materials in IFMIF and ESS

P.V. Vladimirov*, A.  Möslang
Forschungszentrum Karlsruhe, Karlsruhe, Germany 
* (Pavel.Vladimirov@imf.fzk.de)

Investigation of the fusion materials behaviour under irradiation conditions close to those expected for future fusion reactor is one of the most critical issue for the design of demonstration power reactor DEMO and fusion reactor prototype ITER. Among other facilities the International Fusion Materials Irradiation Facility (IFMIF) was selected and approved to be suitable for proper simulation of fusion irradiation [1-3]. The design of the European Spallation Source raised a discussion of suitability of this neutron source for fusion materials irradiation. The present study is devoted to comparison of the irradiation conditions for both facilities with respect to their ability to simulate DEMO reactor environment.

Geometry models of these facilities were designed to perform Monte Carlo simulation of neutron spectra at different parts of the installations. Using calculated neutron and primary knocked-on atom spectra various damage characteristics, namely, damage and gaseous atom production rates as well as spallation rates were calculated and compared. In particular it was shown that He/dpa ratio for reflector position (at least in Fe based alloys) is between 5-6, that is about a factor of two lower than expected for DEMO fusion reactor. While the H/dpa ratio at the same position is about 33-36, which is a factor of about 1.5 below DEMO reactor specific ratios.

On the basis of the work the ESS target position initially proposed for allocation of fusion materials irradiation rigs was ruled out as having too hard neutron spectra producing substantial amount of spallation products and resulting in changing phase composition and material properties deterioration of irradiated structural materials. It was also confirmed that although ESS reflector position could be used for obtaining some preliminary results (in case the ESS will be constructed several years earlier than IFMF), the IFMIF facility is necessary for proper simulation of the fusion irradiation conditions and comprehensive investigation of fusion relevant materials behaviour under irradiation.

References

- Möslang, K. Ehrlich, T.E. Shanon, M.J. Rennich, R.A. Jameson, T. Kondo, H. Katsuta, H. Maekawa, M. Martone, V. Teplyakov;  Nuclear Fusion 40(3Y) 619-627 (2000)

- Yu. Lizunov, A. Möslang, A. Ryazanov, P. Vladimirov, ICFRM-10, 14-19- Oct. 2001, Baden-Baden, Germany, submitted to J. Nucl. Mater.

- Möslang, P. Vladimirov, ISFNT-6, 7-12 Apr., 2002, San Diego, submitted to Fusion Eng. and Design

New Structural Material for Fusion Reactor Based on

Ferritic Stainless Steel-Clad V-Ti-Cr Alloy

А.V. Vatulin1, G.P. Vedernikov1, А.V. Vertkov2, S.N. Votinov1, I.N. Gubkin1,

V.A. Evtikhin2, I.Е. Lyublinskiy2, D.V. Sokolovskiy1, А.K. Shikov1

1A.A. Bochvar Research Institute of Inorganic Materials, Moscow, Russia

2FSUE “Red Star”, Moscow, Russia

As a low neutron activated structure material the vanadium alloys of V-Ti-Cr system are more promising materials for lithium energetic reactors (tokamaks). This is due to favorable combination of their physical and mechanical properties, good compatibility with liquid lithium, high resistance to irradiation-inducted damage. V-4Ti-4Cr and V-10Ti-5Cr alloys have good resistance to swelling during irradiation and have not susceptibility to irradiation embrittlement above 400 C. Mechanical properties and particular elongation of V-10Ti-5Cr alloy are more stable, then V-4Ti-4Cr. Integration and survey of different characteristic data base allow to conclude, that maximum operation temperature of V-10Ti-5Cr alloy could be 750-800 C in fusion system. However general disadvantage of vanadium based alloys is contamination with interstitial impurities, such as oxygen, carbon, nitrogen, and hydrogen, which cause degradation of mechanical properties and workability. This disadvantage has substantially limited their application as structure materials. To avoid attack of the surroundings the vanadium alloys have been suggested to clad by ferritic stainless steel. Sandwich consisting of V-4Ti-4Cr alloy and ferritic stainless steel plates has been hot and cold deformed. Good adhesion these materials has been achieved. Thus, opportunity of making new low neutron activated, hot temperature strength, corrosion resistant and irradiation resistant structure material for fusion application has been shown.

Study of the Effect of Tritium and Reactor Irradiation on Properties of Materials in the First Wall of Fusion Reactors

Yu.N. Zouev*, B.N. Goshchitskii**, V.V. Sagaradze**

*Russian Federal Nuclear Center – Institute of Technical Physics, Snezhinsk, Russian Federation (y.n.zouev@vniitf.ru)

**Institute of Metal Physics, Ural Branch RAS, Ekaterinburg, Russian Federation

As is known, one of the most important aspects ensuring reliability, radiation and ecological safety of installations in nuclear and thermonuclear power engineering is the effect of tritium, which is accumulated during operation (nuclear and salt liquid reactors) and/or is used as the fuel (fusion reactors), on materials and its penetration to the environment. This problem especially applies to selection of materials and development of the manufacturing technique of such energy-intensive elements of fusion reactors (FR) as the diverter and the first wall.

The present report covers some schedule of work intended to obtain experimental evidence on the effect of tritium, radiogenic helium and the reactor irradiation on the structure and properties of materials and bimetallic elements in the first wall and the diverter of magnetic- confinement fusion reactors. The objects of study will be samples of radiation-resistant steels and a steel/bronze (SS316L/CuA115) bimetallic element of the first wall, which will be supplied by J.F. Stubbins and Celia Elliott (Illinois University, USA).

The fulfillment of the Project work will provide the following information:

- parameters of the penetration process and accumulation of heavy hydrogen isotopes in constructional materials of fusion reactors;

- concentration and localization of hydrogen in the structure of the samples;

- effect of hydrogen on mechanical properties of constructional materials exposed to long-term extension stresses;

- interaction of tritium atoms with radiation-induced defects in the materials studied;

- effect of the surface condition on the interaction between tritium and the materials.

The anticipated results will be very significant from the scientific and practical viewpoints for a reasonable choice of materials and designs of thermonuclear installations ensuring a minimum leakage of tritium to workrooms and the environment.

The experimental basis and the team of researchers, which were formed during fulfillment of the ISTC Project No. 019-94, provide good grounds for implementation of the planned work. The team of researchers not only strives to advance the success achieved under the Project No. 019-94, but also looks for consolidation of the cooperation between the researchers at the Russian Federation Ministry of Power Energy, the Russian Academy of Sciences and the international scientific community.

The penetration processes and the yield kinetics of tritium will be studied using hydrogen permeability and thermal desorption methods. The concentration will be measured by the liquid scintillation spectroscopy method. The microautoradiography method will be used to determine the distribution of hydrogen isotopes in the structure of the materials. The interaction of hydrogen isotopes and radiogenic helium with defects of different origins (dislocations, grain and subgrain boundaries, interfaces, etc.) will be deduced from the variation of mechanical properties, electric resistance, and the residual concentration of tritium. In addition, the methods of X-ray diffraction analysis, positron annihilation, electron microscopy, and nuclear microanalysis will be used at their utmost.

The condition of the interface between the layers in bimetallic structures will be studied on special samples prepared of bimetallic plates. The samples will be tested before and after loading with tritium and radiogenic helium.

The adverse effect of tritium and neutron irradiation on mechanical properties of FR materials exposed to long-term extension stresses presents a special interest from the viewpoint of their service characteristics. Standard short-term tests cannot reveal the real effect of hydrogen on embrittlement of materials under continuous loads (which occur most frequently in service), while long-term tests allow determining how plastic properties of constructional materials are affected even by a small concentration of gas impurities.

The goals of the proposed study fully comply with the ISTC objectives, since it provides an opportunity of alternative peaceful activities for specialists in nuclear weapons, who will be able to use their experience and knowledge for solution of worldwide problems concerned with generation of thermonuclear power, environmental protection, and safety of fusion reactors. The study will facilitate the integration of Russian scientists into the world scientific community.

Effects of Actual Aging (Self-Irradiation) of Delta-Stabilized Pu Alloy with Gallium on Microstructure, Mechanical Properties, Phase Transformation Macrokinetics in Weak Shock-Waves

Е.А. Коzlov*, L. F. Тimofeyeva**, V.I. Таrzhanov*, I.V. Теlichko*, D.М. Gorbachev*, D.G. Pankratov*, А.N. Grachev*, А.V. Vorobyev*, V.G. Shmygin*, V.S. Sakov*, V.I. Cherkasov*, Yu.N.Zouev*, N.N. Маrkelov*, А.V. Zimin*, I.L .Svyatov*, N.А. Tsepilov*, D.V. Таskin*, I.V. Podgornova*
* Russian Federal Nuclear Center – Academician E.I. Zababakhin Research Institute of Technical Physics, Snezhinsk, Russia (kozlov@gdd.ch70.chel.su)
**А.А. Bochvar Research Institute of Inorganic Materials, Moscow

Peculiarities of dynamic behavior and properties of newly cast delta-stabilized plutonium alloys with gallium have been already investigated in the weak shock -waves [1-3].
    Accumulation of the radiogenic helium in the crystal lattice of alloy, because of -decay of plutonium nuclei, at the room temperature during the prolonged real-time self-irradiation, can effect not only on the mechanical properties of the alloy at its quasi-static and high-rate deformations in the initial δ−phase state, but also on the kinetics of the δ−α'−phase transition in stress waves.
    The set-up of explosive experiments and the first investigation results of the high-rate elasto-visco-plastic deformation in the region of the initial –phase state as well as macrokinetics of δ−α'−phase transition in weak shock waves of the actual 16-years aged -alloy are presented. Taking into account [4-8], the features of the microstructural changes of the prolonged self-irradiated alloys, which are responsible to the kinetics change of the δ−α'−phase transformation, are discussed.

References

- Kamegai M., J. Appl. Phys. 46, # 4, 1618 (1975).

- Коzlov Е.А., Timofeyeva  L.F., Мysyrya А.К., Macrokinetic Features of  Phase Transformation in  -Plutonium at Threshold Pulse Loading, Russ. J. Chem. Phys. 14, #1, 62 (1995).

- Коzlov Е.А., Timofeyeva  L.F., Dendritic Liquation in Delta–Phase Plutonium Alloys and the Peculiarities of Phase Transitions Proceeding in Weak and Strong Shock Waves, in  Abstracts of Russian Conference “Nuclear Technics Materials”, devoted to Academician A.A.Bochvar’s Centenary, VNIINM, 2002, p.113.

- Dooley D., Martinez B, Olson D., Olivas D., Ronquillo R., Rising T., Diffusion of Helium in Plutonium Alloys, in Conference Transactions Plutonium Futures – the Science,  eds. K.K.S.Pillay and  K.C.Kin,  American Institute of Physics,  Santa Fe, New Mexico, USA, 2000, p.428.

- Murphy S.M., Radiation-Induced Changes in Microstructure, in 13th Int. Symp. ASTM STP 995, eds.  F.A.Garner, N.H.Packan and A.S.Kumar, American Society for Testing and Materials, Philadelphia, USA, 1987, p.330.

- Freibert F., Martinez B, Baiardo J.P., Olivas J., Ronquillo R., Effects of Self-Irradiated Damage on Physical Properties of Stabilized Pu Alloys, in Conference Transactions Plutonium Futures – the Science, eds. K.K.S.Pillay and  K.C.Kin,  American Institute of Physics,  Santa Fe, New Mexico, USA, 2000, p.431.

- Thomas Zocco, Mark Wall, Adam Schwartz, Bill Wolfer, Paul Roussel, Mary Esther Lucero and Michael Ramos, Transmission Electron Microscopy to Observe Helium Bubbles in Plutonium, in Nuclear Materials Research and Technology, 4th quarter 2001, p. 1.

- Robert Hixson, John Vorthman and Benjamin Lopez, Shock – Wave Research on Plutonium Yields New Information Concerning Dynamic Material Properties, in Nuclear Materials Research and Technology, 4th quarter 2001, p.4-5

### Effects of Prolonged Self-Irradiation on Shear Strength of Unalloyed Pu

# under Explosive Loading

Е.А. Коzlov, V.I. Таrzhanov, I.V. Теlichko, D.М. Gorbachev, D.G. Pankratov,  А.N. Grachev,

А.V. Vorobyev, V.G. Shmygin, V.S. Sakov, V.I. Cherkasov, Yu.N. Zouev, N.N. Маrkelov,

А.V. Zimin, I.L. Svyatov, N.А. Tsepilov, D.V. Таskin, I.V. Podgornova 
Russian Federal Nuclear Center – Academician E.I. Zababakhin Research Institute of

Technical Physics, Snezhinsk, Russia (kozlov@gdd.ch70.chel.su)

Accumulation of the radiogenic helium in the unalloyed Pu crystal lattice and defects, which were induced by prolonged self-irradiation of the material during its storage, can result in lowering of its mechanical properties, particularly in shear strength. In addition to [1-2], the set-up of explosive experiments and the first investigation results with the samples of the prolonged actual aged unalloyed Pu are presented. The effect of self-irradiation during the 1 – 15 years on the kinetics of elastic precursor relaxation and change of Pu shear strength in the weak shock- waves were experimentally estimated.

References

- Коzlov Е.А., Тimofeyeva L.F., Коvalenko G.V., Peculiarities of - Phase Transformation of Unalloyed Pu in Weak and Srong Shock-Waves, in Abstracts of Russian Conference “Nuclear Technics Materials ”, devoted to Academician А.А.Bochvar’s Centuries, VNIINM, 2002, p.20.

- Gorbunov S.I., Selesnev А.G., Crystal Structure and Ageing of Metallic Pu-238, in Abstracts of Russian Conference “ Nuclear Technics Materials ”, devoted to Academician А.А.Bochvar’s Centuries, VNIINM, 2002, p.111

Features of Microstructural Changes in Unalloyed Coarse-Grained Anisotropic Depleted Uranium after Shock-Wave Loading in the Range of 20-50 GPa at Loading Impulse Duration of 0.5-1.3 s

E.A. Kozlov*, V.G. Vil'danov*, A.O. Borshevsky*, Yu. N. Zouev**, I.V. Podgornova** 
Russian Federal Nuclear Center – Academician E.I. Zababakhin Research Institute of Technical Physics, Snezhinsk, Russia:* Shock Wave Physics Department (kozlov@gdd.ch70.chel.su),
** Material Science Department (zuyev@vniitf.ru)

The set-up of five shock-wave experiments and the first results of microstructural investigations of the loaded and recovered samples are presented.

The high anisotropy and inhomogeneity of intragranular plastic deformation of blocks, differently oriented to the shock wave front, have been revealed. The completeness of this effect in stress waves of different amplitude хх  =20…50 GPa and duration =0.5…1.3 s is analyzed. The observed changes in microstructure and microhardness of coarse-grained depleted uranium are discussed. A feasibility of proceeding the polymorphous ---transformations in unalloyed uranium after its shock compression during the unloading is analyzed with allowance made for [1,2].

References

1. Коzlov Е.А.,   Litvinov B.V.,   Каbin I.G.,   Аbakshin Е.V.,   Оrlov V.К.,   Teplinskaya V.М., Кislyakov S.S., Кruglov А.А., Phase Composition and Microhardness of the Balls of Unalloyed Uranium and Two its  Alloys after  Loading  in  Spherical  Stress Waves, in  Int. Conf.  Shock   Waves   in   Condensed   Matter, July 18 - 22, 1994, St.-Petersburg, Russia, 1994, Abst. 18-6, p.31.

2. Orlov V.K., Teplinskaya V.M., Formation of polygonizated structures at polymorphous transformations in uranium, in Jubilee Collection devoted to A. A. Bochvar's centenary, Proceedings of VNIINM, Moscow, 2002, Vol. 2, p.117.

Structural Changes in Reactor Alloy of the Hastelloy  Type during Long-Time High-Temperature Exposure

I.I. Kositsyna1, V.V. Sagaradze1, V.G. Subbotin2, Yu.N. Zouev2

1 Institute of Metal Physics, Ural Division RAS, Ekaterinburg, Russian Federation (vsagaradze@imp.uran.ru)

2 All-Russia Institute of Technical Physics – Russian Federal Nuclear Center, Snezhinsk,

Russian Federation

A CrNi89MoNb nickel alloy of the Hastelloy type, which contained (mass %) ~0.05 C, 8 Cr, 11 Mo, and 1.4 Nb, was proposed as a promising constructional material for salt liquid nuclear reactors [1]. This alloy has a relatively large corrosion and embrittlement resistance at high temperatures. The goal of the present study was to determine structural changes, which take place in the alloy of the Hastelloy type during long-time exposure at 650-750 C. If secondary phases precipitate at boundaries during long-time aging, one may predict proneness of the alloy to intercrystalline corrosion and corrosion stress cracking. The alloy was studied in two structural states after high-temperature rolling and after quenching from 1200 C. In the former case, the deformed alloy had a large density of dislocations and high hardness (HRB 110). In the latter case, the alloy contained coarser grains with a small density of dislocations, which was characteristic of the quenched state. The alloy hardness was HRB 82. From the Table it is seen that hardness changed little when the deformed alloy was annealed at 550-650 C. Hardness decreased to HRB 94.5 during annealing at 750 C. This was due to recrystallization. Hardness of the quenched alloy remained unchanged when it was held at 550 and 750 C. Hardness increased from HRB 82 to HRB 89 when the alloy was held for 1000 hours at 650 C. Aging took place at this temperature. Niobium carbides could only be identified among strengthening phases in the electron diffraction patterns. Some carbides were located as sparse chains at grain boundaries. This could have some adverse effect on corrosion and corrosion-mechanical resistance of the alloy. Dispersed carbides or intermetallics were not detected at boundaries of fine grains in the hot-deformed alloy. Therefore, one may think that the hot-deformed state of the Hastelloy surpasses its quenched state regarding resistance to intercrystalline corrosion and corrosion-mechanical cracking.

Table

Hardness HRB of the Hastelloy vs. Exposure Time at 550-750 C

| Aging temperature, ºС | Aging time, h |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | 0 | 20 | 50 | 100 | 500 | 1000 |
| 550* | 110 | - | - | 110 | 110 | 109.5 |
| 650 | 110 | 110 | 109 | 109 | 109.7 | 108.5 |
| 750 | 110 | 102 | 101.0 | 98 | 94.5 | 94.5 |
| 550** | 82 | - | - | 82 | 82 | 83 |
| 650 | 82 | 84.5 | 88 | 87 | 89 | 89 |
| 750 | 82 | 83 | 83.5 | 82 | 83.5 | 82 |

*Initial alloy after hot deformation. **Alloy after water quenching from 1200 C (30 min).

This study was supported by the International Scientific and Technical Center (Project No. 1606).

References

- Novikov V.N., Ignatiev V.V., Fedulov V.I., Cherednikov V.N. Salt-Liquid Nuclear Power Installation: Perspectives and Problems. Moscow, Energoatomizdat, 1990, 192 p.