- Effect of Irradiation on Changes in Microstructure and Properties of Metals

and Alloys

NDT Measurements of Irradiation-Induced Void Swelling in EBR-II Materials

I. I. Balachov*, F.A. Garner**, I. Isobe***, H. T. Tang****
*SRI International, Menlo Park, California, USA (iouri.balachov@sri.com)
** Pacific Northwest National Laboratory, Richland, Washington, USA

***Nuclear Fuel Industries, Inc., Osaka, Japan

****Electric Power Research Institute, Palo Alto, California, USA

Irradiation-induced void swelling has been postulated as a potential degradation mechanism for core internals of commercial Pressurized Water Reactors (PWR).  While evidence of void swelling in PWR materials has not been directly obtained, similar materials from fast breeder reactors show swelling under PWR relevant temperatures and dpa.  US DOE and EPRI sponsor an effort to develop an in-situ void swelling inspection technique based on non-destructive examination of core internals for the US Nuclear Industry.

The principle of in-situ detection of void swelling [1] is based on the previous work performed in the US and Russia where almost linear correlation between swelling and measurable material parameters (electrical resistivity and Young’s modulus) have been observed.  Important limitation in practical application is that the inspected component (such as a baffle plate) may be accessed only from one side. This limitation eliminates several attractive techniques (for example, resonance ultrasonic technique) from the list of candidates for field use. Initial screening of the candidate techniques included (1) eddy current, (2) Barkhausen noise, (3) electropotential or four probe resistivity measurements, (4) guided waves, and (5) conventional ultrasonic technique.  Proof of concept was performed on a set of surrogate materials with elastic and electrical properties changed by power metallurgy technology and cold work.  The following three techniques have been downselected for testing on irradiated materials (1) ultrasonic, (2) eddy current and (3) electropotential technique [1].  These three techniques have been tested on irradiated materials with known amount of swelling (determined by immersion density measurements in the previous work).  The set of materials included 26 disks punched from a hexagonal sheath of the EBR-II reflector. Nominal dimensions of disks are 19 mm in diameter and 1 mm thick.  Temperature range is 378 to 414 C, dose varied from 4 to 35 dpa, which covers a range of void swelling from 0.128 to 2.808%.  Most of the specimens (21 out of 23) have been irradiated at temperatures 378 to 390C.  The exposure is represented relatively uniformly between 4 and 35 dpa.  Distribution in swelling was shifted towards lower swelling in order to estimate sensitivity threshold of the void swelling sensors.

Most encouraging results have been obtained by using UT technique.  First, a reliable correlation between sensor signal and void swelling was observed.  Second, the sensitivity of the method defined in experiments with EBR-II disks seems to be sufficient for practical applications.  Success with UT technique indicates that dominant changes in elastic properties of EBR-II disks have been induced by formation of voids, which is the expected situation for SS304 material exposed to PWR conditions.

Results of EC and EP method are more difficult to interpret.  Both methods produced extremely repeatable results, which indicates to adequate design of sensors and experimental conditions.  At the same time, measured electric properties of EBR-II disks seem to have no correlation with void swelling.  The major questions are: «What kind of inclusions change the electrical properties of EBR-II disks in addition to voids?» and  «Are these inclusions in EBR-II disks caused by operating conditions of the EBR-II reactor relevant to PWR operating conditions?»  The answers to this questions have to be obtained yet from examination of microstructure and microchemistry of EBR-II materials.

References

- Balachov I., Garner F., Isobe Y., In-Situ NDT Measurements of Irradiation-Induced Swelling in PWR Core Internal Component, Phase 1: Testing of Unirradiated Surrogate Materials, EPRI, Palo Alto, CA: 2001. 1006583

Peculiarities of Martensitic Transformation Kinetics
in a Monocrystal of Cu-Al-Ni Alloy Being Irradiated
by Reactor Neutrons in Low-Temperature Helium Loop

S.P. Belyaev, R.F. Konopleva, I.V. Nazarkin, V.A. Chekanov
Petersburg Nuclear Physics Institute, Russian Academy of Sciences, Gatchina, Russia (spb@smel.math.spbu.ru)

The temperature kinetics of the martensitic transformation in a monocrystal of the Cu-3,4%Al-5%Ni alloy have been investigated with the use of technique of in-reactor measurements of resistivity in the process of irradiation in the low-temperature helium loop of the WWR-M nuclear reactor at the temperatures of 120-350 К. In the experiments, the isothermal irradiation has been alternated with thermal cycles through the martensitic transformation temperature interval. So the temperature dependencies of the resistivity have been obtained in various irradiation periods. The isothermal irradiation temperatures have been selected so that they should correspond to various structural state of the material (austenite, martensite or two-phase).

It has been established that in the area of small fast neutron fluences (<6·1018 cm-2), the resistivity of the Cu-Al-Ni alloy rises linearly with the fluence growth. The resistivity growth rate significantly depends upon the structural state of the material: in the austenite state it is more than by five times as less as compared with the martensite state. Upon irradiation in the two-phase or martensite state, there is a considerable (by 25-30 К) growth of temperatures of the reverse transformation “martensiteaustenite”. Such growth is observed once only in the process of the first heating being implemented directly after the isothermal irradiation and proportional to the integral neutron dose. At subsequent thermal cycles, the martensite transition occurs at lesser temperatures, and the hysteresis temperature dependence of the resistivity shifts towards lower temperatures with the growth of fluence. So the radiation effect leads to a stable decrease of critical transformation temperature and to a single (unstable)  growth of the reverse transformation temperatures. The first of these effects is caused by the disordering of the crystal lattice at the reactor irradiation, similar to the situation, which is also observed in TiNi-based alloys. The single effect is perhaps connected with the violation of coherence of the interphase and interdomain boundaries in the course of irradiation. The boundary mobility, in this case, decreases and an additional thermodynamic stimulus is required for the transformation development. Special experiments indirectly prove this supposition.

Dose Dependences of Mechanical Properties and Composition of Titanium Alloy Surface During Si+ and Ar+ Ion Irradiation

P.V. Bykov, F.Z. Gil’mutdinov, A.A. Kolotov, V.Ya. Bayankin

Physical-Technical Institute, Ural Branch of RAS, Russia (less@fti.udm.ru)

A comparative study of fatigue strength, microhardness, the compositions of the surface layers and microstructures of ruptures of the Ti-2,2Al-0,6Mn alloy samples irradiated with Ar+ и Si+ ions (Е = 40 KeV, j = 10 А/cm2) has been conducted depending on the radiation dose (D=1015, 1016, 21016, 31016, 51016 ion/cm2).

Fatigue strength tests were performed by means of the console bending method at maximal alternate bending stress over the section (9 x 2 mm2) max.24 - 45 kgf/mm2 and at frequency of 22,5 Hz. The composition of the surface layers was studied with the use of the mass-spectrometer MC-7101M. Microhardness was measured by means of a conventional technique with the use of PMT-3 with loads of 20 and 100 g. Rupture microstructures were studied by means of the scanning electron microscope SEM-200. Additionally, the X-ray structure analysis and microstructure investigations were conducted.

The microhardness of the samples exposed to silicon and argon ions increases by 10-30% as compared to the initial value. A maximum increase of the microhardness (the applied load on the indentor is 20 g) is attained either after the silicon or argon ion irradiation with the dose 1016 ion/cm2.

The fatigue tests show that the samples irradiated with silicon and argon (with the dose 1016 – 3x1016 ion/cm2) have endured a much larger number of cycles before they rupture than the initial samples at the same stresses over the section. The maximal increase of the fatigue strength takes place at the 1016 ion/cm2 dose just as the maximal increase of the microhardness does. When exposed to the Ar+ ions with the dose 1015 ion/cm2 the sample ruptures prematurely.

The analysis of the chemical composition of the implanted samples after the rupture shows a significant enrichment of the surface layers with aluminium and manganese atoms. Besides, the transformation of the concentration profile of the interstitial silicon atoms can be observed. At the rupture itself, large amounts of aluminium, manganese and silicon and only traces of titanium can be found. It may point to the precipitation of the alloying components along the rapture boundary and the silicon atom migration to the surface during the fatigue tests.

The results of the X-ray structure analysis do not reveal any changes in the structure-phase states in the bulks of the samples irradiated with Si+ and Ar+ ions as compared to the initial samples. Consequently, the fatigue strength increase of the irradiated samples is due to the changes of the structure and composition of the surface layers caused by the ion implantation.

Atomic Mechanisms of the Microcrack Propagation in Titanium

During Ion Irradiation

A.Yu. Drozdov, M.A. Baranov, V.Ya. Bayankin

Physical-technical Institute, Ural Branch of RAS, Izhevsk, Russia (less@fti.udm.ru)

The process of the microcrack propagation in the model crystallite with the close-packed hexagonal lattice at the uniaxial tension has been studied after the implantation of inert gas ions with the use of the molecular-dynamic simulation; titanium is used as an example. The attempt has been made to clarify the influence of ion implantation on the microcrack propagation in model metals with the hcp-lattice. The comparative study of the microcrack propagation in metals with different types of lattice at the uniaxial tension has been conducted.

The computer-based experiment is performed with the use of the MMDYN programme, which allows to solve the set of many-particle equations of Newton by means of numerical methods. The potentials of pairwise interaction are used to describe the interatomic interactions; these potentials have been calculated based on the model Heine-Abarenkov-Animalu pseudopotential. Energy removal from the system is realized by introducing viscous forces. The initial atomic configuration of the crystallite was a three-dimensional film with the thickness of 20 atomic layers. The surface (001) was free; on the surfaces (100) and (010), the cyclic boundary conditions were superimposed. A system consisting of 4000 atoms was calculated in each computer experiment. The crack was simulated by the removal of a certain number of atoms from two neighboring planes at a depth of 10 atomic layers.

In the area of the mouth of a crack a heat peak was simulated for the period of 800010000; the thermodynamic parameters of the system, i.e., temperature T and potential energy U, were stabilized near a certain value. After the crystallite had reached a stable state over the range of the times under study, the uniaxial tension along [100] direction was performed. The relative strain was  = 5%, 10% и 15%.

The analysis of the atomic structure of the crystallite shows that the microcrack does not recover after the ion irradiation; it transforms into a micropore. As this takes place, the propagation of the region enriched with defects deep into the crystallite does not occur. The transition from the microcrack to the micropore occurs in accordance with the vacancy mechanism. The propagation of the microcrack deep into the crystallite is not observed at the 5% and 10% uniaxial tension of the irradiated crystallite. The widening of the microcrack can be observed; migrations of separate atoms are possible only along the boundaries of the microcrack. The atomic rearrangements caused by the ion irradiation lead to the strength increase of the crystallite. The peculiarities of microcrack propagation in metals with different types of lattice (bcc, fcc, hcp) have been studied. It has been shown that the propagation of the microcrack in pure metals has a viscous character.

The work has been financed by the Russian Foundation for Basic Research (project № 02-0216670).

Disordering of LaMnO3-Based  Compounds by  Fast Neutrons

S. F. Dubinin*, V. E. Arkhipov*, V. D. Parkhomenko*, S. G. Teploukhov*,

Yu. G. Chukalkin*, Ya. M. Mukovskii**

*Institute of Metal Physics, Ekaterinburg, Russia

**Moscow Institute of Steels and Alloys, Moscow, Russia

The perovskite –type compound La0.85Sr0.15MnO3 was exposed to fast neutrons (F = 21019cm-2, Tirr   = 340K) and then the structure of this monocrystal was studied by the thermal neutron diffraction  method at 300C.  Areas of small size were found in the crystal lattice of the oxide affected by fast neutrons; the structure and the size of the areas being related to the peculiarities of branching of the atomic cascade collisions  in the compounds  of  this  class.  For the first  time  it  was found ,  that  anti - site  defects

( ~15% of diamagnetic cations transferred into the sites of manganese sublattices) had been formed in a  crystal of the oxide exposed to fast neutrons. It was shown by the example of the La0.8Ba0.2MnO3  exposed to F = 31020 cm-2 at  Tirr   = 340K that, a defect pattern  of the perovskite crystal does not  considerably  depend on the element of the dopant.

The Influence of Displacement Rate on Void Swelling in model Fe-Cr-Ni Alloys Irradiated with Either Neutrons or Nickel Ions

F. A. Garner*, T. Okita**, T. Sato** and N. Sekimura**

*Pacific Northwest National Laboratory, Richland WA, USA (frank.garner@pnl.gov)

**Department of Quantum Engineering and Systems Science, University of Tokyo, Tokyo, Japan

The results of two companion experiments exploring the effect of dpa rate and composition on void swelling will be presented. These experiments used simple Fe-Cr-Ni ternary alloys irradiated over a wide range of dpa rates to determine the influence of dpa rate on both microstructural evolution and macroscopic swelling.

The first experiment involved irradiation of three simple alloys (Fe-15Cr-16Ni, Fe-15Cr-16Ni-0.25Ti, and Fe-15Cr-16Ni-0.25Ti-0.04 C) in FFTF at ~400ºC over a range of dpa rates, 8.9 x 10-9 to 1.7 x 10-6 dpa/sec. The results show very clearly that the effect of increasing dpa rate is to extend the transient regime of swelling for the two carbon-free alloys, but without any change in the steady-state swelling rate of ~1%/dpa. The microstructural origin of this process arises primarily from the sensitivity of Frank loop formation, interaction and unfaulting to dpa rate. The primary requirement to attain steady-state swelling is the resultant formation of a mobile dislocation network. The addition of carbon suppresses the flux sensitivity, however, and the microstructural origins of this response are currently under investigation.

The second experiment involves nickel ion irradiation of Fe-15Cr-16Ni only, but at three temperatures, 300, 400, 500ºC, and three dpa rates between 1 x 10-4 and 1 x10-3 dpa/sec.

At these higher dpa rates the transient regime is longer than that observed in the neutron irradiation experiment, and increases further as the dpa rate increases.  Once again the most important results are the sensitivity of Frank loop behavior to dpa rate, and the decrease of swelling at every tested temperature as the dpa rate increases.

The implications of these findings on the interpretation of other experiments conducted on neutron-irradiated commercial alloys will be discussed. In general these latter studies also show that swelling decreases as the dpa rate increases, primarily due to an extension of the duration of the transient regime.

Radiation-Enhanced Amorphism: Comparison of Materials and Influence Techniques

N.N. Gerasimenko

Moscow Institute of Electronic Engineering, Zelenograd, Russia (rmta@miee.ru)

In this work an attempt is made of analytic comparative review of experimental results and theoretical conceptions about amorphism in semiconducting materials (monatomic and multicomponent) and metals. The following problems are considered:

- Is it possible to get amorphism during irradiation by:

  - fast-moving electrons;

  - protons;

  - neutrons.

- The difference in carbon and silicon amorphism processes.

- The existing models of amorphism for ion bombardment of silicon. Accumulation of defects critical concentration: spatial separation of internodal and vacancy defects (either by means of different mobility or due to dividing agents – boundary surfaces, force fields, getters and so on).

- Statements about amorphism processes in metals. Does critical concentration of defects exist?

- Amorphous state and glass. Formation processes: irradiation, fast cooling of melts, laser treatment.

- Phase transition monocrystal – amorphous state and vice-versa. Consideration from the synergetic position. Could one expect self-organization under such transitions?

Offered report does not have one-valued answers on majority formulated problems and its aim is drawing attention on the set of known experimental results and approaches to their description. An attempt is made to compare known approaches of description between semiconducting and metal materials.

- Phase Transformations in Ion Irradiated NiTi Thin Films

- T. LaGrange*, R. Schäublin**, D. S. Grummon***, C. Abromeit**** and R. Gotthardt*

*Swiss Federal Institute of Technology Lausanne (EPFL), Lausanne, Switzerland (rolf.gotthardt@epfl.ch)

**CRPP-EPFL Fusion Technology-Materials, Villigen, Switzerland

***Michigan State University, E.Lansing, Michigan, United States of America

****Hahn-Meitner Institut, Berlin, Germany

SMA thin films have an anomalously high strain energy storage output and large transformational strains which have stimulated a current interest for their use as active elements that require large force and displacement outputs.  We have studied a novel processing technique using ion irradiation to develop a thin film micro- actuator.  The main experimental approach has been to irradiate one side of martensitic TiNi thin film that has been pre-deformed in tension.  With sufficient irradiation dose, the martensitic transformation can be suppressed in the beam-damaged layer, whose thickness can be on the order of half the film’s thickness.  During heating to austenite phase, only the un-modified martensite structure can recover and contract to its original length, and the differential strain between the damaged and unmodified layers causes the film to bend out of plane.  The partial energy stored in the damaged layer by the prior heating transformation is available to deform the martensite on subsequent cooling, which thus causes an uncurling of the film and thereby creates a two-way motion during thermal cycling.

Grummon et al [4] noted the dependence of the TiNi film’s thermomechanical properties (after a 5 MeV Ni2+ ion irradiation) with the irradiation fluence, and they also observed an unusual and unpredictable motion in the samples irradiated with a low fluence (1 x1013 ions/cm2).  In a similar study by LaGrange et al [3], they observed monoclinic and BCC nanocrystallites surrounded by an amorphous matrix in this damaged layer with an irradiation temperature of 30C.  Barbu et al. have performed ion irradiations in electron stopping regimes and concluded that martensite has undergone transformation to amorphous and austenite phase in the tracks[3]. We have explored the electron stopping effects using 350 MeV Au ions.  Amorphous and crystalline phase transformations were observed within the tracks and due to the electron excitations by HRTEM, and in addition, BCC TiNi phase nanocrystalline particles were observed, which were surrounded by an amorphous matrix within the track.  The deformed 1x1012 ion/cm2 diffraction spectrum and microstructure was very different as compared to the undeformed 1x1012 ion/cm2.  Thus, there was an effect of the predeformation on irradiation effects, which has not been previously observed.  Whether this crystalline structure has undergone a reserve martensitic phase transformation due to irradiation itself or due to the stress surrounding crystal imposed by newly nucleated amorphous material, is still unclear.

- References

- Grummon D.S. and Gotthardt R., Acta. Mater. 48 (2000), p. 635-46

- LaGrange, T., R. Schaublin, D.S. Gummon, and R. Gotthardt, J. Physique IV, (2002)

- Barbu, A. et al, Nucl. Instr. And Meth. in Phys. Res. B, 145 (1998) 354-72

# Radiation-Induced Enhancement of Critical Current Density

in YBa2Cu3O7-x Superconductors

E.M. Ibragimova*, M.A. Kirk** 
* Institute of Nuclear Physics, Tashkent, Uzbekistan (eibragim@suninp.tashkent.su)
** Argonne National Laboratory, Argonne, Illinois

The application of high temperature superconductor materials in industrial energy is hindered because of an exponential decrease of the critical current density with increasing temperature up to 77 K and the magnetic field up to 2 Tesla (working field of motors). This paper reviews successful attempts for significant improvement of magnetization and transport critical current densities (Jc and Ic) of YBa2Cu3O7-x (YBCO) single crystals, ceramics, films and tapes by means of irradiation-induced modification of structure. The irradiation with moderate doses of fast neutrons and charged particles was found to result in such an effect at magnetic fields of 1-5 T because of generation of flux pinning centers. The temperature dependence of Jc became weaker, but the initial Tc and the conductivity decreased because of carrier localization at the irradiation induced defects. The irradiation also caused the decrease of initial anisotropy of structure and Jc. Most researchers ascribe the strongest pinners to linear and columnar defects, and weaker ones to point defects. Most data are related to improvement of Jc in bulk – intra-granular magnetization critical current, which is much higher than the real inter-granular transport critical current Ic limited by weak contacts. However, the effects of granularity and anisotropy were also mentioned. The problem is to form the particular texture ensuring enhancement of the inter-granular contacts by minimizing both off-plane and in-plane grain misorientation during synthesis. Much less studied is the effect of irradiation on the inter-granular critical current Ic and conductivity. Several authors found some increase of current carrying ability of YBCO ceramics, crystals and films after X-ray, gamma-ray, oxygen plasma, electron and proton irradiations. It would be attractive for industry application because of no induced radioactivity. Magnetization in strong fields at 10 K proved to depend on granularity, and that at 77 K - on the texture degree of YBCO ceramics sintered in gamma-field. The transport Ic at 77 K in self-field increased with the texture degree growth. Highly ionizing 18 MeV proton irradiation at 300 K caused anisotropic stress and texturing of YBCO ceramics, both depending on the dose rate, and the conductivity along the exposed surface increased.

The second generation of HTSC tapes are based of less anisotropic coated YBCO thin film which has much higher Jc ~1 MA/cm2 at 77 K at several Tesla, though its disadvantage is improper texture. The latest experiment of the authors on 9 MeV proton irradiation of the films at elevated temperatures (150-300 C) demonstrated a noticeable increase of the transport Ic at 77 K and a significant increase of the normal state conductivity, while the initial value of Tc decreased just by 2-3 K.

Monitoring an Insulator-Metal Transition in Icosahedral AlPdRe by

Neutron Irradiation

A. E. Karkin *, B. N. Goshchitskii*, V. I. Voronin*, S. J. Poon**, V. Srinivas***, and O. Rapp***
*Institute for Metal Physics, Ural Branch of Russian Academy of Sciences, Ekaterinburg, Russia (karkin@uraltc.ru) 
** Department of Physics, University of Virginia, Charlottesville, USA

***Solid State Physics, IMIT, Kungliga Tekniska Hogskolan 229, 164 40 Kista, Sweden

Icosahedral i-AlPdRe samples can be made with low-temperature resistivity  and resistance ratios R = (4.2 K)/(295 K) varying over wide ranges of values. Already early studies of high- samples with R ~ 100 suggested insulating properties. It is only recently, however, that more direct evidence of a metal-insulator transition (MIT) in i-AlPdRe has been found. The magnetoresistance (MR) at large R was found [1] to obey variable-range hopping (VRH) theory for electron transport in insulators. From the metallic side, MIT is suggested both from analyses of the metallic MR at small R [2] and from a scaling approach to the conductivity (T) of metallic samples at temperatures T > 400 mK. These different investigations all give estimates that an MIT occurs in the region R ~ 20–30. However, the most perspicuous results on an MIT are normally expected for low-temperature (T), but such results for i-AlPdRe have remained controversial. Descriptions in terms of VRH theories have given widely different results. A major difficulty is the saturation of (T) observed at very low temperatures ( 20 mK in high-R samples) and incompatible with VRH. Recent results indicate that a finite (0 K) is a property of the icosahedral phase, which may suggest that at large R and low T two channels contribute to (T), e.g., VRH and quantum tunneling. We therefore started with an insulating sample and irradiated it by fast neutrons at Tirr = (33010) K with a series of doses D up to 7*1018 cm-2. Samples had nominal composition Al70.5Pd21Re8.5 were prepared by melting in an arc furnace followed by annealing at 940 and 600–650 °C. Details of these preparation techniques and structural characterizations have been given previously [2]. Using a single sample focuses on the effect of varying intrinsic disorder. For increasing D the icosahedral phase was preserved, peak x-ray intensities (volume of the coherent icosahedral phase) and R decreased, and an insulator-metal transition was traversed. The MR vs R across the MIT was found to be independent of sample history.

References

1. V. Srinivas, M. Rodmar, S.J. Poon, and O. Rapp, Phys. Rev. B 63, 172202 (2001).

2. M. Rodmar, M. Ahlgren, D. Oberschmidt, C. Gignoux, J. Delahaye, C. Berger, S.J. Poon, and O. Rapp, Phys. Rev. B 61, 3936 (2000).

Martensitic Transformations and Shape Memory Effect in TiNi Alloys in

the Process of Neutron Irradiation in Low-Temperature Helium Loop

R.F. Konopleva*, S.P. Belyaev**, A.E. Volkov**, I.V. Nazarkin*, V.A. Chekanov*
*Petersburg Nuclear Physics Institute, Russian Academy of Sciences, Gatchina, Russia (krf@pnpi.spb.ru)
**Research Institute of Mathematics & Mechanics, St. Petersburg State University, St. Petersburg, Russia

The investigations of martensitic transformations, shape memory effect and peculiarities of kinetics of the radiation damage of equiatomic TiNi alloys in the process of irradiation in the low-temperature helium loop of the WWR-M nuclear reactor at the temperatures of 120-350 К have been performed. The method of resistivity measurement has been used, which is sensitive both in respects to radiation defects of the crystal lattice, and in respect to martensitic phase transitions in crystals. The shape memory effect has been investigated by means of a spring sample loaded by an elastic element. The deformation has been measured by a variable-induction pickup.

It has been established that the resistivity of the TiNi alloy grows proportional to the fast neutron fluence. The resistivity growth rate in the martensitic state is by 3-4 times as much as in the austenitic state. Such behaviour has been caused by different contribution of radiation defects into the resistivity and by fragmentation of the polydomain martensite structure under irradiation. The critical temperatures of martensite transitions in TiNi alloys decrease with the fluence growth according to the following law: Tph=d[exp(-Ф/Ф0)-1] where Tph is the increment of the temperature corresponding to the structural transformation; Ф is the fluence; d and Ф0  are constants. The temperature hysteresis of the transformation rises. These regularities can be detected under irradiation both in the martensitic state and in the austenitic state. A short-term temperature rise for the samples irradiated by the fluence of 71018 cm-2, up to temperature of 450 К leads to the return of the resistivity and the temperature kinetics of martensitic transformations. The activation energy of the property return has been determined.

It is assumed that the change of transformation kinetics under irradiation and subsequent annealing are connected with the change of the degree of long-range order S of the ordered solid solution. The evolution of the long-range order degree is proposed to describe by the equation: dS/dt=a(S-S)I+b(S0-S)exp(-U/kT) where t is the time, T is the temperature, S and S0 is the long-range order parameter at the fluence Ф and at Ф=0 respectively, I is the neutron flux, U is the activation energy of the radiation defect annealing, a and b are constants.

The  Percolation Model of  Radiation Porosity Influence on Austenite 
Steel Strength

A. V. Kozlov, I. A. Portnykh, S. V. Bryushkova, E. A. Kinev

Suse "SB RDIPE", Zarechny, Russia (sfti@uraltc.ru)

The model of the influence of radiation porosity characteristics on a strength of austenite steels is presented. It accounts for the mechanical strains induced by pores and other defects and for a probability of a pore alignment along the surface, where conditions of damage are being fulfilled. The model was used to estimate the changes of ultimate strength of the austenite steel ChS–68 (20% c.w.), which had operated as fuel claddings in the BN–600 reactor and accumulated different damage dozes. Ultimate strength values were calculated by using the results of quantitative electron microscopy study and compared to the experimental data obtained from short–term mechanical tests on tension of ring samples. The samples were made of fuel claddings irradiated in the BN–600 reactor.

The main statements of the model are as follows:

- the pores, which are forming under  neutron irradiation, can randomly align along some surface, where the damage conditions are being fulfilled;

- vacancy pores induce mechanical strains in the steel due to surface tension and, hence, the external loads needed to fulfill the damage conditions are smaller.

The expression for the strain, sB,  produced by the external load and with which the damage proceeds by the above mechanism was obtained

se=(sg - sv) ×(1 - P/Pth)2/3),                                                           (1)

where sg is the strain in a matrix induced by pores due to surface tension and which can be described through the characteristics of the pore assembly in the material;

P and Pth are porosity and its threshold value, respectively, at which self damage occur, i.e. with no external load applied. The quantitative microstructure investigations of the samples of the fuel claddings made of ChS–68 and irradiated to damage doses in the BN–600 reactor were made by the electron microscopy methods. The ultimate strength was calculated from these results and by formula (1). Then ring samples were cut out of the same areas for short–term mechanical tests. For different ranges of irradiation temperatures the experimental dependencies of ultimate strength values were plotted against swelling. The dependencies were compared to the values calculated by the model. It was found that the manner of the swelling dependence of calculated and experimental values of the ultimate strength were similar, however, the experimental data (corresponding to swelling higher than 8 %) are decreasing with the growing swelling faster than the calculated ones.

It is shown that the observed difference is owing to the additional influence of two factors, i.e. a preferential aligning of radiation pores along twins and a presence of corrosion cracks on the internal side of the fuel elements, the cracks are strain concentrators in the mechanical test performance.

Temperature Dependence of Radiation Swelling of ChS-68 Steel Analyzed by Different Models

A.V. Kozlov*, Yu. V. Konobeev**, I. A. Portnykh*, E. A. Kinev*.

*Suse "SB RDIPE", Zarechny, Russia (sfti@uraltc.ru)

**Sue "FRC RF PEI", Obninsk, Russia.

The fuel claddings made of ChS-68 steel (20% c.w.) were irradiated in the BN–600 reactor, swelling of specimens of the claddings was measured and the data obtained were used for examination. The data were divided into two groups with respect to the fuel irradiation in different modifications of the BN-600 core, which differed in a height of the core and a maximum speed of attaining a damage dose. In different groups the composition of the cladding ChS–68 steel differed in the micro alloying dopants: boron and vanadium. Three alternative models were used for a quantitative description of swelling. In the empirical model A swelling S was given by the equation.

S=K1×GK2×DK3                                                                        (1)

where G is the speed of attaining the dose in the units of  10—6 dpa/s; D is the damage dose; K1 and K2 are the parameters independent on irradiation temperature; K3 is the temperature dependent T– function

K3= a3 + a4× T + a5×T2                                                              (2)

where a3 , a4  and a5 are constant coefficients.

In the model B equation (1) was used, where K1 and K2 were the parameters independent on irradiation temperature and K3 was given by equation

K1=exp(a3 + a4× T + a5×T2)  	                                                       (3)

Model C describes swelling as

S = A × ( D – D0) × (1 –exp ( -p × (D- D0)))                                             (4)

where A - is the speed of swelling at a stationary stage; D0 - is the incubation swelling dose; p - is the coefficient characterizing the speed with which the condition of stationary swelling is attained.

The parameters in the equations of radiation swelling dependence on irradiation conditions were determined by an optimization with the criteria c2. In order to estimate an adequacy of the descriptions by the above models the obtained values of c2  were compared to the reference value c20.05, which usually corresponded to the applied level of significance of 0.05. The results obtained by the three models were compared. The data obtained was used to plot a temperature dependence of swelling against different levels of damage doses. The dependence of peak swelling temperature on accumulated damage dose and a possible existence of two local temperature peak of swelling were analyzed.

About the Surface Erosion Mechanisms under the Pulsed Ion Beams Irradiation

G.A. Bleikher, V.P. Krivobokov, O.V. Paschenko

NPI at TPU, Tomsk, Russia (krivobokov@npi.tpu.ru)

Irradiation of solids by high intensity submicrosecond ion beams is accompanied by active surface erosion. It was developed yet at the first stages of the investigation of their interaction with matter that every pulse is able to remove from surface the layer of near micron thickness. Thus, the erosion coefficient can reach up to 5105 atoms/ion. It is near five orders more than under continuous irradiation. The estimation of partial contributions of atoms that are sputtered by quick particles and evaporated as a result of surface heating is one of unexplored questions. The first group of ions landed the surface interacts with cold solid and sputters it.  Then the irradiating surface is heated quickly (with the rate up to 1011 K/s) up to and above the boiling temperature. The intensive evaporation is able to arise on such surface.

Therefore we divided the stream of atoms leaving the surface to two parts: quick (concerned with collision processes) and heat (caused by evaporation). Accordingly, total erosion coefficient D is equal to the sum of two coefficients: sputtering (S) and evaporation (Q) ones (D=S+Q).

The aim of present work was to study the features of irradiated surface erosion under the power pulsed ion beam, in particular, the calculation of erosion coefficient D taking into account the surface temperature change and phase state, as well as the calculation of the partial components S and Q.

As a result of this work the following conclusion was formulated. In the range of power density of pulsed ion beams up to (1..5)106 W/cm2 sputtering is the main mechanism of erosion. In this case the erosion coefficient does not exceed several tens. It the range of (0,5..1)108 W/cm2 and more the erosion is concerned mainly with atoms evaporation as a result of surface heating by beam particles up to boiling temperature and above. In this case the erosion coefficient achieves 104..105 atoms/ion (for E2 MeV). The intermediate range of power density (~5106 ..5107 Vt/cm2) is not yet well studied. We expect that the contribution from sputtering and evaporation occurred on activation mechanism can be comparable. But the total erosion coefficient is below in orders there than under the intensive evaporation at boiling point.

# Formation of Nanoscale Intermetallic Phases at High-Intensity Ion Implantation

E.V. Kozlov*, A.I. Raybchikov**, Yu.P. Sharkeev***, I.A. Kurzina*, I.B. Stepanov**, S.V. Fortuna*, D.O. Sivin**, T.S. Prokopova*, I.A. Mel’nik*

* Tomsk State University of Architecture and Building, Tomsk, Russia (kozlov@mail.tomsknet.ru)

** Nuclear Physics Institute at Tomsk Polytechnical University, Tomsk, Russia

*** Institute of Strength Physics and Materials Science of RAS, Tomsk, Russia

# The high intensity ion implantation of metal ions using the vacuum-arc ion-beam and plasma flow source “Raduga-5” uncloses wide perspectives for modification of constructional metal materials. Major advantages of the source “Raduga-5” are the high dose rate of the implanted metal ions, plasma-assisted deposition, heating-up of a target by ion beam up to necessary temperature and opportunity of forming the modified ion beam surface layers, the thickness of which equal to several micrometers. The vacuum - arc ion-beam and plasma flow source “Raduga-5” can be applied for formation of nanoscale intermetallics phases in the surface layer of the micrometer thickness with the purpose to increase the wear resistance and heat resistance of constructional metal materials.

The aim of the paper was the investigation of an opportunity of the formation surface layer, thickness of which exceeds the ion projected range on some orders, with the nanoscale intermetallic phases by the method of the high intensity implantation of the Al ions in polycrystalline nickel and titanium.

It was established that the fine dispersed intermetallic precipitates are arisen in the nickel and titanium surface alloyed layers. Compositions of these intermetallic precipitates are closed to NiAl, Ni3Al Ti3Al and TiAl phases which are characterized by a set of unique properties as high melting temperature, high heat resistance and wear resistance. Besides the solid solutions of aluminum in nickel and titanium are formed. The intermetallic phases on the sizes of grains 30-100 nm are the nanoscale phases.

The increase of the target temperature both by the increase of the ion flux density and the ion treatment duration allows us to increase the modified surface layer thickness from one micrometer up to several micrometers. One should expect that such surface layers with the high density of the nanoscale intermetallic phases would have not only the high temperature strength but also the high wear resistance.

# Vacancy Clusters in Titanium Nickelide Irradiated with Fast  Neutrons

V.D. Parkhomenko*, S. F. Dubinin*, S. G. Teploukhov, E. Z. Valiev*, A. V. Kozlov**,

E. N. Scherbakov**

*Institute of Metal Physics, UB RAS, Ekaterinburg, Russia.(parkhomentko@uraltc.ru).

** SUSE "SB RDIPE", Zarechny, Russia.

Amorphous alloys of titanium nickelide of 2 types (one was prepared by affecting with fast neutrons, second was obtained from a melt) investigated for homogeneity by the methods of small angle scattering, dilatometry and electronic microscopy.

It was found that the effect of small angle scattering takes place only in the titanium nickelide amorphized with fast neutrons. Then small angle neutron scattering was measured in the irradiated alloys. The measurement results were processed with the assumption that microareas rich in vacancies are formed in titanium nickelide under irradiation.

The observed experimental situation can be explained admitting that the scattering object is a cluster, which is a three – dimensional fractal object in mathematics. In the above case the fractal cluster is understood as the microarea, which is rich in vacancies, has a rough surface and numerous thin barriers.

The cross sections of the neutrons scattered with the vacancy clusters were calculated, the calculation data in a log–log scale are shown as solid lines in Figs. 1, 2. The full profile of the calculated curve in a regular scale is in the figure insertion.

As based on the combined analysis of the data, obtained by the three methods, the inhomogeneity of the titanium nickelide (amorphized with fast neutrons) was attributed  to the formation of the microareas with a high concentration of vacancies  under irradiation at 340K. The sizes and the volume fraction of the clusters rich-in vacancies were also determined.

Swelling and Microstructure of EP-753 and Nimonic PE-16 High Nickel Alloys after Neutron Irradiation to High Doses

S. I. Porollo, Yu. V. Konobeev*, and F. A. Garner**

*State Scientific Center of Russian Federation, Institute of Physics and Power Engineering,

Obninsk, Russia (porollo@ippe.ru)

**Pacific Northwest National Laboratory, Richland, USA

The temperature dependence of swelling in the majority of pure metals and alloys look is described by a bell-shaped curve, the position of maximum on which is determined by both the type of a material and irradiation conditions. However, data are available on a more complicated temperature dependence of swelling, when the swelling temperature curve has two and even three maxima. Several swelling maxima were observed in austenitic steels, nickel alloys, and also in some pure metals irradiated with neutrons, ions and fast electrons.

For the present, mechanisms responsible for occurrence of several swelling temperature peaks are not established exactly that is presumably due to a lack of experimental data on the microstructure of materials demonstrating several swelling maxima.

In this report data on the swelling temperature dependence and microstructure for two high nickel alloys EP-753 (1Х20Н40М5Б) and Nimonic РЕ-16 (6Х17Н44М4ЮТ) irradiated with neutrons up to maximum dose of 44 dpa are presented. The alloys were irradiated as pin cladding structural in the BOR-60 fast reactor (Dimitrovgrad) in the temperature range of 320600C. Data on pin diameter measurements and TEM-data give evidence about the existence of two swelling maxima located at temperatures of 390 and 590C in the EP-753 alloy and at temperatures of 420 and 585С in the Nimonic РЕ-16 alloy. The appearance of the second, high-temperature maximum is, probably, a result of formation and growth of voids with elevated helium content due to accumulation of helium in nuclear reactions and its migration to the voids at temperatures above 500С.

Long-Range Effect in Ion Implantation-Ordered Alloys

N.N. Syutkin, V.V. Alehin

Institute Electrophysics UB RAS, Ekaterinburg, Russia (micros@iep.uran.ru)

The long-range effects, i.e. the possible phase transformation in the material and the formation of structural defects at depth which the implanted ions did not reach, were observed in the some cases.

The radiation doses for the Cu3Au and PdCuAg alloys were 1015-1018 argon ion/cm2, j=100-340 μA/cm2, E=20-40 keV.

A region of the ordered materials lying at a depth of more than 0.5 μm  from the irradiation surface were examined in detail.

It was revealed that implantation leads to the formation of a large number of defects identified  in the ion micrograph as a regularity interruption in the annular pattern of the superstructural low-index poles.

A Short Range Order In The Amorphous Ribbon of Ti0,5Ni025Cu0,25              Irradiated by Fast Neutrons

V. D. Parkhomenko, S. F. Dubinin, S. G. Teploukhov

Institute for Metal Physics, UB RAS, Ekaterinburg, Russia (parkhomenko@uraltc.ru)

It was  shown by the authors in Refs [1,2] that the type of a short atomic order in intermetallics and compounds, amorphized   under fast neutron irradiation, is relevant to the type of an initial crystal lattice. It was especially noted, that the type of the short range order of the amorphous substances, prepared by quenching a melt, was relevant to a random close pack of atoms and   its main features were independent  of an atomic content.

In order to investigate an effect of neutron irradiation on the  structural state of the  amorphous alloy prepared by the fast quenching of a melt the amorphous ribbon of Ti0.5 Ni0.25 Cu0.25 was exposed to fast neutrons, = 1 10 20 cm-2 , at 340 K. The packet was investigated by the neutron diffraction method before and after fast neutron irradiation. The obtained diffraction patterns are shown in the Figure. They revealed some portion of a crystal phase in the unirradiated sample. In the pattern the crystal phase portion is absent because  the crystal phase has been amorphized by irradiation. The type of a short range atomic order  determines a diffusion peak at K~2A-1. Since the form of the peak has not changed it may be concluded that the fast neutron irradiation has no effect on the type of the short range order in the alloys amorphized by quenching a melt.

References

- S.F.Dubinin, V.D.Parkhomenko, V.G.Pushin, S.G.Teploukhov. FMM, 2000, v.89, n.1, p.70-74

- S.F.Dubinin, V.D.Parkhomenko, S.G.Teploukhov. FMM, 2001, v 91, №4, p. 91-103.

Structural Phase Transitions in Intermetallic Compounds Y2Fe17 and Ce2Fe17 after Irradiation with Fast Neutrons

# V.I. Voronin, E.F. Berger, A.E. Karkin, A.G. Kuchin, Yu.G. Chukalkin, B.N. Goshchitskii

# Institute of Metal Physics, UB RAS, Ekaterinburg, Russia (Voronin@imp.uran.ru)

In earlier papers [1-3] we showed that change of magnetic properties of intermetallic compounds R2Fe17 (R=Y, Ce, Lu) at their doping with transition elements is caused by lattice transformation. A dependence of the Curie temperature on interatomic distance was found. The main difficulty in the experimental study of doped systems is that the process changes the sample composition, and hence, the set of parameters depending on composition, such as: effective ion valence, ion sizes, their quantity, etc. The radiation exposure method permits to avoid the majority of these difficulties, since the irradiated sample preserves its original stoichiometry. As experiment shows, the cell size and the ions local environment in the lattice usually vary at irradiation with fast neutrons. Such distortions must affect the magnetic properties of the irradiated materials as well. Really, at irradiation with fast neutrons, antiferromagnetic ordering in Ce2Fe17 is suppressed, and the compound turns into a ferromagnet with TC = 300 K, and in Y2Fe17 the Curie temperature grows significantly. The purpose of this work was investigating the crystalline structure of compounds Ce2Fe17 and Y2Fe17 after irradiation with fast neutrons with an energy over 0.1 MeV, and finding the structure – magnetic properties correlations. Irradiation was carried out in the vertical irradiation channel of reactor IVV-2M (Zarechny) at 370 K in a broad range of fluences up to Φ = 3 ×1020 cm–2. Quite unexpected was the Curie temperature drop from 300 to 170 K at fast neutrons fluence increase to Φ = 3 ×1020 cm–2. Crystalline structure was investigated using X-ray and neutron diffraction methods at room temperature. It was established that change in the symmetry of crystal lattices took place under intermediate fluence, while under maximum fluence, amorphous state was realized in the bulk of the material.

Work supported by State Scientific Research Program “Topical Problems in Physics of Condensed Matter”, direction “Neutron Investigations of Condensed Matter” (State control No. 40.012.1.1.11.50) and Program for Support to Leading Scientific Schools of Russia (Project No. 00-15-96581).

References

- V.I. Voronin, I.F. Berger, A.G. Kuchin, FMM, 5 (2002) 93.

- V.V. Serikov, N.M. Kleinerman, A.G. Kuchin, V.I. Voronin, FMM, 94 №2 (2002) 59-66.

- V.I. Voronin, I.F. Berger, A.G. Kuchin, D.V. Sheptyakov, A.M. Balagurov, J.of All. Comp. 315 (2001) 82.

Comparison of the Effects of Radiation- and Strain-Induced Defects on the Phase  Transformation in Iron Alloys

V.V. Sagaradze, A.R. Kuznetsov

Institute of Metal Physics, Ural Branch RAS, Ekaterinburg, Russian Federation (vsagaradze@imp.uran.ru)

It was analyzed on the comparative basis [1-4] how point defects of different origins (radiation- and strain-induced defects) influenced the progress of anomalous phase transformations in steels and alloys at low temperatures (200-400 K). It was shown that atomic decomposition of Fe-Ni, Fe-Cr-Ni, Fe-Ni-Ti, and Fe-Cr-Ni-Ti solid solutions took place irrespective of the origin of point defects, which were formed both during a severe cold deformation and under irradiation with high-energy particles. A relatively stable ultrafine-grain structure with grains ~100 nm in size appeared during a severe cold deformation. Boundaries of those fine grains were preserved during a strong deformation and they served as efficient sinks of point defects. As in the case of irradiation, the reverse Kirkendale effect led to enrichment of the boundaries with nickel, which was attested to by a large rise of the Curie temperature in the near-boundary regions in the Fe-Cr-Ni austenite. Profiles of the near-boundary segregation of nickel in the Cr12Ni30 alloy caused by diffusion of strain-induced vacancies to sinks were calculated in [1].

Low-temperature dissolution of strengthening particles (intermetallics, etc.) in the austenitic matrix during an intensive cold deformation was discussed in [2]. This is analogous to a certain extent to dissolution of fine particles in displacement cascades under low-temperature irradiation [3]. It should be noted that the deformation effect differs from irradiation since not only defects, but also dislocations are formed in the former case. Dislocations complicate considerably the character of structural and phase transformations. Calculation [4] demonstrated that dissolution of fine particles of secondary phases under cold deformation (200-300 K) can be explained by strain-induced transfer of atoms of the particles to interstices and subsequent migration of the interstices to the stress field of moving dislocations.

This work was supported financially by the Russian Foundation for Fundamental Research (Projects  Nos. 01-03-96446, 01-02-16877 )

##### References

- Deryagin A.I., Zavalishin V.A., Sagaradze V.V., Kuznetsov A.R. Low-temperature mechanically induced atomic decomposition in chromium-nickel steels. Fiz. Met. Metalloved., 2000, v. 89, No. 6, pp. 82-93.

- Sagaradze V.V. Nonmartensitic phase transformations in steels during cold deformation. Fiz. Met. Metalloved., 2000, v. 90, supplement 2.

- Sagaradze V.V., Koloskov V.M., Shabashov V.A., Lapina T.M., Arbuzov V.L., Goschitsky B.N., Parkhomenko V.D. Dissolution of intermetallics in displacement cascades during neutron irradiation of precipitation-hardening alloys. Letters to ZhTF, 2001, v. 27, No. 6, pp. 26-33.

- Kuznetsov A.R., Sagaradze V.V. On possible mechanism of low-temperature strain-induced dissolution of intermetallic phases in Fe-Ni-Ti alloys with an FCC lattice. Fiz. Met. Metalloved., 2002, v. 93, No. 5, pp. 13-16.

The Long-Range Effect in Metal Foils under Ion and Photon Irradiation

D.I. Tetelbaum*, A.Yu. Azov*, E.V. Kuril’chik*, Yu.A. Mendeleva*, V.Ya. Bayankin**,

F.Z. Gil’mutdinov**, A.V. Nikitin** 
*Physico-Technical Research Institute of University of Nizhny Novgorod, Nizhny Novgorod, Russia (Tetelbaum@phys.unn.ru) 
** Physico-Technical Institute, UB RAS, Izhevsk, Russia

The review of the original studies on the long-range effects in metals under various type (ions, photons and so on) irradiations is presented. The essence of the effect is the change in the material properties over distances by several orders of magnitude exceeding the thickness of an ultimate energy deposition region. Unlike the other phenomena, where the change can be explained as due to the strong heating of the region, such heating does not play a significant role in our case. Moreover, the phenomenon considered (low-dose long range effect - LDLRE) differs from the other “long-range effects” investigated by various groups under ion irradiation: the changes take place at significantly lower doses and at the doses exceeding some critical one the effect becomes less pronounced.

LDLRE is characterized by the following anomalous features: the non-monotonous dose dependence, the existence of the threshold ion energy (independent on the ion type, dose, and dose rate), the ability to penetrate through the interfaces between the foils and to redistribute the alloy species and impurities at super-deep distances, etc.

Recently, anomalously deep change in the metal mechanical properties was found at certain conditions also under light (photon) irradiation of metal foils having several m (and higher) thicknesses. The effect regularities, their similarity and difference from the LDLRE were investigated. It has been demonstrated that the necessary condition of the phenomenon manifestation is the existence of thin dielectric layer (natural oxide) on the irradiated surface of the foil but not the heating. The phenomenon was named “photo-memory of metals – PMM”. The PMM is characterized by the complicated non-monotonous dependence of mechanical properties (microhardness) on the dose, by a relaxation in the changes after stopping irradiation and by a number of unusual specific features. The possible mechanisms of all mentioned phenomena are discussed from the single point of view.

The new encompassing concept is suggested concerning the interaction of energy flows with solids having a strongly non-equilibrium structure. The problems concerning the non-observation in more early experiments of the considered effects and their application in practical purpose are discussed.