- Radiation-Enhanced and Radiation-Stimulated

Phenomena

Segregative Manifestation of the “Long-Range Action Effect” During Irradiation of Permalloy Foil with Boron and Phosphorus Ions

A.V. Nikitin*, F.Z. Gil’mutdinov*, D.I. Tetelbaum**, V.Ya. Bayankin*

*Physical-Technical Institute, Ural Branch of RAS, Izhevsk, Russia (less@fti.udm.ru)

**Physical-Technical Institute Nizhny Novgorod State University, Nizhny Novgorod, Russia

In the given paper, boron and phosphorus are used as examples for demonstrating a new manifestation of the small dose effect of long-rage action, which is an anomalous penetration of impurity atoms, implanted into the permalloy foil.

A foil from permalloy-79 with the thickness of 20 m was irradiated with B+ and P+ with the dose 1015 cm-2. The ion energy varied over the range from 15 to 40 keV. Current density was 3 A/cm2, and the temperature of the samples was not higher than 1500 C. The sides of some samples, adjacent to a flange, were covered with chemically stable varnish (CSV). Distributions of the components from both sides were determined by the methods of X-ray photoelectron spectroscopy (XPS) and secondary-ion mass-spectroscopy (SIMS).

The most interesting result of the work lies in the fact that in the irradiated samples boron and phosphorus are revealed on both sides of the foil. It also is important that boron is present on the back surface in both uncoated samples and CSV-coated samples, though for latter ones the penetration of impurities from gas phase is very unlikely. Besides, the ratio between the back side boron concentration and the irradiated side boron concentration grows sharply at E > 30 keV, i.e., the energy threshold appears, which agrees with the data on the microhardness changes. From the results on boron profiles, it follows that boron is predominantly concentrated in thin near-surface layers (to 8 nm). In addition to the boron penetration through the foil, the “effect of long-range action” is also manifested in the influence of irradiation on the distribution of the main component, nickel, in the near-surface layers on the back side, where the energy threshold for the main component redistribution is observed as well.

The study of the small dose effect of long-range action has been conducted with the use of permalloy foils; when irradiated with phosphorous ions, a part of a sample has been shielded from the ion flux. The measurements show, that at the ion energy of 40 keV, similar processes of the redistribution of the main components of the alloy take place on both the front and the back sides of the foil in the area of irradiation.

The results obtained should be considered as preliminary ones. It is necessary to conduct further verification of these results for some other impurities and metals. The features of the phenomenon should be studied more thoroughly, especially the role of the conditions of irradiation and hold of samples after irradiation.

The work has been financed by the Russian Foundation for Basic Research (project № 02-0216670).

The Radiation-Enhanced and Radiation-Induced Phenomena in

Fe-16Cr Based Alloys

A.L. Nikolaev

Institute of Metal Physics, UB RAS, Ekaterinburg, Russia (nikolaev@imp.uran.ru)

By means of resistivity the processes occurring under electron irradiation at 300-420 K are investigated in the undoped and impurity (Si and Cu) doped Fe-16Cr-based alloys. Two processes with clearly different contributions to residual resistivity were found to proceed in the Fe-16Cr alloy under irradiation. The first one resulting in a resistivity drop is a well-known radiation-enhanced short-range ordering (SRO). The second process leads to resistivity increase. The similar, but a more pronounced effect was found in the Fe-22Cr alloy. Thus the most probable origin of the resistivity increase is the alloy decomposition under irradiation into α (Cr depleted) and α' (Cr enriched) phases well known due to the so-called 475 ˚C fragility. The compatibility of such explanation with variations of the other alloy properties, sensitive to Cr concentration, had been tested and found to be satisfactory:

1. Resistivity. The concentration dependence of the Fe-Cr alloys resistivities at 4.2 K (residual) and 373 K was determined. Since the alloy 4.2 K resistivity was found to be almost independent on Cr concentration over a wide concentration range (9-50 at. %), the 4.2 K resistivity rise can be easily understood as due to conduction electron scattering at elastic distortions around α' precipitates, whereas the matrix resistivity stays nearly unchanged. The variation of the 373 K resistivity due to irradiation agrees with the solid solution depletion with Cr.

2. Stage I of resistivity recovery. The amplitude of stage I resistivity recovery (after low temperature irradiation) depends on the Cr concentration. It is shown that this amplitude in the Fe-16Cr alloy irradiated at 420 K increases and in our particular case is close to that in the Fe-13.4 Cr alloy.

The simple decrease in irradiation temperature from 420 K to 300 K also decreases the rate of both processes pointing to the radiation enhancement nature of the latter. But sequential alternation of irradiation temperature between 300 K and 420 K leads to abrupt increase in resistivity rise rate at 420 K. This means that the rate of the alloy decomposition is not determined only by a non-equilibrium defect concentration (that is typical for the radiation enhanced process) but also can be affected by reactions between defects such as clustering and that is the sign of the radiation-induced process.

The same processes taking place under irradiation are observed in the Fe-16Cr alloys doped with Si (0.2-1.5 at. %), although the rate of resistivity variations associated with the SRO in these alloys is strongly decreasing with the dopant concentration.

Principally different picture of resistivity variations under irradiation is observed in the Fe-16Cr alloy doped with 0.1 at. % Cu. In all alloys except the latter the resistivity decrease (associated above with the SRO) demonstrates a tendency to saturation with the irradiation dose, and this is a typical sign of the SRO, since the degree of the SRO and corresponding resistivity are moving during irradiation towards their equilibrium (saturation) values, which depend on irradiation temperature only. When the resistivity variation due the SRO becomes sufficiently small, the resistivity increase due to the Fe-16Cr solid solution decomposition can be detected. In the Fe-16Cr-0.1Cu alloy only resistivity drop without sign of the saturation is found. Such resistivity behaviour can be interpreted only as the copper solid solution decomposition. This is natural, since the copper solid solution in our case is strongly oversaturated. By comparing resistivity change in the Fe-16Cr-0.1Cu with that in the other alloys, the value of excess resistivity drop in the copper doped alloy can be found, and efficiency of copper atom removal from the solid solution estimated. The efficiency factor turns out to be close to unity – one copper atom is removed from the solid solution by approximately one freely migrating defect. Such high efficiency almost unambiguously points to the interstitial (mixed dumbbell) mechanism of copper atom migration and the lack of defect recombination effect on the decomposition process. The latter means that copper atoms are transported to the distances sufficiently less than the mean distances between the defects. The only physically preferred distance of a such scale is the distance between copper atoms, and therefore the most probable mechanism of the copper solid solution decomposition seems to be the clustering of the neighbouring copper atoms. It is hard to classify unambiguously whether this process is solely radiation-enhanced or radiation-induced: the process is obviously accelerated by non-equilibrium defects, but the mechanism of decomposition is typical for radiation-induced phenomena.

Theory of Solute Segregation in the Boundary of

Finite Size Grains in Polycrystals

V.V. Slezov 1, L.N. Davydov1, O.A. Osmayev2,1

1Institute for Teoretical Physics, NSC “Kharkov Institute for Physics & Technology”,

Kharkov, Ukraine

2Ukraine State Academy for Railway Transport, Kharkov, Ukraine

(oleg_osmayev@kipt.kharkov.ua)

A solute segregation from a grain of a finite size into its boundary was first studied analytically in [1]. The results allowed to describe correctly the grain boundary segregation in a polycrystalline material. As shown in [1], the segregation process and the amount of the segregated solute are determined not only by the diffusivity and initial solute concentration in the grain and its boundary, but also by the finiteness of the grain size, i.e. by a limited amount of a solute present in the grain. The influence of the grain shape was also studied in [1], where a flat, spherical and cylindrical grain were considered. In [2] the case was investigated, when an essential role in diffusion processes is played by a solute being constituent of a complex (solute atom – vacancy). The general case was considered when mass transfer is due both to diffusion of "free" unbounded solute atoms, and to solute atoms bounded in complexes with vacancies. For grains of the plate, spherical and cylindrical shape the time dependence was found [2] for: (a) solute concentration profile in a grain; (b) solute concentration in grain boundaries in case of weak solution in boundary. A simple algebraic equation for solute concentration in boundary as function of time was obtained in [2], which is valid in both cases of weak and strong boundary solution of solute. A segregation of a solute from a grain of finite size into grain boundary was investigated in [3] for a case, when the supply of matter to the grain boundary is a very fast process as compared to the process of incorporation of a solute into the boundary. A kinetics of the solute redistribution, i.e. enrichment of the boundary with a solute or its depletion (drift of a solute into the grain), was considered in [2] and [3] for both limiting processes. A segregation of one kind of solute was considered in paper [4], and the role of local (competing for a place) and non-local interaction of solute atoms was clarified. Also, general equations were obtained in [4] for the case, when different solute atoms are present. The conditions were determined when the concentration of one of the solute atoms reaches transiently a maximum.

References

1. V.V.Slezov, L.N.Davydov and V.V.Rogozhkin, Fizika Tverdogo Tela, 37, 3565 (1995).

2. V.V.Slezov, O.A.Osmaev and V.V.Rogozhkin, Fizika Nizkikh Temperatur, 23, 218 (1997).

3. V.V.Slezov, O.A.Osmaev and V.V.Rogozhkin, Metallofizika, 19, 47 (1997).

4. V.V.Slezov, L.N.Davydov and V.V.Rogozhkin, Fizika Tverdogo Tela, 40, 251 (1998).

Acceleration of the Rate of Short-Range Layering in Alloy Fe+15at%Cr

under Irradiation with Gaseous and Metallic Ions

V.V. Ovchinnikov, B.Yu. Goloborodsky, N.V. Gushchina, L.S. Chemerinskaya,

V.A. Semyonkin, E. Wieser*, W. Möller*

Institute of Electrophysics, UB RAS, Ekaterinburg, Russia (vladimir@iep.uran.ru)

* Institute of Ion Beam Physics and Materials Research, Forschungszentrum, Rossendorf, Germany

A comparative investigation of the effect of irradiation with gaseous and metallic ions on the atomic structure of alloy Fe+15at%Cr was carried out. The fact of radiation-dynamic contribution to change in the structure and properties of solid solutions under exposure to accelerated ions was proved.

For this purpose, samples of the alloy in the form of 30-μm-thick foils were quenched from 1200 ºC, underwent cold plastic deformation and were further treated under 5·10–5 mm Hg vacuum at 450 ºC as follows: 1) irradiated with a beam of light of 1-2 W/cm2 power density; 2) irradiated with gaseous Ar+ ions at E=20 keV, j=50-100 μA/cm2, of the same power density; 3) irradiated with metallic Fe+ ions at E=40 keV, j=25-50 μA/cm2.

For irradiation with continuous Ar+ ion beams, the samples were suspended on thin threads of small sectional area and low heat conductivity, for heat removal to be ensured practically by irradiation only (in cases of irradiation with ions and a beam of light). For irradiation with Fe ions, the sample was placed in a cell which was more inertial in relation to heating with an ion beam than the foil suspended on thin threads. The cell was equipped with an electric heater. Combined use of the heater and the ion beam, with subsequent heater turning-off, allowed us to ultimately bring the rate of heating close to the curve of heating with the Ar+ ion beam.

The Mössbauer effect was used to investigate short-range ordering in alloy Fe+15at%Cr. In determining short-range order parameter α, use was made of the fact of linear dependence between this parameter and the mean value <H> of the effective magnetic field on 57Fe nucleus.

It was established that the value of short-range order parameter α for a quenched alloy and for an alloy irradiated with visible light at 450 ºC during 30 min was equal to zero within the measurement error limits, while in case of samples irradiated with gaseous and metallic ions, the value of α was equal to 0.12 and 0.10±0.2, respectively. The high positive values of the short-range order parameter testify to a high degree of short-range layering after irradiation with ions.

Work was carried out with the financial support of the Russian Foundation for Basic Research (grant No. Ural 01-02-96428) and the Program for government support to leading scientific schools of the Russian Federation (grant No. 00-15-96581).

# The Laws Governing Radiation-Dynamic Effects in Alloy Fe+8.25at%Mn under

Combined Electromagnetic and Ion Irradiation

V.V. Ovchinnikov, B.Yu. Goloborodsky, N.V. Gushchina, L.S. Chemerinskaya,

V.A. Semyonkin, A.V. Luzgin

Institute of Electrophysics, UB RAS, Ekaterinburg, Russia (vladimir@iep.uran.ru)

Investigation of the laws governing the effect of accelerated Ar+ ions on structural change in quenched alloy Fe+8.25at%Mn was carried out with a view to find out which parameters, or combinations of parameters (particularly, ions energy E, ion current density j, temperature T, irradiation dose D), are critical in initiating RD-transformations, as well as to study their kinetics.

Samples of the alloy in the form of 25-μm-thick foils, after quenching in water from 820 ºC (under 5·10–5 mm Hg vacuum), were irradiated with a beam of light  of power density within 1-2 W/cm2 during 10 min, and with gaseous Ar+ ions at different values of ion beams energy (E=10, 15, 20 keV) and ion current density (j=15, 40, 75 μA/cm2). The target temperature, and hence, the intensity of thermostimulated processes, were kept stationary under ion beam energy and density varying over a broad range at the expense of a combined exposure method, when part of the ion beam power was replaced with electromagnetic irradiation.

The results of the investigations carried out confirmed the presence of radiation-dynamic effects under ion irradiation. So, radiation-dynamic α → γ (BCC → FCC) phase transformations under irradiation with Ar+ ions (E=20 keV, j=75 μA/cm2) at 480 ºC occurring during 20 s (with formation of ~ 8 % γ-phase) were registered, while samples heated and held at 480 ºC under a light beam during 10 min remained single-phase. The existence of a critical ion current density jc caused by the α → γ transition was established, and found to be in the limits of 40 < jc < 70 μA/cm2. Additional experiments will be required for more accurate definition of current critical density, in case of j < jc, no α → γ transformation takes place at the above temperature. For α → γ transformation to occur under irradiation, certain values of ions energy are required; in the case under consideration, this value should be not lower than 20 keV. It is not unlikely that the product of Ej, i.e., power critical density, is the critical parameter. At ion current density j ≤ 40 μA/cm2, the radiation-dynamic effects manifest themselves through abrupt acceleration of the process of short-range layering. In all cases of combined irradiation, the maximum degree of short-range layering is reached already after 20 s of exposure, while in the course of light irradiation, the same result is obtained after about 10 min of exposure.

Work was carried out with the financial support of the Russian Foundation for Basic Research (grant No. Ural 01-02-96428) and the Program for government support to leading scientific schools of the Russian Federation (grant No. 00-15-96581).

Effect of Ion Irradiation on Oversaturated Solid Solution

Decomposition in Alloy Al-4%Cu

V.V. Ovchinnikov, N.V. Gushchina, B.Yu. Goloborodsky, L.S. Chemerinskaya

Institute of Electrophysics, UB RAS, Ekaterinburg, Russia (vladimir@imp.uran.ru)

Decomposition of oversaturated solid solution in alloy Al-4%Cu under irradiation with Ar+ ions was investigated using the methods of microhardness measurement and X-ray diffraction analysis (precision evaluation of solid solution lattice parameters). The alloy initial samples in the form of 100-μm-thick foils were homogenized at 520 ºC and quenched in water. Irradiation with continuous argon ion beams was carried out using a cold hollow-cathode reflecting discharge source. For irradiation, the sample was placed in a copper cell. Irradiation was carried out in the course of continuous heating and after reaching a stationary temperature. Irradiation dose varied in the course of the experiment, the energy of irradiation was 10-20 keV, ion current density was maintained within 50-200 μA/cm2.

It was established that radiation-enhanced solid solution decomposition takes place in alloy Al-Cu under irradiation.

Work was carried out with the financial support of the Russian Foundation for Basic Research (grant No. Ural 01-02-96428) and the Program for government support to leading scientific schools of the Russian Federation (grant No. 00-15-96581).

On the Laws and Nature of Long-Range Dynamic Effects under

Corpuscular Irradiation

V.V. Ovchinnikov

Institute of Electrophysics, UB RAS, Ekaterinburg, Russia ((vladimir@imp.uran.ru)

In the recent years, intensive investigations have been undertaken of radiation-dynamic (RD) processes initiated by corpuscular irradiation, not related to doping and defects formation in the ion path zones or atoms migration (i.e., to thermo- and radiation-stimulated processes), but, presumably, caused by microshock waves generation on dense cascades of atomic collisions initiating structural and phase transformation on their wavefront.

In the course of irradiation with low-energy (up to 50 keV) ions, RD-processes cause long-range effects consisting in changes in the structure and properties of materials at depths exceeding the projected ranges of ions of the said energies by several orders of magnitude. In case of neutron irradiation, primary recoil atoms act as analogs to ions.

The detected phenomena permit formation of unique electrical, magnetic, tribological and other properties of crystalline, polycrystalline and amorphous materials. Unfortunately, the laws governing RD-processes have been insufficiently studied yet.

Further investigation of the conditions of initiation and course of RD-processes depending on ions energy and mass, ion current density, as well as temperature, composition and structure of the target is needed. The talk will be dedicated to analysis of the laws and nature of RD-processes in metastable metal alloys based on the currently available and published data, as well as the latest  investigations undertaken at the Institute of Electrophysics of the Ural Branch of Russian Academy of Sciences, jointly with the Institute of Ion Beam Physics of the Research Center at Rossendorf, Germany. The latter relates to the data obtained with the use of metallic ions, which corroborate and supplement the results obtained in exposure to gaseous ion beams, as well as use of combined ion and electromagnetic irradiation.

Replacement of part of the ion beam power density (0 to 100 %) with light irradiation, while maintaining unvaried the target stationary temperature, allowed us to vary the energy of ions and the ion current density over a wide range. The irradiation dose and kinds of ions also varied. The kinetics of RD-processes for gaseous and metallic ions, as well as the critical values of ions energy and ion current density initiating RD-transformations, were investigated for metastable iron-chromium, iron-manganese and iron-palladium-gold alloys.

Mössbauer Effect Observation on 57Fe Isotope in α-Iron under

Ion Bombardment (in situ)

V.V. Ovchinnikov*, B.A. Semyonkin**, B.Yu. Goloborodsky*

*Institute of Electrophysics, UB RAS, Ekaterinburg, Russia (vladimir@iep.uran.ru)

**Ural State Technical University, Ekaterinburg, Russia

Using the Mössbauer effect featuring high sensitivity to changes in the electrical and magnetic superfine interactions in crystals as well as to the dynamic state of atoms, an attempt was made in this work to detect lattice (phonon) and electronic excitations under ion bombardment (in situ) in α-iron which naturally contains nuclei of the Mössbauer isotope 57Fe.

In this investigation, use was made of a set-up on the base of the SM 2201 Mössbauer spectrometer. The spectrometer axis intersected with the ion beam axis at an angle of 45º. The center of the target sample, presenting a thermostat entrance port, was located at the point of intersection of the above axes. Irradiation was carried out with Ar+ ions (E=20 keV, j=5 μA/cm2).

The negative isomer shift (–0.04±0.02 mm/s) testifies to increase in electron charge density on nucleus in the course of irradiation, which may be due to redistribution of both s- and d-electrons (which do not account for density on the nucleus, but screen the s-electrons). Since the Mössbauer experiment geometry was carried out for transmission, the said effect characterizes the state of the whole bulk of the 10-μm-thick foil, and not just the zone of ions penetration (20-30 nm).

Most probably, de-localization of both s- and d-electrons in the bulk of the target takes place under irradiation. However, the contribution of de-localization in the spectrum shift is greater, which may play an important role in explaining such unusual effects as the long-range effects under ion irradiation, since de-localization may cause increase in the atoms diffusion mobility and phase transition points shift. Exactly the latter was observed in some alloys under exposure to accelerated ions.

The presence of Zeeman sextets with quadrupole splittings of opposite sign (+0.22±0.02 and –0.26±0.02 mm/s) in the Mössbauer spectrum points to an opportunity of elastic oscillations generation in the sample: longitudinal standing waves (and respectively, regions of compression and rarefaction) as a result of radiation-dynamic influence of bombarding ions.

Modeling of Accelerated Embrittlement in Reactor 
Pressure Vessel Steels at High Neutron Fluences

V.A. Pechenkin*, Yu.V. Konobeev*, I.A. Stepanov*, Yu.A. Nikolaev**
* SSC RF Institute of Physics&Power Engineering, Obninsk, Russia (vap@ippe.obninsk.ru)

** Russian Research Center “Kurchatov Institute”, ORM, Moscow, Russia

The shift of ductile-brittle transition temperature in irradiated VVER pressure vessel steels is usually represented by standard guides with a power dependence on fast neutron fluence multiplied by a material constant. However, from recent data on surveillance specimens for several units of VVER-440 a strong irradiation embrittlement enhancement have been revealed at neutron fluences exceeding (2-3)1020 n/cm2 (E>0.5 MeV) with a significant deviation from the standard guide. This points out to possible involving an additional mechanism of irradiation embrittlement at high fluences.

In the present study it was supposed that such an additional mechanism could be the intergranular embrittlement caused by grain boundary phosphorus segregation. A threshold dose is used which accounts for that the intergranular embrittlement contribution occurs after a sufficient phosphorus segregation when a critical stress for intergranular fracture falls below one for cleavage fracture. The modeling of phosphorus accumulation on grain boundaries is performed taking into account the radiation-enhanced phosphorus diffusion via vacancy and interstitial mechanisms, the radiation-induced segregation in the matrix near grain boundaries and the Gibbsian adsorption on grain boundaries. Predictions of such a composite model are in qualitative agreement with surveillance data for VVER-440.

### Significance of Radiation-Induced Segregation in Alloy Properties

Alteration under Irradiation

V.A. Pechenkin*, Yu.V. Konobeev*
* SSC RF Institute of Physics & Power Engineering, Obninsk, Russia (vap@ippe.obninsk.ru)

The report presents a review of experimental and theoretical investigations on radiation-induced segregation (RIS) in metallic alloys. Mechanisms of RIS are considered. Experimental data on RIS in base, alloying and impurity chemical elements in model alloys (Fe-Cr-Ni) and commercial austenitic steels, ferritic/martensitic steels and reactor pressure vessel steels in PWR and VVER are discussed. The methods of RIS investigation are considered.

It is concluded, that RIS effects essentially on precipitation, swelling, irradiation-assisted stress corrosion cracking and embrittlement of these materials. A conclusion is made that a necessary stage of new radiation-resistant alloys development should be a preliminary investigation of RIS phenomenon and radiation-induced formation of precipitates in charged-particle simulation studies. The irradiation of alloys with heavy ions of MeV-energy seems as most appropriate method of such investigations.

Grain Shape Effect on the Solute Segregation

in Elastic Stressed Polycrystal

R.V. Shapovalov*, V.V.  Slezov*, O.A. Osmayev**

*Institute for Teoretical Physics NSC “Kharkov Institute for Physics & Technology, Kharkov, Ukraine ( oleg_osmayev@kipt.kharkov.ua. for R. Shapovalov)

**Ukraine State Academy for Railway Transport1, Kharkov, Ukraine

Polycrystal materials are subjected to an exterior mechanical loading in many practically important cases. If the temperature is low enough (it hasn't exceed 0.4 the material melting point) and the loading is small (smaller, than polycrystal yield point) it is possible to consider a sample were in an elastic stressed state and to neglect inappreciable plastic deformation processes in these requirements. Mechanical loading and a material maintenance long-lived time (20-30 years) essentially influence on the solute diffusion processes in a single crystallite. The solute redistribution between a crystallite and an intercrystallite boundary (solute segregation) changes materials mechanical properties and, as a rule, results in deterioration of their performances. For practical purposes it is important to know how to predict a material safe maintenance time, which in many cases is defined by limit impurity concentration in a grain boundary (the importance of phosphorus in materials of atomic engineering is known).It would be more important to operate on grain boundary impurity concentration and, thus to prolong working hours of materials and articles.

The kinetics of grain boundary solute segregation in an elastic stressed material was studied in our work. Time evolution of grain boundary impurity concentration for arbitrary grain shape was found. The influence of an elastic field was considered. It was shown, that amount of an impurity diffused into a grain boundary depended on the boundary site orientation respectively an exterior loading. Processes in a spherical shape grain were explicitly investigated. It was obtained that even in case of a spherical symmetry of a grain the anisotropic loading gave rise to formation anisotropically located grain boundary precipitate. It was shown, that by means of short-term raise of temperature (in comparison with time of exploitation) the grain boundary impurity concentration could be diminished up to a safe level. The kinetics of grain boundary solute segregation in grains of the symmetric shape was devoted article [1].

References

1 Shapovalov R.V., Slezov V.V., Osmayev O.A MFiNT, 2002, in print.

The Effect of Impurities and Grain Boundaries on

Radiation-Enhanced Diffusion in Zirconium

E.A. Smirnov,  A.A. Shmakov

Moscow Engineering Physics Institute, Russia (smirnov@phm.mephi.ru)

This paper has the goal to discuss the influence of the «impurity-vacancy» complexes (IVC) and grain boundaries on radiation-enhanced diffusion in Zirconium [14]. The possibility of the formation and disintegration is considered for the IVC, some kinetic equations are solved for the reducing (Sn) and accelerating (Fe) impurities, their diffusion and influence on the mutual recombination of point defects are estimated. All obtained data are compared with the experiments [3].

Using our model [3], considering the peculiarities of grain boundary diffusion (GBD) [5] and segregation effects, the coefficients of GBD are calculated for Zirconium under irradiation. At the assumption that grain boundary is the phase with the increased concentration of point defects all obtained data on radiation-enhanced GBD are analyzed in the frame of the models [13].

References

- Smirnov E.A., Abstr. of the III Intern. Ural Seminar on Radiation Damage Physics of Metals and Alloys, Snezhinsk, 1999, p. 2.

- Smirnov E.A., Shmakov A.A., Abstr. of the VI Russian Conf. on Reactor Material Science, Dimitrovgrad, 2000, p. 124.

- Smirnov E.A., Shmakov A.A., Defect & Diffusion Forum. 194-199, 1451 (2001).

- Smirnov E.A., Shmakov A.A., Dyomin D.V., Trans. of the XV Intern. Conf. on Radiation Physics and Materials Science, Alushta, 2002, p. 129.

- Smirnov E.A., Shishov V.N., Shmakov A.A., Abstr. Intern. Workshop «Diffusion, segregation and stresses», Moscow, 2002, p. 65.

Kinetics of Intragranular and Intergranular Radiation-Induced Phosphorus

Segregation in Reactor Pressure Vessel Steels

I. A. Stepanov, V. A. Pechenkin and Yu. V. Konobeev

SSC RF Institute of Physics & Power Engineering, Obninsk, Russia (sia@ippe.obninsk.ru)

Both the intragranular and intergranular segregation of phosphorus may significantly contribute to irradiation embrittlement of reactor pressure vessel steels [1]. The modeling of phosphorus radiation-induced segregation at cylindrical (dislocations), spherical (precipitates and voids) and flat (sample surfaces, grain boundaries (GB)) point defect (PD) sinks has been carried out in order to compare the kinetics and extent of segregation at various PD sinks. Dilute Fe-0.026P (at.%) alloy relevant to model and VVER-440 pressure vessel steels was considered.

Fig. 1 and Fig. 2 show the dose dependence of P accumulation on the surface of precipitate and on a GB which were carried out at a dose rate K=310-10 dpa/s, temperature T=270 OC and various precipitate densities Np [2] and grain sizes L. The time to reach steady state P concentration near dislocation or precipitate is much less than that near GB. Although the steady state P concentration near dislocations or precipitates is much less than that near GB, a “fast” P segregation at these sinks may lead to decreasing the free P content in the matrix and to reducing its subsequent accumulation on GBs at high densities of these internal sinks. A more significant effect on the kinetics of GB phosphorus segregation could be caused by the contribution of precipitates to PD sink strength. Fig. 1. Dose dependence of P concentration on the surface of a spherical precipitate at two precipitate densities Np

Fig. 2. Dose dependence of P concentration on a GB

This work was supported by the Russian Foundation for Basic Research under Project №01-02-16822.

# References

1.	Gurovich B.A., Kuleshova E.A., Nikolaev Yu.A., Shtrombakh Ya.I., J. Nucl. Mater. 246, 91 (1997)

2.	Gurovich B.A., Kuleshova E.A., Shtrombakh Ya.I., Zabusov O.O., Krasikov E.A., J. Nucl. Mater. 279, 259 (2000)

Modeling of Radiation-Induced Segregation in Fe-Cr-Ni alloys

I. A. Stepanov and V. A. Pechenkin

SSC RF Institute of Physics & Power Engineering, Obninsk, Russia (sia@ippe.obninsk.ru)

Radiation-induced segregation (RIS) effects significantly on the phase composition, void swelling, corrosion and embrittlement of alloys. In particular RIS of Fe-Cr-Ni alloy components results in nickel enrichment and chromium depletion near point defect (PD) sinks (sample surface, grain boundaries (GB), vacancy voids, dislocations, dislocation loops and others). Moreover the ferrite regions in austenite matrix and austenite regions in ferrite matrix can reveal due to RIS near these PD sinks [1].

In the present work mathematical model is proposed and calculations of Fe-Cr-Ni alloy component segregation are carried out near motionless as well as moving GB under irradiation. The binding energy of nickel atoms with iron and chromium atoms in mixed dumbbells is estimated using experimental data of low temperature segregation of Fe-Cr-Ni alloy components near GB [2] for taking into account interstitial mechanism of RIS. The modeling of RIS near GB, void and dislocation are performed in Fe-Cr-Ni alloy at various irradiation temperatures. The physical model for explanation of decreasing both RIS and void swelling in austenitic steels after doping with oversize substitutional atoms (titanium, niobium, tantalum, zirconium or hafnium [3, 4]) is proposed. The calculations of desegregation kinetic near GB in Fe-Cr-Ni alloy are carried out for isothermal post-irradiation annealing conditions.

This work was supported by the Russian Foundation for Basic Research under Project 
№ 01-02-16822.

# References

1.	Dumbill S.and Williams M., Materials for nuclear reactor core applications, in Proceedings of the International Conference (27-29 October 1987), British Nuclear Energy Society, London, 1987, v.1, p.119

2.	Watanabe S., Sakaguchi N., Kurome K., Nakamura M., Takahashi H., J. Nucl. Mater. 240, 251 (1997)

3.	Ohnuki S., in Sumposium on Diffusion in Materials (Sapporo, October 23-24, 1997)

4.	Ohnuki S., Takahashi H., Kato T. and Hamilton M.L., in Program and Abstracts of 21st Symposium on the Effects of Radiation on Materials (Tucson, Arizona, June 18-20, 2002), p.33

# Redistribution of Phosphorus in Reactor Pressure Vessel Materials

# During Operation

#### O.O. Zabusov

Russian Research Centre “Kurchatov Institute”, Moscow, Russia (zabusov@orm.irtm.kiae.ru)

Investigations of reactor pressure vessel materials by atom probe [1] and electron microscopy [2] have shown significant changes in the microstructure of both weld and base metals occurred during irradiation, post-irradiation annealing and re-irradiation following by noticeable redistribution of admixtures and alloying elements and leading to degradation of mechanical properties of the materials. The formation of copper-enriched clusters with phosphorus segregated on its surfaces and phosphorus-enriched atmospheres both not associated with any microstructure feature in the ferrite matrix and elongated along dislocation lines could be considered as the most important consequences of such processes. As the result the significant depletion of the ferrite matrix by phosphorus takes place – from 0.03% at. to 0.01-0.02% [3]. Thus when considering the radiation-induced grain boundary segregation of phosphorus its redistribution on microstructure features of the material must be taken into account because the matrix depletion can affect the segregation process. This phenomenon was showed for model alloys [4].

The estimation of phosphorus content on microstructure features has been carried out in this work at different conditions of the material on the basis of an atom probe investigation of VVER-440 weld metal [1]. The calculation of phosphorus content on grain boundaries of the base metal through the reactor pressure vessel wall thickness has been made using the modified McLean model [5] and the kinetic model of radiation damage of steels [6] with taking into account the depletion of the ferrite matrix by phosphorus.

The calculation has shown that the phosphorus content on grain boundaries can reach its maximum in the inner part of a reactor pressure vessel wall where the fluence does not reach its highest value.

References

- O.O. Zabusov. E.A. Krasikov, M.A. Kozodaev, A.L. Suvorov, P. Pareige, B. Radiguet. Redistribution of alloying elements and admixtures in VVER-440 pressure vessel steel under operational factors. – Proc. of the 15th Int. Conf. On Physics of Radiation Phenomena and Radiation Material Science, June 10-15, 2002, Alushta, Ucraine (in russian).

- B.A. Gurovich, E.A. Kuleshova, Ya.I. Shtrombakh, O.O. Zabusov, E.A. Krasikov. Intergranular and intragranular phosphorus segregation in Russian pressure vessel steels due to neutron irradiation. – J. Nucl. Mater. 279 (2000) 259-272.

- P. Pareige, S. Duval, J.P. Massoud, J-C. Van Duysen. Microstructural Evolution in Neutron-Irradiated Pressure Vessel Steels. A Tomographic Atom-Probe Study. – Report at 6th Russian Conference on Reactor Materials Science, Dimitrovgrad, 2000.

- J. Kameda, Y. Nishiyama, T.E. Bloomer. Non-equilibrium intergranular segregation and embrittlement in neutron-irradiated ferritic alloys. – Surface and Interface Analysis, 2001, v. 31, pp. 522-531.

- Nam-Hoe Heo. Theory of nonequilibrium segregation in an Fe-Mn-Ni ternary alloy and a ductile-brittle transition. – Acta Mater., 1996, v. 44, No 7, pp. 3015-3023.

- A.V. Nikolaeva, Yu.A. Nikolaev, Yu.R. Kevorkian, O.O. Zabusov Effect of radiation-induced grain boundary segregation of phosphorus on operational behavior of nuclear pressure vessel materials. –  Atomic Energy, V. 91, Iss. 5, 2001, pp. 343-353 (in Russian).

Radiation-Induced Crystallization of Amorphous Materials

# I.A.Antoshina, V.S.Khmelevskaya

## Obninsk Institute of Nuclear Power Engineering, Obninsk,, Russia (khmel@iate.obninsk.ru)

By the X-ray diffraction methods and also by measurements of the properties related to both an ionic and an electronic subsystems a crystallization of the amorphous materials has been studied. These materials are of the Fe-Cr-B and the Co-Fe-Si-B systems and were produced by a speed tempering from a liquid. Initial materials were in a completely amorphous state as X-ray diffraction data show. Then the alloys were annealed at various temperatures and also were irradiated in an accelerator by Ar+ ions with energies 20-50 keV up to fluences 5.1017  - 1.5.1018 ions/cm2 at different temperatures of a target. The comparison of these processes show that the beginning of a crystallization under irradiation are shifted to less temperatures in comparison with a thermal activated crystallization and the shift value is considerable (150 – 2000C). This

effect can be caused by the difference of processes of clusters formation due a thermal activation and under a radiation influence.

Both strong hardening and embrittlement are observed during an amorphous materials crystallization. This reaches a maximum within a narrow range of parameters near  the phase transformation point (in an amorphous-crystalline material). In the some cases the maximum hardness registers before the X-ray lines corresponding to the crystalline phase appear. It can be assumed that this is connected with the crystalline clusters which can not be observed by a X-ray analysis. At the same time the considerable changes in an electronic subsystem were registered which indicate the metallization of  an interatomic bonding.

A crystallization of amorphous alloys is also accompanied by an appearance of metastable phases which are not character for equilibrium states of these systems.