- Implanted and

Transmutational Gaseous

Impurities Behavior in

Irradiated Metals and Alloys

Determination of Hydrogen Permeation Reduction Factor (PRF) for Different Protective Coats on Vanadium

S.E. Afanaseva, T.V. Kulsartova, V.P. Shestakova, E.V. Chikhraya, D. Smithb.

a)NIIETF, Kazakh State University,. Almaty, Kazakhstan (istcvova@kazmail.asdc.kz)

b) Argonne National Laboratory, Argonne, USA

Selection of the structural material for liquid-metal system as for another system and constructions of nuclear energy plant must be carried out and based on appointed request depending on conditions of functioning this materials.

Their compatibility with liquid metals is a specific request. The pile creation with liquid-metal heat-transfer (Li, PbLi17) reproducing tritium requests additional clause to structural materials. This creation of structural material or protective barrier with minimum acceptable value of tritium permeation through them or with maximum permeation reduction factor- PRF.

Vanadium and vanadium alloy planed to use as a blanket structural material like nuclear energy plants.

Workable on a first stage vanadium must have stability characteristics at temperature 800C hydrogen influence.

Given work shows experiments results by testing protective coats on vanadium- glass-ceramic coating which based on CaO. Permeation reduction factor (PRF)for every coating and its changing depending on thermocapacity of vanadium sample with coating was determinate by method of hydrogen permeation.

The experiments results will be used at the development of pile protection outlines with liquid-metal heat-transfer.

Gas Bubble Evolution peculiarities in the Ferritic and Austenitic Steels

and Alloys under Helium Irradiation

S.Yu. Binyukova, I.I. Chernov, A.N. Kalashnikov, B.A. Kalin, Mitkhal Abu Kharroub*

Moscow Engineering Physics Institute (State University), (binu@phm.mephi.ru)

* Dept. of Phys., Atomic Energy Commission of Syria, Damascus, Syria

Austenitic and ferritic-martensitic steels of Cr13 type are considered as candidate structural materials for the fusion reactors first wall. A significant quantity of helium will be accumulated in the structural materials via (n, ) or other transmutation reactions, as well as it may be implanted from plasma through the first wall surface. Helium can have a pronounced effect on the radiation damage of materials and often may be an important reason in catastrophic degradation of their properties and shortening of the useful life of reactor constructional elements. In this connection considerable attention has been given to the helium problem in fission and fusion materials. One of these problems is the role of helium in enhancement of radiation swelling.

The aim of this paper is to investigate the peculiarities of gas swelling at high helium concentration and to compare the gaseous swelling level for materials with ferritic and austenitic structures.

By means of transmission electron microscope the gas bubble development in model alloys of Fe-C system, ferritic-martensitic steels of Cr13 type, nickel and austenitic steels has been investigated after   40-keV helium-ion irradiation up to a fluence of 51020 m-2 at the temperature of 650 OC.

It was shown that helium-ion irradiation at high temperature in Fe and ferritic-martensitic steels Cr12MoWSiNbVCeB and Cr12MoWSiNbVCeNB resulted in formation of bubbles with a greater size and a smaller density, than those in nickel and austenitic steel Cr16Ni15Mo2Mn2TiV. Thus the gas swelling of ferritic-martensitic steels may be high and over the gas swelling for some austenitic steels. In Fe-C alloys as well as in ferritic-martensitic steels, large gaseous bubbles in ferritic component are uniformly distributed in grains body. The bubbles with higher density and smaller size than those in ferritic component are formed in martensitic grains of steels and Fe-C alloys with a high carbon content (NC  0,01%), which leads to a small level of swelling of martensitic in comparison with ferritic. In addition, the bubbles in martensitic grains have a tendency to ordered distribution.

The standard heat-treatment (quench + temper) of ferritic-martensitic steel results in an increase of gas swelling that significantly exceeds the swelling of martensitic grains. In this, the swelling of ferritic grains is several times higher than that of martensitic grains.

Hydrogen Accumulation and Retention in Materials of

Reactor VVER-1000 Vessel Components

I.M. Neklyudov, B.A. Shilyaev ,A.N. Morozov, A.A. Parkhomenko, V.V. Bryk

National Research Center “Institute of Physics and Technology”, Kharkov, Ukraine

(morozov@kipt.kharkov.ua)

Investigation of Concentration and Temperature Dependences of Processes of

Hydrogen and Helium Accumulation and Desorption in Steel 08Cr18Ni10Ti

V.V. Bryk, O.V. Borodin, V.N. Voyevodin, I.M. Neklyudov, V.V. Ruzhitsky, G.D. Tolstolutskaya

National Research Center “Institute of Physics and Technology”, Kharkov, Ukraine (bryk@kipt.kharkov.ua)

### Hydrogen Thermodesorption from Helium Ions-Implanted Steel 08Cr18Ni10Ti

A.N. Morozov, I.M. Neklyudov, V.V. Bryk, V.G. Kulish, V.I. Zhurba

National Research Center “Institute of Physics and Technology”, Kharkov, Ukraine

(morozov@kipt.kharkov.ua)

Influence of Interstitial and Substitution Elements on Helium and Hydrogen

Behavior in FCC and BCC Metals

I.I. Chernov, B.A. Kalin

Moscow Engineering Physics Institute (State University), Russia (chernov@phm.mephi.ru)

The main experimental results obtained by authors during the last 20 years on ion-implanted helium and hydrogen behavior and microstructure evolution under different irradiation conditions and post-irradiation treatment of structural steels and alloys, as well as of model alloys of Ni-С, Ni-Х (Х = Be, Si, Mo, W, Al, Ti, Ta, Sn, Zr), Fe-С, V-Ti systems, are presented.

It was shown that the helium thermodesorption (TDS) peaks are displaced to higher temperatures and the effective activation energy for helium desorption grows with increasing carbon concentration in metals by changing of bubbles migration mechanism from surface diffusion in pure metals to volume diffusion in alloys because of carbon segregation in the bubbles near-surface volume. Influence of carbon on deuterium behavior is similar. During post-irradiation annealings small-sized and high density bubbles are formed in the alloys of Fe-C system than that in Ni-C alloys owing to higher binding energy of helium-vacancy complexes in iron. In contrast, after high-temperature (650 OC) implantation by helium large bubbles with small density are formed in iron and ferritic-martensitic steels of Cr13 type than bubbles forming in nickel and austenitic steels.

Decrease of matrix atom self-diffusion coefficient in Ni-Al alloys can result in a decrease in bubble migration rate and shift of TDS peaks to the higher temperatures with increasing Al concentration. To the contrary, in the V-Ti alloys the TDS peaks are displaced to lower temperatures with increasing Ti content because of increase of vanadium atom self-diffusion coefficient by titanium doping. However in both systems of alloys the effective activation energy for helium desorption grows with alloying element concentration due to the change of bubble migration mechanism from surface diffusion (for pure metals) to an increase of the role of volume diffusion (for alloys) because the volume diffusion coefficient is greater than that for surface diffusion.

It is found that the most thermally stable complexes of the HemMekVn type (where He and Me are helium and alloying element atoms, V is a vacancy) are formed along with simple complexes of HemVn type in the case of positively discrepancy between matrix atoms and atoms of alloying elements in the substitution alloys. As the result, small bubbles and high density are formed in the alloys during post-implantation annealing.

The obtained regularities of gas swelling for Ni-Х alloys under helium-ion irradiation are in a good correlation with data for alloying influence on swelling by neutron or heavy ion irradiation, namely, the swelling has maximum if the number of bonding d electrons in the alloy is equal to three.

Investigation of Tritium Permeation Process Produced in Lead-Lithium Eutectic Pb83Li17 Through Tube Steel Sample F82H- in Reactor Irradiation Conditions

T.V. Kulsartova, V.P. Shestakova, E.V. Chikhraya, E.A. Kenzhinb, A.N. Kolbaenkovb,

Hiroshi Kawamuraс and Masaru Nakamichiс

a) NIIETF, Kazakh State University,. Almaty, Kazakhstan (istcvova@kazmail.asdc.kz)

b)Institute of Nuclear Energy, NNC RK, Semipalatinsk-21, Kazakhstan

c) Blanket Irradiation and Analysis Laboratory at JAERI, Higashi Ibaraki-gun, Ibaraki-ken 311-13, Orai-machi, Japan

The problem of hydrogen permeation structural materials (KM) of fusion reactor arise and exist as a result of using tritium in future fusing reactors, which has diffusion leakage and as calculations show, they are great and make line of constructional hardship and will request great expense as for defense personnel and environment as for cleaning a heat-transfer from tritium.

Lithium-lead eutectic (Li17Pb83 further denote as Li-Pb) is one of more useful material of heat-transfer as applied to shell of tritium breeder due to its high-level of tritium reproduction, low reactivity and workability as a heat-transfer. It is very important to study the process of tritium ejection by breeder material and process of leakage through structural material, surrounding alloy.

Low-activity alloy F82H suppose to use as a main structural material of system by accumulation tritium of the future fusion plants.

In this work were produced the experiments by study of permeation tritium process through F82H steel from PbLi eutectic at reactor irradiation.

The experiments were made by hydrogen permeation method on IVG1.M NNC RK reactor. Sample of F82H steel was produced by Japan institute of nuclear energy. The tritium flow dependence through sample were got during reactor irradiation. By them were made model, which describe the process of permeation tritium from lead-lithium eutectic.

Investigation of Helium-3 Buildup Operation in Structural Materials

by “Tritium Trick” Method

I.L. Malkov, V.G. Klevtsov, A.A. Yukhimchuk, S.V.  Zlatoustovski

Russian Federal Nuclear Center – All Russian Scientific Research Institute of Experimental Physics (RENC-VNIIEF), Sarov, Russia

The investigation of the effects of dissolved helium-3 and hydrogen isotopes on physical and mechanical properties of metals is defined as one of the fundamental lines in metal physics and has practical importance.

In RFNC-VNIIEF, the accelerated buildup of the helium-3 concentrations of ~100-500 appm (~8-40 cm3He/100 g Me) was performed by “tritium trick” through the exposure the samples of the investigated material in gaseous tritium at higher temperature and pressure. For the future radiation safety research of the effects of dissolved helium-3 on material structure, mechanical properties and hydrogen permeability the samples should be detritiated

The setup of the detritiation was implemented and the method of the samples detritiation was selected.

The tritium and helium-3 tests in the structural materials were carried out by the setup developed on basis of the gas-analyzer “ELTRA”. The experimental results of helium-3 test were in reasonable agreement with the calculated helium-3 concentrations. Dependence of the tritium desorption rate on the detritiation time was obtained. It was found that the process of the detritiation has some stages.

Hydrogen Permeation Through Thin Coatings

#### A.A. Kurdyumov

Research Institute of Physics, St. Petersburg State University, St. Petersburg, Russia.

The main idea of this research is based on the fact that high activation energy of adsorption should be an effective barrier for hydrogen transport in the case when gaseous molecular hydrogen is in temperature equilibrium with a membrane. If in addition to sufficiently high adsorption barrier (several eV), hydrogen dissolution in the bulk of material is hindered, this material can be used as a thin lightweight coating, which will be as effective as a massive fusion claddings of materials having activation energy of permeation of about a fraction of eV.

The necessary properties, which are governed by a low density of states on Fermi level and low concentration of free carriers, can have some composite materials or nonmetal materials - semiconductors and insulators.  In contrast to well-studied metals, hydrogen interaction with these materials has not been adequately investigated. The complex of techniques, which includes the method of analysis of permeation isotherms and concentration pulses method in permeation mode, has been created in our laboratory. These techniques allow to obtain information about hydrogen interaction with thin films from the data obtained from the studying of  two-layer systems: thin film on the permeable substrate.

Nickel oxide, amorphous silicon and titanium nitride were chosen as the objects for investigation.

Nickel oxide does not adsorb hydrogen at all and  hydrogen permeation occurs via diffusion along the grain boundaries. The rate of diffusion is independent on temperature and the obtained value of preexponential factor of about 1*10-10 cm2/s is characteristic of a diffusion process along grain boundaries. Correspondingly, nickel oxide does not practically dissolve and accumulate hydrogen.

Amorphous silicon. Silicon although slowly and with great activation energy does adsorb hydrogen, which dissociates into atoms on the surface. Hydrogen migration through the bulk is also very slow. Preexponential factor of diffusion coefficient  (“released” from the effects of the trapping and detrapping rates) is as low as 10-8 cm2/s, though the activation energy has a rather common value. The peculiarities of hydrogen transport in amorphous silicon could be accounted for on the assumption that hydrogen transport is accompanied with reconstruction of local bonding.

Titanium nitride. There are two principally different mechanisms of hydrogen permeation through TiN in different temperature regions. The first one is highly activated permeation at high temperature. The second one  is characterized with a common for permeation process activation energy of about 0.6 eV and occurs at lower temperatures. Kinetics of the steady state flux onset for the coated membrane appears to be very slow and can not be described in the framework of an ordinary diffusion. The observed temperature dependence of permeability is characteristic of the materials having two parallel channels of  hydrogen transport with strongly different activation energies.

It has been established that the high temperature part of permeation curve presents the true permeation through TiN crystallites and  the rate of hydrogen adsorption on TiN surface  has a marked influence on the rate of permeation under conditions of our tests. It is most likely that permeation at low temperature is due to molecular diffusion along grain boundaries.

Development of Helium Bubbles near Grain Boundaries in Nickel-Carbon Alloys

I.V. Reutov 1 and V.F. Reutov2

1 RCS Kurchatov Institute, Moscow, Russia

2 Flerov Laboratory of Nuclear Reactions, JINR, Dubna, Russia

( reutov@nrsun.jinr.ru)

The peculiarities of development of helium bubbles near grain boundaries in nickel with different carbon content in the process of post-irradiation isothermal annealing are studied in the present paper. The samples of nickel with carbon content of 0.002, 0.007, 0.010, 0.039 and 0.065 % have been uniformly doped with helium up to 2 • 10-2 at.% concentration and annealed in vacuum at 800°C for 1, 5, 10 and 50 hours. The development of helium bubbles in near-boundary zone has been investigated by means of optical and electron microscopy (ТЕМ).

It is stated that at this annealing temperature intensive nucleation and growth of bubbles are observed in near-boundary region whose width grows both with the increase of annealing time and carbon content. Anomalous restraining of the development nearby boundary zone with helium bubbles in nickel samples with 0.007% carbon has been noted.

The ТЕМ investigations have shown that near-boundary zone the process of bubble growth is non-uniform: bubble size increases and their density decreases as the distance from grain boundary is increased. The effect observed is discussed from the point of view of formation of two zones with different level of swelling in a grain (nearby boundary and matrix) and, consequently, hydrostatic stress as well conditioning the flux of vacancies and helium-vacancy complexes from matrix to grain boundary.

Radiation Microstructure, Helium, Hydrogen in Reactor VVER-1000 Vessel Structure Elements

V.N. Voyevodin, V.V. Bryk, O.V. Borodin, B.A. Shilyaev, I.M. Neklyudov

National Research Center “Institute of Physics and Technology”, Kharkov, Ukraine

A computational method was used to analyze the sources of transmutational helium and hydrogen in stainless steel Cr18Ni10Ti in the reactor core (reflection shield) and between the reactor core and the pit. The dynamics of H, He generation and cascade vacancy clusters formation in a standard neutron flux from the source material atoms is described with a system of connected differential equations accounting for the rates of their formation and disappearance, or transformation to other structure elements.

References

- I.M. Neklyudov, A.G. Rudenko, B.A. Shilyaev, Transactions of the 2nd International Conference “Nuclear and Radiation Physics”, ICNR-99, Almaty, Kazakhstan, 1999, p. 61- 62.

- S.M.Brumer, E.P.Simonen, P.M.Scott, P.L.Andresen, G.S.Was, J.L.Nelson, J. Nucl. Mater., 274 (1999) 299-314.

- J.D.Hunn, E.H.Lee, T.S.Buyn, L.K.Mansur, J.Nucl.Mater.,282(2000)131-136.

Formation and Growth of Hydrides in Irradiated Zirconium Alloys

A.A. Shmakov,  A.G. Ioltukhovsky1),  B.A. Kalin,  E.A. Smirnov

Moscow Engineering Physics Institute, Russia (shmakov@phm.mephi.ru)

1) All-Russia A.A.Bochvar Research Institute of Inorganic Materials, Moscow, Russia

Zirconium-niobium fuel cladding tubes pick up about of 50-100 ppm H during their service in VVER and RBMK reactors [1]. This hydrogen is quite mobile, it accumulates in the regions with high tensile stress and low temperature. When hydrogen content exceeds the terminal solid solubility on such parts, the local brittle hydride zones form in material. It creates the danger of delayed hydride cracking (DHC) in the acting and spent fuel rods [2]. In order to prognosticate the above phenomenon the calculation experiments can be especially useful.

The temperature dependence of DHC in the alloys Zry-2 and E110:

 Irradiated Zry-2, experiment [4]

 Irradiated Zry-2, our calculation

 Unirradiated E110, experiment [5]

 Unirradiated E110, our calculation

 Irradiated E110, our calculation

Our paper has the aim to estimate the possibility and characteristics of DHC in the fuel claddings with the deep (up to 500 m) nodular and fretting damages. The most reliable database on diffusion and solubility of hydrogen in zirconium materials, new calculation model on DHC and some of the obtained results (for example, see Figure) will be demonstrated and discussed.

Reference

- Shmakov A.A., Bibilashvili Yu.K., Kalin B.A., Smirnov E.A. Hydride Cracking in Zirconium-Based Fuel Cladding Tubes: Prognostication of the Possibility (Moscow, MEPhI, 1999).

- Ioltukhovsky A.G., Kalin B.A., Shmakov A.A. Hydrogen Embrittlement and Hydride Cracking in Zirconium Components of LWR (Moscow, MEPhI, 2001).

- Efsing P., Pettersson K. Zr in the Nucl. Ind.: XII Intern Symp., ASTM STP 1354, PA, 2000, pp. 340355.

- Ivanova S.V., Nikulina A.V. Studies of Hydrogen Induced Processes in Thin-Walled Zirconium Components of Fuel Assemblies, Trans. of the VI Russian Conf. on Reactor Material Science, Dimitrovgrad, Russia, 2000, pp. 128145.

Structural Factors Influence on Hydrogen Extraction from Irradiated

Construction Materials

# A.G.  Zaluzhnyi, V.P. Kopytin, A.L. Suvorov, D.M. Uspenskyi

Institute of Theoretical and Experimental Physics,

Moscow, Russia   (zaluzhnyi@itep1.itep.ru)

Researching of holding hydrogen isotopes in metals in different heating regimes have been studied deeply recently because of need to find and work out the possible materials for first wall of thermo- nuclear reactor (TNR).  Fist of all, it connects to a problem of service safety of TNR and loosing of valuable fuel (tritium)

In the present work the results of the researching of kinetic for hydrogen extraction from the samples of austenitic steal, saturated with hydrogen in reaction with deuterium plasma, and from samples earlier irradiated in water- water reactor (WWR) in temperature of 590 K till the fluence (0.4-0.9)*1025 m2 (after the irradiation the samples during 5 years were in normal temperature), are presented. We received that, being heated, the samples, irradiated in the reactor, extract a big value of hydrogen in high temperatures. It means that atoms of hydrogen in the irradiated sample were caught by traps (the energy of bounding with the traps is 0.3 eV).

During the researching of the austenitic steal, which had reacted to deuterium plasma, the anomalously big blisters with the thickness of –1 μm were obtained. The blisters contained some hydrocarbons, methane for example. The blisters were found out to be destroyed, if methane pressure (before the temperature of methane dissociation) is higher then the pressure, needed to destroy blisters. If in the temperature of methane dissociation the pressure of methane in the blisters is not enough to destroy them, than the blisters stay safe even in the further heating.

Giving the result of the researching on prior cold deformations and grain sizes on hydrogen holding in construction materials. That is why the researching of hydrogen penetration through the construction materials with the given structure characteristics in the process of bombardment by accelerated hydrogen ions, had place. It was found out that the prior cold deformation as well as decreasing sizes of grains, increase the hydrogen penetration through the studied materials during the hydrogen ions bombardment.

Specific Features of Interaction of Heavy Hydrogen Isotopes and Radiation-Resistant Cr16Ni15M03Ti1 and SS316L Steels

Yu.N. Dolinsky*, Yu.N. Zouev*, I.A. Lyasota*, I.V. Podgornova*, I.V. Saprykina*, V.V. Sagaradze**

*Russian Federal Nuclear Center – Institute of Technical Physics, Snezhinsk, Russian Federation (y.n.zouev@vniitf.ru)

**Institute of Metal Physics, Ural Branch RAS, Ekaterinburg, Russian Federation

The knowledge of parameters of interaction between heavy hydrogen isotopes and constructional materials of nuclear and fusion reactors is very important for maintaining their in-service properties at an adequate level and minimizing the contamination of the environment with tritium thanks to a decrease in the tritium penetration through metal walls and development of technologies for removal of tritium from used structures.

The present paper reports results of a study dealing with penetration of deuterium and tritium through samples of Cr15Ni16Mo3Ti1 and SS316L austenitic steels from the gaseous phase. The steady-state flow method was used. Experimental temperature dependences of the permeability, diffusion coefficients, and solubility, and also calculated constants of the corresponding processes have been discussed. It was supposed that titanium caused a deviation of the temperature dependences of diffusion coefficients and solubility of the Cr15Ni16Mo3Ti1 steel from the Arrhenius dependence. This supposition was confirmed to a certain extent by results of experiments with the 12Cr18Ni10Ti steel.

Mechanism by Which Titanium Influences Formation of Radiation-Induced Segregation of Deuterium in Cr16Ni15Mo3(Ti1) Steel

G.A. Raspopova, V.L. Arbuzov, V.V. Sagaradze, N.L. Pecherkina, V.A. Pavlov,

K.V. Shalnov, A.P. Druzhkov

- Institute of Metal Physics, Ural Branch RAS, Ekaterinburg, Russian Federation (raspopova@imp.uran.ru)

A radiation-induced segregation (RIS) of hydrogen is formed in hydrogen-containing metals and alloys exposed to ion irradiation. The appearance of RIS is attested to by a high concentration of hydrogen in irradiated zones (as compared to an average concentration in the bulk) and an equal distribution of hydrogen atoms and vacancies in the radiation-damaged region. Our earlier study showed that the deuterium RIS in the Cr16Ni15Mo3Ti1 austenitic steel was  unsta-

ble after an anomalous "collective" pattern: when irradiation was stopped, the segregation was enhanced thanks to an inflow of deuterium from the nonirradiated volume of the target.

It was supposed that an anomalous behavior of the segregation could be related to specific features of the composition and (or) the structure of the steel. However, RIS proved to be free of this type of instability in nickel, which is a model material of austenitic (FCC) steels, and BCC Fe-Cr alloys. The goal of the present study was to determine the role of titanium in formation and an anomalous behavior of the deuterium segregation in the Cr16Ni15Mo3Ti1 steel.

The effect of titanium on the microstructure of the Cr16Ni15Mo3(Ti1) steel was examined by the methods of transmission electron, scanning electron, and tunneling microscopy. The nuclear reactions methods combined with concurrent irradiation with deuterons and measurements of the deuterium concentration in the segregation was used to determine the role of titanium in formation of RIS in the steel.

It was found that addition of 1% Ti changed the steel structure and favored an increase in the deuterium segregation. It was shown that the solid-solution titanium initiated formation of hydrogen vacancy traps at room temperature and caused precipitation of particles of titanium-containing compounds (carbides and intermetallics), which facilitated an additional capture of deuterium atoms, during aging. An anomalous collective-type instability of the segregation (after irradiation was stopped) was observed both in the titanium-loaded and titanium-free austenitic steel.

This study was performed with a financial support from the Russian Fund of Fundamental Research (Projects Nos. 01-02-16877 and 00-15-96581).

### The In-Pile Experiments on the Reactor IVG.1M

V.P. Shestakov*, T.V. Kulsartov*, E.V. Chikhray*, U.L. Zheldak*

A.N. Kolbaenkov**, E.A. Kenzhin**, V.V. Zverev**, I. V. Prozorova**, U.N. Gordienko**,

A.F. Incov**

*NIIETF, Kazakh State University,. Almaty, Kazakhstan (istcvova@kazmail.asdc.kz)

**Institute of Nuclear Energy NNC RC,  Semipalatinsk-21, Kazakhstan

Given work shows experiments results by study tritium permeation which generated from lithium -lead eutectic, through steel MANET with different covers. The results by tritium and helium evolving from lithium -lead eutectic were shown.

The results of neutron-physical and thermal-physical calculations of canal experimental devices (CED) were shown in detail. The design philosophy (CED) were discussed.

The first experimental results by study tritium steam-out from lithium-titanium ceramic were adduced.