- Some Aspects of Physics

of Radiation Phenomena

in Semiconductors

and Insulators

Effect of the Nanoparticle Size and Structural Defects on Magnetic Properties of Antiferromagnetic and Ferromagnetic Oxides

T.I. Arbuzova*, S.V. Naumov*, B.A. Gizhevskii*, V.L. Arbuzov*, K.V. Shal`nov*, E.A. Kozlov**

* Institute of Metal Physics, Ural Branch of RAS, Ekaterinburg, Russia (naumov@imp.uran.ru)

** Russian Federal Nuclear Centre - Russian Research Institute of Technical Physics, Snezhinsk, Russia

Magnetic nanoparticles have attracted a lot of attention in recent years. The magnetic properties of bulk materials and nanoparticles may be different. Near surface the orientation of magnetic moments may be altered due to the loss of three-dimensional structural periodicity and broken exchange bonds. The surface and interface effects, such as the spin disorder and superparamagnetism, were found in the cases of magnetic metals and ferromagnetic spinels [1]. The understanding of the intrinsic properties of nanoparticles is of extreme interest not only from the fundamental point of view, but also for the technological application of the nanocrystal materials.

In this work we report study on effects of particle sizes, microdeformations and radiation defects on the magnetic susceptibility (Т) for nanocrystalline ionic compounds CuO and Mn3O4. The nanoparticle sizes were determined by means of scanning tunnelling microscope. CuO is a low-dimensional antiferromagnet, which transforms into 3D state at TN=230 К. Near TN a maximum of the susceptibility typical for 3D-antiferromagnets is absent and only the slope of the (Т) curve changes [2]. Mn3O4 is a ferrimagnet with TN=41.9 К and has the complicated magnetic structure. The triangular spin ordering of Yafet-Kittel type is realized below Т=33 К. The temperature dependence of the reciprocal susceptibility 1/(Т) has a hyperbolic shape in the wide range of temperatures TN < T < 400 K and obeys the Cure-Weiss law at T > 400 К [3].

The single-phase nanocrystalline samples CuO were prepared by two methods. The high-dense nanoceramics with average grain size d=5-100 nm were obtained by the action of spherical shock waves. It has been found that the decrease of a grain size d < 70 nm leads to the increase of the susceptibility and the appearance of the contribution ~1/Т in the low temperature range T < 140 К [4]. At high temperatures T > 230 K the values of  are coinciding for all samples. After three years of storage the grain sizes in shocked CuO remain invariable. The disappearance of the contribution ~1/Т may be due to a relaxation of microdeformations and transition of grain boundaries into equilibrium state. The loose nanopowders CuO with the particle size of 15, 45 and 60 nm were prepared by gas condensation and oxidation of copper. For nanopowder CuO the susceptibility decreases at increasing Т in the range Т=80-600 К. The correlation between susceptibility and nanoparticle size is observed for both series of nanocrystal samples CuO. Nanoceramic samples Mn3O4 with the minimal grain size d=0.06 m prepared by the action of shock waves have a higher values of the susceptibility than polycrystals. At Т=300 К the value of  decreases as the magnetic field increases.

Thus, in oxide nanomaterials the susceptibility is strongly influenced by the particles size, density and microstructure details of both core and surface. The observed magnetic properties of the nanocrystal samples CuO and Mn3O4 are explained by the breaking of exchange bonds for surface ions and the destruction of long-range order.

The work is supported by Russian Foundation for Basic Research, grant No. 01-02-96403 and contract of the Ministry of Science and Technology №40.012.1.1.1153

# References

- R.H.Kodama. JMMM, 200, 359 (1999)

- T.I.Arbuzova et.al., FTT, 40, 1876 (1998)

- B.Boucher et.al., J.Phys.Chem.Solids, 32, 2429 (1971)

- T.I.Arbuzova et.al., FTT, 43, 846 (2001)

# Quantitative Model of Irradiated Semiconductor

# V.N. Brudnyi*, S.N. Grinyaev*, N.G. Kolin**

*V.D. Kuznetsov SFTI at TGU, Tomsk, Russia (brudnyi@ic.tsu.ru)

**FGUP L.Ya. Karpov NIFHI, Obninsk, Russia

Radiation processes complexity hampers creation of irradiated semiconductor quantitative model suitable for use in radiation technologies and in radiation resistance assessments. In spite of the data bulk they don't meet the main point viz. why under irradiation some materials obtain eigen conductivity and in other low-ohmic n(n+)-  or  p(p+)-zones form. Therefore at present basic way of researches is data storage on radiation defects (RD) characteristics that requires experiment bulk. In such a way radiation physics of Si has been developing. However in the main part of the compound materials these data are until fragmentary for imaging overall picture of radiation damages. It causes developing prognostic models of irradiated semiconductors.

It displays the model for quantitative analyses of electrical properties and for estimation of stationary (limiting) Fermi level position (Flim) in irradiated semiconductors. In the model Flim value is identified with a deepest defect level EB of the crystal. The model allow for the fact that RD are deep states and so only integral characteristics of crystal energy spectra are important for them. It allows to calculate position EB as a single energy level in semiconductors with analogous chemical bond type [1]:

21/(EB - Enk)3 == 0,

where Enk is energy spectra of the crystal, G0(EB) is Green function of the perfect crystal. It should note that the model of the deep level doesn't connect with some specific defect of the crystal. In the model just a single basic feature of the deep center is considered namely the most powerful localization of its wave function among other defect states of the crystal. This circumstance ensures weak sensitivity of this level both to a character of the defect and crystal matrix of semiconductor.

As is seen from the table values ЕВ are neighbours to experimental ones Flim in irradiated semiconductors and their changes depending on material band-gap width are similar. On the base of research it can conclude that defect states, which levels close to the level ЕВ(=Flim), are the most steady in the crystal since they have the smallest generation energy. Consequence of this is: (1) generation processes of complexes of dopants and RD with deep levels in doped semiconductors that are well known for Si; (2) clusterization of RD during further annealing or high-temperature irradiation; (3) stability of deep defect levels to heat treatment.

Table

Calculated values of minimum band-gap Еg , levels ЕB and experimental quantities Fsa (in relation to valence band ceiling, eV) and equal limiting electrical parameters of irradiated semiconductors

| Crystal | Eg | ЕB [1] | Fsat [2] | Electrical parameters |
| --- | --- | --- | --- | --- |
| Si | 1.20 | 0.47 | 0.39 | p-type, 105 Ohm·cm |
| Ge | 0.78 | 0.26 | 0.13 | p-type, p1016 cm-3 |
| AlSb | 1.60 | 0.63 | 0.5 | p-type, 106 Ohm·cm |
| GaP | 2.37 | 1.16 | 1.0 0.2 | 2х1013 Ohm·cm |
| GaAs | 1.51 | 0.77 | 0.6 | 108-9 Ohm·cm |
| GaSb | 0.87 | 0.24 | 0.02-0.05 | p+-type, p+3·1018 cm-3 |
| InP | 1.43 | 1.03 | 1.0 | n-type, n(3-6)·1012 cm-3 |
| InAs | 0.39 | 0.52* | 0.52 | n+-type, n3·1018 cm-3 |
| InSb | 0.14 | 0.09* | 0.0 | p+-type, p7·1017 cm-3 |

Thus under irradiation Fermi level of the crystal is shifted in the most deep state for the crystal that define evolution of semiconductor electrical parameters and its limiting electrical characteristics. It allows to predict processes of radiation modification and estimate semiconductor radiation resistance especially where there isn't reliable experimental data.

The work has been made under financing of ISTC (project #1630).

## References

1. Brudnyi V.N., Grinyaev S.N., Kolin N.G. Materialovedenie, 2002 (in printing)

2. Brudnyi V.N., Grinyaev  S.N.,  Stepanov V.E.  Physica B, 212, 429 (1995).

Fermi-Level Pinning in Irradiated Non-Metallic Materials

V.N. Brudnyi*, S.N. Grinyaev*, N.G. Kolin**

*V.D. Kuznetsov Siberian physical technical institute, Tomsk, Russia (brudnyi@ic.tsu.ru)

**Obninsk Branch of State Research Center "L.Ya. Karpov Institute of Physical Chemistry",

Obninsk, Russia

The presence of the energetic gap in the band structure of the non-metallic materials (semiconductors, dielectrics) results in theirs high sensitivity to the various violations in the lattice structure (intrinsic lattice defects, dislocations, etc.). The lattice defects accumulation in these materials upon the high energy radiation results to the tremendous change of theirs electronic properties that is widely used in practical aims but at the same time it results the small radiation hardness of these materials in comparison with metals. The history of radiation effects investigation in such materials are usually based on the data about the electronic and microscopic nature of the defective states are generated in the crystal lattice upon bombardment. It requires a huge volume of the data about radiation-induced defects (RID) properties. Meantime, the nature and origin of these defects unknown in the most of materials. Therefore, main aim of these researches is to develop such approach, which can give a fundamental understanding of radiation-induced effects with scarce information about the nature and parameters of RID.

It is known that a common effect for non-metallic materials is the pinning of the electronic chemical potential (Fermi level) in a final (ultimate) position Fult upon irradiation. It enables to consider the radiation effects in these materials in the frame of the unified approach that gives the opportunity to predict theirs electronic properties after bombardment without the detailed information about the nature and the behaviors of RID. The present paper focuses on the general approach to the Fermi-level pinning in the great group (more than 20) semiconductors upon irradiation. The correlation between the electronic properties, the Fult -position after irradiation and the peculiarities of the band spectra of the crystals are revealed. These correlation were analyzed using some theoretical models: (1)- the model of the radiation "compensation" [1], (2)-the charge (local) neutrality models [1,2]; (3) the model of the "deepest" defective state [3,4]. The calculations obtained proved good correspondence with experimental data in the irradiated semiconductors and explains the correlation between different theoretical approaches to the problem of the Fermi-level pinning in these materials.. The data are presented here can be used for analysis the general totality of the experimental results in the irradiated semiconductors and for prediction theirs electronic properties after high energy bombardment.

# References

1. Brudnyi V.N. Grineaev S.N., Stepanov V.E., Physica B.Cond.Matter.212 429 (1995).

2. Brudnyi V.N., Grinayev S.N., Semiconductors 33 284 (1998).

3. Brudnyi V.N., Grineaev S.N., Kolin N.G., Materialovedenie (2002, in publishing)

4. Brudnyi V.N., Grineaev S.N., Kolin N.G., Physica B.Cond.Matter. (2002, in publishing).

11B and 25Mg NMR Estimates of Electron Density-of-States in

Superconducting MgB2 Disordered by n1-Irradiation

### A.P. Gerashenko, K.N. Mikhalev, S.V. Verkhovskii, A.E. Karkin and

### B.N. Goshchitskii

Institute of Metal Physics, UB RAS, 620219 Ekaterinburg,  Russia (gerashenko@imp.uran.ru)

The influence of structural disorder on the electron states in conduction band of MgB2 is question of great interest both in physics and technology. As known high-pressure technology in sintering of the compacted MgB2-materials results in stressed crystal structure accompanied by decrease of Tc and broad superconducting transition in comparison with as grown at ambient pressure crystals. Radiation disordering by neutrons is probably the purest method to study the influence of the induced structural disorder on the physical properties regarding to the motion of carriers in conduction band.  As shown in [1] superconducting temperature Tc drops below 10 K whereas the initial crystal structure  is  preserved under n1-irradiation up to  the fluence of thermal neutrons Φ =1.1019cm-2. The moderate irradiation leads to anisotropic expansion of the crystal lattice with increase of the c/a ratio resulting in increase of the interlayer distance. The Rietveld analysis refinement of X-ray diffraction patterns yields some decrease in the occupation number at Mg-sites.

NMR line shift and nuclear spin-lattice relaxation rate T1-1 of 11B and 25Mg were measured in superconducting MgB2 (Tcons =38 K) structurally disordered by nuclear reactor neutrons up to the fluence of thermal neutrons Φ =1.1019 cm-2. The temperature of superconducting transition was shifted down to Tc,irradons =7 K under irradiation. The change due irradiation in the partial electron density of states (DOS) at the Fermi energy of boron and magnesium  were traced by taking into account that T1-1 of 11B and 25Mg are determined by hyperfine magnetic interactions with carriers. According the NMR data obtained

- the partial DOS of s-states is not influenced by disorder;

- substantial decrease in DOS of 2p-states occurs under irradiation;

The NMR estimates for DOS using the McMillan formula show that critical temperature decreases in irradiated MgB2 mainly due to reduction in the partial DOS of p states of boron.

References

- A.E.Karkin, V.I.Voronin, T.V.Dyachkova, A.P.Tyutyunnik, V.G.Zubkov, Yu.G.Zainulin and

B.N.Goshchitskii,  cond-mat/010344 v2 (2001).

- A.Gerashenko, K.Mikhalev, S.Verkhovskii, T.D'yachkova, A.Tyutyunnik, V.Zubkov, , Appl. Magn. Reson. 21, 157 (2001).

- A.P.Gerashenko, K.N.Mikhalev, S.V.Verkhovskii, A.E.Karkin and B.N.Goshchitskii, Phys Rev.B 65, 132506 (2002).

Long-Lived Radiation Defects on Implanted Silicon

N.N. Gerasimenko (junior)*, N.N. Gerasimenko**, V.Yu. Troitskii***

*Russian Scientific Center, Microtechnology Institute (Nikolai_Gerasimenko@srisa.ru)

The existence of radiation defects on implanted silicon surface was discovered by means of recently developed technique, based on measuring of optical constants connected with thermal conductivity change. These defects alter optical constants (complex index coefficient, reflection coefficient) of irradiated silicon surface, and then during the storage of irradiated sample these alterations relax over a long period of time: up to month after implantation.

Investigations were carried out allowing to ascertain that long-term relax does not connect with absorption–desorption processes, and that it is defined by structural alterations of irradiated silicon layer and long-term processes of reconfiguration.

Investigations of observed effect were carried out for ion species, which are most frequently used in silicon implantation: boron, phosphorus, and arsenic, also for ions, neutral by transistance, in particular, argon.

Well-founded conclusions about observed effect nature were stated.

Investigation of Defectiveness of Nanocrystal Ceramics CuO  by Positron

Annihilation Method

A.P. Druzhkov*, B.A. Gizhevskii*, V.L. Arbuzov*, E.A. Kozlov**, S.V. Naumov*,

K.V. Shal’nov*, D.A. Perminov*, N.V. Kostromina*
*Institute of Metal Physics, Ural Branch of the Russian Academy of Sciences,

Ekaterinburg, Russia (gizhevskii@imp.uran.ru)
**Russian Federal Nuclear Center – Academician E.I.Zababakhin Research Institute of

Technical Physics, Snezhinsk, Russia

The unique properties of promising materials such as radiation-modified and nanocrystal ones, are defined by their structure and specified set of defects. The positron annihilation method is the effective tool to investigate structural and electronic properties, in particular, vacancies and their agglomerates, microvoids and changes in the electronic structure associated with defects. In the current paper the high-density nanoceramics and CuO microceramics with the size of crystallites of 15-90 nm and 5-15 m, correspondingly, have been investigated by the method of angular correlation of annihilation radiation (ACAR). The CuO nanoceramics has been produced by loading of the blank of CuO microceramics by spherically converging shock waves [1-3]. The loading has been provided by detonation of the layer of RDX-based composition of thickness hHE= 8 mm at the surface of the spherical sealed casing made of 12C18N10T, with the inside CuO sphere with the initial diameter of 49 mm and density of 70% of the theoretical one. The sizes of crystallites of the compressed core material after its meridian cut has been estimated [3] by means of the scanning tunnel microscopy, as well as from the broadening of X-ray diffraction lines.

Based on ACAR spectra produced in the course of the current work, the pulse distribution of CuO valence electrons is shifted to rather high values as compared to these of metallic cooper, that is associated with the chemical bond nature, in particular, with Cu 3d –O 2p hybridization. The defectiveness of nanoceramics produced in the process of explosive processing is essentially higher than in the case of initial CuO microceramics produced by static pressing with subsequent sintering. The nature of nanoceramics defectiveness is defined by the high concentration of oxygen vacancies and/or their agglomerates grouped on crystallite boundaries. The large free volumes (microvoids) have not been revealed, that is consistent with the high density of nanoceramics. To estimate the region of the temperature stability for the produced nanoceramics, its isochronous isothermal annealing has been provided at atmospheric pressure. The increase in sizes of crystallites starts at temperatures higher than 400Ñ. According to ACAR data the defectiveness of nanoceramics begins to change from about 300Ñ up to the beginning of recrystallization and growth of crystallites [4].

The work has received support of RFFI and the Government of Sverdlovsk region, grant 01-02-96403, as well as FCNTP – 40.012.1.1.1153.

References

- Kozlov E.A., Abakshin E.V., Tarzhanov V.I., The Dynamic Processing of Materials. Patent of Russian Federation # 2124716 with the priority dated 24.12.97

- Kozlov E.A., Gizhevskii B.A., The Dynamic Compaction of CuO Copper Oxide Ceramics by Spherically Converging Shock-Isentropic Waves, Preprint RFNC-VNIITF  #137 dated July 30, 1998

- Gizhevskii B.A., Kozlov E.A., Ermakov A.E., et al., Russ. J.Phys.of Met. & Metallog.  92, 52 (2001)

- Druzhkov A.P., Gizhevskii B.A., Arbuzov V.L. et al.,  J.Phys.: Condens. Mater. 14, 7981 (2002)

Neutron Diffraction Studies of Structural State of Mn3O4 after

Shock Wave Loading

V.I. Voronin*, B.A. Gizhevskii*, E.A. Kozlov**, T.I. Arbuzova*, S.V. Naumov*, N.V. Kostromina*, L.Z. Akhtyamova*
*Institute of Metal Physics, Ural Branch of the Russian Academy of Sciences, Ekaterinburg

(gizhevskii@imp.uran.ru)
**Russian Federal Nuclear Center – Academician E.I.Zababakhin Research Institute of

Technical Physics, Snezhinsk, Russia

In some of papers a change in the valent state is pointed out as well as the cause of the oxide reduction when irradiated by charged particles and/or loaded by shock waves [1]. The shock-wave mechanism is invoked to explain the emergency of defects in the process of irradiating the solids by ions at depths considerably greater than the proposed ones [2]. In the current work the neutron diffraction studies of Mn3O4 ceramics from the spherically explosive-compressed and recovered compact have been carried out to clarify the nature of damages of Mn3O4 crystal lattice following the shock wave loading. Mn3O4 has a spinel structure and represents a ferromagnetic with Neel temperature of TN=41.9 K. The shock-wave loading has been provided by means of detonation the PETN-based high explosive composition layer with thickness hHE=5 mm at the surface of the spherical sealed casing made of 12C18N10T with the inside blank fabricated from statically pressed and sintered Mn3O4 microceramics with the initial diameter of 49 mm and density 70% of the theoretical one. The loading parameters as to amplitude and length have been somewhat lower than ones realized in [3]. As a result of spherical shock-isentropic compression the single-phase high-density (98%) ceramics has been produced with the size of crystallites of 0.06-2 m. The diffraction lines of the loaded Mn3O4 are in a tetragonal correspondence to the damaged spinel and have been broadened as compared to the initial powder, that is associated with small sizes of crystallites and emerged internal stresses. At small angles on the diffraction patterns the wide anomaly is observed, which is associated, possibly, with the short-range magnet order in the compressed material. The parameters of the explosive-loaded Mn3O4 lattice are close to the parameters of the initial powder and are as high as a = 5.7457, c = 9.4318 Å. The processing of neutron-diffraction patterns by using the program Fullprof has shown that in the explosive-loaded Mn3O4 the anionic sublattice is the most defective. If in the initial Mn3O4 the filling of the oxygen sublattice is somewhat greater than the stoichiometric value, then in the loaded sample this value is as high as 3.9. This corresponds to some reduction of the oxide and to the increase in the concentration of Mn2+ ions. As a magnet moment of Mn2+ is higher than that for Mn3+, the magnetic susceptibility can be increased, as it has been observed in paper [5]. The similar partial reduction of CuO oxide in the course of shock-wave loading is pointed out in paper [1].

The work has received support of RFFI and the Government of Sverdlovsk Region, grant 01-02-96403.

References

- Gizhevskii B.A., Galakhov V.R., Zatsepin D.A., et al., Russ. J.Sol.State Phys. 44, issue 7, 1318 (2002)

- Pavlov L.V., Sumin Yu.A., Sonrov V.D., et al., Russ. J.Phys.&Tech. of Semiconductors 20, 503 (1986)

- Kozlov E.A., Gizhevskii B.A., Dynamic Compaction of Copper Oxide Ceramics by Spherically Converging Shock-Isentropic Waves, Preprint RFNC-VNIITF #137 dated July 30, 1998.

- Gizhevskii B.A., Kozlov E.A., Ermakov A.E., et al., Russ J.Phys.of Met.&Metallog. 92, 52 (2001)

- Arbuzova T.I., Gizhevskii B.A, Naumov S.V., et al., in Proceedings of XVIII International School-Seminar, New Magnet Materials in Microelectronics, June 2002, Moscow State Universities, Physical Department, Moscow, 2002, p.288.

Development of Compacting Technology and Processing of Non-Metal Materials Using Spherical Explosive

E.A. Kozlov*, B.A. Gizhevskii**, S.V. Naumov**
*Russian Federal Nuclear Center – Academician E.I.Zababakhin Research Institute of Technical Physics, Snezhinsk, Russia
 **Institute of Metal Physics, Ural Branch of the Russian Academy of Sciences, Ekaterinburg

(gizhevskii@imp.uran.ru)

The goal of this work is the development of the new method for obtaining the high-density nanocrystal (with crystals of nanometric size) ceramics based on oxides, nitrides and others non-metal materials by means of spherical shock-wave loading. These nanoceramics have high mechanical properties (density, strength, plasticity) and also series of the interesting physicochemical properties being candidates for practical usage.

The spherical explosive systems developed in RFNC-VNIITF [1] to process the materials are the foundation of this method. Shock- wave loading performs by the explosion of HE layer on the surface of the spherical sealed casing with the initial material inside. Initial material is a statically pressed ingot of microceramics with the density of 70% from theoretical. In the process of the shock-wave loading of microceramics it is compacted up to 99% from the theoretical density and as result of compression and shear deformations we obtain the nano-scale material structure, which is regularly changed along the radius of compact being obtained. Integrity of the sealed casing during the explosive loading is saved. By means of this method [1] copper oxide (CuO), manganese oxide (Mn3O4) and some manganite (LaMnO3) nanoceramics were obtained. The density of nanoceramics is up to 99% from theoretical. Sizes of crystals are 0.01-0.2 m. Microhardness increases considerably. Copper oxides are a base of the high-temperature-superconductors and some applications in the area of catalysis and gas sensors. Маnganites are candidates for spin electronics usage .

The advantages of the suggested method are: 1) combination of obtaining the nanocrystal structure and the material compaction in one technological process; 2) high purity of nanoceramics;  3) possibility to produce the nanoceramics with average size of crystallites varying along the compact radius, that makes it possible to obtain in one explosive experiment  and to choose the material with the optimal combination of its operating properties and with required crystallite sizes. The developing method can be used for promising nanocrystal materials in the field of catalysts, high hardness and high recrystallization temperature materials and also some functional materials.

The work is performed in the framework of the RFFI Project 01-02-96403 “Ural”.

References

1. Коzlov Е.А., Аbakshin Е.V., Таrzhanov V.I., Patent of Russia Federation  # 2124716 of 24.12.97

Effect of Indexed-Spectrum and 14-MeV Neutrons on

Arsenide - Gallium Schottky Field-Effect Transistors

V.T. Gromov*, O.V. Tkachov*, V.P. Shukaylo*, S.V. Obolensky** 
*RFNC-VNIITF, Snezinsk, Russia (c5@five.ch70.chel.su) 
** Nizhny Novgorod State University, Nizhny Novgorod, Russia

In the present work, the effect of indexed-spectrum and 14-MeV neutrons on evolution of characteristics of power 3P602G-2 Schottky FETs was investigated. Measurements were carried out on the basis of YAGUAR reactor and NG-12I neutron generator.

As measurements have shown, the parameter most sensitive to neutron action is threshold voltage which decreases with fluence increase.

Block diagram of power transistor (3П602Г-2)

Since the value of threshold voltage U is proportional to concentration of dope N,

ΔUU≃ΔNN.	(1)

Assuming that the removal of charge carrier is related to formation of defect clusters, and this effect prevails, then:

.,

where:  – concentration of clusters;

vk - volume of a cluster, that proves to be true in experiment.

Proceeding from the experimental data and data given in [1], we obtain an estimate of the radiation-induced defect cluster radius (~70 nm).

Clusters concentration increases approximately 2.6 times under irradiation with 14-MeV neutrons.

With a view to analyze the results of the experiment, the size and form of collision cascades(clusters) emerging in GaAs under neutron irradiation were calculated. For calculation, the program TRIM based on Monte-Carlo procedure was utilized [2].

As a result of calculations it was found that the defect clusters are 70-150 nm in size, which weakly depends on the energy of neutron irradiation in the range of 105-107 eV. Clusters concentration grows  3-4 times with increase in neutrons energy from 1 to 14 MeV.

References

- Kladko V.P., Plyatsko V.P.. FTP.1998.v.32, p.261-263.

- Diersack J.P., Computer Simulations of Sputtering, Nuclear Instruments and Methods in Physics Research, B27,21-36(1987).

Effect of Reactor Neutron Irradiation on InP Single Crystal Structure

N.G. Kolin *,  V.T. Bublik **, M.I. Voronova **, D.I. Merkurisov *, K.D. Scherbachev **

* Branch of FSUE “Karpov Institute of Physical Chemistry”, Obninsk, Russia (fci@meteo.ru)

**Moscow State Institute of Steel and Alloys (Technological University), Moscow, Russia

The method of precision measurements was used to study the effect of reactor irradiation (full neutron spectrum with т  б  2) on InP single crystal lattice spacing. Initial InP samples were undoped (n=1.81016 cm-3) and Te-doped up to n=3.91018 cm-3.

Figure 1 shows the dependence of lattice spacing on carrier concentration in the initial material irradiated with thermal neutron fluence of Fт =  2.11019 cm-2. It should be noted that the change of lattice spacing is uncommon for the crystals with radiation defects. At small tellurium concentration lattice spacing decreases under irradiation. And just at n=3.91018 cm-3 it increases as compared with the initial value (а=5.910-4 Å).

Fig. 1

Fig. 2

Figure 2 presents the dependencies of lattice spacing on thermal neutron fluence for InP single crystals with Te concentrations: 1 - n=1.81016 cm-3; 2 - n=4.01017 cm-3. It is seen that lattice spacing decreases with increasing neutron fluence, and this decrease becomes even more intensive with the growth of Te concentration. As regards high Te concentration (n=3.91018 cm-3), it is obvious that properties of irradiated material are determined not only by the concentrations of tin atoms introduced by thermal neutron transmutation doping, generated radiation defects and initial Te concentration. It is the interaction character of these components that makes the main contribution. According to the estimates, an increase of lattice spacing will be an order of magnitude lower even if all Te leaves the solution because of solid solution degradation. The same is true about non-stoichiometry defects. It is evident that residual concentration of radiation defect interstitial components increases at high tellurium concentrations in the initial material. At low Te concentrations vacancy-type defects are predominant.

The work has been done in the frame of ISTC Project #1630.

Influence n- Irradiations on Physical Properties of SiC-Based Diodes

N.G. Orlov*, V.T. Gromov*, V.P. Shukaylo*, A.A. Lebedev**, A.M. Strelchuk**, N.S. Savkina**
*RFNC-VNIITF, Snezinsk, Russia (c5@five.ch70.chel.su)

** PTI Ioffe, St. Petersburg, Russia

Silicon carbide (SiC) – is a perspective material of extreme electronics capable to maintain serviceability at high temperatures and levels of irradiation. There were explored 6H-SiC p-n structures received in PTI Ioffe by the method of sublimation epitaxy of р+ stratum on the basis of n+ Lali substrate under vacuum. P-n junctions were grown on SiС face (0001), with Al (p-type) as a dope. Concentration of non-compensated impurity in p+ stratum was (Na-Nd) = 5-7·1018 cm-3, and in n+ substrate, (Nd-Na) = 3·1018 cm-3. The thickness of epitaxial p+-type stratums was 1-2 microns, thickness of a n-type substrate, 400 microns. For investigation, fast pulsed reactor (YAGUAR) with u~1 ms, Ēu=1.1 MeV, and slowing-down radiation unit IGUR-3 (u=25 ns, Ē=1 MeV) were used.

It is shown, that contact potential difference under irradiation preserves its initial value (Uв~2.6 V). The angle of slope of characteristic С-V of the sample irradiated with neutrons is greater than that of non-irradiated, which points to increase in the degree of neutralization of the dope, i.e. generation of donor-like small defects by neutron irradiation. On the assumption of abrupt symmetric p-n junction, concentration of these defects was estimated at Фn=7⋅1015ncm2: Nd=3.6⋅10171cm3. The dependence of ionization current on dose rate at u=1 ms (YAGUAR) is linear. At τu=25 ns (IGUR-3) there exists a section of superlinear dependence for both the irradiated and non-irradiated samples. To all appearance, these features of the experiment point to existence of biographic and radiation shallow saturation carrier trapping centres with the recharging time of the same order of magnitude as radiation pulse duration (u=25 ns). For experiment interpretation, a simple model taking into account carriers entrapment on saturation and non-saturation levels was analyzed. Satisfactory agreement with the experiment at reasonable values of adjustable parameters was obtained.

Charge Stability of Submicron Integral CMOS-Transistors Based on

Silicon-on-Insulator Structures

V.P. Shukaylo*, V.Т. Gromov*, I.V. Vorozhtsova*, T.N. Krushinsky*,

V.P. Popov**, N.V. Sapozhnikov**, А.А. Frantsuzov**

*RFNC-VNIITF,. Snezhinsk, Russia (c5@five.ch70.chel.su)

** IFP SB RAS,. Novosibirsk, Russia

The basic direction of development of microelectronics is the making a VLSI circuit on the basis of heterostructures. In them the active elements are formed in submicron layer of silicon isolated from a substrate by a layer of oxide.

These structures, having the highest extent of integration, speed and minimum consumed power, are stable to action of neutrons. However, the presence of heterolayers puts under doubt the charging stability depended by accumulation of carriers in layers of oxide and on a heterolayers border.

In this work the initial data on charging stability of experimental submicron CMOS transistors, obtained in IFS SB RAN on technology Dela-Cut, are submitted.

The examination of influence of radiations on the drain-shutter character of the MOS transistors with different design data and at miscellaneous potentials on a substrate at the moment of an irradiation was represented.

Under irradiation, at the expense of accumulation of positive charge in subshutter oxide, there occurs decrease of threshold (Vт) of the n-channel and increase of Vт of the р-channel transistor. Besides at the expense of accumulation of positive charge in the hidden oxide there is a n-type conduction in the channel on back border, that leads to opening of the n channel transistor.

In the work is shown, that the charging stability is higher for transistors with the smaller sizes of heterolayers. Besides, the changes of Vт essentially depends on potential on a shutter and substrate, which are applied at an irradiation. Is shown, that the best version from a point of view of radiation stability, when at an irradiation on a substrate concerning datum is given negative bias.

The negative voltage, applied to a substrate after an irradiation, improves the performances of transistors, trying to return them to initial values (up to an irradiation). This effect is reversible.

Ge/Si Nanostructures with Quantum Dots

Grown by Ion-Beam Assisted Heteroepitaxy

- A.V. Dvurechenskii, Z.V. Smagina, R. Groetzschel*, A.K. Gutakovskii

Institute of Semiconductors Physics, Siberian Branch of RAS, Novosibirsk, Russia

* Research Center Rossendorf, Dresden

(dvurech@isp.nsc.ru)

Recently the effects of low energy (~ 100 eV) ion irradiation on surface islands nucleation and growth were found under Ge molecular beam epitaxy (MBE) on Si(100) and (111) with pulsed self-ion beam action on the growing layer. The irradiation results in reduction of critical thickness of pseudomorphic Ge layer at which a transition from layer-by-layer to three-dimensional growth occurs [1]. Reduction of the average island sizes and their dispersion, and increase in their density are revealed [2]. Here we present the results of crystallinity investigation of Ge quantum dots embedded in Si structures grown under low energy ion irradiation.

The structures investigated were grown by MBE of Ge (of 4-10 monolayers thick) on Si(100), covered with Si cap layer. The three types of Ge layers were grown:

- conventional Ge MBE on Si;

- epitaxy under irradiation with continuous Ge+ ion beam;

- epitaxy under irradiation with pulsed Ge+ ion beam, correlating in time with the completion of the growing monolayers  at layer-by-layer growth mode.

The substrate temperature varied in the range of 300-5000C during Ge heteroepitaxy. The cap layer of 150 nm Si was grown at 500 0C by the conventional MBE (no irradiation). Structures were analyzed by Rutherford backscattering/channeling technique with 1.2 MeV He+ ions. The backscattering yield for perfect crystal of Si(100) is about 3%. The perfect structure of 2.5 % backscattering yield was found in a mode of a pulse irradiation for 1-5 monolayers deposited at temperature 350°C. For lower temperature 300°C the yield exceeded 5 % in the similar structures. The enlarged yield was found also in the structures formed with continuous beam irradiation at 300-350°C temperatures. Transmission electron microscopy studies indicated defect-free Ge dots and Si layers for the initial stage of heteroepitaxy (£ 5 monolayers) in pulsed irradiation growth mode at 350°C. Continuous beam irradiation was found to induce dislocation around Ge dots.

This work was supported by the RFBR, Grant 02-02-16020, 02-02-06543 and INTAS-2001-0615, University of Russia, project УР.01.01.019.

References

- A.V. Dvurechenskii, V.A.Zinoviev, Z.V.Smagina, V.A. Kudryavtsev, Pis.Zh.Eksp.Teor.Fiz.,2000, V.72, №3, p.190-194 [JETF Letters, 2000, Vol.72, №3, p.131-133]

- A.V.Dvurechenskii, V.A.Zinoviev, Z.V.Smagina, Pis.Zh.Eksp.Teor.Fiz.,2001, V.74, №5, p.296-299 [JETF Letters, 2001, Vol.74, №5, p.267-269]

Radiation Processes in Si Single Crystals

L.S. Smirnov

Institute for Semiconductor Physics SB RAN, Novosibirsk, Russia

Due to their high purity and perfection Si single crystals are the best material to be used as a model in solid state physics.

Study of generation and behavior of the point defects in Si with the modern techniques has led to the discovery of unexpected high mobility of vacancies and interstitials. Formation of different defect and impurity complexes and the dependence of the defect-impurity reactions on the intimate processes in crystals.

The systematic approach based on the dominating role of the defect-impurity subsystem extremely sensitive to external influences is presented. An attempt is made to explain such "long-term" problems as: diffusion, non-equilibrium, long-range effects, amorphisation.

We  believe the presented approach is valid in its main parts for all solid states, naturally taking into account the specific properties of atoms and structure.

Properties of Р-Channel Transistors on Silicon Gate Oxide Created Using BF2+ Ions for Drain/Source Areas

A.N. Tarasenkov*, N.N. Gerasimenko**, E.V. Kuznetsov**, E.Yu. Denisenko***

*MSIEE, SMC "Technological Centre", Moscow Institute of Electronic Engineering, Zelenograd, Russia (pebtm@tehcen.zgrad.su)

Investigations of electrical parameters of p-channel MOS transistors gate oxide were carried out. During drain/source regions formation ion BF2+ was used. Investigations were carried out of implanted fluorine influence on electrical parameters of obtained dielectric layers by means of accumulating diagrams and Veibull distribution tracing for dielectric charge disruption definition. Implantation of ion BF2+ was carried out using different energies. As a result extrinsic defects in test MOS-structures gate oxide decreased three times irrespective of implantation energy. Energy level allowing breakdown current increase from 1 to 5-6 mA was obtained experimentally, effective charge of gate oxide reduced, wafer yield increased. Threshold voltage and gate oxide effective thickness increase needs additional investigations, which are realizing at present time.

Investigation of Solid-Phase Processes in Insulator and Semiconductor Materials under Influence of Powerful Electron Irradiation

A.P. Surgikov, A.M. Pritulov, V.V. Peshev, T.S. Frangulian, A.V. Chernyavski, R.U. Usmanov, B.B. Moyzes, S.A. Gyngazov

Tomsk Polytechnic University, Tomsk, Russia (ghyngazov@tpu.ru)

Results of the investigations of the processes proceeding in inorganic materials with ionic and covalent bonds under the influence of intensive high-energy electron flows heating the samples up to high temperatures are represented. These processes are called radiation-thermal (RT) ones. The investigations were carried out in the following directions:

- RT sintering and property modification of different oxide ceramics types;

- studying diffusion processes in model (alkali halide monocrystals) and real (ferrites) structures in powerful radiation fields;

- studying electroactivation of implanted semiconductors by radiation-thermal method.

The results obtained are following:

1) The effect of considerable sintering activation of various ceramic materials (i.e. Li-Ti ceramics, high-temperature superconducting ceramics, instrumental corundum-zirconium ceramics) has been established at compacts heating with electron beam. Thereby in comparison with simple thermal annealing the decreasing of sintering temperature by about 200 oC was reached. The radiation activation mechanism of compacting powder materials has been suggested. Data on features of structure and functional characteristics formations of the ceramic materials at RT-sintering of oxide powders and at RT-modification of samples sintered thermally have been represented. The RT-influence was shown to promote phase homogenization of complex oxide ceramics, ferrite ceramics production with minimum level of mechanical stress and defects. The ceramics made by the RT-technique was characterized with improved operational properties.

2) As a result of studying cation impurities diffusion in potassium bromide by using SIMS, it was shown that the intensive electron irradiation didn't affect on high-temperature diffusion of isovalent sodium impurity, but intensified heterodiffusion of multivalent Al+3 and Mg+2 cations. The temperature dependences of diffusion coefficients, which were determined for the cases of thermal and radiation-thermal annealings, have been analyzed. The analysis of possible mechanisms being responsible for intensification of the investigated diffusion process has been done.

The investigations on affecting powerful electron beam on oxygen diffusion in the polycrystalline Li-Ti ferrites have been performed. The characteristics of oxygen diffusion in nonstoichiometric ferrites were determined by using the original method based on measurement of electrical conduction activation energy. This method allows determining coefficients of grain boundary Db and volume Dv diffusions. It was shown that in comparison with the thermal annealing the RT one led to increase of both the grain boundary and volume diffusion coefficients. Thereby coefficient of the grain boundary diffusion changed most substantially. The nature of the effect has been discussed.

3) A comparative analysis of electrophysical parameters of ion-implanted structures made of various types of semiinsulating gallium arsenide was performed at different kinds of post-implantation annealings. The technique of annealing ion-implanted gallium arsenide structures by powerful electron beam, energy of which was higher than defect formation threshold, has been suggested. This method has more advantages than the other ones.

# Defect Detection in Binary Zinc-Blende Compounds - Experimental (part-2)

A. Kisiel1, B.V. Robouch 2(guest scientist), E. Burattini2, A. Marcelli2, M. Cestelli Guidi2,

P. Calvani2, A. Nucara2, E.M. Sheregii3,  J. Polit3,  J. Cebulski3

# 1Instytut Fizyki im. Mariana Smoluchowskiego, Universytet Jagiellonski, Krakow, Poland

# 2 Laboratori Nazionali di Frascati INFN, DANE-L lab., Frascati (rm), Italy

# 3Institute of Physics, Rzeszow University, Rzeszów, Poland

At the 2001 Ural-4 Seminar, we presented (part-1) a theoretical analysis of the effects, defects in zinc-blende binary compounds produce in far IR and EXAFS measured spectra, and made a guess estimation as to the level at which such defects would be detectable.

Availing of the DAΦNE-L synchrotron intense far IR (inaugurated Oct. 2002) and x-ray (expected Dec. 2002) beams, we aim at 1)- checking the level of sensitivity of each of the two methods, 2)- comparing the quantitative effects induced with those predicted by the theoretical treatment.

Crystals of CdTe [a,b], HgTe [c], GaAs [b] both perfect [a] (PVT method), as well as with vacancies [a,b], with H-insite loading [a], with induced LE2 antisites [b] (with monitored content) are considered. Results obtained are meant to be presented.

Part of the work was supported by EU TARI-project contract HPRI-CT-1999-00088.

### Samples were graciously provided by:

- A.Mycielski, Institute of Physics, Polish Academy of Sciences, Al. Lotników 32/46, 02-668 Warszawa, Poland.

- A.Zappettini, IMEM-CNR, Viale delle Scienze, 43100 Parma, Italy

- Rzeszów Institute of Physics and collaborating Institutes

Authors Index

# A

# Abramenko S.I.   67, 75, 80

Abromeit C.   3, 23

Abu Kharroub Mitkhal   39

Afanas’ev V.N.   89, 97

Afanasev S.E.   39

Akhtyamova L.Z.   111

Alehin V.V.   32

Antoshina I.A.   63

Arbuzov V.L.   4, 5, 9, 47, 105, 110

Arbuzova T.I.   105, 111

Arkhipov V. E.   12, 21

Aryutkin V.S.   101

Asiptsov O. I.   77

Avilov M.S.   99

Azov A.Yu.   36

#### B

# Babaev V.P.   11

Balachov I. I.   17

Balagurov A.M.   89

Baranov M.A.  20

Bateev A.B.   74

Bayankin V.Ya.   19, 20, 36, 51

Belozerov S.V.   79

Belyaev S.P.    18, 26

Berger E.F.   34

Binyukova S.Yu.   39

Blanter M.S.   67

Bleikher G.A.   29

Borodin O.V.   40, 45

Borshevsky A.O.   86

# Brudnyi V.N.   106, 107

# Bryk V.V     40, 45

Bryushkova S. V.   27

Bublik V.T.   114

Burattini E.   119

Bychkov V.   89

Bykov P.V.   19

##### C

Calvani P.   119

Cebulski J.   119

Chakin V.P.   79

Chekanov V.A.    18, 26

Chemerinskaya L.S.   54, 55, 56

Cherkasov V.I.   84, 85

Chernov I.I.   39, 41

Chernov V.M.   5, 10

Chernyavski A.V.   118

Chikhray E.V.    39, 42, 48, 96

Chineykin M.T.   92

Chuev V. V.   68

Chukalkin Yu. G.   21, 34

Constantinescu B.   70

##### D

Danilov S.E.   4

Davydov L.N.   53

Denisenko E.Yu.   118

Devyatko Yu.N.   5, 10, 11

Dmitriev S.N.   94

Dokichev V. A.   102

Dolinsky Yu.N.   47

Drozdov A.Yu.   20

Drozdovskyi A.   91

Druzhkov A.P.   5, 9, 47, 110

Dubinin S. F.   21, 30, 33

Dvurechenskii A.V.   116

###### E

Evseev A.L.   72

Evtikhin V.A.   82

##### F

Fedichkin I. L.   95

Fil’chagin S.V.   101

Filippov V.P.   74

Filyakin G.V.   72

Fortuna S.V.    30

Frangulian T.S.   118

Frantsuzov A.A.   98

G

Garas’ Yu.G.   92

Garner F. A.   8, 17, 21, 32, 71

### Gerashenko A.P.   108

Gerasimenko N.N.   22, 109, 118

Gerasimenko N.N. (junior)   109

Gil’mutdinov F.Z.   19, 36, 51

Gizhevskii B.A.   105, 110, 111, 112

Glazkov V.P.   67

Gloushkova N. V.   73

Goloborodsky B.Yu.   54, 55, 56, 57

Golosov O.A.   71

Golubov S.I.   6

Goncharenko Yu.D.   72, 79

Goncharov I.N.   7

Gorbachev D.М.   84, 85

Gordienko U.N.   48

Goshchitskii B.N.   25, 34, 82, 108

Gotthardt R.   23

Grachev А.N.   85, 84

# Grinyaev S.N.   106, 107

Groetzschel R.   116

Gromov V.T.   113, 115

Grummon D.S.   23

Gubin K.V.   99

Gubkin I.N.   82

Guidi M. Cestelli   119

Gulevich A.V.    90

Gushchina N.V.   54, 55, 56

Gutakovskii A.K.   116

Gyngazov S.A.   118

I

Ibragimova E.M.   24

Incov A.F.   48

Ioltukhovsky A.G.   45

Isobe I.   17

Ivanov V.   80

J

Jenkins M.L.   13

##### K

Kalachikov V. E.   73

Kalashnikov A.N.   39

Kalin B.A.   39, 41, 45

Kandiev Ya.Z.   93, 99

Karkin A.E.   25, 34, 108

Kawamura Hiroshi   42

Kazakov V.A.   72, 79

Kenzhin E.A.   42, 48, 96

Kharlamov V.S.   11

## Khmelevskaya V.S.   7, 63

Khmelnitsky D.V.   97, 48

Kinev E. A.   27, 28

Kirk M. A.   13, 24

Kiryushkin S.V.   98

Kisiel A.   119

Klevtsov V.G.   42

Kobyliansky G.P.   74, 76, 78

Kolbaenkov A.N.   42, 48

# Kolin N.G.   106, 107, 114

Kolotov A.A.   19

Konobeev Yu. V.   8, 28, 32, 58, 60, 90

Konopleva R.F.    18, 26

Konovalov L.N.   67

Kopytin V.P.   46

# Kordyukov V.N.   75, 80

Korostin O. S.   68

Kosarev V.V.   92

Kositsyna I.I.   86

Kostenko B.F.   7

Kostromina N.V.   110, 111

Kot N.Kh.   99

Kozikov A.N.   98

Kozlov A. V.   27, 28, 77

Kozlov E.A.   86, 105, 110, 111, 112

Kozlov E.V.    30

Kozlovsky A.V.   95

Kozmanov E.A.   71

Kozodaev M.A.    91, 92

Krivobokov V.P.   29

Krushinsky T.N.   115

Kuchin A.G.   34

Kulikov D.V.   11

Kulinich Y.A.   92, 102

Kulish V.G.   40

Kulsartov T.V.   39, 42, 48, 96

Kupriyanov I.B.   79

Kurdyumov A.A.   43

Kuril’chik E.V.   36

Kurochkin A.V.   98

Kuryakin A.V.   101

Kurzina I.A.    30

Kuzina T.L.   71

Kuznetsov A.R.   3, 35

Kuznetsov E.V.   118

Kuznetsov V. R.  80

###### L

LaGrange T.   23

Latypov R.N.   79

Laushkin A.V.   67

# Lazarev N.E.   11

Lebedev A.A.   115

Levakov B.G.   92

# Litvinov B.V.   75

Litvinov D.A.   94, 101

Logatchev P.V.  99

Loginov B.A.   92

# Lokhtin L.N.   67

Lukin A.V.   98

Lukin G.V.   93

Luzgin A.V.   55

# Lyasota A.M.   75, 80

Lyasota I.A.   47

Lysitsin G.Yu.   92

Lyublinskiy I.Е.   82

# M

# Magda E.P.   75, 92, 98, 102

Makeev O.N.   91, 92

Malakhov A.A.   93

Malkov I.L.   42

Maltsev V.V.   68

## Malynkin V.G.   7

Malyshkin G.N.   93

Marcelli A.   119

Marchenkov V.V.   12

Markelov N.N.   84, 85

Markovsky S. N.   95

Martyshkin P.V.   99

Mashinin V.A.   99

Medvedeva E.A.   71

Mel’nik I. A.    30

Melder R.R.   79

Mendeleva Yu.A.   36

Merkurisov D.I.   114

### Mikhalev K.N.   108

Modestov D.G.   93

Mokichev G.V.   98

Möller W.   54

Morozov A.N.    40

Morozov S.N.   99

Möslang A.   81

Moyzes B.B.   118

Mukovskii Ya. M.   21

###### N

Nakamichi Masaru  42

Naumov S.V.   105, 110, 111, 112

Nazarkin I.V.    18, 26

# Neklyudov I.M.   3, 40, 45

Neustroev V.S.   75

Nikitin A.V.   36, 51

Nikolaev A.L.   52

Nikolaev Yu.A.   58

Nikulina A.V.   78

Novoselov A.E.   76, 78

Nucara A.   119

##### O

Obolensky S.V.   113

Obukhov A.V.   76

Ogorodov A. N.   68, 71

Okita T.   21

Orlov N.G.   115

Orlov V.K.   67

Osmayev O.A.   53, 59

Ostrovsky Z.E.   72, 75, 76, 78, 79

Ovchinnikov V.V.   54, 55, 56, 57

##### P

Panchenko V. L.   77

Pankratov D.G.   84, 85

Parkhomchuk V.V.   99

Parkhomenko A.A.   40

Parkhomenko V. D.   21, 30, 33

Paschenko O.V.   29

Pavlov V.A.   4, 5, 9, 47

Pechenkin V.A.   8, 58, 60, 61, 90

Pecherkina N.L.   47

Pechyorin A.M.   72

Peregud M.M.   76, 78

Perminov D.A.   5, 9, 110

Peshev V.V.   118

Petrov D.D.   67

Pevtsov D.V.   79

Plokhoi V.V.     93, 99

Podgornova I.V.   47, 84, 85, 86

Polit J.   119

Poon S.J.   25

Popov V.P.   98, 115

Porollo S. I.   32

Portnykh I. A.   27, 28, 77

Pribiš J.   7

Pritulov A.M.   118

Prokopova T.S.    30

Prozorova I. V.   48

Pugachev R.N.   74

R

Rapp O.   25

Raspopova G.A.   47

Raybchikov A.I.    30

Reshetnikov F. G.   68

Reutov I.V.   44

Reutov V.F.   44, 94

Robouch B.V.   119

Rogozhkin S.V.   5, 10

Romanov V.A.    90

Rusov V.D.   79, 94, 99, 101

Ruzhitsky V.V.   40

Rybin P.V.   11

S

Sagaradze V.V.  35, 47, 82, 86

Sakov V.S.   84, 85

Saksagansky G.L.   95

Samarin S.I.   93, 99

Sapozhnikov N.V.   115

Saprykina I.V.   47

Sato T.   21

Savkina N.S.   115

Schäublin R.   23

Scherbachev K.D.   114

Sekimura N.   21

Semerikov V.B.   71

Semkov A.L.   98

Semyonkin V.A.   54, 55, 57

Sergeev V.M.   67

Shaaban I.Yu.   94

Shal`nov K.V.   4, 5, 47, 105, 110

Shamardin V.K.   72, 75, 76

Shamovsky V.G.   49

Shapovalov R.V.    59

Sharkeev Yu.P.    30

Shcherbakov E. N.   77

Sheregii E.M.   119

# Shestakov A.E.   67

Shestakov V.P.   39, 42, 48, 96

Shikov А.K.   82

Shilyaev B.A.   40, 45

Shimansky G.A.   79

Shishov V.N.   76, 78

Shiyankov S.V.   99

Shmakov A.A.   45, 60

Shmygin V.G.   84, 85

Shukaylo V.P.   113, 115

Singh B.N.   6

Sivin D.O.    30

Skalozubov V.I.   99

Skryabin L. A.   77

Slezov V.V.   53, 59

Smagina Z.V.   116

Smirnov E.A.   45, 60

Smirnov L.S.   117

Smith D.   39

Sokolov N. B.   68

Sokolovskiy D.V.   82

Somenkov V.A.   67

Spirina S.G.   93

Srinivas V.   25

Starostenko A.A.   99

Stepanov I.A.   58, 60, 61

Stepanov I.B.    30

Stepovik A.P.   97, 98

Strelchuk A.M.   115

Subbotin V.G.   86

Sumin V.V.   10

Surgikov A.P.   118

Suslov D.N.   79

# Suvorov A.L.   11, 12, 46, 92

Svidlov V.G.   92

Svyatov I.L.   67, 84, 85

Syutkin N.N.   32

T

Tang H. T.   17

Tarasenkov A.N.   118

Tarasov V.A.   79, 94, 99, 101

Tarzhanov V.I.   84, 85

Taskin D.V.   84, 85

Tecchio L.   99

Telichko I.V.   84, 85

Teploukhov S. G.   21, 30, 33

Tetelbaum D.I.   36, 51

Timofeyeva L. F.   84

Timokhin A.N.   80

Tkachov O.V.   113

Tolstolutskaya G.D.   40

Tomilov Y.V.   102

Trinkaus H.   6

Troitskii V.Yu.   109

# Troshev A.V.   75, 80

Trushin Yu.V.   11

Tsepilov N.А.   84, 85

Tsvetokhin A.G.   102

Tsygvintsev V. A.   73, 80

Twesten R. D.   13

U

Usmanov R.U.   118

Uspenskyi D.M.   46

###### V

Valiev E. Z.   30

Vatulin А.V.   82

Vedernikov G.P.   82

### Verkhovskii S.V.   108

Vertkov А.V.   82

Vil'danov V.G.   86

Vinogradov Yu.I.   101

Vladimirov P.V.    81

Volkov A.E.    26

Vorobyev А.V.   84, 85

Voronin V.I.    25, 34, 111, 114

Voronova M.I.   114

Vorozhtsova I.V.   115

Vostrikov V.A.   99

Votinov S.N.   82

Voyevodin V.N.    40, 45

W

Weber H.W.   12

Wieser E.   54

###### Y

Yukhimchuk A.A.   42

Yusupov R. I.   102

Z

Zabusov O.O.   62

# Zaluzhnyi A.A.   11

# Zaluzhnyi A.G.   11, 46

# Zheldak U.L.   48

# Zhurba V.I.   40

Zimin А.V.   84, 85

Zlatoustovski S.V.   42

Zouev Yu.N.   47, 75, 82, 84, 85, 86

Zverev V.V.   48