- Some Aspects of Physics of Radiation Phenomena in Semiconductors and Insulators

Fractal Analysis of Self-Organized Structures in Implanted Semiconductors

S. A. Aprelov1, N. N. Gerasimenko1, N. A. Medetov2

1Moscow Institute of Electronic Engineering (Technical University),

Moscow, Russia (rmta@miee.ru)

2 Kostanay Technical-Social University, Kostanay, Kazakhstan

The processes of self-organization in single crystal semiconductors under ion bombardment is the item of increasing interest at the last time. These processes can lead either to recentralization after amorphization in the continued process of ion bombardment, or to creation of ordered three-dimensional (3D) systems of clusters which present associations of structural defects and impurity atoms. In some cases such clusters can demonstrate quantum dimensional properties with regard to electrophysical, optical, luminescent and other parameters.

The problem of analysis of order degree of elements in such a system is a self consistent task. We solve this problem by means of fractal analysis in combination with other analytical methods (Fourier transform) and with the use of experimental methods of investigation (AFM-microscopy, Auger-spectrometry with high space resolution, Raman scattering of light, low temperature photoluminescence) for comparison.

It was shown that fractal dimension serve as quantitative parameter characterizing the degree of order for nanodimensional elements. In some cases this parameter will discover the ordering even if when other methods can not give the possibility disclose the ordering and make a quantitative estimation of its degree.

The computer simulation of systems consisting of different structure elements with different level of ordering was carried out. This procedure gave the possibility to estimate of ordering level quantitatively. In some cases the dependence of this ordering on fractal dimension demonstrate non monotonic (in separate cases - oscillating) character. For system with the dense space structure of clusters the dependence of fractal dimension on degree of organization exist as quasilinear and its angle coefficient increase with growing of cluster density.

Analysis of Results of Precision Measurements of

Multilayer Structures Parameters

S. A. Aprelov1,2, A. G. Turyansky1, N. N. Gerasimenko1,2, A. N. Tarasenkov3

1Moscow Institute of Electronic Engineering (Technical University),

Moscow, Zelenograd, Russia (rmta@miee.ru)

2Institute of X-Ray Optics, Moscow, Russia

3 Technology Centre of MIEE, Moscow, Zelenograd, Russia

Surface and Volume Defects in Irradiated Nanocrystalline CuO

T. I. Arbuzova*, S. V. Naumov*, E. A. Kozlov**, V. L. Arbuzov*, B. A. Gizhevskii*

*Institute of Metal Physics, UB RAS,

Ekaterinburg, Russia (naumov@imp.uran.ru)

**Russian Federal Nuclear Center – All-Russia Research Institute of

Technical Physics, Snezhinsk, Russia

The present study deals with the effect of the grain size, elastic stresses and electron irradiation on the magnetic susceptibility (T) of a dense CuO nanoceramic, which was prepared by the shock-wave method. The magnetic order in CuO is determined by a strong antiferromagnetic superexchange of Cu2+ ions (S = 1/2) through oxygen ions. The shape of the temperature dependence of the susceptibility is typical for 1D and 2D antiferromagnets, which pass to the 3D state with decreasing temperature. Near TN = 230 K maximum of susceptibility is absent and only the slope of the (T) curve changes. It was found that as the grain size decreased up to 5 nm  d  70 nm, a "paramagnetic" contribution in magnetic susceptibility  ~ 1/T appeared at T < 140 K. The anomalous behavior of the susceptibility was explained by break of Cu-O-Cu exchange couplings of surface spins, whose number increased with diminishing d. The concentration of disordered Cu2+ spins depends not only on the size of nanoparticles, but also on their mutual interaction. This conclusion is supported by larger  values in loose CuO nanopowders at the same d values.

The effect of the microstructure and the state of interfaces is manifested more clearly in compacted nanomaterials. It was found that the relaxation of elastic stresses in the compact nanoceramic led to the recovery of the antiferromagnetic order and the standard shape of (T) in CuO while the grain size did not change. The (T) dependences remained unchanged for CuO nanopowders after 3 years of storage. This fact points to the absence of relaxation processes in these nanopowders.

Not only surface defects, but also volume defects may cause the frustrations of antiferromagnetic couplings. Oxygen and copper ions may be displaced from their sites under electron irradiation and, consequently, exchange parameters may be altered. It was shown that at small irradiation doses, Ф  2.41018 cm-2, the dependences (T) change little for annealed nanoceramics, but at Ф = 51018 cm-2 the susceptibility  includes a considerable paramagnetic contribution, which increases as the grain size diminishes. Thus, a large number of defects both in surface layers and the bulk of CuO nanoparticles leads to the frustration of exchange couplings between Cu2+ ions and causes the increases in the susceptibility.

This study was supported by the Project of the Department of the Physical Science of RAS N 19, 490 and the Federal Targeted Scientific-Technological Program  40.012.1.1.1153.

Effect of Gamma Radiation on Diamond Transformation 
under Reactor Irradiation

V. A. Nikolaenko, V. G. Gordeev, O. O. Zabusov, I. V. Bachuchin 
RRC “Kurchatov Institute” (zabusov@orm.irtm.kiae.ru)

The problem of fast neutron flux effect on radiation damage is still under discussion because of conflicting experimental data. An investigation of radiation damage of diamond has been carried out. Initial properties of diamonds from different deposits as well as artificial diamond are stable and its change under irradiation at identical conditions is the same. Thus effects of such factors as impurities content and differences in fabrication methods can be excluded.

Crystal lattice expansion was the property of interest of this work and in some cases this data were duplicated by electrical resistance.

The paper shows diamond to be transformed under high dose of neutron irradiation (about 1021 n/cm2). At the same irradiation temperature and fast neutron flux fluence of transformation depends on -irradiation flux: the higher the -irradiation flux, the higher the neutron fluence for beginning of transformation.

Radiation Effect of Reactor Neutrons and Temperature on the Structure of

Single Crystals InP

### V. M. Boiko, V. T. Bublik*, M. I. Voronova*, N. G. Kolin, D. I. Merkurisov, K. D. Shcherbachyov*

### Obninsk Branch, Federal State Unitary Enterprise “Karpov Institute of Physical Chemistry”, Obninsk, Russia (ngkolin@mail333.com)

*Moscow State Institute of Steel and Alloys (Technological University),  Moscow, Russia

The structural characteristics of single crystals InP have been investigated depending on the radiation effects produced by fast and full spectrum neutrons and subsequent heat treatment procedures.

Precise measurements of the lattice period were made by the Bond method using CuK1 irradiation at =0.154059340.00000082 nm and asymmetric reflection (337). A lattice parameter was measured with an accuracy ±1·10-6 nm. Radiation-induced microdefects were investigated by the method of X-ray diffusion scattering. In addition to microdefects identified in the form of new phase particles and dislocation loops, this technique enables to detect the clusters of point defects, which are above the detection sensitivity of the electronic transmission microscopy. The clusters are coherent with the matrix, have a diffusive boundary and low field displacement gradient. These defects can arise in the course of neutron irradiation and due to degradation of the disordered regions that causes redistribution of the point defects and annihilation of interstitial and vacancy defects.

A lattice period in single crystals InP decreases under neutron irradiation as opposed to other semiconductor compounds AIIIBV. Lower values of the lattice period are observed in the whole range of Te concentration in the initial material after irradiation, as well as in the samples containing Sn in the initial state. A drastic decrease of the lattice period occurs in the single crystals with nin  8.01017 cm-3. Fast neutrons make the main contribution into the change of the lattice period. Availability of the thermal neutron component initiates the formation of Sn atoms in the material, but does not make a significant influence on the change of the lattice period.

Heat treatment of the irradiated samples up to 600 ºС causes the annealing of radiation defects and recovery of the lattice period. With increasing neutron fluences a lattice period becomes even higher than before irradiation.

The analysis of the obtained experimental data enables to assume that antistructural defects PIn mainly contribute to the lattice period decrease during neutron irradiation of InP. In this case antistructural imperfections produce an effect similar to that of vacancy defects.

Point Defects in Semiconductors: Electronic Structure, Chemical Tendencies

V. N. Brudnyi*, S. N. Grinyaev*, N. G. Kolin**

V. D. Kuznetsov S.F.T.I at Tomsk State University, Tomsk, Russia (brudnyi@ic.tsu.ru)

L.Ya. Karpov  Sc.Res.. Ph. Ch. I.., Obninsk branch, Russia

The simple point defects – anion VA and cation VC vacancies and anti-site defects AC and CA in the binary III-V group of the semiconductors are examined as the basic defects responsible for the electrical properties change of material under high energy irradiation. The numerical calculation of the intrinsic point defect state levels was fulfilled using the model of non-local pseudo-potential method and the large unit cell. The deep levels of the defects are identified with the super-lattice states from the periodical defects, with the wave vector of the super-lattice equal to zero. As it follows from the presented data, the deep levels for the "strongest" defects from the anion vacancies in the whole group of the investigated III-V semiconductors have the same energetic position at about 4.51 eV with respect to the vacuum level position. These data are in agreement with the corresponding calculation position for the model deep level EBabs 4.63 eV, which plays executes the role of the local Fermi level in the irradiated semiconductor [1]. It was found that with the decrease of the "capacity" of the defects the mean value of these deep defect levels differs from the results of the corresponding calculation of the model EBabs – level position. The averaging of the energetic level positions upon the corresponding pairs of the defect levels CA-AC or VC-VA and upon the whole combination of the defect levels have been presented in the work gives the mean energetic level Eav4.9 eV, which plays the role of the Fermi level in the defective material. The presented work reveals the role of the point defects in the irradiated semiconductors and shows that point intrinsic defects on the base of the anion vacancies, the most "powerful" defects between the structural defects in the crystal lattice of the III-V semiconductors, have been presented in the this work, play the special role. Theirs energetic level positions are close to the position of the most deep model state of the EB - defect. Therefore, the VA – levels are the universal energetic levels ("marks"), i.e. the single levels for the group of semiconductors with the relative type of the chemical bonding. The presented investigations does not exhaust the possible set of the intrinsic defects in the irradiated semiconductors because the character of the radiation induced defects depends upon the condition of irradiation and such defects are the point defects upon -rays or electron irradiations and associated defects (clusters) in the material after the fast neutrons or ions bombardment.

#### References

- V. N. Brudnyi, S. N. Grinyaev, N. G. Kolin. Physica B, 348, 213 (2004).

# Theoretical Computation, Modeling and Experimental Investigation of Ultra-Fast Electronic Processes of 10-18…10-12 s in Insulating Material under High-Intensity Electron or Laser Beams

D. I. Vaisburd, K. E. Evdokimov

Tomsk Polytechnic University, Tomsk, Russia (vaisburd@tpu.ru)

The present work is devoted to ultra-fast electronic processes of characteristic time of 10-18…10-14 s induced in a dielectric by an intense electron or laser beams. The primary effect of beam – material interaction is generation of electrons of energies exceeding the ionization potentials of quasi-atomic levels and filled bands of material. Due to impact and Auger-ionization the high-energy electrons and holes generate electrons and holes of lower energies which ionize the matter in their turn. This process stops when the electrons and holes became ionization-passive i.e. lost the ability to ionize the medium. The structure of the track of a fast electron can be represented as a sequence of small domains of secondary ionization (so called “spurs”). The distance between the consequent “spurs” is much more than the diameter of a single “spur”. The main goal of this work was calculation of the so called “instantaneous” energy distribution of ionization-passive electrons and holes in “spurs” established before electron-phonon relaxation. This distribution is the initial one for solving all kinetic equations describing subsequent relaxation of electronic excitations in irradiated material via interaction with lattice.

A technique was developed for calculation of the “instantaneous” energy distribution of non-ionizing electrons and holes in a dielectric under intense electron or laser irradiation. It is based on the solution of a system of integro-differential kinetic equations which are describing the evolution of energy distributions of electrons in conduction band and holes in valence band and on quasi-atomic levels. It takes into account the processes of impact ionization of the matter by the electrons, Auger-ionization of the matter by the holes, and recoil of the holes due to momentum conservation. The evolution of the distribution in NaCl from initial energy distribution (spectrum) of primary beam of high-current-density electron accelerator of GIN type to “instantaneous” one was calculated. The electronic spectrum of NaCl calculated in [1] and the formula for ionization cross-section suggested in [2] were used.

References

- N. O. Lipari, A. B. Kunz Phys. Rev. B, 3, 2, P.491 (1971)

- D. I.. Vaisburd, K. E. Evdokimov, Rus. Phys. J., 11, P. 81 (2003)

Thermooptical Effects Related to Surface

Structural Disturbances on Silicon

N. N. Gerasimenko (Jr.)1, N. N. Gerasimenko2, Yu. N. Parkhomenko3, V. Yu. Troitsky1

1Institute of System Research of RAS, Moscow, Russia (nikolay_gerasimenko@srisa.ru)

2Moscow Institute of Electronic Engineering (Technical University), Moscow, Zelenograd, Russia

3Moscow Institute of Steel and Alloys (Technical University), Moscow, Russia

Comparative Study of Radiation Conductivity of Ion Dielectric

Monocrystals and Natural Diamonds Under Irradiation with

Electron and X-Ray Beams of Nanosecond High-Current Accelerator

D. I. Vaisburd, E. V. Golov, E. G. Tavanov
Tomsk Polytechnic University, Tomsk, Russia (golov@mail2000.ru)

Study of Properties of Carbon Nanotube and Nanowire-Containing Polymers

A. M. Grekhov1, M. A. Kozodaev1, A. B. Tarasenko1, S. N. Blinov2, I. G. Ivanov2, P. V. Gvasaliya3

1ITEP, Moscow, Russia (grekhov@nm.ru)

2RCTU, Moscow, Russia

3TIPS, Moscow, Russia

Carbon nanostructures (nanotubes and nanofibers ) with different topology were obtained by Chemical Vapor Deposition (CVD) method. Subsequently they were embedded into the polymer. The dependence of physical properties of these composites on nanotubes concentration and topology was investigated.

Vacancy Clusters (pores) in Semiconductors:

Electronic Structure, Optical Properties

V. N. Brudnyi*, S. N. Grinyaev*, N .G. Kolin**

V. D. Kuznetsov S.F.T.I at Tomsk State University, Tomsk, Russia (brudnyi@ic.tsu.ru)

L.Ya. Karpov  Sc.Res.. Ph. Ch. I.., Obninsk branch, Russia

Vacancy associations (pores) are formed in the semiconductors upon the fast neutron and the heavy mass ions irradiation. Moreover in the last time such clusters are prepared during the crystal growing or by the selective etching of the material. Irrespective of the intensive investigations of the porous semiconductors the nature of the electronic states of the vacancy clusters, the electric parameters of this material and the origin of the optical absorption and luminescence bands remains the subject for discussion up to date because of the complexity of the interpretation of the quantum-sized effects for the electronic states in the clustered semiconductors. Meanwhile, the investigation of the electronic states and the absorption and photoluminescence bands nature in the porous materials is essential to use such material in electronics and opto-electronics devices. For this the detailed analysis of such semiconductors optical properties is need, because it permits to reveal the types of the critical points for the optical transitions as the function of the material porous degree.

In the presented work the theoretical investigation of the electronic states and the optical properties of the porous Si and GaAs with the vacancy clusters, has been fulfilled using the model pseudo-potential method and the large unit cell. The tetrahedral clusters consisting of up to 329 vacancies in all are located in the successive coordination spheres. It was revealed that vacancy clusters perform as many charged centers with the electronic structures are formed as the result of "interaction" between the isolated vacancies states. As the size of the vacancy cluster increases then the energetic level position of the cluster state increases too. At the same time the number of the corresponding deep levels are pushed out from the valence band increases. Upon the growing of the cluster size the large number of states in the energetic spectrum of the bulk crystal nearly the top of the valence band are emptied. These changes in the electronic structure of the porous semiconductor are displayed in the spectral displacement and in the change of the optical absorption peaks intensities. The origin of the most intensities absorption peaks of the porous material was revealed. The dependence of the deep energetic levels positions and the character of the absorption spectra versus the charged states of the clusters are investigated. The opportunity for the describing of the cluster states in the porous semiconductors in the frame of the effective mass method with the smooth potential at the heteroboundary was shown.

Defect Production in Glasses under Influence of the Separated

Gamma-Component of the Reactor Radiation

E. M. Ibragimova, M. U. Kalanov, М. А. Mussaeva
Institute of Nuclear Physics, Tashkent, Uzbekistan (ibragimova@inp.uz)

Radiation defect production in oxides is of great interest for atom and solar energy, and also for nuclear waste storage. The combined influence of neutron flux and gamma-radiation on materials was studied widely, and only neutrons were believed to be able to displace atoms. Although it turned out, that 1.25 MeV- 60Co gamma-quanta can shift light anions (О, F) by the inelastic mechanism. The aim of this work was to study defect production in pure fused quartz and barium-silica glasses, containing nano-crystalline inclusions, and also nano-porous glass under influence of 0.2-7 MeV- gamma-radiation in the quenched reactor. The period was chosen when practically constant current of ~10-20 nA is established in the ionization chamber, that corresponds to the average gamma-flux of 15-30 Gy/s. Single crystals of LiF were used for comparative dose monitory of gamma-fluxes in the reactor and 60Co source by the well-known absorption band of F-center (a fluorine vacancy trapped an electron).

Spectra of optical absorption and photoluminescence, and also the glass structure were studied. The charged oxygen vacancy accumulation rate with the dose growth turned out to be higher in the barium silica glass than in pure SiO2 since at small Z the Compton scattering and photonuclear reactions prevail, and for Ba with high Z – just the opposite case of domination of the photoelectric effect. The radiation-induced growth of crystalline phase precipitates was found in the both glasses, which had been ascertained only to knocking out atoms (i.e. elastic displacements) by high fluencies of fast neutrons. The point defect production efficiency (for example, E’-centers and non-bridging oxygen atoms) in the glasses under the gamma-irradiation even in the quenched reactor turned out much higher than that under the exposure to the equivalent dose in ~1.25 MeV 60Co gamma-source at the dose rate of ~7 Gy/s (and even earlier when it was as high as 45 Gy/s). Because of water vapor radiolysis on the glass pore surface under the gamma-irradiation, a 100-times increase in the surface proton conductivity occurred.

The work was accomplished by the grant F 2.1.2 from the Center of Science and Technology of Uzbekistan.

Сomparative Optical and Electrical Study of 4H-SiC Irradiated with

Neutrons and Heavy Ions

E. V.  Kalinina*, G. F. Kholujanov*, G. A.. Onushkin*, D. V. Davydov*, A. M. Strel'chuk*, A. O. Konstantinov**, V. A.  Skuratov***

* Ioffe Physicotechnical Institute, RAS, St. Petersburg, 194021 Russia (evk@pop.ioffe.rssi.ru)

** AMDS AB, Österögatan 3, 164 40 Kista, Sweden

*** Joint Institute of Nuclear Research, Dubna, 141980 Russia

The influence of irradiation with swift neutrons and heavy ions (Bi and Kr) on both SiC defect structure and electrical properties of diode structures formed in this material has been studied.

4H-SiC chemical vapour deposited 26 m thick epitaxial layers with Nd-Na = (5-8) × 1015 cm-3 were used. Cr Schottky barriers (SBs) were thermally evaporated in vacuum and p+-n-n+ diode structures were formed by ion implantation of Al with energy 150 keV and dose 5 × 1016 cm-2 followed by short high temperature annealing. Initial samples and diode structures were irradiated with 1 MeV neutrons with total fluence equal to 6 × 1014 cm-2, as well by 710 meV Bi ions with fluences 1.4 × 109 to 1 × 1013 cm-2 and 245 MeV Kr ions with fluence ranged from 5 × 109 to 5 × 1010 cm-2.

Defect centers in samples were investigated by spectral PL measurements at 77 K and  using capacitance-voltage (CV) and DLTS methods at temperatures 80-700K. The current–voltage measurements of diode structures were performed under DC conditions in the temperature range 293-700 K.

According to PL, CV and DLTS data, the neutrons and high energy ions introduced in SiC identical defect centers, some of them were annealed at temperature of 700 K. Thus, the formation of the defect structure in SiC is independent of the processes related to the relaxation of energy losses by ionization in the tracks of high-energy ions up to a level 34 keV/nm and is controlled by radiation damage produced as a result of elastic collisions. Also, for the first time, the possibility to increase the radiation resource and lifetime of  SiC-based devices at high temperatures has been shown. It was revealed that diode structures, that has been degraded after irradiation, recovered  their rectifying properties at temperature of  700 K.

References

- E. Kalinina, G. Kholuyanov, G. Onushkin, D. Davydov, A. Strel'chuk,, A. Konstantinov,  A. Hallén, A. Nikiforov , V. Skuratov, К. Havancsak. Semiconductors 38, 1 (2004).

- E. Kalinina, G. Kholujanov, G. Onushkin, D. Davydov, A. Strel'chuk, A. Zubrilov, Hallén, A. Konstantinov, V. Skuratov, J. Staňo. Materials Science Forum, 433-436, 467 (2003).

Connections Between the Energy Spectrum of Carriers and Multiwalled Nanotubes Topology

N. G. Kiryudchev, V. G. Valeev, M. A. Kozodaev

ITEP, Moscow, Russia (grekhov@nm.ru) (__nicholas__@rambler.ru)

The model nanotube, used in many theoretical works, is ideal, thin, single-walled and, therefore, hard to obtain. That is why the results of experimental and theoretical works are never the same. Topological properties of nanotubes are one of the main causes of that.

This paper proposes a model describing the connection between energy spectrum of carriers and multi-walled nanotubes topology. Experiments on nanotubes with known topology show good agreement between the theoretical predictions and the measurement results.

# References

- M. Kociak, A. Yu. Kasumov, S. Gueron, B. Reulet, I. I. Khodos, Yu. B. Gorbatov, V. T. Volkov, L. Vaccarini, and H. Bouchiat, Physical Review Letters, Vol. 86 (2001), p. 2416

- Yuanhe Huang, Mayumi Okada, Kazuyoshi Tanaka and Tokio Yamabe, Physical Review B, Vol. 53 (1996), p. 5129

# Semiconductors Modification with Proton Beams

V. V. Kozlovsky

St. Petersburg Polytechnic University, St. Petersburg, Russia (kozlovski@tuexph.stu.neva.ru)

Silicon Irradiation Defects: Relationship Between Surface and Bulk

T. S. Balashov, A. A. Golubev, M. A. Kozodaev, A. L. Suvorov

ITEP, Moscow, Russia (M_Kozodaev@vitep1.itep.ru)

Silicon specimens were irradiated with carbon ions of energy 1200 GeV and fluence 2∙1012  cm-2, with different incident angles. The specimens surface was examined by means of scanning probe microscopy, and the bulk defects – by means of Pronotium Annihilation method. Relationship between surface and bulk defects was investigated.

# Single Crystals of Semiconductor Compounds АIIIBV

### D. I. Merkurisov, V. M. Boiko, N. G. Kolin, O. L. Kukhto

### Obninsk Branch, Federal State Unitary Enterprise “Karpov Institute of Physical Chemistry”, Obninsk, Russia (ngkolin@mail333.com)

Full cross-sections have been measured by the time-of-flight method to study the interaction of slow neutrons in the single crystals of semiconductor compounds АIIIВV (GaAs, InP, InAs and InSb) in the energy range from 1 meV to 1 eV. The comparison of experimental and calculated data showed good agreement.

Depth distribution of the thermal neutrons was calculated for the wafers irradiated on one and two sides based on the approximation solution of the transfer equation (the first order perturbation theory).

#### Transfer characteristics of the neutron diffusion were calculated, and inhomogeneous distribution of the neutron flux was determined for strong absorption substances in the collimated and isotropic radiation conditions. An optimal geometry size was calculated for the samples of GaAs, InP, InAs and InSb for practical application in the nuclear doping technology.

According to the obtained results, depth distribution of the thermal neutrons after irradiation on both sides is about 10, 12 and 13 % for 2 mm thick wafers of InSb, InAs and InP, respectively. However, taking into account a 600-μm thickness of the wafers applicable in manufacturing, inhomogeneous distribution of the doping impurity throughout the bulk does not exceed 1 % for all the investigated materials.

Based on the Customers’ requirements to homogeneous distribution of the doping impurity throughout the crystal depth and the dependencies obtained in our experiments, it is reasonable to conclude that in real conditions nuclear doping of gallium arsenide could be achieved by slow neutron irradiation on both sides of the sample with at least one outer size ≤ 50 mm.

Inhomogeneous distribution of the thermal neutrons throughout a 50-mm diameter single crystal ingot of GaAs does not exceed 8 %.

Ionization Currents in Microelectronics Dielectric Materials at

High Intensity Pulse Irradiation

V. T. Punin, A. V. Grunin, A. M. Molitvin, E. I. Bursikova, A. A. Gerasimenko, A. V. Grishin,

S. A. Gornostaj-Pol’ski, S. A. Lazarev, D. V. Tkachuk

RFNC – All-Russia Scientific Research Institute of Experimental Physics, Sarov, Russia (a-molitvin@expd.vniief.ru)

One of the reasons of operability violation in modern functionally complicated integral microcircuits is associated with a fact that under the effect of pulse ionizing radiation there occurs redistribution of potentials on the internal electrodes due to parasite ionization currents flowing along the supply circuit. The dynamics of these currents is defined by intensity of electric field in a substrate and its physical parameters: life time and mobility of non-equilibrium charge carriers.

The paper gives the results of kinetics investigation of radiation-induced conduction (RIC) in silicon oxide crystals under the effect of a short (~1 ns) pulse of BETA accelerator [1] electron radiation, with absorbed dose power lying in the range from 51012 to 21014 rad(SiO2)/s, and of two types of sapphire crystals produced by SPA (Scientific Production Association) “ELMA” under the effect of LIA-30 [2] bremsstrahlung, with pulse duration at half-height being ~(15-20) ns and power of absorbed dose lying in the range from 1010 to 21013 rad (Al2O3)/s. The dependence of the RIC maximal value on the power of absorbed dose P for the sapphire of the first type is linear while for the sapphire of the second type and silicon oxide it is of power law their exponents being correspondingly equal to  = 0.46  0.07 and  = 0.68  0.06. With the increase of absorbed dose power (at P > 1012 rad (Al2O3)/s) the effect of the process of charge carriers recombination is noticeable in conduction kinetics of both sapphire types. Under the effect of a short (~1 ns) pulse of ionizing radiation the RIC delayed component of the investigated dielectrics becomes noticeable.

The instability of radiation characteristics of sapphire samples produced basing on different technologies is noted. This circumstance imposes particular obligations on the technology of producing sapphire substrates of integral microcircuits.

The given electro-physical parameters of substrates of modern integral microcircuits can be used to evaluate redistributions of potentials on the internal electrodes because of stray ionization currents flowing across the power circuit.

# References

- Belkin N. V., Tarakanov M. Y u., Tarasov M. D. // PTE, 1987, No6, p.133.

- Pavlovskii A. I., Bossamykin V. S., Gerasimov A. I. et al. // PTE, 1998, No2, p.13.

## On the Effect of Adsorbed Water on Radiation Effects in

Oxidized Aluminium and Silicon (100)

S.  N. Novikov, S. P. Timoshenkov

Moscow Institute of Electronic Engineering (Technical University),

Zelenograd, Russia (spt@chem.miee.ru)

Influence of Neutron Radiation on Characteristics of sic p-n Structures

N. G. Orlov, V. T. Gromov, V. P. Shukailo
RFNC-VNIITF, Snezhinsk, Russia (c5@five.ch70.chel.su)

Silicon carbide (SiC) is a promising material of the extreme electronics, it can operate at high temperatures and levels of radiation. The 6H-SiC p-n structures produced at the Ioffe Physicotechnical Institute by р+ layer sublimation epitaxy in vacuum on the basis of n+ Leli substrates were studied. P-n transitions were grown on the facet (0001) SiС, while Al (p-type) was used as a dopant. Concentration of non-compensated impurity in n+ substrate (Nd-Na) was equal to 3·1018 cm-3. Thickness of p+- type epitaxial layers was 1-2 µm, and thickness of n-type substrate was 400 µm. In the research pulsed reactors YAGUAR and IGRIK with τu ~ 1 ms, Ēu = 1.1 MeV were used.

C-V measurements demonstrated that dopant concentration in р+ layer (Na-Nd) р was 5.5·1016 cm-3 for the studied samples.

Dependence of the degree of epitaxial layer radiation compensation versus neutron fluence was found. The data fit well with a linear dependence, the  slope of which determines the speed of charge carriers moving-off in the semiconductor. The speed is, correspondingly, 5.3 cm-1.

Value of the relative change of diode direct branch resistance depending on neutron fluence, experimental values of which are given in Fig. 1, can be estimated through defect concentration:

Fig.1. Relative change of diode direct resistance

vs. neutron fluence

Fn, cm-2

R/Ro

RRo=11−a⋅Фnno

The solid line in Fig.1 is calculation at: а = 5.3 cm-1; n0 = 2.7 1016cm-3; a⋅Фn<no.

Our estimate shows that impurity conductivity is practically completely compensated for this set of devices at fluence about 4·1015n/cm2 and semiconductor conductivity approaches its own one. Thus, fabrication of semiinsulating SiC is possible with the help of neutron radiation. The obtained value of specific resistance of semiinsulating layer at neutron fluence 5.6·1015 n/cm2 was 2.8·105 Ohm·cm.

Dose Hardness of Submicron Integrated CMOS SOI-Transistors

V. P. Shukailo, V. T. Gromov, T. N. Krushinskaya, I. V. Vorozhtsova

FSUE “RFNC-VNIITF”, Snezhinsk, Russia (c5@five.ch70.chel.su)

Gamma-radiation effect on the drain-gate characteristics of n-channel transistors with the embedded oxide having different thickness was investigated. A dependence of threshold voltage shift on the rate of γ-radiation doze accumulation was observed.

A possibility to minimize the effect of space charge on the shift in the drain-gate characteristics both through the neutrons effect, and the electric potential applied to the structure substrate was considered.

On the assumption of the bi-molecular character of recombination, the pulsed reaction of the insulating silicon oxide was numerically simulated in [1, 2]. A self-consistent problem was solved with the regard for external fields and the field of radiation-induced charges. Numerical simulation of the charge generation, recombination, transfer, capture, and annealing in IC CMOS dielectric insulation layers demonstrated the portion of the captured charge to decrease by an order of magnitude in the case of high intensities and weak external fields. This effect was observed at P > 106R/s (solid lines in Fig. 1). Estimates of the threshold voltage shift normalized to the shift at Р = 100 R/s were obtained at the 100 krad dose per pulse. Calculation results correspond to the time of irradiation completion at the least dose rate (t = 1000 s).

The plot in the Figure shows estimates and experimental results averaged over five samples. Similarly to presented estimates, these experimental results are normalized to the shift at the minimum dose rate (Р = 20 R/s). Experimental results are taken for three values of the accumulated -radiation dose: 0.3; 0.9 and 1.5 Мrad.

Fig. 1 Normalized residual shift of threshold

voltage vs irradiation dose rate

ΔU(P)/ΔU(Po)

P, P/c

Therefore, the experiment demonstrated the threshold voltage shift to obviously depend on the -irradiation dose rate. With the 0.3 Мrad irradiation dose, the experimental results were noted to correlate with the data calculated at Е=330 kV/cm.

Yet, with the 108 R/s dose rate, experimental points have significant scatter and this discrepancy with calculations increases with the dose. Measurements were performed with the n/ field used for irradiation at the pulse reactor. The neutron irradiation dose was noted to increase with the -dose and a positive charge in the dielectric was noted to monotonously decrease apparently due to accumulation of electron-trapping centers.

Authors of 3 demonstrated the neutron irradiation to reduce the radiation-induced electric conductivity of the quartz crystal. When SOI-transistors are exposed to the gamma-neutron irradiation, it is possible to assume that decrease both in the accumulated positive charge, and in the radiation-induced electric conductivity of SiO2 is caused by the formation of electron-trapping centers and so, due to electrons trapping, electric conductivity is reduced on the one hand, and a positive charge of holes is compensated on the other hand.

The empirical expression describing the threshold voltage shift in SOI-transistors in the case of the gamma-neutron irradiation is:

ΔUUn=α1+β⋅Ф⋅	, where: α,Do- constants; β - parameter obtained in the studies of radiation-induced electric conductivity of SiO2 [3].

The expression shows that neutron pretreatment when an active area of the instrument  (i.e. insulated silicon substrate) is left untreated, what is basically possible with the SOI-technology, can minimize the effect of the accumulated charge on the output characteristics of the device.

# References

- A. Yu. Nikiforov, A. V. Sogoyan «Simulation of specificities in the behavior of insulating structures under the action of pulsed ionizing radiation», Radioresistance of electronic systems «Radioresistance 2002», scientific collection, issue 5,2002.

- A. Yu. Nikiforov, A. V. Sogoyan «Simulating the dependencies for dose degradation of insulating oxides on the dose rate of ionizing radiation and electrical field intensity», Radioresistance of electronic systems «Radioresistance 2002», scientific collection, issue 5,2002.

- V. T. Gromov, V. P. Shukailo “Radiation-induced electrical conductivity of silicon dioxide”, Journal of Technical Physics, v. 61, issue 6, 1991, p. 194.

Ge-Si Nanostructures Obtained by Deposition from Ion-Molecular Beams

Zh. V. Smagina, A. V. Dvurechensky, V. A. Volodin, V. A. Armbrister

Institute of Physics of Semiconductors, SB RAS, Novosobirsk, Russia (smagina@isp.nsc.ru)

Investigation of the Formation Processes and Properties of Ion-Beam Synthesized Silicon-Based Nanostructures in PTRI UNN

D. I. Tetelbaum, A. A. Ezhevskii, A. V. Ershov, A. N. Mikhaylov, M. Yu. Lebedev,

Yu. A. Mendeleva, A. I. Belov 
Physico-Technical Research Institute of University of Nizhny Novgorod, Nizhny Novgorod, Russia (Tetelbaum@phys.unn.ru)

Formation of nanostructured silicon layers is an important task for the modern electronic technique in connection with the problem of fabrication of light-emitting devices on the basis of silicon, the main microelectronic material. To reach these tasks, the ion-beam methods – ion implantation and ion defect engineering – is widely employed. In the last years during some latest time, investigations contributing to the development of fundamentals of the given methods were carried out at the PTRI UNN

When fabricating the luminescent nanostructured systems by silicon ion implantation into SiO2 followed by annealing (SiO2:nc-Si), the impact of the Si+ dose and annealing temperature on the formation of light-emitting nanocrystals were studied. The model of coalescence (Ostwald ripening), which explains the nonmonotonous dependence of the photoluminescence (PL) intensity on the Si dose and annealing temperature was developed. It was shown for the first time that the PL enhancement can be achieved by the phosphorus ion doping.

Preliminary research regarding the fabrication of light-emitting structures by Si+ implantation into sapphire and thin Al2O3/Si films was performed. The nonmonotonous change of the green PL with the annealing temperature was established.

The method of formation of light-emitting Si layers by ion irradiation was suggested, proved and realized. It was theoretically and experimentally shown that the highest PL intensity is achieved in the dose range that precedes complete amorphization of the surface layer. This is caused by formation of composite structure composed of Si nanocrystalline inclusions (residual crystallinity) in the amorphous silicon matrix. In addition, it was shown that at Ne+ irradiation a second dose region exists (significantly exceeding the amorphization dose), where intensive PL takes place. Nanostructuring is caused by the secondary processes associated with blistering and recrystallization of the amorphous layer in the presence of high mechanical stresses.

The work was supported by the Russian Ministry for Education (grant No. А03-2.9-507, programme "Scientific research of higher school in the priority fields of science and technique"), joint programme of Russian Ministry for Education and CRDF (BRHE REC-001), FP6 Programme (STREP No. 505285-1), grants of INTAS (No. 00-0064) and RFBR (Nos. 00-02-17488, 04-02-16493).

Estimates of Transition Temperatures  in Silicon Wafers Under Ion Bombardment with the Beam Power in the Kilowatt Range

E. G. Tishkovsky, I. A. Shuller

Institute of Semiconductor Physics SB RAS, av. Acad. Lavrentyev 13,

630090  Novosibirsk, Russia (tish@thermo.isp.nsc.ru)

Implanters created for purposes of solid-state synthesis must provide ion implantation up to the doses  1  × 1018 cm-2 with the energies 200 – 300 keV and the beam current up to the tens or hundreds of milliamperes. First of all, the irradiation with the beams of this power sets the problem of the mechanical strength of Silicon wafers, at first moments after the beam switching, especially. Besides, the influence of planes with gettering ability (interfaces) that inserted into crystal is very important when solid-state synthesis is proceed. With the rise of beam power up to certain kilowatt the state of melting or near this one may be the cause of appearance of planes with such properties.

To estimate possibility of this event the special program package was created. It provides simulation of thermal history in Silicon wafer starting from the irradiation parameters (ion energy, beam current, dose) at the input. As a heat source function in heat transport boundary problem the sum of two external arrays calculated by SRIM2003 is used – the array of ionization losses and the nuclear losses one (for example, for oxygen ions with the energy 100 keV they constitute 70% and 30%  of total ion energy, respectively). It is the melting state or near that that must be checked in simulations, so the heat conductivity boundary problem was approximated by simplest absolutely stable finite differences scheme with the adiabatic boundary conditions. The influence of radiative losses was taken into account by the additional iteration procedure, though it is not the optimal use of computer memory and  time.

The results of the transition temperature modeling in Silicon wafers during irradiation by the ion beams with kilowatt power are reported. The results correlation between our and known data concerned  to the wafers thermal history under irradiation with a mean power ion beams is carried out.

Defects Influence on Processes of Formation of Non-Monotonous Impurities Distributions During Recovery of Silicon Layers Damaged by Ion Bombardment

E. G. Tishkovsky, V. I. Obodnikov, L. I. Fedina

Institute of Semiconductor Physics SB RAS, av. Acad. Lavrentyev 13,

630090  Novosibirsk, Russia (tish@thermo.isp.nsc.ru)

It was found that splitting of impurity distributions into several peaks (layered distributions) under high temperature annealing of silicon implanted with heaviest in the investigated raw Se+, so as with more lighter B+ and O+ ions took place [1-3]. These distributions were studied by secondary ion mass-spectrometry measurements in conjunction with transmission electron microscopy investigations. In all cases investigated the splitting of impurity distribution proceeds under scenario of consecutive addition of a mobile component of impurity subsystem. As a result the quasi molecules having selective advantage or the precipitates selected at the coalescence stage of a supersaturated solid solution evolution were formed. Both above entities are well adopted topologically to silicon lattice and highly coherent to the host crystal. The subsystem of defects appears by the way, at which direct interaction of vacancies and self interstitials with the impurity atoms take place at the very beginning of the formation of layered distributions – at the stage of formation of initial and boundary conditions for the more slowly proceeded process of a supersaturated solid solution destruction. And this behavior is appeared independently of crystal lattice disorder (damaged layer is amorphous or there are no amorphous inclusions).

The results of experiments aimed to resolve the defects subsystem influence on these processes with the use of the layered impurity structure peculiarities are reported. It concerns the very earliest stages of damaged layers recovery, especially. On the base of the analysis of data obtained the hypothesis is proposed in which the recovery of a disturbed by ion bombardment layers considered as the process of supersaturated solid solution destruction. This solid solution consists of self-interstitial silicon atoms, amorphous nuclear and micro crystallites produced by implanted ions and silicon recoils in nuclear collision events.

References

- A. A. Taskin, B. A. Zaitsev, V. I. Obodnikov, E. G. Tishkovsky. Semiconductors. 34 (2000) 312.

- V. I. Obodnikov, E. G. Tishkovsky Semiconductors. 32 (1998) 372.

- E. Tishkovsky, K. Feklistov, A. Taskin, M. Zatolokin. Vacuum. 70 (2003) 153.

The Effect of Neutron Radiation On Heterostructural GaAs Field Transistors

V. T. Gromov, V. P. Shukailo, O. V. Tkachyov1,  S. V. Obolensky

RFNC-VNIITF, Snezhinsk, Russia

1NGU, Nizhny Novgorod, Russia (fax +7-35172-51101))

The progress in microelectronics has led to the creation of instruments with nanosize of isolated regions, that is commensurable with the size of radiation clusters formed at ion or neutron radiation. Such a condition can lead to specific features both in cluster configuration conditioned by the geometry, material of structural elements, and directivity of a radiation field, and specific response of similar devices to radiation [1].

In this work the effect of fission spectrum neutrons and 14-MeV neutrons on evolution of FET characteristics was considered. Measurements were taken on the basis of the IGRIK reactor and NG-12I neutron generator.

The experimental transistors made from GaAs with a Schottky-gate having a v-type gate were investigated.

The investigations were performed on experimental Schottky-gate field-effect transistors (FET) made from GaAs. The transistors of two types with standard buffer layer and transistors with a hetero-buffer were investigated. The transistors differed only in the buffer layer.

The stock-gate and the voltage-current characteristics of the transistors depending on the fluence of neutrons acting on the sample were obtained in the course of measurements.

The relative change in threshold voltage of the samples (ΔU/U) versus the total neutron fluence of the fission spectrum (IGRIK) is presented in the figure.

On the basis of the hypothesis for the removal of charge carriers associated with the formation of defect clusters and prevailing of this effect, a relative change in concentration of carriers can be estimated from the following expression:

Δnn0=1−ℓ−ϕkT⋅1−ℓ−vk⋅α⋅Ф

where vk – is the volume of the area of cluster space charge (SCA) formed by neutron radiation, and a (cm-1) – is the proportional coefficient characterizing the efficiency of cluster formation, Ф – is the fluence of radiation neutrons, ϕ - is the average height of cluster’s potential barrier.

Relative change dependences of threshold voltage of samples

(ΔU/U) vs total neutron fluence of fission spectrum (IGRIK)

– transistors with a heterobuffer; – homofield transistors;

  – transistor 3П602Г-2

Ф, 1014 n/cm2

∆U/U

A satisfactory description of the experiment is provided at the following parameters: at the action of fission spectrum neutrons a = 0.2 cm-1, ϕ=0.047 eV,  for 14-MeV neutrons а = 0.95 cm-1,  = 0.017 eV; for heterotransistors the SCA radius is 55 nm, for homostructures the radius is 80 nm.

Therefore, in the course of investigations the following information was obtained:

- the transistors with a heterobuffer are characterized by lower sensitivity to neutron radiation as compared to the homofield transistor;

- the response of high-power transistors with a standard gate to neutron radiation is close to the response of homofield transistors with a “v” type gate;

- the leading factor defining the lower sensitivity is the high concentration of main carriers in the operative channel area that is attained by the presence of a buffer layer.

References

- Obolensky S. V., Kitaev M. A.. Self-consistency of sizes of radiation defect clusters at their introduction into field transistor channel. N. I. Lobachevsky State University, Nizhny Novgorod.

- Gromov V. T., Shukailo V. P., Tkachyov O. V. VNIITF Report Inv. No PS 02.8529/2

- Obolensky S. V. Calculation of electrical-physical characteristics of FETs with a v-type gate. N. I. Lobachevsky State University, Nizhny Novgorod.

# Ultra-fast and Fast Stages of Relaxation of Insulating Materials Excited 
by High Current-Density Electron Beams

D. I. Vaisburd

Tomsk Polytechnic University, Tomsk, Russia (vaisburd@tpu.ru)

High-current electron and ion accelerators whose parameters are adjusted within intervals 0.1-1.0 MeV, 10-10000 A/cm2, 0.1-100 ns were designed and built in the mid-60s. These accelerators, along with nuclear explosion and lasers, became one of the most powerful man-made sources of radiation and particle beams. Their application in the research and treatment of materials for about 40 years has brought along new experimental methods and much information on fast electronic processes and structure defects. The present work is a short review of the main results obtained in this field by means of experiment, theoretical analysis and numerical simulation of the basic processes. A high-power electron beam causes an intensive inflation process covering the time interval of 10-18 to 102 s in an insulating material. This process results in increasing the number and simultaneous lowering of the average energy of transient electronic and lattice excitations. The present work deals with the time sequence of the stages of this inflation process. 10-18–10-17 s: primary impact and Auger ionization in the material and generation of secondary electrons and holes. 10-17–10-15 s: time evolution of the excited electrons energy distribution from the primary beam to the “instantaneous” one, formed prior to electron-phonon scattering. 10-15–10-12 s: time evolution of excited non-ionizing electrons and holes and their energy-momentum distributions from the “instantaneous” to quasi-stationary ones in the process of electron-lattice relaxation. The contribution of short-wavelength phonons is especially large in this stage. 10-12–10-11 s: thermalization of excited electrons and holes filling the edges of the energy bands. The contributions of long-wavelength optical and acoustic phonons are decisive at this stage. 10-11-10-7 s: various trapping/detrapping processes including thermostimulated tunneling from trap to band and back (Poole-Frenkel effect), impact and Auger ionization of traps, and electron-hole recombination. 10-11-10-7 s: strong electric field formation due to trapping the electrons of primary beam in the insulating material, the effects of electron-hole space redistribution and heating in a high electric field. 10-9-10-7 s: formation of strong thermoelastic and shock mechanical fields of two types: an acoustic one which propagates with sound velocities, and a quasi-static one which propagates with thermal conductivity. 10-7–10-3 s: decay of primary acoustic fields into intrinsic modes: longitudinal, flexural, etc., generation and motion of dislocations and cracks, plastic deformation, and brittle destruction of materials. 10-3–102 s: slow thermostimulated diffusion of defects in quasi-static mechanical fields.

The complexity of the processes grows with the increase of a stage duration. The situation is far from a comprehensive description or even understanding. Nevertheless, many new effects observed were explained.