- Radiation-Enhanced and Radiation-Stimulated

Effects

Dose and Temperature Dependences of Radiation-Stimulated Decomposition of Fe-36.5% Ni and Fe-36.5% Ni-0.1% P Invar Alloys

S. E. Danilov, V. L. Arbuzov, V. A. Pavlov

Institute of Metal Physics, Ural Branch RAS, Ekaterinburg, Russia (danilov@imp.uran.ru)

Alloys of the Fe-Ni system form the basis of a large class of steels and alloys, which are widely used in industry and nuclear power engineering. A thermal treatment of these alloys may cause structural and phase transformations (SPT), such as decomposition, ordering, etc. Irradiation accelerates these processes and provides states, which are unachievable upon thermal treatments. Studies of the generation, migration and annealing of point defects reveal regular features of SPT, which also depend on phosphorus alloying that inhibits radiation swelling. Residual resistivity represents a convenient measure of SPT and gives an insight into details and specific features of these processes.

The Fe-36.5% Ni (Ni36) alloy quenched from 1373 K was studied. The Fe-36.5% Ni-0.1% P (Ni36P) compound was prepared by doping of the Ni36 compound with phosphorus from a gaseous phase. The compounds were irradiated by 5 MeV electrons to dose of 51018 cm2 in a linear accelerator and were isochronally annealed in pure helium.

When the alloys were irradiated from 270 to 573 K, the decomposition of solid solution is obtained and the degree of decomposition was a maximum near 420 K. The explanation for this temperature dependence is that the decomposition is weaker at low temperatures owing to the recombination on vacancy clusters formed under irradiation. At high temperatures (573 K) the weak decomposition is due to the decrease in the degree of the equilibrium decomposition. Phosphorus atoms interact with vacancies in the Ni36P alloy under irradiation and stimulate the formation of vacancy clusters. As a result, the concentration of these complexes is larger than in Ni36.

When the irradiated alloys were isochronally annealed, the decomposition continued over the interval from 400 to 500 K. This was due to the dissociation of vacancy clusters and the appearance of freely migrating vacancies. The analysis of the dose dependence showed that the additional decomposition decreased with increasing irradiation dose. The decomposition depended on the concentration of migrating vacancies and the diffusion path of their migration. The effect of phosphorus on SPT mechanisms was analyzed.

The present study was supported financially by RFBR (Project Nos. 04-02-16053 and 04-02-96089).

Structure Metastability and Irradiation Resistance

of Ni-Cr Alloys

V. P. Kolotushkin, S.  N.  Votinov

FSUE A. A. Bochvar All-Russia Research Institute of Inorganic Materials (VNIINM),

Moscow, Russia (kami@bochvar.ru)

The comparison of the results of studying the electrical resistance (Fig. 1) and structure (Fig. 2) of alloys having different Cr contents after holding at temperatures 450 C has demonstrated that in the tempering process the alloys of the composition corresponding to the Ni2Cr phase experience a homogeneous formation of an ordered phase. (Fig. 2a) attended by a significant reduction in their electrical resistance. As the composition deviates from the stoichiometry the precipitations intensity of Ni2Cr particles decreased.

Fig. 1. Influence of Cr content on specific resistance of Ni-Cr alloys as aged at 450 C

The short-range order (SRO) structure developed in alloys containing 39-41 mass % Cr (Fig. 2b). The electrical resistance of those alloys decreased only after long-term ageing. With the Cr content increase above 41 % a discontinuous decomposition (DD) resulted (Fig. 2c) that was attended with the precipitation of  - phase platelets, i.e. the solid solution separation into layers. In the scope between the  - phase platelets Ni2Cr domains were formed.

a                                                 	b                                        	           c

Fig. 2 – Structure of Ni-Cr-Mo system alloys as aged for 40 thousand hours at 450 C:

a) ~32.0; b) ~41.0; c) ~44.0 % mass Cr, respectively

Thus, in Ni – 32-39 % Cr alloys the formation of the Ni2Cr long-range order (LRO) phase proceeded homogeneously while at the contents of 41-47 % Cr the solid solution separated at first to form  - phase platelets and then the ordered phase precipitated. The formation of the platelets started from grain boundaries. The alloy with ~41 % mass Cr revealed the highest stability of the structure during tempering at 350-450 C.

The tendency of the alloys toward ordering or separating into layers might be judged from the sign of the ordering energy that has to be taken into account by the absolute value. With the deviation of the Cr content of Ni-Cr alloys from the compositions corresponding to Eord ~0 the alloys acquire the tendency toward the structure stabilization, in other words, toward ordering or separating into layers.

The study into the Ni-Cr alloy solid solution decomposition at 300 and 450 C by the X – ray diffraction analysis allows one to assume that the alloy density increases with the degree of SRO and decreases with its reduction. The degree of the density increase grows as the composition is moving away from ~41 % Cr. Since at 450 C in the alloys with 39-41 % Cr the SRO structure developed without any indications of the phase decomposition it might be assumed that Eord of those alloys is close to zero. Under open system conditions, i.e. under neutron irradiation, the degree of the SRO in the structure might continuously vary. This is explained by the fact that the precipitating phases change the composition of the surrounding matrix. In this instance the degree of SRO and Eord of a new matrix have to change. The physical characteristics vary respectively with a change in the short range order.

Thus, under the effect of temperature and neutron irradiation the degree of the SRO and density of the  alloy shall continuously grow and diminish in various parts of a matrix. It might be expected that such kinds of changes via creating continuously renewable sinks and traps for vacancies and interstitials shall enforce the degree of their recombination which will promote  the stabilization of the properties of an alloy under irradiation.

Summing up the above discussion, one may suggest a concept of the behaviour of metastable alloys under in-pile neutron irradiation:

Alloys resistant to neutron irradiation have a metastable structure with the energy of ordering close to zero. Those alloys show about the same propensity for separation into layers or ordering while with a deviation from the composition with Eord ~0 they acquire the tendency toward ordering or separation into layers. Under neutron irradiation the dynamic equilibrium arises in the alloy structure with Eord ~0. The continuously renewable vacancy and interstitial sinks and traps enforce the degree of their recombination which promotes the stabilization of the alloy properties under irradiation.

The Effect of Impurities on Radiation-Enhanced

Diffusion in Alloyed  Iron

K. V. Miturev, E. A.Smirnov.

Moscow Engineering Physics Institute, 115409 Moscow, Kashirskoe sh., 31

(smirnov@phm.mephi.ru)

To develop notions about kinetic radiation – enhancement diffusion (RED) in the alloys an experimental data and methods to prognostication RED in the Iron and in Iron alloys are analyzed with take into consideration influence  impurities and alloying. To evaluate characteristic RED in -Fe the method described in [1] was used in this work. The temperature dependence DRED in -Fe was calculated using the following formula:

DRED=(7,37−0,67+1,84)⋅10−13exp[−1,19±0,02eVk⋅T], сm2/s.

and the value of Evm  is in agreement with the literature data.

Within the frame of the dilute solution model the approximate solution of the kinetic equations for RED considering reactions of formation and dissociation of vacancy – impurity atom complexes are analyzed. The obtained expressions for enhancement coefficient RED with impurities are analyzed [2]. The values the binding energy Eb of the pair vacancy – impurity atom for Cr and Mo in  - Fe -(0,760,13) and –(0,720,58) accordingly are presented [3]. The estimations of RED enhancements and temperature dependences of RED coefficient for different concentrations impurities Cr and Mo are obtained.

### References

- E. A. Smirnov, A. A. Shmakov. Defect and Diffusion Forum, 2001, v. 194-199, p.1451.

- E. A. Smirnov, A. A. Shmakov.  Trans. of the Firth Ural Seminar “Radiation Damage Physics of Metals and Alloys”, Snezhinsk, 2003, p. 63

- B. Million, Diffusion in iron alloys, Brno, Institute of Metallurgy, 1981

Two Types of Decomposition under Electron Irradiation

at 420 K in Fe-16Cr Alloys

A. L. Nikolaev

Institute of Metal Physics Ural Branch RAS, 18 S. Kovalevskoi Str., Ekaterinburg GSP 170,

620219, Russia (nikolaev@imp.uran.ru)

Concentration dependencies of ideal and residual resistivities were revealed in Fe-Cr system. Basing on these dependencies the analysis of available data on resistivities and decomposition parameters, obtained by neutron small angle scattering, was done. The interrelations between resistivities variations, on one hand, and fraction of  phase and chromium solid solution depletion, on another one, were found in Fe-Cr alloys. Obtained data on resistivity variations in Fe-16Cr alloy under electron irradiation at 295-420 K were analyzed basing on found interrelations.

Two stages of decomposition were found in initially homogeneous alloy under electron irradiation in Fe-16Cr alloy at 420 K. First stage is characterized by reduction in residual resistivity. It is caused by increase in short-range order parameter due to  precipitate nucleation. The second one is seen as residual resistivity rise and characterized by growth of nucleated  particles. The continuous increase of chromium content in  precipitates is observed through both stages and under doses used is still below equilibrium values. It is likely that the observed process is radiation-induced spinodal decomposition. In equilibrium conditions Fe-16Cr alloy lies far from spinodal area (~30 at. %) in Fe-Cr system.

Another kinetics of decomposition is observed at 420 K if alloy has been preliminary irradiated at 295 K. This case is characterized by fast rise of residual resistivity due to fast rise of  precipitates and interpreted as radiation-enhanced decomposition. It is likely that  phase nucleus formed at defect clusters under 295 K irradiation and further irradiation at 420 K leads to growth of these nucleus.

Change of Structure in the Bulk of Alloy Pd40Cu60

Under Irradiation with Cu and Ar Ions

L. S. Chemerinskaya1, F. F. Makhinko1, N. V. Gushchina1, V. V. Ovchinnikov1, I. N. Sachkov2,

F. Eichhorn3, E. Wieser3

1Institute of Electrophysics, UB RAS, Ekaterinburg, Russia (vladimir@iep.uran.ru)

2Ural State Pedagogical University, Ekaterinburg, Russia

3Institute of Ion Beam Physics and Materials Research, Rossendorf, Germany

The stability of phase state of alloy Pd40Cu60 under irradiation with Cu+ and Ar+ ions was studied. This alloy undergoes active ordering at annealing within the temperature range of 300-500 ºС after preliminary deformation.

Alloying of pure components (Pd 99.99 and Cu 99.99) was performed, The alloy was homogenized at 1000 ºС and quenched in water. After rolling, 25 μm foil was obtained.

Irradiation was carried out in accelerator IMSA-100 (Research Center Rossendorf, Germany) with a scanning beam of Cu+ ions (beam s.a. 5 mm, frequency 10 Hz, scanning area 4  4 cm2, energy of ions E = 40 keV, ion current density in beam j = 100 μA/cm2), doses 1016 ion/cm2 ( = 11 min) and 1017 ion/cm2 ( = 106 min). Heating of the samples did not exceed 210 ºC. The temperature of irradiation was selected proceeding from the resistivity temperature dependence (~ на 120 ºС below the thermal phase transformation А1В2).

To ensure direct comparison of the nature of the effects of light (which in fact is heating) and ion irradiation on the state of alloy Pd40Cu60 samples, use was made of an incandescent lamp. The sample heating temperature was 210 ºC, irradiation time 106 min.

After irradiation with ions (stationary temperature Т = 206 С) and light (Т = 210 С) the samples phase composition was studied by X-ray structural analysis in copper emission band with the use of a monochromator; at that foil was analyzed on both the irradiated and non-irradiated sides.

Under irradiation to the dose D = 1017 ion/cm2 the sample becomes two-phase: beside the FCC phase lines, the ordered B2 phase lines are observed – on both the irradiated and the non-irradiated sides of the sample. In case of heating by lamp and exposure under the above conditions only one phase, A1 (FCC), is observed. At the ion beam irradiation dose D = 1016 ion/cm2 the X-ray patterns of both foil sides display the FCC phase lines only.

In case of the irradiation-initiated transition А1В2, the transition temperature shifts by approximately 120º.

## Studying Deformation-Induced Segregation

## in Fe-Cr-Ni Alloy

S. A. Starikov*, A. R. Kuznetsov*, V. V. Sagaradze*,

I. A. Stepanov**, V. A. Pechenkin**, M. Giersig***

*Institute of Metal Physics UB RAS, Ekaterinburg, Russia (Starikov@imp.uran.ru)

**FRC RF Institute of Physics and Power Engineering, Obninsk, Russia

**Hahn-Meitner-Institute Berlin, Germany

The aim of this work [1] is to study processes of deformation-induced segregation of Ni, by which was explained experimentally seen formation of ferromagnetic clusters at room temperature as a result of a large plastic deformation in stable austenitic steels 12Cr-30Ni and 12Cr-40Ni, in an Fe-Cr-Ni alloy based on a numerical solution of diffusion equations. Fluxes of point defect, their birth and absorption at sinks, and their mutual recombination were taken in account. The alloy studied is modeled as a three-component one. The method of direct resolution of a crystal lattice has been applied for the study of 12Cr-30Ni steel structure after deformation, and also for the study of its composition with the purpose of verifying and refining of the theoretical model.

Numerically solving a set of diffusion equations for a ternary Fe-Cr-Ni alloy, we calculated concentration profiles for the alloy components that arise during severe plastic deformation depending on temperature and the initial alloy composition. We showed that at relatively low temperatures T = 350-400 K a noticeable enrichment of a near-boundary region with Ni and its depletion of Fe and Cr is possible. The dependence of averaged values of the component concentrations and of the width of the enrichment zone at grain boundaries on the temperature of the alloy and nickel content in it has been obtained. The model used permits one to explain the experimentally observed formation of clusters with an enhanced Curie temperature in this alloy after severe plastic deformation. The effect of a sharp increase in nickel segregation to grain boundaries with increasing temperature to 600-800 K is predicted. The structure of grains and their boundaries has been studied using the method of the direct resolution of a crystal lattice. The segregation studied was shown to occur without the formation of nuclei of new phases.

# References

- Kuznetsov A. R., Starikov S. A., Sagaradze V. V., Stepanov I. A., Pechenkin V. A., Giersig M., Phys. Met. Metallogr. 98, No. 3 (2004).

#### Specific Features of Structural-Phase Transformations in

Materials Under Irradiation

S. N. Votinov, V. P. Kolotushkin

FSUE A. A. Bochvar All-Russia Research Institute of Inorganic Materials

(VNIINM), Moscow, Russia ((kami@bochvar.ru)

Using as an example nickel-chromium alloys, austenitic and ferritic - martensitic stainless steels as well as vanadium alloys the paper shows that the effects of in-pile (neutron) irradiation (strengthening, embrittlement, swelling) are directly related to the processes of decomposition of a non-equilibrium solid solution that is characteristic of all commercial steels and alloys, in other words, to the metastability of the structure-phase state.

It is demonstrated that it is the non-equilibrium metastable nature of the initial structure that predetermines the degree of changes in the material properties. This proposition is well illustrated by the results of the investigation of nickel-chromium alloys having various compositions. As quenched and tempered structure of alloys having various chromium contents reveals the following:

- quasiperiodic arrangement of domains upon the long-range ordering of alloys containing ~33 % mass Cr;

- stage of transition  from quasiperiodic to modulated structure in alloy containing ~39 % mass Cr;

- modulated structure (tweed contrast) of alloys containing 39-41 % mass Cr;

- discontinuous decomposition of alloys containing >41 % mass Cr.

The above mentioned structure-phase features effected by different chromium contents in nickel alloys under neutron irradiation at 350 C lead to evolution of different structures of irradiation induced defects. The alloys having the non-equilibrium metastable modulated structure (tweed contrast, short-range ordering) evolve a “stable” irradiation induced structure, i.e. the structure in which traps for point defects are formed. As a result of this, the mobility of point defects decreases and their recombination degree increases which provides for their high mechanical properties and the unavailability of pores.

One  of the most important factors that control the aftereffects of the irradiation damages in steels and alloys, particularly, the time range of the incubation period upon irradiation induced swelling is the stability (to be more exact to say the instability) of their structure-phase state under neutron irradiation. The processes of metastable phase precipitation, short-range ordering, solid solution lamination might be managed by both alloying also including impurity elements-modifiers (B-type) and by heat treatments.

The conclusion is drawn that no pores are observable in the material subjected to the temperature ranges within which the structure-phase transformations of the short-range ordering type, lamination, G-P zones formations etc proceed. In the temperature range in which in the end the stable structure is formed with time we observe porosity and property degradation.