        - General Problems of Radiation Damage Physics

### Modeling Radiation Damage Effects on the Ductility of Polycrystalline Metals

A. Arsenlis*, B. D. Wirth**, and M. Rhee*

*Materials Science and Technology Division,

Lawrence Livermore National Laboratory, Livermore, CA, USA (arsenlis@llnl.gov)

**Department of Nuclear Engineering, University of California, Berkeley, CA, USA

Performance degradation of structural steels in nuclear environments results from the formation of a high number density of nanometer scale defects.  The defects observed in copper-based alloys are composed of vacancy clusters in the form of stacking fault tetrahedra and/or prismatic dislocation loops that impede the motion of dislocations.  The mechanical behavior of irradiated copper alloys exhibits increased yield strength, decreased total strain to failure and decreased work hardening as compared to their unirradiated behavior.  Above certain critical defect concentrations (neutron doses), the mechanical behavior exhibits distinct upper yield points.  In this paper, we describe the formulation of an internal state variable model for the mechanical behavior of such materials subject to these (irradiation) environments.  This model has been developed within a multiscale materials modeling framework, in which molecular dynamics simulations of dislocation – radiation defect interactions inform the final coarse-grained continuum model.  The plasticity model includes mechanisms for dislocation density growth and multiplication and for irradiation defect density evolution with dislocation interaction.  The general behavior of the constitutive (homogenous material point) model shows that as the defect density increases, the initial yield point increases and the initial strain hardening decreases.  The final coarse-grained model is implemented into a finite element framework and used to simulate the behavior of tensile specimens with varying levels of irradiation induced material damage.  The simulation results compare favorably with the experimentally observed mechanical behavior of irradiated materials.

This work was performed under the auspices of the U.S. Department of Energy by University of California Lawrence Livermore National Laboratory under contract No. W-7405-Eng-48.

Study of Accumulation and Annealing of Radiation Defects in FCC Fe-Ni Alloys

with Al and Ti Additives

#### A. P. Druzhkov, V. L. Arbuzov, D. A. Perminov, K. V. Shalnov, V. A. Pavlov

Institute of Metal Physics, Ural Branch RAS, Ekaterinburg, Russia (druzhkov@imp.uran.ru)

It was supposed that small solute additions to reactor stainless steels have considerable effect on microstructural and microchemical evolution under irradiation. Impurity atoms interact either with interstitial atoms (sub-sized impurities) or with vacancies (over-sized impurities) in a solid solution. As a result, mobility of point defects in steels may decrease. If the concentration of impurity additions exceeds the solubility limit, dispersed particles of secondary phases, specifically intermetallics, may precipitate during thermal or radiation-induced aging. It is known that intermetallic particles retard void swelling of stainless steels .

The present study deals with the effect of Al and Ti  impurities both in the solid solution and as part of precipitates like Ni3Al(Ti) on evolution of radiation defects in a model FCC Fe-Ni alloys. Radiation defects were induced under electron irradiation at temperatures from 280 to 573 K. Defects were diagnosed by positron annihilation spectroscopy, which is highly sensitive to vacancy-type defects. The initial microstructure of the alloys was certified after different heat treatments (quenching, aging) using transmission electron microscopy and scanning tunneling microscopy.

Titanium atoms (over-sized impurity) interacted efficiently with vacancies and represented nuclei of vacancy clusters. Vacancy clusters decorated with Ti atoms were thermally stable up to 450 K.

Although aluminum is an over-sized impurity, its interaction with vacancies was not observed. It was found however that coherent intermetallic nanoparticles like Ni3Al inhibited accumulation of vacancy-type defects. Efficiency of this process increased with the irradiation temperature. Results of annealing of defects in Fe-Ni alloys with different initial microstructures have been reported. Mechanisms by which intermetallic nanoparticles influence evolution of radiation defects in austenitic alloys have been discussed.

This study was supported by the Russian Foundation for Basic Research (project No. 04-02-16053) and the Program of Support to Leading Scientific Schools (project No. NSh-639.2003.2).

### Atomic Structure of Interfaces after Radiation and

### Other Intensive External Influences

# V. A. Ivchenko

Institute of Electrophysics, UB RAS, Ekaterinburg, Russia (ivchenko@iep.uran.ru)

In this report are the results of original researches of changes of atomic structure of interfaces in materials after intensive external influences, including radiation, using field ion microscopy (FIM) and atom probe FIM (AP/FIM). The FIM method makes it possible to carry out direct precise investigation of real structure of surface and subsurface layers of a crystal lattice of metallic solids during controllable and sequential removal of surface atoms by an electric field at cryogenic temperatures. The AP/FIM, representing an ultimate-resolution (one-dimensional) mass-spectrometer, allows the chemical nature of an individual surface atom to be defined by means of moving its image to the probing aperture and the subsequent field evaporation with the help of an additional high-voltage pulse. Thus, the chemical composition of individual clusters or particles of a precipitating phase, getting within the microscope field during controllable removal of one atom layer after another, is registered. The tomographic atom probe of field ion microscope (TAP/FIM) allows reconstruction of element atoms distribution of the investigated object in the volume of 15×15×L nm3 during sequential field evaporation of atoms from the sample surface.

The purpose of the work was not only comparison of parameters of the above planar interfaces at an atomic level (i.e., boundary area width, structure of defects, etc.), but also analysis of the kind of influence which had caused occurrence of such disturbance of the material crystal lattice.

The study of ion-implanted materials by the method of field ion microscopy revealed the radiation effects of influence of charged particles beams (E = 20 keV, D = 1018 ion/cm2, j = 300 μA/cm2) on the subsurface volume of atomic-ordering alloys (Cu3Au) and solid solutions (50Pd30Cu20Ag), which decompose with precipitation of an atomic-ordered phase. Formation of an ultradispersed block structure on the surface and in the subsurface volumes of pure metal (iridium) as a result of implantation of argon ions was revealed.

As a result of study an atomic structure of planar defects in metallic W, grade NO polycrystalline Ni, Cu and Ir formed after various intensive external influences, and in mechanically alloyed Cu80Co20, a varying structure of their boundary area was established using the FIM, AP/FIM and TAP/FIM methods. It was shown that the nature of materials atomic structure directly depends on the type of external influence and finally defines their physical and mechanical properties.

The research described in this publication was made possible due to grants No. 04-02-96069-р2004ural_а, and No. 03-02-16560-а of the Russian Foundation for Basic Research and the Program for State Support to Leading Scientific Schools of the Russian Federation (grant No. NSh-639.2003.2).

### Field Ion Microscopy of Radiation Defects in Pt after Neutron Irradiation

# E. V. Popova, V. A. Ivchenko, A. V. Kozlov, V. V. Ovchinnikov

Institute of Electrophysics, UB RAS, Ekaterinburg, Russia (ivchenko@iep.uran.ru)

* FSUE All-Russia Research Institute of Reactor Materials, Zarechny, Sverdlovsk Oblast, Russia

Investigation of radiation defects (individual points defects and their small complexes, as well as radiation clusters formed in non-overlapping cascade regions) in pure platinum irradiated in reactor RWW-2M at temperature ~310 K up to fluence of fast neutrons 6.71021 n/m2 and 6.71022 n/m2, using field ion microscopy (FIM), was the aim of this study. FIM allows carrying out precision research on an atomic scale of changes in the real structure of subsurface layers of metals and alloys crystal lattice occurring as a result of irradiation. At the same time this method gives an opportunity to analyze the structure of a sample in volume by controllable and sequential removal of surface atoms by an electric field.

As a result of irradiation of pure platinum with fast neutrons to a fluence 6.71021 n/m2, the radiation damage was, as a rule, represented by vacancies and their small complexes, atoms, displaced from equilibrium positions (ideal lattice sites) and zones of displaced atoms with the sizes comparable to interatomic spacing.

In the course of study of the structure of pure platinum after irradiation up to fast neutrons fluence of 6.7×1021 n/m2 by the FIM method, the presence of a large number of radiation clusters was revealed. These defects represented depleted zones (areas with locally raised concentration of vacancies) with a “belt” of interstitial atoms. The average concentration  of vacancies in the depleted zones reached 9 %, and concentration of interstitial atoms, 1.5 %. The form of the depleted zones studied with field evaporation was extremely irregular, which complies with the Seeger model. The average size of radiation clusters defined on the basis of calculation of local radii of curvature of top of the emitter and the respective linear distances were ~4 nm. Analysis of multiple micrographs of the irradiated platinum surface allowed the radiation defects density to be determined in the volume. The experimentally measured density was 4  1024 m-3.

Simulation of field ion images of radiation defects in pure platinum by fast neutron irradiated was carried out.

The research described in this publication was made possible by grants No.  04-02-96069-р2004ural_а, and No. 03-02-16560-а from Russian Foundation for Basic Research and Program of State Supporting of Leading Scientific Schools of Russian Federation (grant No. NSh-639.2003.2).

Cluster Structures in Irradiated Solid Solutions and Intermetallics

V. S. Khmelevskaya
Obninsk State Technical University of Nuclear Power Engineering, Obninsk, Russia (khmel@iate.obninsk.ru)

The ion-irradiated (Ar+, 30 keV) metallic solid solutions of the Fe-Cr-Ni, Fe-Cr and V-Ti-Cr systems and some intermetallics (the alloys of the Cu-Mn-Al system containing the Heusler phase) were studied by the methods of structural experiments and mathematical modelling. It was found that some nonequilibrium radiation-induced states with considerable changed structure and properties appear within a certain range of radiation parameters (doses, target temperatures and flux intensities). Electron microscopic investigations show that  the states have the nanocluster structure where small (3-4 nm) clusters are placed within a matrix and  occupy  the better part of the volume. Both microhardness and electronic properties of solid solutions change within the specific range of parameters. At the same time the X-ray diffraction patterns also change. Analysis of the diffraction effects and modelling by the methods of molecular dynamics allow us to propose a concept of clusters formation due to local restructuring of the crystal lattice in the vicinity of the radiation defects. As a result, these clusters have a symmetry different from the matrix icosahedral symmetry. The possibility of the cube-octahedron (polyhedron of the FCC structure) – to the icosahedron transformation, and the stability of the icosahedral cluster within the FCC matrix were studied. The determining role of the special features interatomic interaction potentials was shown. The supposition about icosahedral symmetry of the clusters observed is confirmed by the Moessbauer spectroscopy results. There were found the areas of different symmetry within a matrix, and the isomer shift changes were similar to those in quasi-crystals. The similar radiation-induced state also appears in the Heusler phase and this is accompanied by the magnetic properties changes. The totality of the results allow us to suppose that Td - clusters (the intersection of four icosahedrons) are formed in this case. As the magnetic properties are determined by the spatial arrangement of the atoms with the magnetic moment (Mn atoms), the appearance of cluster leads to changes in the observed magnetic properties.

Calculation of Primary Knocked-on Atom Spectra and

Dose Rates for WWER Vessel Steels

Yu. V. Konobeev, V. A. Pechenkin, I. V. Pyshin

State Scientific Center of Russian Federation, A. I. Leipunsky Institute of Physics and Power Engineering,

Obninsk, Russia (konobeev@ippe.obninsk.ru)

For comparison of data on irradiation embrittlement of reactor pressure vessel steels in WWERs as well as of other structural materials irradiated at different locations in such reactors, it is necessary to calculate the damage dose in terms of displacements per atom (dpa). For a development of theoretical models of irradiation embrittlement and physically based regulatory guides it is important also to calculate "effective" dpa and spectra of primary-knocked-on atoms (PKA).

The results of calculating dose rates and PKA spectra at internal and external vessel surfaces, and also for locations of surveillance samples in WWER-440 and WWER-1000 are presented. As input data, the results of 3D-calculations of neutron and gamma spectra in these reactors were used. Dose rates in dpa were calculated using known differential displacement cross sections as well as by convolution of PKA spectra with NRT-standard model recommended by IAEA. It is shown that the dose rates at the location of reactor pressure vessel steels surveillance samples are approximately by one order of value higher than at the internal surface of the WWER-440 vessel. The calculations of "effective" dpa were made using data on the PKA cascade efficiency available in the literature on molecular dynamics simulations of displacement cascades. The calculation results of gamma-quanta contribution into dose rates are also presented.

This work was supported by the Russian Foundation for Basic Research under the Project # 04-02-17278

On Strength and Failure of Metals and Alloys under Thermal Shock

V. T. Punin, A. V. Grunin, A. M. Molitvin, A. V. Grishin, S. A. Gornostaj-Pol’ski

Russian Federal Nuclear Center – All-Russia Scientific Research Institute of Experimental Physics,

Sarov, Russia (a-molitvin@expd.vniief.ru)

The production of different power and irradiating facilities has stimulated the study of mechanical properties of materials under the effect of high power radiation fluxes: electron, X-ray, laser, ion beam fluxes etc. Widely studied are surface and deep strengthening of metals and alloys under irradiation, generation of elastic and shock waves, failure of materials under thermal shock etc, (see, for example, [1-5] and references to them). The interest towards investigation of materials failure under thermal shock is conditioned to a considerable extent by the fact that stresses occurring under thermal shock can lead to destruction of the components of power and irradiating facilities themselves. The results of spalling fracture under thermal shock assist in the development of the theory of solids failure.

The report gives the results of spalling fracture research of metals and alloys under thermal shock, the investigation results of the effect of irradiated object geometry to the pattern of its thermal-mechanical failure. Within the frames of kinetic approach to the problem of spalling considering spalling as a process proceeding in time there are found time dependencies of spalling strength of copper, nickel, titanium, brass, bronze, molybdenum, tungsten, tantalum, cadmium, lead, zinc, silver and steels under thermal shock. It is demonstrated that the longevity of metals and alloys under thermal shock decreases exponentially with the growth of amplitude of rupture stresses.

Within the framework of energy approach based on the comparison of the energy store in the sample and failure operation there are found time dependencies on the critical specific energy of failure for the above-mentioned metals and alloys under thermal shock. It is demonstrated that the critical specific energy of material failure required to carry out the operation of detachment, separation to segments of the object incurred to thermal shock, grows with the increase of the duration of tensile stresses effect in the spall cross-section.

The geometric effects conditioned by cumulation of stresses, occurrence of cumulative ejection of material, loss of stability under the effect of intense fluxes of penetrating radiation energy to cones, conic shells, discs and rods can lead to the decrease of fracture threshold and to the increase of the degree of object failure under thermal shock.

# References

- Eliezer S., Gilath I., Bar-Noy T. // J. of Appl. Phys. 1990, v. 67, No 2, p. 715.

- Vorobiov S. A., Lopatin V. S., Pogrebnyak A. D. et al. // ZhTF, 1985, v. 55, No 6, p. 1237.

- Bonyushkin Ye. K., Glushak B. L., Zavada N. I. et al. // PMTF, 1996, v .37, No 6, p. 105.

- Molitvin A. M., Borin I. P., Bossamykin V. S. // PMTF, 1996, v. 37, No 5, p. 162.

- Molitvin A. M. // PMTF, 2003, v .44, No 1, p. 163.

Plastic Deformation of Materials under Irradiation

P. A. Selyshchev, V. V .Moskalenko

Kiev National Taras Shevchenko University, Faculty of Physics,

Glushkov Avenue,6, Kiev-022,02022, Ukraine(selyshchev@mail.univ.kiev.ua)

The problem of material creep inside reactor plants, where beside the force and thermal factors, an the important role is played by the factor of continual irradiation, is all the more actual nowadays in the situation of intensive development of nuclear power engineering.

This paper is a theoretical research to explain non-linear characteristics (bends, kinks) of the dose-dependent creep speed of impurity materials under irradiation. These characteristics were observed experimentally many times.

The dynamics of transfer creep of pure materials is studied in [1]. Of special interest is the analysis of the influence of impurity atoms, which are always present in real metals,  on creep.

The investigation was carried out within the framework of the “climb-creep” model. It was supposed that the speed of creep is proportional to the module of difference of fluxes of interstitial atoms and vacancies. It was assumed that a climbing dislocation entraps vacancies. An impurity binds free vacancies and interstitial atoms in low-mobility complexes.

It was found that, depending on irradiation conditions and behaviour of the irradiated specimen, one or two stationary creep states can be realized. The concrete stationary creep state is defined by reference states of the sample. The creep speed tends to a stationary value monotonically or passing an extreme. At the moment of fluxes on vacancies and interstitial atoms locations becoming equal, the creep speed will be zero. This results in kinks of the dose-dependent creep curve.

The change in impurity concentration leads to modification of the stationary values of creep speed and concentration of defects. But it does not bring about qualitative modification of the dynamics of non-stationary creep. The phase portraits get deformed, though staying topologically similar. All qualitative effects (breaks, kinks,  hysteresis, collapse of creep speed) are inherent to creep in the irradiated materials, and take place both in pure materials and in the materials with admixtures.

The obtained results allow us to predict the materials behaviour and to determine optimal conditions of their exploitation.

References

- Selyshchev  P. A.  Samoorganizatsia radiatsionnoi phisiki// Kiev: Aspect poligraf, 2004, p. 240

Properties of Point Defects and Anomalous Features of

Stage III in Fe-16Cr Alloy

A. L. Nikolaev

Institute of Metal Physics, Ekaterinburg GSP-170, 620219 Russia (nikolaev@imp.uran.ru)

The resistivity recovery (RR) after low temperature electron irradiation was investigated in Fe-(14-16)Cr alloys, non-doped and doped with impurities (about 0.1 at. % of Au, N and Si). A modification of the method using two samples of the same alloy with different initial defect concentrations and permitting identification of the short-range order (SRO) establishing onset in course of post irradiation anneal was applied. The reliable identification of the SRO establishing onset required further method modification: a difference between RRs in these samples was introduced. The onset of the SRO establishing in impurity-doped alloys is shifted as compared to that in non-doped alloy by about 20 K. This temperature interval was attributed to difference between free migration onsets of vacancies and interstitial atoms (IAs). In non-doped alloy onset of vacancy free migration initiates the SRO establishing while in doped ones vacancies are trapped at impurity atoms and the SRO manifestation is driven by onset of IA migration at higher temperature.

Respective RR peak is seen only for IAs at 225 K and no peak for vacancies can be found in RR spectra at all. According to the shift in onset temperatures of free migration the vacancy peak (stage III) should be positioned around 205 K.

Comparison of RR data in Cr16 and Cr16Si alloys around 205 K demonstrates that replacement of unknown vacancy reactions in Cr16 with vacancy trapping at Si atoms in Cr16Si is accompanied with increase in RR and appearance of invisible before vacancy peak. This result indicates that dominating reaction in which participate migrating vacancies is vacancy clustering with no visible signs of recombination. Analysis and comparison of present data with available data on RR and positron annihilation in close Fe-15Cr [1] lead to conclusion that vacancy clustering is stopped at di-vacancy formation step. This situation is possible in BCC lattice, in contrast to FCC one where di-vacancies are always more mobile than vacancies. Dominating di-vacancy formation in stage III will actually result in negligible RR giving negligible and unobservable RR peak. Di-vacancy formation is also not resolved by spectroscopy of positron lifetime since the latter is very close in vacancies and di-vacancies [2]. Thus, stage III is almost invisible for positrons too.

Following di-vacancy formation the IA migration at slightly higher temperatures (around 225 K) leads to recombination of IAs with immobile di-vacancies resulting in release of mobile mono-vacancies. Since both type defect migration contribute to defect annealing over these temperatures, their mutual migration enhances as defect recombination as SRO establishing and, therefore, gives rise to large RR peak. Since the annealing processes in this stage to large extent are determined by di-vacancies formed in preceding stage III and vacancies released due to recombination, this stage RR peak height is strongly affected by vacancy traps.

It is shown with available experimental data that with application of traditional experimental methods and approaches such as RR (one sample), positron lifetime and slight doping (~0.01 at. % of impurity vacancy traps) only, the RR peak at 225 K (attributed to IA migration) demonstrates distinct classical signs of vacancy migration stage (stage III). And only thorough analysis with use of additional data obtained within different approach can unmask this miracle.

The work was carried out with the financial support of Russian Foundation for Basic Research (grant # 04-02-16053).

References

- Dimitrov C., Benkaddour A., Corbel C. and Moser P., Ann. de Chimie (France) 16, 319 (1991)

- Puska M. J., Niemenen R. M., J. Phys. F: Met. Phys. 13, 333 (1983)

Determining the Temperature of Atomic Displacement Cascade Regions at

Thermal Peak Stage

V. V. Ovchinnikov, B. Yu. Goloborodsky, F. F. Makhinko, V. I. Solomonov, O. A. Snigireva

Institute of Electrophysics, UB RAS, Ekaterinburg, Russia (Vladimir@iep.uran.ru)

An -iron sample (armco-iron 99.99 Fe) was irradiated under vacuum at residual pressure < 10-5 mm Hg, with a continuous Ar+ ion beam, with the ions energy varying from 5 to 20 keV and at ion current density between 50 to 150 μA/cm2. The target glow spectrum was measured with the use of a multichannel photodetector on the basis of an OS-12 diffraction spectrographer and a CCD rule in the range from 360 to 850 nm. Equipment spectral resolution over the entire range was 2 nm; wavelength measurement error, not worse than 1.2 nm. The light flux from the irradiated sample was transmitted to the photodetector via a multiple fiber light conductor, the receiving end of which was placed at a distance of 1 cm from the sample edge and at an angle of 60º to the sample surface. The light flux from the surface about 6 mm in diameter was measured.

In all spectra, two broad bands of thermal Planck radiation are present. The first band with the maximum at wavelength ml (varying from 500 to 570 nm) corresponds to Planck surface plasma radiation. The second band maximum at wavelength m2 is located in the IR spectrum region inaccessible for the photodetector. This band is observed in the form of its short-wave wing only and is determined by thermal radiation of the target heated by the action of the beam.

Against the background of these broad bands, significantly narrower non-equilibrium radiation bands are observed in all spectra.  Of them at least two narrowest bands, one at 1 = 659.2 nm (the strongest in all spectra) and its weaker satellite at 2 = 794.2 nm, are in good agreement with the iron atoms radiation. Besides, eight comparatively broad bands (maximums) are observed in the short wave part in all spectra. Evidently, all these bands present a recombination radiation of iron atoms, and the band with the longest wave length corresponds to the Fe2+ ions radiation. In the long-wave part of the spectrum, a series of strong narrow bands is observed, one of which may be attributed to the argon atom radiation.

The smallest wave length λml = 500 nm for the Planck radiation maximum is observed at the Ar+ ions energy of 5 keV. According to the Wien law, T=b/λm1, this corresponds to the temperature of plasma T  5796 K (b = 0.002898 mK – Wien constant). The Planck radiation broad short-wave band is connected with the thermal peaks radiation emerging as a result of evolution of dense atomic collision cascades. The fact that density of the energy liberated in the cascade, and respectively, the thermal peak temperature, grows with decrease in the ions energy (while wave length decreases) is in agreement with the calculation results in Ref. [1]. The results of work present direct temperature measurements of an ion subsystem in a thermalized cascade.

Work was carried out with the support of the Russian Foundation for Basic Research (grant No. 04-02-17602-a).

## References

- Ovchinnikov V. V. et al. Transactions of X International Conference “Solid-State Radiation Physics”, 2000, p. 391-394.

Role of Mobile Vacancy Clusters in Swelling of Metals

V. А. Pechenkin, Yu. V. Konobeev, I. V. Pyshin, A. M. Minashin, S. A. Podgornov

State Scientific Center of Russian Federation – A. I. Leipunsky Institute of Physics and Power Engineering, Obninsk, Russia (vap@ippe.obninsk.ru)

As a rule, diffusion fluxes of di-vacancies and larger vacancy clusters are not taken into account in existing theories of nucleation and growth of voids in metals and alloys under irradiation. However, it is known that diffusivities of di-vacancies and three-vacancies in FCC. metals are higher than diffusivity of monovacancies. Therefore, in such metals diffusion fluxes of smallest vacancy clusters may essentially contribute to the void formation and growth under irradiation. According to limited literature data, in BCC metals the diffusivity of di-vacancies is less or comparable with the monovacancy diffusivity.

Binding and migration energies of di-vacancies in -Fe were calculated using the molecular dynamics method. Pairwise interatomic potential and “embedded atom” potential have been used for the calculation. It was found that the most stable configuration of di-vacancy is two monovacancies separated by the second neighbour distance, while the binding energy of di-vacancy with monovacancies separated by the nearest neighbour distance appears to be less than 0.1 eV. For -Fe the calculated effective migration energy of di-vacancy is comparable with that of monovacancy.

Steady-state concentrations of monovacancies, di-vacancies and interstitials in FCC. (Сu, Ni) and BCC (V, Fe) metals were calculated in the case of homogeneous generation of point defects as well as the case of cascade-forming irradiation. It was shown, that in FCC metals the diffusion flux of di-vacancies may essentially exceed the flux of monovacancies and determine the void growth at relatively low temperatures. As an example, for nickel it was shown that the account of di-vacancy mobility in the framework of the homogeneous void nucleation theory leads to an essential increase of void nucleation rate in the whole temperature range of swelling.

The model calculations of swelling rate in metals under neutron, electron and ion irradiation were performed. It was shown that the account of di-vacancy mobility can result in an essential increase of swelling rate of FCC. metals, especially at temperatures, at which concentrations of point defects are determined by their mutual recombination. In BCC metals mobile di-vacancies do not bring any essential contribution to the swelling rate. Thus, a relatively high mobility and thermal stability of small vacancy clusters in FCC. metals can be one of the reasons of higher swelling of these metals as compared with BCC metals.

This work was supported by the Russian Foundation for Basic Research under the Project # 04-02-17278.

The Mechanism of Influence of Ni3Al Intermetallic Nanoparticles on Evolution of Radiation Defects in Model FCC Iron-Nickel Alloys

D. A. Peminov, A. P. Druzhkov, V. L. Arbuzov

Institute of Metal Physics, Ural Branch of RAS, Ekaterinburg, Russia (d_perm@rambler.ru)

Aged austenitic alloys are one of perspective structural materials for nuclear reactors. Intermetallic Ni3Ti(Al, Si) precipitates which arise in these alloys decrease radiation defect accumulation and, consequently, radiation swelling.  Nevertheless, the mechanism of influence of precipitates on defect behavior are not completely known. The purpose of this work was investigation of influence of intermetallic Ni3Al precipitates on the accumulation and annealing of vacancy-type defects in model austenitic alloys at an early stage of radiation damage (104-103 dpa).

Fe-Ni and Fe-Ni-Al FCC alloys were studied in this work. Part of Fe-Ni-Al alloy samples was aged on 823 К and 923 К during some time for creating of coherent Ni3Al intermetallic particles. The particles size was 0.4 to 7 nm. All samples were irradiated by 5 MeV electrons at 300 К, 423 К and 573 К in linear accelerator. The angular correlation of annihilation radiation (ACAR) method was used to investigate defect structure. This method is very sensitive to vacancies and vacancy agglomerates but insensitive to interstitial atoms and their agglomerates. In addition, ACAR can provide information about local chemical composition of environments of positron trapping site.

Positron states were detected in “defect-free” nano- and subnanosized intermetallic particles. This effect permits to investigate the atomic structure of particles [1]. The Ni3Al particles decrease defect accumulation under irradiation at 423 К and 573 К. At the same time, the effect of precipitates on defect behaviour under 300 К irradiation was not detected. Due to presence of positron states in Ni3Al particles it was defined that vacancy agglomerates mainly create in the matrix but not in particles. Taking in the work data show that defect accumulation loss is caused by recombination mechanism showed in [2].

This study was supported by Russian Foundation for Basic Research (project No. 04-02-16053) and program of the Presidium of Russian Academy of Sciences "Fundamental Problems of Physics and Chemistry of Nanosized Systems and Nanomaterials" (project No. 7 of the Institute of Metal Physics, Ural Division of the Russian Academy of Sciences).

References

- Druzhkov A. P., Perminov D. A., Arbuzov V. L., Stepanova N. N. and Pechorkina N. L., J. Phys: Condens. Matter 16 6395-6404 (2004)

- Turkin A. A., Bakai A. S., J. Nucl. Mater. 270 349-356 (1999)

Calculation of Defect Creation Efficiency by Mesoscopic Model of Cascade

S. V. Rogozhkin1, 2, Yu. N. Devyatko1, A. A. Plyasov1

# 1Moscow Engineering Physics Institute (State University), Moscow, Russia

2State Scientific Center of Russian Federation, A.  I. Alikhanov Institute

of Theoretical and Experimental Physics (rpcm@mephi.ru)

At the initial development stage of an atom-atomic collision cascade there are a lot of displaced and knocked-on atoms in the damaged area. However, after fast annealing only a small part of defects remain in the cascade area, which is characterized with the coefficient of cascade efficiency.

Calculation of the efficiency of the cascade as a source of radiation defects arouse a broad interest. The main investigation method of the cascade relaxation is molecular dynamics (see, for example [1, 2]).  However, the range of this method is restricted with initial stages of the cascade relaxation (~10-10 c). Moreover, results obtained using the method of molecular dynamics critically depends on interatomic interaction parameters used.

In the work presented the cascade efficiency is investigated on the base of the mesoscopic model of cascade processes [3, 4] and the influence of the change in the thermal conductivity mechanism during cascade relaxation is studied. The calculations are completed for cascades in the iron at different material temperatures and energies of primary knocked-on atom. The results showed that the mechanism of phonon thermal conductivity, which dominates at the beginning of the diffusion stage, leads to efficient decrease in the number of defects in cascade area. The results obtained for fast annealing (~10-10c) are in accordance with those by the molecular dynamics method. It is shown that further cascade relaxation leads to increase of annealed defects part and, correspondingly, to decrease of the coefficient of the cascade efficiency.

This work was possible due to partial support of the Russian Foundation for Basic Researches (grants 02-02-17489 and 04-02-17064).

## References

- English C. A., Foreman A. J. E., Phythian W. J., Bacon D. J., Jenkins M. L., Materials Science Forum, 97-99, 1 (1992)

- Stoller R. E., Journal of Nuclear Materials, 276, 22 (2000)

- Devyatko Yu. N., Klimov M. V., Makletsov A. A., in: Ionizing radiations and laser materials, Energoatomizdat, Moscow, 1982, p. 101

- Devyatko Yu. N., Chernov V. M., Pliasov A. A., Rogozhkin S. V., VANT (Materials science and new materials), 1(62), 288 (2004)

### Radiation Defects In Ion Implantation Alloys With Long -Range Order

N. N. Syutkin

Institute of  Electrophysics, Ural Branch of Russian Academy of Sciences,

Ekaterinburg, Russia (micros@iep.uran.ru)

Field ion microscopy (FIM) was used to investigate atomic structure of alloy with long-range order  after  implanting them by gas ions.

Ionic irradiation is shown  to create various defects in ordered alloys, such as  : dislocation, dislocation barriers, accumulation of dislocation, atomic  segregation, vacant voids, etc.

Distribution and dimensions types of the defects were estimated. The defects, which arise in the process of ion implantation, are established as finding at depths exceeding their projected track.

The obtained results are discussed.

### Simulation of Atomic displacement cascades in zirconium by molecular dynamic method

M. Yu. Tikhonchev, G. A. Shimansky
Federal State Unitary Enterprise “State Research Centre of Russian Federation – Research Institute of Atomic Reactors, Dimitrovgrad, Russian Federation (dns@niiar.ru)

Damage dose is one of important radiation influence characteristics used for investigation physical and mechanical properties of materials under long period of irradiation. Its reliable evaluation allows to compare different irradiation conditions and forecast material behavior in operating and designed reactors depending on measure of radiation effect. Procedure of damage dose calculation corresponding to NRT-standard [1] is stipulated by specialists in area of reactor materials science and reactor dosimetry.

Substantial value that is used for damage dose evaluation according NRT-standard is average threshold displacement energy Ed. The very value includes practically all information about crystal lattice, where displacements occur, and displacement action. Ed is determined presently by means of rather laborious experiments or via computer simulation. The role of the latter permanently increases.

Also, new radiation damage models were developed during last years. They are destined for more correct evaluation of damage ability of several energy groups of neutron spectrum. Under displacement cascade evolution part of generated defects annihilate or go in immobile clusters. Therefore at present many researches trend to account fractions of freely migrating defects (FMD) [2,3,4] for comparison material irradiation results in various spectra of impinging particles.

Present paper is dedicated to computer simulation of atomic displacements in zirconium by molecular dynamic method [5]. N-body inter-atomic potential based in embedded atom method [6] was used. Atomic displacements in zirconium from primary knocked-on atom (PKA) with energy up to 10 KeV were simulated. Threshold displacement energy values for different crystallographic directions were calculated in temperature range from 0 to 600 K. It is shown that Ed value for zirconium has rather low temperature dependence. At the same time decreasing of threshold energy anisotropy under temperature rise is well observed. Evaluations of part of "survived" defects under cascade evolution are performed.

Obtained results may be used for radiation damage evaluation in zirconium and its alloys.

Authors would like to thank A. N. Balashov and E. I. Shamarina from the Tver State Technical University for their invaluable aid.

References

- Norgett N. J., Robinson M. T., Torrens I. .M., The proposed method of displacement doze rate calculation, -Nucl. Eng. and Design, 1975, 33, p. 50-56.

- Wiedersich H. Effects of the primary recoil spectrum on microstructural evolution. - J. Nucl. Mater. 179-181 (1991) 70.

- H. L. Heinisch. Simulating the production of free defects in irradiated metals.// Nuclear Instruments and Methods in Physics Research B 102 (1995), pp. 47-50.

- B. Petrovic, A. Haghighat, A. Motta, V. Kucukboyaci, J. Kwon. Contribution of gamma irradiation to material damage at BWR core shroud and pressure vessel. Proceedings of the 1998 ANS Radiation Protection and Shielding Division Topical Conference “Technologies for the New Century”, April 19-23, 1998, Nashville, Tennessee, USA, V. 2, pp. 25-32.

- V. V. Kirsanov. Computer experiment in atomic science of materials. Moscow, Energoatomizdat, 1990 (in Russian)

- Oh D. J., Johnson R. A. Simple embedded atom method for FCC and HCP metals.// J.Mater.Res., 1988, v. 3, p. 471.

Model of Atomic Displacement Cascades in Monocrystal Materials under Irradiation with He+ and Ar+ Ion Beams with Wide Energy Spectrum

N. V. Volkov, B. A.Kalin, I. V.Oleynikov

Moscow Engineering Physics Institute (State University), Moscow, Russia (volkov@vlk.mephi.ru)

In a number of cases the technique of simulation experiments supposes the use of ion beams with a wide energy spectrum distribution (ion implantation, action by thermonuclear plasma and others).  One of the main moments of such experiments is the adequacy of forming the atomic collision cascades that generate defects, determines, at the first stage,  the mass transfer in an irradiated layer, and later on the structure-phase state of the investigated material surface layers.

The present paper shows the results of calculating the form of a cascade function in case of materials irradiation (Be, monocrystals: diamond, Si, Cu, Fe, Ni, Mo, W) by a beam of He+, Ar+ ions with a wide Gaussian energy spectrum in the 1-50 keV energy range, at a mean energy of ions of 1, 5, 10, 20, and 30 keV.

The form of the cascade function, which takes account of the energy spectrum of ions, was chosen on the basis of a comparison of the calculated sputtering yields and the parameters of atomic mixing with experimentally measured data, such as the sputtering yield Sp, the penetration depth of ions Rp, and the penetration depth of PKA from a film into the substrate represented as a matrix Xm.

The formation of radiation defects was investigated by transmission electron microscopy. The regularities of a mass transfer under irradiation were studied by mass-spectrometry of secondary ions, Rutherford back-scattering and the method of nuclear recoil.

TRIM-Sp and TRIM-Rp codes (which uses Bearsak-Cigler potential) were chosen as the most suitable test program. They gave a good agreement  with the experimental results for the irradiation of monocrystal targets with mean and big atomic masses (Cu, Fe, Ni, Mo, W).  However, under irradiation of Be and monocrystals of C and Si (110), the difference between the calculated and experimental results was equal to or more than 200-500%.

Also it has been shown that the TRN-standard satisfactorily describes the experimental results obtained under irradiation of materials by Ar+ ions with the energy more that 20 keV. But for the energy range of 1 – 20 keV, the calculated number of displaced atoms appears to be overstated in comparison with those obtained from the experiments. These deviations seem to be connected to the distribution peculiarities of radiation defects along the target depth, their interaction with sequential cascades of the atoms displacement, as well as with radiation-stimulated processes under irradiation of materials by an ion beam with a wide energy spectrum.