- Facilities and

Techniques of

Experiment

Integral Method of Measuring Electron Beams and

Photon Emission Energy Spectra

A. G. Berezovsky, V. P. Pudov

FSUE RFNC – All-Russia Research Institute of Technical Physics, Snezhinsk, Russia (dep5@vniitf.ru)

On Angular Distribution of High-Power Accelerator Electron Beams

Ejected to Atmosphere

A. P. Stepovik, V. S. Blinov, T. V. Kupyrina
FSUE RFNC – All-Russia Research Institute of Technical Physics, Snezhinsk, Russia (dep5@vniitf.ru)

### Silicon Carbide Detectors with High Energy Resolution

E. V. Kalinina*, N. B. Strokan, A. M. Ivanov, G. F. Kholuyanov, G. A. Onushkin, G. N. Violina**

*Ioffe Physicotechnical Institute, RAS, St. Petersburg, 194021 Russia (evk@pop.ioffe.rssi.ru)

** St. Petersburg State University of Electrical Engineering, St. Petersburg, 197376 Russia

In this paper the energy resolution of 4H-SiC detectors based on high pure epitaxial layers has been studied using -particles.

4H-SiC epitaxial layers with thickness of 50 m and a concentration of uncompensated donors Nd-Na = 6 × 1014 cm-3 were grown by chemical vapor deposition (CVD) on commercial 4H-SiC wafers. Cr Schottky barriers (SBs) with thickness of  0.1 m and areas 1×10-2 cm2  were made by thermal vacuum evaporation. The diode structures were irradiated by -particles with energies of 5.1-9.0 MeV using the isotopes 239Pu, 240Pu, 241Am and 238Pu.

The structures of the defective centers in samples studied with photoluminescence (PL) at temperature of 77 K, from capacitance-voltage characteristics (CV) and DLTS data at the temperatures ranged from 93 to 700 K. The diffusion length of minority charge carriers - holes (Lp) were evaluated from the dependence of the photo-current on reverse voltage. These data were compared with those obtained from the dependence of the charge collection efficiency  (CCE) under irradiation. Forward and reverse current-voltage characteristics of  diode structures  were measured under DC conditions.

PL spectra and DLTS data of the investigated samples revealed a small quantity of the impurity centers caused to enough high values of  Lp into CVD epitaxial layers, 9-13 m. The width of the space-charge region in diode structures under 400 V were commensurable with  -particles ranges with energy of  9 MeV, reverse currents of SBs were less than 1 nA.  As a result, the saturation of  the dependence of a detector signal as a function of the reverse bias was observed in the range of 100-200 V indicated that all nonequilibrium charges generated by -particles were collected, i.e. CCE = 1. The spectra of -particles showed that detectors based on 4H-SiC CVD epitaxial layers clearly resolved lines being 18.8 keV apart, which allowed to reveal the fine structure peaks in the -decay spectra, that corresponded to the energy resolution equal to 0.35 %. Such energy resolution was commensurable with Si-detectors and was obtained for the first time, that allows to use its for spectrometry of nuclear irradiation under extreme conditions - at high temperatures and in chemical aggressive environments.

References

- A. M. Ivanov, E. V. Kalinina, A. O. Konstantinov, G. A. Onushkin, N. B. Strokan, G. F. Kholujanov, A. Hallén: Technical Physics Letters 30, 575 (2004).

- N. B. Strokan, A. M. Ivanov, E. V. Kalinina, G. F. Kholujanov, G. A. Onushkin, D. V. Davidov, G. N. Violina. Accepted for publication in Semiconductors, 39 (2005).

New Reactor Source of Neutrons of Microsecond Duration

A. V. Lukin, E. P. Magda, D. V. Khmelnitsky, Yu. I. Chernuhin

FSUE RFNC – All-Russia Research Institute of Technical Physics, Snezhinsk, Russia (dep5@vniitf.ru)

The most powerful neutron pulses are generated in reactions of fission of heavy nucleus in pulse nuclear reactors. At the minimal width of a pulse ~50 µs the output of neutrons can make ~1017. One of the ways to significant reduction of duration of a neutron pulse in reactors is to provide an effective feedback on reactivity. For this purpose it is offered to use metal plutonium in -phase as a material for core. At temperature ~100-120 C plutonium undergoes phase  transformation with change of density by ~10 %. For a core consisting of metal plutonium in -phase such change of density would correspond to change of reactivity also by ~10 %. For generating a pulse of fissions of duration  10 µs in a reactor with time of generation of instant neutrons  ~10-8 s it is necessary to provide efficiency of a feedback ΔK≥6Λτ~10-2. Therefore core with the effective feedback based on phase transformation of plutonium, can consist to the most part of uranium and to a smaller part from plutonium. For example, for research of nuclear pumped lasers such source of neutrons could appear rather promising. Its application in research of radiating resistance of the radio-electronic equipment is possible.

Bremsstrahlung Generation in Plant MIG in

Electron Beam Deep Pinching Regime

N. A. Ratakhin1, V. K. Petin1, S. V. Shlyakhtun1, Yu. A. Sukhovatitsyn1, A. F. Korostelev1,

E. N. Volkov1, V. F. Fedushchyak1, A. G. Berezovsky2, V. B. Bychkov2, O. V. Zatsepin2, Ya. Z. Kandiev2, V. D. Lartsev2, D. G. Modestov2, V. P. Pudov2

1Institute of High-Current Electronics SB RAS, Tomsk, Russia

2FSUE RFNC – All-Russia Research Institute of Technical Physics, Snezhinsk, Russia (dep5@vniitf.ru)

Measurement of Grǜneisen Parameter for Anisotropic Carbon Material

with the Use of Electron Accelerators

A. P. Stepopvik 
FSUE RFNC – All-Russia Research Institute of Technical Physics, Snezhinsk, Russia (dep5@vniitf.ru)

In recent years, the direction associated with study of mechanical properties of materials, when radiation energy is rapidly released, is being developed intensively. Energy absorption over times much less then mechanical sluggishness of material results in occurrence of thermoelastic stresses in it.

Composite materials are one of the promising and interesting materials from the practical and physical standpoint. Separate area of composites is carbon-carbon composites, i.e. materials obtained from carbon fibers with filling of matrix with carbon. Sufficiently complicated pattern of stresses can be realized in carbon-carbonic composites during pulse heating by radiation. This experimental work was performed with the aim to study possible behavior of such materials during pulse liberation of radiation energy in them.

Oscillogram of stress pulse in 4KMS composite specimen 10 mm thick. Marks – 1 μs.

Anisotropic material – carbon-carbonic composite 4KMS and two-dimensional material – pyrolytic carbon (pyrocarbon) UPV-1 were investigated. Grǜneisen parameter was selected as parameter, characterizing material behavior. Work was performed with the use of electron accelerators: for composite 4KMS – with IGUR-3 accelerator [1] (average electron energy is about 2 MeV, half-height pulse duration is about 5∙10-8 s );  for pyrocarbon – with the use of less powerful installation with maximal electron energy of about 1 MeV, average energy of 0,3…0,5 MeV, and half-height pulse duration is about ~1,3∙10-7 s. Electron flux was incident on front side of specimen, to back side of which piezoelectric transducer is glued with interposition of acoustic delay with small value of attenuation. There were recorded amplitude of thermoelastic stresses by means of piezoelectric transducer and value of energy flux, incident on specimen surface. Oscillogram of stress pulse, obtained during one of experiments, is given in the figure. It is seen that tensile wave (negative pulse) arrives at transducer first and not compression one, as it is observed in isotropical material.

| The experimental results for composite 4KMS are given in Table 1. #### Table 1 |  |  |  |  |
| --- | --- | --- | --- | --- |
| Electron energy fluence, J/cm2 | 42 | 49 | 40 | 53 |
| Maximal heating-up of 4KMS, K | 65 | 76 | 63 | 82 |
| Specimen thickness, mm | 10 | 10 | 15 | 15 |
| Grǜneisen parameter (G) | - 0,012 | - 0,015 | - 0,006 | - 0,005 |

It follows from Table 1 data that in the region of temperature of about 340 K Grǜneisen parameter for 4KMS has negative sign. Moreover value of this parameter is very small when compared to the other materials.

| In order to measure Grǜneisen parameter of pyrocarbon there were manufactured two specimens 10 mm thick with different orientation of planes with respect to direction of carbon deposition: perpendicularly and parallel to deposition plane, in direction “a” and “c” (“a” – along plane of carbon deposition, “c” – perpendicularly to it) [2]. Measured values of Grǜneisen parameter and sound speed for pyrocarbon UPV-1 are given in Table 2 as well as similar data for two foreign pyrolytic graphites PG3 and CAPG (that differ in manufacturing method) at temperature of 300 K [3, 4] for comparison. Table 2 Experimental values of Grǜneisen parameter and sound speed for pyrolitic graphites [2-4] |  |  |  |  |
| --- | --- | --- | --- | --- |
| Material | Direction |  |  |  |
|  | “c” |  | “a” |  |
|  | G | c, cm/s | G | c, cm/s |
| UPV-1 | 0.26 ± 0.04 | 0.36 ± 0.04 | 0.17 ± 0.03 | 0.53 ± 0.05 |
| PG3 | 0.3 | 0.36 | 0.2 | 0.61 |
| CAPG | 0.48 ± 0.03 | 0.38 ± 0.05 | - 0.99 ± 0.15 | 2.2 ± 0.1 |

It follows from the obtained results that parameters of thermoelastic stresses, occurring in anisotropic materials during pulse heating of them by radiation, differ substantially from behavior of isotropic homogeneous materials. Depending on orientation of specimen structure relative to radiation incidence direction both magnitude of stresses and their sign can vary. Hence, even at large value of energy release, value of occurring stresses can be sufficiently small and even close to zero..

# References

- Diyankov V. S., Kovalev V. P., Kormilitsyn A. I. et al . FMM 81, Issue № 2, 119 (1996).

- Stepovik A. P. PMTF No. 4. 150 (1992)

- Benson D. A., Gauster W. B. Phil. Magazine 31, № 5, 1209 (1975)

- Gauster W. B. Phil. Magazine 25, № 3, 687 (1972)

Measurement Procedure of Gamma-Radiation Dose

on the Basis of Capacitor Sensor

V. L. Stryakhnin, V. T. Gromov

FSUE RFNC – All-Russia Research Institute of Technical Physics, Snezhinsk, Russia (dep5@vniitf.ru)

The type K-52 Capacitor with low sensitivity to neutrons is used as an actuating medium of the capacitor gamma-radiation sensor. This makes possible measuring the dose using gamma- and neutron-radiation installations. A dose is measured remotely in the automatic mode with concurrent calibration of the measurement path. The uncertainty in the dose measurement does not exceed ±20.

The technique includes two main devices: the capacitor gamma-radiation dose sensor (CDS) and the “INDIRA” control-process device.

The actuating medium of the capacitor sensor is a tantalum electrolytic capacitor К52-11-16V-100 μF. The capacitor consists of an anode sintered from tantalum grains, liquid electrolyte and a body. A dielectric layer of the Та2О5 oxide being on the surface of tantalum grains represents an element sensitive to gamma-radiation. At the action of gamma-neutron radiation, due to high atomic weight of the oxide, the associated neutron radiation is weakly absorbed in the oxide and practically does not increase the RIC of the capacitor dielectric. Consequently, the capacitor sensor  preliminary charged up to the voltage Uo is discharged mainly due to the action of gamma-radiation. A gamma-radiation dose relates to a voltage drop on the capacitor sensor by an exponential dependence. Technical characteristics of the capacitor sensor are presented in the table.

| ###### Table Technical characteristics of the capacitor dose sensor (CDS) |  |
| --- | --- |
| Range of measured doses | D = 103÷5  105 Р |
| Contribution of neutrons to sensor discharge at irradiation in experimental channels and in windows of biological shielding of reactors IGRIK, YUAGUAR (average neutron energy ~1 MeV) | KnKγ⋅ФnD≤ 0.11 (≤ 11 %) |
| Allowable preliminary irradiation by neutron fluence and dose | D∑ ≥ 2  107Р Фn ≥ 2 1016n/cm2 |
| Sensitivity to gamma-radiation with energy ~1 MeV | Kγ= 5.5 10-6 1/Р |
| Sensitivity to neutrons of the reactors IGRIK, YUAGUAR | Кn = 7  10-16 cm2 /n |
| Voltage on the sensor prior to irradiation | U0 = 16V |
| Temperature range | Т = (+20±5) 0С |
| Dimensions Mass | Dia. 16×50 mm 20 g |

A copyright to the gamma-radiation dose sensor designed by us is protected by the inventor’s certificate and patent of Russia.

The “INDIRA” control-process device is intended for remote control of the capacitor sensor and for matching the sensor with standard voltage meter. The “INDIRA” device (design documentation No R56-L2191) contains a voltage follower with 200 МOhm input resistance, a stabilized constant-voltage source U0 = 16V to charge the sensor and an automation system to control operation of the sensor and to calibrate the measurement path as a dose is measured. The fractional uncertainty in the dose measurement does not exceed ±20% at the confidence probability of 0.95, that corresponds to GOST requirements. The dose accumulation at generation of two radiation pulses in one start-up of the IGRIK reactor is shown in the figure.

Fig. Dose accumulation at

generation of two radiation

pulses at start-up of IGRIK

reactor

Branch Scientific and Technical Center of Atomic-scale Research at ITEP.

Work Development

A. L. Suvorov, V. N. Dikarev, A. G. Zaluzhniy, M. A. Kozodaev

SSC RF Institute for Theoretical and experimental Physics

B. Cheremushkinskaya Str., 25, 117218 Moscow, Russia (alex.suvorov@itep.ru)

As it was reported earlier, the Branch Scientific and Technical Center (BSTC) has been established in SSC RF ITEP recently. The main object of the research in the Center is to receive detailed information about radiation effects on at atomic scale (first of all, structural defects, their formation and behavior, defect structure evolution) in materials.

The main lines of investigations are as follows:

- atomic-scale research of radiation defects formation and behavior in reactor structural materials – metals, alloys, steels;

- atomic-probe investigations of radiation effects in multi-component current-conducting structural materials;

- investigations of interaction between strong flows of irradiation and material surface;

- investigations of radiation damage in silicic detectors, development of beam technologies for making “ silicon on isolator” structures.

Besides, other “by- lines” of investigations are being developed:

- interaction between gases and materials of nuclear and thermonuclear plants;

- nanostructures formation and investigation of their properties;

- investigation of strong electrophysical effects on current-conducting materials;

- characterization and investigation of processes dynamic (desorption and field evaporation, field electron emission, surface migration) in strong electric fields;

- working out and production of physical devices, including ones for modern market of scientific and technical apparatus.

We list here the main lines of investigations conducted at BSTC pointing out their objectives in more detail.

- Field-ion microscopic investigations of radiation effects in structural reactor materials accenting fissionable materials, fist of all uranium and its alloys, and then plutonium. The aim is to clear up and analyze physics of the process of degradation properties for the mentioned materials, and to renew overhaul-period.

- Development of researches on optical tomographic atom probe; analyses of components distribution and redistribution in different materials (structural reactor steels, some fissionable and semiconductive materials) as a result of radiation, thermal, mechanical and corrosive effects.

- Development of investigations of surface and bulk effects in structural reactor materials, including fissionable materials first uranium and then plutonium, by means of scanning tunnel and atom-force microscopy both in open air and, first of all, in vacuum and using specially designed devices.

- Studying  of mechanism of energy transfer from fast multicharged heavy ions to atomic target depend upon ions charge; studying results of interaction between strong flows of laser plasma (the intensity of ions flow in plasma is 1022-1023 ion/cm2s) and condensed matter; modelling the conditions, met by an aircraft at approaching the planets of the solar system, with the help of laser plasma; applying “indelible” coatings onto different samples.

- Hydrogen penetration through materials (for example candidate materials for first wall of TNR), influence of boundary condition, irradiation regimes (ions energy, irradiation dose, separate and combined irradiation by several ions) on this process, surface and material structure state (grains size, dislocation density and others).

- Hydrogen retention in materials during heating. Effect of irradiation type (neutrons, plasma, ions bombardment) and structure of studied materials on hydrogen isotopes retention during heating have been investigated. It is very relevant because of safe TNR exploitation and possible waste of expensive fuel (tritium).

- Obtaining original data about radiation degradation of silicic detectors, elaborated to be used in conditions of high fluence (up to 1016 particles/cm2) and formulating the recommendations on their production. The object is to elaborate a new generation of radiation-stable detectors, which are in a big demand for strong electro-physical plant production.

Nowadays BSTC ITEP activity includes:

- efforts (and means) integration to conduct joint investigations on BSTC ITEP equipment according to the lines mentioned above;

- custom researches fulfilled by BSTC ITEP according to the mentioned lines and financed by the customer;

- production, delivery and setting up the original equipment (atomic-scale microscopes) both for joint researches (partial payment) and for independent researches (full payment);

- work teaching (probation) on devices (investigations in atom scale) for research officers and for students (contractual stipulations).

Application of Capillary X-Ray Facilities in Precision Measurements of Parameters of Multilayer Structures

A. N. Tarasenkov1, A. G. Turyansky2, N. N. Gerasimenko2,3, S. A. Aprelov2,3

1Technology Centre of MIEE, Moscow, Russia (A.Tarasenkov@tcen.ru)

2Institute of X-Ray Optics, Moscow, Russia

3Moscow Institute of Electronic Engineering (Technical University)

Features of 13C Isotope-Based Graphite-Like Material After

Irradiation with Electron Beam

I. L. Svyatov, I. V. Podgornova, A. E. Shestakov, S. M. Novgorodtsev, V. V. Plokhoi
 FSUE RFNC – All-Russia Research Institute of Technical Physics, Snezhinsk, Russia (dep5@vniitf.ru)

Properties of 13C Isotope-Based Material of Neutron Targets Before and After Exposure to Irradiation with High-Power Electron Beam

E. I. Zhmurikov2 , A. I. Romanenko 1, K. V. Gubin2, P. V. Logachev2, V. B. Fenelonov3,

S. V. Tsybulya3, E. V. Burgina3, L. Tecchio4

1Institute of Inorganic Chemistry, SB RAS, Novosibirsk, Russia

2Institute of Nuclear Physics, SB RAS, Novosibirsk, Russia (E.I.Zhmurikov@inp.nsk.su)

3Institute of Catalysis SB RAS, Novosibirsk, Russia

4Laboratori Nazionali  di Legnaro -  Istituto Nazionali di Fisica Nucleare,

Legnaro, Italy

Pulse-Periodic Accelerator of Electrons (PPAE) with Inductive Store and Semiconductor Opening Switch

V. B. Bratchikov, V. M. Zverev, A. I. Kormilitsyn, V. V. Pereshitov, S. N. Rukin*, A. V. Ponomarev*

FSUE RFNC – All-Russia Research Institute of Technical Physics, Snezhinsk, Russia (dep5@vniitf.ru)

* Institute of Electrophysics, UB RAS, Ekaterinburg, Russia

Pulse-periodic accelerator of electrons with completely solid system of energy commutation and frequency of pulse sequence from 1 to 100 Hz was developed. The section of evacuated electron beam is 5010 см2 (in anode plane). Maximum amplitude of voltage pulse on accelerating tube is Umax = 750 kV, density and duration of pulse of current of evacuated beam are jē = 1А/cm2 (at S = 500 cm2) and ē = 57 ns, respectively. Duration of bremsstrahlung pulse  = 25 ns ,dose per pulse D  3 P (on anode).

References

- S. N. Rukin. Generation of powerful nanosecond pulses on the basis of semiconductor opening switches.//Thesis for a degree of doctor of technical sciences. Ekaterinburg. 1998.

- Mesyats G. A. Physics of electron emission from metal-dielectric cathodes // In. Proc: X Int. Conf. High Power Particle Beams. San-Diego, CA, 1994. p.р. 207-210.