- Effect of Irradiation on Changes in Microstructure and Properties of Metals

and Alloys

The Effect of Fast Neutron Irradiation on Structural and Phase Changes in Phosphorus-Doped Fe-36%Ni Alloys

V. L. Arbuzov, B. N. Goschitskii, S. E. Danilov, A. V. Karkin, V. D. Parkhomenko

Institute of Metal Physics, UB RAS, Ekaterinburg, Russia (arbuzov@imp.uran.ru)

Austenitic Fe-Ni alloys are good model materials for the study of regular features and mechanisms of the radiation damage of constructional stainless steels. Alloying with phosphorus has a strong effect on the properties of these steels: on the one hand, radiation swelling is reduced, but, on the other hand, phosphorus is a harmful embrittling impurity.

This study is concerned with the effect of fast-neutron irradiation on the formation and properties of vacancy clusters and structural-phase changes (decomposition) in Ni36 compounds and phosphorus-alloyed Ni36 compounds depending on the irradiation dose.

The subjects of study were Fe-36.5% Ni (Ni36) and Fe-36.5% Ni-0.1%P (Ni36P) quenched from 1373 K. The compounds were exposed to neutrons (E > 0.1 MeV) in an IVV-2 reactor at a temperature of 340 K and a fluence from  31017 cm2 to 51019 cm2.

It was shown that neutron irradiation of the Ni36 and Ni36P compounds caused formation of vacancy clusters, which dissociated at temperatures above 450 K. In this case, phosphorus alloying led to the increase in the concentration of these clusters. Such vacancy clusters represented the efficient sinks of point defects.

When the neutron fluence increased, the concentration of vacancy clusters became larger and, correspondingly, the diffusion path of migrating vacancies was reduced. In the limiting case, this might inhibit radiation-induced processes. The effect of phosphorus on radiation-induced processes was analyzed and the cascade (neutron) and noncascade (electron) radiation compared.

This study was supported financially by RFBR (Project No. 04-02-16053).

Effects of B+ and Ar+ Ion Implantation on Composition of Surface Layers of Ni-Cu Foil

V. Ya. Bayankin*, F. Z. Gilmutdinov*, A. A. Kolotov*, S. N. Korshunov**

*Physical-Technical Institute, UB RAS, Izhevsk, Russia (less@fti.udm.ru)

**Russian Scientific Centre “Kurchatovsky Institute” Moscow, Russia

The effect of boron and argon ion implantation on the variation of the composition of the Ni-Cu foil surface layers was studied on both the irradiated (the face) and the non-irradiated (reverse) sides at varying ion current density.

A rolled foil 40at.%Ni-60at.%Cu, 40-μm thick, was used for the investigation. Irradiation was performed using ILU-2 device with parameters: E = 40 keV, D = 1×1017 ion/cm2, j = (10 – 50) μA/cm2. The X-ray electron analysis of the composition was conducted with the use of an ES-2401 spectrometer, together with ion etching of sample surfaces; the estimated etching rate was 1.0 nm/min. The analysis was performed in the depth range of 20 to 25 nm. In addition, the microhardness on the face and reverse sides of the samples was measured by a microhardness tester PMT-3 (indentation load 10 g); the interatomic distance in the samples was determined using the X-ray  structural analysis before and prior irradiation.

Both B+ and Ar+ radiation was found to change the composition of the surface layers on both sides of the foil depending on the current density. At B+ ion implantation, a certain threshold value of the current density is observed; when this value is exceeded, the microhardness value and boron content in the surface layer on the reverse of the foil change abruptly. Unlike the case of the initial samples where the monotonous dependence of the Ni/Cu content ratio is observed, in the irradiated samples, whatever type of ions are present, the non-monotonous dependence is exhibited, which is characterized by minima and maxima of the Ni/Cu ratio. This dependence is non-monotonous due to the ion current density as well. The interatomic distance in the irradiated samples is shown to differ from that in the initial samples. It remains the same within the error of measurements for all current densities as opposed to the case of the Ar+ ion implantation at 50 μA/cm2, which indicates that the initial atomic structure remains after irradiation (except the last variant) regardless of the type of ions and the current density.

It may be suggested that the paths of anomalous migration of boron atoms to the reverse of the foil could be linear and planar defects. Alloy samples are rolled, i.e. their structures are initially strongly non-equilibrium, strained and having large density of dislocations. It is possible that ion radiation can cause a certain relaxation in the initially non-equilibrium structure (due to the generation of elastic waves, for instance). Ion implantation generates elastic shock waves and, at their front, the spread of boron atoms throughout the bulk occurs; simultaneously the transformation of the defect structure and apparently partial relaxation of the residual stresses in the sample bulks take place. In this case, the boron atoms, as a surfactant, enrich the surface.

The formation of the non-monotonous dependence of the Ni/Cu ratio in the surface layers can relate to the structural-phase transformations induced by ion bombardment causing local gradients of mechanical stresses.

The work is sponsored by RFBR (project №02-02-16670)

Change of Martensitic Transformation Kinetics in TiNi and Cu-Al-Ni Alloys in the Process of Neutron Irradiation in Low-Temperature Helium Loop

S. P. Belyaev, R. F. Konopleva, I. V. Nazarkin, V. A. Chekanov
Petersburg Nuclear Physics Institute, Russian Academy of Sciences, Gatchina, Russia (spb@pnpi.spb.ru)

The investigations of martensitic transformations in equiatomic TiNi alloy and monocrystal of the Cu-13,4%Al-5%Ni alloy were performed in the process of irradiation in the low temperature helium loop of the WWR-M nuclear reactor at temperatures between 120-350 К. The used resistivity measurement method was sensitive both with respect to the crystal lattice radiation defects, and to martensitic phase transitions in crystals.

It was established that the critical temperatures of martensitic transitions in TiNi alloys decrease with the fluence growth according to the following law: Tph=d[exp(-/Ф0)-1] where Tph is temperature increment corresponding to the structural transformation; Ф is the fluence; d and Ф0  are constants. These regularities can be detected under irradiation both in the martensitic and in the austenitic states. A short-term temperature rise for the samples irradiated to fluence of 71018 cm-2, up to temperature of 450 К, results in recovery of the resistivity and the temperature kinetics of martensitic transformations. The activation energy of return of properties was determined. It was assumed that the change of transformation kinetics under irradiation and subsequent annealing were connected with a change in the degree of long-range order S of a solid solution undergoing ordering.

In the Cu-Al-Ni alloy, after irradiation in the two-phase or martensitic state, there is observed a 25-30 К rise in the temperature of reverse “martensiteaustenite” transformation. Such rise is observed only once in the course of initial heating just after the isothermal irradiation, being proportional to the integral neutron dose. At subsequent thermal cycles, the martensite transition occurs at lower temperatures, and the hysteresis temperature dependence of the resistivity shifts towards lower temperatures with the growth of fluence. So the radiation effect leads to a stable decrease of critical transformation temperature and to a single (unstable)  growth of the reverse transformation temperatures. The first of these effects is caused by the disordering of the crystal lattice at the reactor irradiation, similar to the situation, which is also observed in TiNi-based alloys. The single effect is perhaps connected with the violation of coherence of the interphase and interdomain boundaries in the course of irradiation. The boundary mobility, in this case, decreases and an additional thermodynamic stimulus is required for the transformation development. Special experiments indirectly prove this assumption.

Decrease of Inclination to Local Corrosion of Oxidized Zr-1%Nb Alloy by Irradiation with High-Intensity Beams of Nitrogen Ions

T. A. Belykh*, N. V. Gavrilov*, D. R. Emlin*, A. M. Murzakaev*,

L. P. Sinelnikov**, A. N. Timokhin**, A. G. Trifanov**

* Institute of Electrophysics, UB RAS, Ekaterinburg, Russia (erd@iep.uran.ru)

** Institute of Reactor Materials, Zarechny, Russia

The Zr-Nb alloys, widely used in reactor building, in addition to the slow continuous corrosion show inclination to an increased rate of local corrosion [1] which restricts the reliable service life of products from the given alloys. The causes of origin of local corrosion can be: macro- and microdefects of structure of a passivating oxide surface layer as well as local inclusions of the intermetallide phases that bring about  developing of electrocorrosion, which is faster than  the chemical corrosion. Earlier it was shown by us [2] that irradiation of the oxide layer-alloy heterostructures with high-intensity beams of the nitrogen ions results in deceleration of the continuous corrosion. This paper studies the effect of irradiation with the pulsewise periodic beams of the nitrogen ions (pulse duration 1 ms, frequency 25 Hz, beam current density 3 mA/cm2 and energy of ions 30 keV) on inclination of the same heterostructures to local corrosion. Changes of the surface morphology were checked by means of electronic microscopy, the corrosion tests were carried out in a solid electrolyte (powder Li+Li2O) within 50 hours at 520 °С. The optimal conditions of the ion beam treatment were determined: 350 < Timpl < 450 °C, radiation dose 1017 – 1018 cm–2. Under these conditions the fraction of local corrosive surface decreases from 20-30 % (reference samples) down to 0.1 - 0.2 % (at optimal implantation conditions). The electronic microscopy analysis showed the morphology change of the surface layer: initially loose films become denser and reveal a texture in the limits of initial crystallites, the defects from machining are smoothed.

The treatment with high-intensity beams of the nitrogen ions improves the structure of the oxide coatings and homogenizes their composition, thus raising the passivating properties of the initial surface layer created by the thermal oxidizing.

References

- Perekhozhev V. I., Sinelnikov L. P., Timokhin A. N. et al., Metallovedenie i termoobrabotka metallov, 2003, No. 10, p. 26-31 (in Russian)

- Belykh T. A., Gavrilov N. V., Emlin D. R. et al., Fizika i khimia obrabotki materialov, 2003, No. 6, p. 14-20 (in Russian).

Structure and Electron Transport in Atomic-Disordered Compound MnSi

I. F. Berger1, А. Е. Karkin2, V. I. Voronin2, Yu.. N. Akshentsev2, B. N. Goshchitskii2

1Institute of Chemistry of Solids, UB RAS, 91 Pervomaiskaya St., Ekaterinburg 620219, Russia (berger@uraltc.ru)

2Institute of Metal Physics, UB RAS, 18 S. Kovalevskoi St., Ekaterinburg 620219, Russia

| The compound MnSi featuring cubic structure B 20 (spatial group P213) without an inversion center develops, at high-pressure suppression of magnetic ordering, a non-Fermi liquid state favorable for appearance of superconductivity with spin-triplet pairing [2]. In this work we studied the effect of neutron irradiation on the structural state and the electron transport properties of poly- and monocrystalline samples of MnSi compound presenting an ideal object for investigating the effects of disordering by the method of neutron diffraction analysis, because of the scattering amplitudes of Mn and Si being different in sign and close in value # Table |  |  |
| --- | --- | --- |
| Fluence | 0 | 5·1019 cm–2 |
| a, Å | 4.5606(1) | 4.5738(1) |
| Mn χ | 0.1387(8) | 0.1355(8) |
| Si χ | 0.8461(6) | 0.8479(6) |
| Biso | 0.10(2) | 0.24(2) |

The structural data of the initial MnSi sample and the sample irradiated with fast neutrons are given in the Table. It may be seen that after irradiation the lattice parameter increases (»0.3 %), and the Debye-Waller factor testifying to emergence of non-correlated static atoms displacement from the lattice sites grows approximately two times. Such effects point to atoms disordering in the lattice.

The resistivity r and Hall constant RH temperature dependences shown in the Figure point to a complex (multizone) nature of electron states in this compound. According to ac susceptibility c(T) measurements, a drop in the temperature of magnetic ordering takes place.

The work was supported by the Basic Research Program “Neutron diffraction studies of materials structure and fundametal properties of matter” of the Department of Physical Sciences of RAS (UB RAS Project No. 14 / Contract No. 26/04), the Program ”Neutron diffraction studies of condensed matter” (State Contract No. 40.012.1.1.1150), the Program of the Russian Foundation for Basic Research No. 04-02-1653 and the Russian President’s Grant for support to the leading scientific schools in Russia No. NSh-639.2003.2.

###### References

- C. Pfleiderer et al., Phys. Rev. B 55, 8330 (1997).

- E. Bauer et al., Phys. Rev. Lett. 92, 027003 (2004).

Dependence of Titanium Alloy Mechanical Properties and Surface Composition on Ion Current Density

P. V. Bykov, F. Z. Gilmutdinov, S .G. Bystrov, V. Ya. Bayankin

Physical-Technical Institute, UB RAS, Izhevsk, Russia (less@fti.udm.ru)

Many machine parts and entire structural units permanently experience alternating loads, and despite the fact that they are much smaller than the material yield strength, under their action, cracks develop starting from the surface and finally leading to the failure of a part. As far as at bending the amplitude of the occurring stresses is maximal in the surface layer of the material, the change of the composition and microstructure of the material surface and near-surface layers caused by the ion implantation can influence the dynamics of the crack formation and development. Thus, the ion implantation can affect the fatigue strength of materials. However, the influence of the radiation parameters (dose, current density and ion energy) and of the type of implanted ions on the increase of the fatigue strength of metals and alloys has not been completely understood yet.

We have selected silicon and argon for implantation due to their relatively large atomic mass that enables the formation of the large cascade area during the interaction with the matrix. The silicon and argon implantation also makes it possible to form Ti-Si compounds with better mechanical properties.

The goal of the given work is the comparative study of the influence of the Si+ and Ar+ ion current density on the mechanical properties and the composition of the titanium alloy surface.

The samples (Ti – 3.4 Al –Mn) were irradiated on the ILU type ion-beam device (Russian Scientific Center “Kurchatovsky Institute”, Moscow) in vacuum not worse than 10-3 Pa. The parameters of silicon and argon ion radiation are: E = 40 keV, D = 1017 ion/cm2, the range of ion current densities from 10 to 50 μA/cm2.

The microhardness of the irradiated samples increases by 20 – 60% in comparison with the initial value. The maximal increase of microhardness (the load of indentation is 20 g) is reached during radiation with the ion current density 10 μA/cm2 for both argon and silicon. Fatigue testing shows that in comparison with the non-irradiated samples, the samples irradiated with Si+ and Ar+ ions have lasted for a larger number of cycles before failure.

The modified layer thickness in the silicon ion irradiated samples exceeds the projected range of silicon ions in titanium for the entire range of the ion current densities.

The work is sponsored by RFBR (grant № 02-02-16670).

Radiation Effects in Manganites with Perovskite Structure

Yu. G. Chukalkin, A. Ye. Teplykh, B. N. Goshchitskii
Institute of Metal Physics, UB RAS, Ekaterinburg 620219, Russia (chukalkin@uraltc.ru)

Using the methods of neutron diffraction analysis, X-ray and magnetic measurements, polycrystalline samples of the system La1-xBaxMnO3 (0  x  0.2) were studied before and after exposure to different fluences (0 to 3  1020 cm–2) of fast neutrons (En  1 MeV). It was established that the so-called anti-site defects, i.e. mutual disordering of the “lanthanum” and “manganese” sublattices, play the central role. Radiation-induced disordering of cations with significantly differing ionic radii causes considerable non-correlated displacements of adjacent ions. At high anti-site defect concentrations this process leads to radiation-induced amorphization; at relatively low concentrations (approx. 5 to 10 %) the crystalline structure is maintained, but with the degree of symmetry higher than the original. For example, under irradiation with relatively low fluences, the following structural transformations were observed: rhombohedral  cubic (x = 0.175, 0.2), phase Оorthorhombic  phase О*orthorhombic (x = 0).

It is known [1] that the magnetic state of mixed-valence manganites is a result of competitive ferro- and anti-ferromagnetic interactions: indirect exchange Mn3+-O-Mn3+ (which may be both negative and positive depending on which orbitals of cations and anions overlap) and kinetic ferromagnetic Mn4+-O-Mn3+ exchange due to electron (hole) delocalization. Anti-site defects formation is the cause of an incidental local potential which exerts significant influence on charge carrier properties and, in the long run, leads to partial or complete localization of the carriers. On the other hand, a rise in the degree of symmetry of the irradiated crystals modifies the scheme of indirect exchange. For example, the JT mode responsible for formation of A-type ferromagnetism in the dielectric  LaMnO3  is suppressed. In the aggregate, these factors lead to transformations of the magnetically ordered states observed under irradiation: anti-ferromagnetic  ferro- (ferri-) magnetic (x = 0), ferromagnetic  spin glass in doped manganites.

Work was carried out with partial sponsorship of the Ministry for Science and Technology of the Russian Federation, Contract No. 40.012.1.1.1150; Grant of the President of Russia for support to the leading scientific schools in Russia No. NSh-639.2003.2; RFBR Project No. 04-02-16053-a.

References

- Coey J. .D., Viret M., von Molnar S. Adv. Phys.. V. 48, 167 (1999)

Effects of Ion Radiation on Dynamics of Microcrack Development in Nickel and Aluminum under Tension

A. Yu. Drozdov, M. A. Baranov, V. Ya. Bayankin

##### Physical-Technical Institute of the Ural Branch of the Russian Academy of Sciences,

##### Izhevsk, Russia (less@fti.udm.ru)

The microcrack development under radiation and uniaxial tension was analyzed by the molecular dynamics method on nickel and aluminum monocrystals. The goal of the work was the study of the dynamics of the crack propagation under tension prior to and after ion radiation with inert gas ions and the clarification of the role of the specific features of the interatomic interaction potentials.

The computer-aided experiment was conducted with the use of a program based on the molecular dynamics method. The set of many-particles Newton equations was solved with the help of numeric methods. Energy removal from the system was carried out by the introduction of viscous forces. The interaction between atoms was described with the use of the potentials of pairwise interaction calculated with the help of the model pseudo-potential of Heine – Abarenkov – Animalu and Show screening function. The initial configuration of the crystallite atoms is a three-dimensional film of 20 atomic layers in thickness. The choice of the boundary conditions and the microcrack model are described in details in work [1].

In the crack mouth area, the argon ion irradiation with the energy of 20 keV was modeled. For the period of 8000 – 10000 , the thermodynamic parameters of the system, i.e. temperature T and energy U, stabilized near a certain fixed value. After reaching by the crystallite of a stable state during the times under study, uniaxial tension was applied along the direction [010]. The relative deformation was   = 5%, 10%, 15% and 20%.

The character of the microcrack propagation in the irradiated samples was found to be viscous for both nickel and aluminum. The initial microcrack was located in the (010) plane. In nickel, at 15 % tension the crack started to propagate in the (111) plane, which is the plane of easy slip for FCC crystals. The analysis of the radial distribution function of atoms shows that after ion irradiation, the crystallite retains the FCC lattice and phase transitions are not observed. In aluminum, the crack is healed completely, and in nickel, it is partially healed. This leads to an increase of the crystallite strength observed for the irradiated samples.

The comparison was carried out for the crack propagation in metals with different lattice types (BCC, FCC and HCP) under uniaxial tension at the atomic level. The comparison shows that the lattice type and the specific features of the interatomic interaction potentials influence the microcrack evolution at the uniaxial tension.

The work is sponsored by RFFI (grant № 02-02-16670).

References

- M. A. Baranov, A. Yu. Drozdov, V. G. Chudinov, V. Ya. Bayankin, ZhTF. 2000. V. 70, N. 4, p. 46-51.

Changing of Physical and Chemical States of Tin Atoms in Zirconium Alloys Oxide Films during Neutron Irradiation

V. P. Filippov1, A. B. Bateev1, R. N. Pugachev1, Yu. A. Shikanova1, A. V. Nikulina2,

V. F. Konkov2, G. P. Kobylyansky3

1Moscow Engineering Physics Institute (State University), Moscow, Russia (filippov@d108.mephi.ru)

2All-Russia Acad. A. A. Bochvar Research Institute of  Inorganic Materials, Moscow, Russia

3Research Institute of Atomic Reactors, Dimitrovgrad, Russia

The oxide films of zirconium alloys (Zr-0.76%Fe-1.6%Sn-0.95%Nb and Zr-0.76%Fe-1.6%Sn.) oxided in autoclave and in reactor irradiation conditions were investigated by Mössbauer spectroscopy method.

The corrosion tests of flat samples placed in tight ampoules from the stainless steel, filled by distilled water, were carried out in a reactor during 37, 80 and 112 effective days(fluency 3·1020 n/cm2, E > 0,5 MeV). Similar samples were tested in laboratory conditions during 40, 80 and 120 day in similar ampoules and identical thermodynamic conditions (350 °C, 16.8 MPa).

The corrosion kinetic curves for corrosion in an autoclave are differed from these obtained at reactor irradiation. These differences are connected with greater corrosion rate in reactor condition. During the same corrosion time the thickness of oxide film obtained in reactor condition is greater than in the  autoclave tests. The thickness of oxide films depending on structure of an alloy differ 2-3 times.

The Mössbauer spectra analyses  have shown, that  tin is present in oxide films as SnO and SnO2, as a solid solution of Sn4+ ions in  ZrO2, and also as a metal phase  β -Sn. The probability of β -Sn formation in oxide films is shown in paper[1].

Concentrations of tin atoms in all chemical states and phases are determined. Comparison of corrosion kinetic curves and results of Mössbauer researches allow to ascertain, that introduction of niobium  influences on corrosion behaviour of alloys more in process of reactor irradiation and than in outside of reactor tests. It is revealed, that high corrosion resistance of some alloy samples is connected with the presence of plastic  phases β -Sn.

# References

- Pêcheur D. Filippov V. P. Bateev A. B. Ivanov Ju. Ju., Mössbauer Investigations of the Chemical States of Tin and Iron Atoms in Zirconium Alloy Oxide Film Zirconium in the Nuclear Industry: Thirteenth International Symposium. ASTM STP 1423, Gerry D. Moan ad Peter Ruling, Eds., ASTM International, West Conshohocken, PA 2002, pp. 135-153.

## Flux Effect on Void Swelling of Austenitic and Ferritic/Martensitic Steels:

## A Review of Recent Data and Insights

F. A. Garner1, N. I. Budylkin2, Yu. V. Konobeev3, S. I. Porollo3, V. S. Neustroev4, V. K. Shamardin4 1Pacific Northwest National Laboratory, USA (frank.garner@pnl.gov)

2A. A. Bochvar Institute of Non-organic Materials, Russia

3Institute of Physics and Power Engineering, Russia

4Research Institute of Atomic Reactors, Russia

Void swelling of PWR austenitic internals has recently been identified as a materials issue that might impact license extension. Data are now becoming available from PWRs that indicate swelling is in progress but still at relatively low levels. Extrapolation of these data to higher, end-of-life exposures requires a better understanding of the parametric sensitivity of swelling. Swelling equations being developed for both austenitic and ferritic-martensitic steels for use in various Generation IV and ADS reactor concepts also require such understanding.

Earlier published studies conducted in Japan, USA and Russia have shown that the atomic displacement rate is unexpectedly one of the most important variables. This paper presents data derived from a number of irradiations conducted on both Russian and Western steels irradiated in a variety of reactors. All data sets support the conclusion that lower dpa rates lead to greater swelling of austenitic and ferritic-martensitic steels irradiated at all reactor-relevant temperatures. Several published data sets are presented that were previously misinterpreted because the strong effect of dpa rate was not recognized at the time of publication.

Effect of Gamma Irradiation Causing Uranium Nuclei Photofission on Critical Current of HTSC Tape (Bi2223+0.8%U-238)/Ag

I. N. Goncharov*, O. D. Maslov*, I. F. Voloshin**, A. V. Kalinov**, L. M. Fisher**

* Joint Institute for Nuclear Research, Dubna, 141980, Russia (ingonch@sunhe.jinr.ru)

**All-Russian Electrotechnical Institute, Moscow, Russia

Large-scale production of long current-carrying tapes of high temperature superconductor (HTSC) has been mastered so far only for a system on the basis of Bi2223 in a silver matrix. However, they are characterized by relatively high critical current anisotropy and rather low Jc values in the range of liquid nitrogen temperatures and magnetic fields above 0.5T. Jc can be increased by generating additional pinning centers along tracks of fast heavy ions, including fission fragments of uranium nuclei doped into HTSC. The published results relate to HTSC doped with U-235 after reactor irradiation by thermal neutrons. Application of this method for Bi2223/Ag tapes, however, is limited due to high radioactivity from isotope Ag110m with half-life period T1/2250 days and significant rise in the tape price due to use of very expensive uranium with high enrichment rate of U-235. Photofission of U-238 nuclei in the energy range of giant resonance (E ~ 1020 MeV) was proposed by one of the authors to eliminate the above mentioned disadvantages [1]. The present paper describes the results obtained at irradiation of a pilot batch of tape (Bi2223+0.8%U-238)/Ag samples by gamma quanta with the energy E  24 MeV at the microtron MT-25 (electron current 15 A). In particular, the following issues are considered: induced radioactivity level and its time decay; change of Jc values of the sample tape and reference tape containing no uranium with dose growth; a possibility to increase significantly uranium content in the samples (above the limiting value ~0.6 % at its uniform distribution in HTSC).

References

- Goncharov I. N., JINR Preprint E8-99-270 (1999); in Proceedings of EUCAS-99 (Sitges, Spain, 14-17 September, 1999). Inst. Phys. Conf. Ser. 167, p.559, 2000 IOP Publishing Ltd.

Ion-Plasma Effect on Changes in Structure and Texture of Shell Pipes Made from Zirconium-Based Alloys

M. M. Grekhov, Yu. A. Perlovich, M. G. Isaenkova, V. A. Fesenko, B. A. Kalin, V. L. Yakushin

Moscow Institute of Engineering Physics (State University), Moscow, Russia (masim@mail.ru)

Influence of Atomic Disordering on Electronic States of Heavy Fermion Systems

A. E. Karkin*, A. S. Krivoshchekov*, Yu. N. Akshentsev*, and B. N. Goshchitskii*

*Institute of Metal Physics UB RAS, 620219 Ekaterinburg, S. Kovalevskoi Str. 18

In heavy fermions (HF) systems the low temperature coherent state, formed by spin polarization clouds around f-atoms, leads to the squared dependence of resistivity (T) = 0 + AT2 with A coefficient, concerned with electron-electronic scattering of quasi-particles with large mass. To understand the role of atomic ordering in the formation of HF states, we have studied an influence of disordering induced by neutron irradiation on (T) and Hall coefficient RH(T) in CeT2X2 (T = Ni, Cu, Pd; X = Si, Ge) compounds. Irradiation leads to significant changes of both (T) and RH(T) at low T, while the high temperature changes are much smaller. Temperature dependencies of (T) and RH(T) in CeCu2Si2 compound (upper Figure) demonstrate the complex band structure with electron-like and hole-like charge carriers with qualitatively different T-dependencies of (T). In the initial sample (light points) the heavy carriers electronic contribution dominates in low-T region, while at high T the prevalence of light holes and electrons is observed.  In the irradiated sample (dark points) the contribution of HF channel disappears, so the logarithmic dependencies, corresponding to magnetic (Kondo-like) scattering, are revealed in (T) and RH(T).

Qualitatively similar behavior of transport is observed in CeNi2Ge2 (lower Figure, curve 1 – initial sample, 2 – irradiated, 3-6 – annealed at temperatures 100-400 ºC), however with another interrelation of the light and heavy partial contributions to electronic transport. Note that in CeCu2Si2 and CeNi2Ge2, displayed  non-Fermi-liquid (NFL) behavior, which leads to the appearances of linear  low-T dependencies of (T) and RH(T), there is no transition to Fermi liquid state under disordering, as well as in HF compounds CeCu2Ge2, CePd2Ge2 and CePd2Si2 the expected transition to NFL behavior is not observed. In all compounds under study the atomic disordering leads to suppression of electronic states revealing at low temperatures, which corresponds to the decrease of heavy carriers concentration.

Effects of Photon Flux on Ni-Cu Foil Properties

A. A. Kolotov, F. Z. Gilmutdinov, V. Ya. Bayankin

Physical-Technical Institute, UB RAS, Izhevsk, Russia  (less@fti.udm.ru)

Recently, the influence of various fields on the structure of materials is the subject of wide discussion in literature. In the given work, the changes of the metal foil on light irradiation are discussed.

Rolled foils 40%Ni – 60%Cu, 30 μm thick, are investigated. Samples were irradiated with halogen lamps of 100 and 200 W in the air at the fixed distance between the lamp and the sample, R = 70 mm. For increasing the heat removal, the sample under study was fixed on the massive metal plate. The microhardness was measured with the help of the device PMT-3 (the load of indentation was 20 g). The distribution of the components at depth of the surface layers prior to and after irradiation was investigated by the secondary-ion mass spectrometry with the use of the surface atomization with argon ions having the energy 4.5 keV and the current density 20 μA/cm2 (the estimated rate of atomization was 3 nm/min) and X-ray electron spectroscopy. The additional studies of the structure were carried out using X-ray structural analysis.

The experimental results show the change of the structure and the chemical composition of the irradiated foils. Irradiation with the halogen lamps of the above wattage results in the change of the microhardness values on both the irradiated side and the reverse of the samples. However, it should be noted that there are threshold values of the radiation doses. Radiation with the doses higher than the threshold values does not result in the stated changes. To clarify the influence of the structure on the manifestation of the “photon effect of long-range action”, the foils annealed at 850 C in a vacuum furnace for 30 min were investigated. As the microhardness measurements of the annealed samples show, the effect is not observed in this case. Light irradiation of the surface leads to the redistribution of the elements in the surface layers.

Thus, based on the experimental results one can suggest that on photon irradiation, the “effect of long-range action” is due to the initial non-equilibrium of the foil structure.

The work is sponsored by RFBR (grant № 02-02-16670).

Formation and Evolution of Radiation Clusters in FCC-Metals under Low-Temperature Neutron Irradiation to Lower Damage Doses

A. V. Kozlov, E. N. Shcherbakov, O. I. Asiptsov, L. A. Skryabin, I. A. Portnykh

FSUE “INM”, Zarechny, Sverdlovsk Oblast, Russia (sfti@uraltc.ru )

A set of FCC-metals, such as, pure Ni and Pt, EI-844 SA steel and ChS-68 20 % CW steel were examined. These materials were irradiated at  310 K to fast neutron fluence from 71021  21022 m–2 (E > 0.1 MeV). Results of precision measurements of change in samples dimensions under heating were obtained and electron microscopy examinations were performed for set of samples.

A quantitative model allowing to describe a process of formation and evolution of radiation clusters under low-temperature neutron irradiation was developed using statistical thermodynamics. Dependencies of both cluster concentration and mean number of vacancies contained in them on irradiation time for different damage rate were plotted in the framework of this model. Concentration of vacancies in the cluster was shown to reduce practically without change of it dimension under recombination of interstitials that diffusing into the cluster.

Equations of the model were used to calculate accumulation of vacancies in the EI-844 and ChS-68 steels under neutron irradiation as well of dimensional change of irradiated samples under annealing. Verification results of calculation dimensional change in samples of the steels mentioned above are in a good agreement with experimental one.

Study of Interrelation Between Сrystal Structure and Physical Properties of Heavy-Fermion Compound CeCu6 Using Radiation-Induced Disordering Method

A .S. Krivoshchekov*, A. Ye. Karkin *, I. F. Berger**, V. I. Voronin*, B. N  Goshchitskii*

*Institute of Metal Physics, Ekaterinburg, Russia (Nimravus@uraltc.ru)

** Institute Chemistry of Solids, UB RAS, Ekaterinburg, Russia

In the systems with heavy fermions (HF) with an ordered arrangement of the f-element atoms (Kondo lattice), Fermi-liquid (FL) state is formed at low temperatures T. Such a state corresponds to coherent motion of charge carriers of anomalously big mass. To learn the role the ordered arrangement of atoms in the Kondo lattice plays in formation of the FL state, a neutron diffraction study was carried out of the crystal structure and galvanomagnetic properties of compound CeCu6 with a big effective mass of electrons irradiated with fast neutrons.

According to neutron diffraction data, CeCu6 has a hexagonal structure described in the Pnma spatial group (curve 1 in the upper Figure). After irradiation with fast neutrons the structure type is preserved (curve 2), but the unit cell volume gets increased by 0.3 %; the Debye-Waller factor also grows in value by 45 %. The occupation numbers for Ce and Cu atoms remain unchanged to an accuracy of 0.01.

The galvanomagnetic properties undergo  more significant changes: atomic disordering, in particular, leads to practically complete suppression of the HF state. Within the scope of a multi-band model, this corresponds to a strong (by 2 orders of magnitude) decrease in the HF concentration, while changes in the light carriers band parameters remain relatively small. Temperature dependences of (T) and Hall constant RH(T) for CeCu6 shown in Fig. 2 show that only light carriers undergoing strong scattering (Condo effect) are present in the irradiated sample (curve 2). The initial state (curve) differs in the presence of an additional conductivity channel corresponding to HF. Thus, in the compounds of this class, the crystal order, and respectively, the Condo lattice order, play the key role in formation of the FL state.

The work was supported by the Program of Basic Research of the Department of Physical Sciences of RAS "Neutron diffraction study of materials structure and fundamental properties of matter” (Project No. 14 UB RAS / Contract No. 26/04), the Program "Neutron diffraction study of condensed matter" (State Contract No. 40.012.1.1.1150), the RFBR Project No. 04-02-1653 and the Grant of the RF President for support to the leading scientific schools of the Russian Federation No. NSh-639.2003.2.

Irradiation-Induced Gamma-Alpha Transition in Stainless Austenitic Steels Irradiated to High Doses and Its After-Effects under Deformation

V. K. Shamardin, V. S. Neustroev, Z. E. Ostrovsky, Yu. D. Goncharenko

FSUE “SRC RF Research Institute of Nuclear Reactors”, Dimitrovgrad, Russia (shamardin@niiar.ru)

Simulation of Martensitic Transitions in Alloys in the Presence

of Local Structure Deviations

A. R. Kuznetsov*, C. Abromeit**, Yu. N. Gornostyrev*

*Institute of Metal Physics, UB RAS, Ekaterinburg, Russia (A_Kuznetsov@imp.uran.ru)

**Hahn-Meitner-Institute Berlin, Germany

The homogeneous nucleation in real (imperfect) materials is usually considered as unlikely, and the key role in a nucleation of a new phase is attributed to structural deviations of the lattice. Nowadays, due to computer techniques development, an opportunity has appeared to study the kinetics of martensitic transitions within the framework of the microscopic approach – the molecular dynamics (MD) method. In the present work the microscopic description of the martensitic transitions kinetics BCC-HCP and BCC-FCC in Zr and in the system Fe-Ni is discussed taking into account defects as vacancies, dislocations and grain boundaries (GB). Also transition B2-L10 at irradiation of NiAl by swift ions with formation of tracks is calculated.

The presented results of MD simulation of direct and inverse kinetics allow to draw general conclusions about a role of local structure deviations of a crystal lattice in initiation of polymorphic transition. At first, the presence of the structure deviations (including swift ion tracks) essentially facilitates the beginning of transition to a close-packed phase, promoting development of lattice instability (the exception are vacancies the presence of which destroys a coherence of phonon modes). However the role of dislocations and GB thus essentially differs. In case of dislocations generated by them strain stimulates locally development of lattice instability. Thus, the transformation starts in isolated places adjoining to dislocations, and the "secondary" nuclei appear as a result of a relaxation of elastic stresses from "primary" nuclei. Equilibrium GB do not create elastic stresses. In this case shift instability is implemented under another scenario, namely, by intensive, correlated emission of partial dislocations from GB, resulting in rearrangement of frontier region to a close-packed phase. In the case of martensitic FCCBCC transformation the shear instability in the system is absent, therefore the mechanisms of defects influence as considered above are not implemented. Our results show that dislocations or close to special GB do not stimulate the transformation. The nucleation of BCC phase has appeared to be possible for a general type GB, which are characterized by enough free volume. It agrees with existing conceptions that during γ → α transformation kinetics in Fe and its alloys the main role is played by volume fluctuations.

Investigation of Straggling Zones in Molybdenum

Irradiated by Alpha-Particles and Protons

O. P. Maksimkin, A. V. Yarovchuk, L. G. Turubarova

### Institute of Nuclear Physics, Almaty, Kazakhstan (maksimkin@inp.kz)

#### One of the most well-known methods of obtaining information on the structure changes and metallic materials properties affected by a high dose irradiation is purposeful to make layers implanted with helium or hydrogen being formed as a result of the irradiating alpha-particles or protons total stagnation. Upon that depending on the particles energy the straggling zones are formed at various depths in a metal irradiated. The method of experimentally identifying the layers implanted used nowadays consists in the high temperature material annealing which not only deforms the particles total stagnation regions microstructure and alters the location of these regions boundaries but also transforms the whole structure.

In the paper the results of discovering the location and width estimation of the straggling zones in metallic molybdenum with the use of a new method of chemical etching have been shown. Commercially pure molybdenum was irradiated by 7 – 50 MeV energy protons and alpha-particles at the U-150 cyclotron facility at a temperature of less than 100 ºC. There have been represented the results of carrying out the identification of the irradiating particles type depending on their various ability to color sample surface being affected by the chemical solution.  The results concerning recrystallization processes peculiarities taking place in the straggling zones have been shown. Molybdenum microhardness changes and the strength and ductility parameters within the total stagnation zones and outside them have been studied. The chemical identification of the straggling zones enables to determine with higher accuracy the location of the layers implanted in the volume of a sample and to estimate the irradiating particles flux absorbed energy value. It was shown that a method of the optical observation of the straggling zones at macro - and microlevel discovering a possibility for carrying out the integrated investigations of the structure and phase changes, the irradiated materials mechanical properties and their corrosion stability is promising and has an importance for practical application.

Quadratic Temperature Dependence of Magnetoresistivity in Perfect and in Irradiated Tungsten and Molybdenum Single Crystals

V. V. Marchenkov*, V. E. Arkhipov*, A. L. Suvorov**, V. L. Arbuzov*,

S. E. Danilov*, H. W. Weber***
*Institute of Metal Physics, Ural Branch of RAS, Ekaterinburg, Russia (march@imp.uran.ru) 
**Russian State Research Center, Institute for Experimental and Theoretical Physics, Moscow, Russia
***Atomic Institute of the Austrian Universities, Vienna, Austria

The transverse magnetoresistivity in perfect and in irradiated tungsten and molybdenum single crystals was measured in the temperature interval 2-50 K and in magnetic fields up to 15 T. The perfect crystals with residual resistivity ratio RRR up to 75 000 were irradiated by krypton ions (E = 305 MeV), protons (E = 20 MeV) and electrons (E = 5 MeV). It was shown that the conduction electron interaction with a surface of unirradiated samples leads to the additional contribution into the magnetoresistivity ρxx, proportional to T2. The introduction of the radiation damages into the crystals by irradiation leads to the following: the quadratic temperature contribution into the magnetoresistivity increases and at low temperatures ρxx is proportional to T2 only. It was demonstrated that the observed quadratic dependence of the resistivity ρxx is caused by two scattering mechanisms of the current carriers: by the interference “electron-phonon-surface” process and by the interaction of the conduction electrons with the radiation-induced defects.

This work was partly supported by the Russian Foundation for Basic Research (project No 02-02-16431) and by Russian Science Support Foundation.

A Comparison of the Tensile Behaviour of Post-irradiation and In situ Tested Iron

Pierre Marmy
CRPP-PSI, Technologie des matériaux, CH-5232 Villigen-PSI, Switzerland (pierre.marmy@psi.ch)

Some components of fusion reactors will experience during service simultaneous plastic deformation and bombardment with high energy neutrons, specially in the region of the first wall. Traditionally, reactor materials are tested in the absence of  stresses, after a static irradiation, in which an irradiation substructure consisting of point defects, dislocation loops and irradiation-induced phases has been formed. In contrary, if plastic deformation occurs during irradiation, the formation of the irradiation substructure is fundamentally different because of two main reasons. First the mobile dislocations are absorbing the point defects and strongly reduce their clustering and second the irradiation is taking  place into a deformation-induced microstructure,  sometimes far different from the as-received structure. Under these conditions, the material response to a specific solicitation is completely different. This situation has been recognised early at CRPP-PSI where an in situ device placed into a 590 MeV proton beam line, has been in use since 1993 [1]. The device has been mainly operated to study the low cycle fatigue of first wall candidate materials [2,3]. In this work, the effect of the in situ deformation on the tensile properties of pure iron will be reported. The sample is tubular and can be loaded in compression. Due to the lack of beam time, a single complex experiment has been designed, in which different tension or compression sub-experiments were conducted near room temperature. In a first phase, the sample has been pulled at a crosshead displacement rate of 200 μm/hr to avoid static irradiation during the elastic part of the curve. The sample was then deformed in compression at 15 μm/hr and the flow stress was measured under beam. Two experiments were then conducted to measure the static hardening under positive and compressive stresses. Finally the sample was pulled at crosshead displacement rates of 10, 5 and 25 μm/hr to measure the influence of the strain rate. The sample was then pulled to rupture at 15 μm/hr. The dose at rupture was around 0.1 dpa. Tensile tests with the same deformation history were conducted for unirradiated and statically irradiated iron.

The differences will be explained and the possible consequences of the irradiation under plastic deformation will be discussed.

References

1. Marmy P., Journal of Nuclear Materials 212-215(1994)594-598
2. Marmy P., Oliver B. M., Journal of Nuclear Materials 318 (2003)132-142

3. Marmy P., Journal of Nuclear Materials 329-333(2004)188-192

Structural Transition Induced by Fast Neutrons  in  La0.85 Sr0.15MnO0.3 Manganite

V. D. Parkhomenko*, S. F. Dubinin*, V. E. Arkhipov*, Yu. A. Dorofeev,

Ya. M. Moukovskii**, S. G. Teploukhov*

*Institute of Metal Physics, UB RAS,  Ekaterinburg,  Russia (parkhomenko@uraltc.ru)

**Moscow Institute of Steel and Alloys, Moscow, Russia

A structural state of La0.85 Sr0.15MnO0.3 manganite exposed to fast neutrons (F = 8  1018 cm–2, Tirr = 340 K) has been investigated by the X-ray diffraction powder method at RT. It has been found that a cascade-forming neutron irradiation induces a structural transition from the orthorhombic phase  to the pseudo cubic one. The arguments are provided to prove that the change in the structure is the effect of the local manganite disordering  produced by fast neutrons.

Charge Ordering in Radiation-Modified Manganite La0.85 Sr0.15MnO0.3

V. D. Parkhomenko*, S. F. Dubinin*, V. E. Arkhipov*, S. G. Teploukhov*,

Ya. M. Moukovskii**

*Institute of Metal Physics, UB RAS,  Ekaterinburg,  Russia  (parkhomenko@uraltc.ru)

**Moscow Institute of Steel and Alloys, Moscow, Russia

A charge ordering in La0.85 Sr0.15MnO0.3 manganite exposed to fast neutrons (F  1019cm-2, Tirr = 340 K) has been investigated by the X-ray diffraction and thermal neutron methods. It has been found that a charge-ordering superstructure in the irradiated manganite is in conformity with the system of wave vectors: q1= (0, 0.8, 0) /b; q2 = (0.5, 0, 0.5) /c. The arguments are provided to prove that a change in  polaron ordering (with respect to an initial order) is due to the changes observed in the structural and magnetic states of the manganite affected by fast neutrons.

Void Formation and Second Phase Precipitates in 16Cr15Ni2MoMn Steel under High-Dose Neutron Irradiation and Their Evolution under Annealing

I. A. Portnykh, A. V. Kozlov, E.  N. Shcherbakov, O.  I. Asiptsov

FSUE «INM», Zarechny, Sverdlovsk Oblast, Russia (sfti@uraltc.ru )

An influence of high-dose neutron irradiation on change in structure of the austenitic steel 16Cr15Ni2MoMn was examined. Samples irradiated at 400, 500 and 600 C to damage doses 49, 86 and 48 dpa, respectively, were studded by electron microscopy. Precipitates of the second phases, including radiation - induced G-phase, and also formation and growth of radiation voids resulted in material swelling are shown to realise at this conditions.

Characteristics of radiation voids, volume ratio as well as particles dimension of the second phase precipitates and dimensional change of tested samples are essentially depended on neutron irradiation temperature. So peak swelling is observed at 500 C and has a value about 7.8 %. It reduces on the order ant 400 and 600 C. Considerable population of voids is formed of G-phase precipitates. Dimension and volume ratio of the G-phase increase with temperature rise. G-phase precipitates have the mean value 10 nm at 400 C, it reaches to 100 nm at 600 C. At the same time volume ratio of precipitates changes from 1 to 5 %. Dilatometry measurements are shown that linear dimension of irradiated samples is increased more slowly than of unirradiated one under heating at 550 C. Differences in dimensional changes are connected with void and precipitates dissolution under heating. Void dissolution brings dominating contribution into necessary dimensional change (shrinkage) under annealing of samples irradiated at 400 and 500 C and precipitates dissolution bring such contribution under annealing of samples irradiated at 600 C. Annealing within 2 hours at 700 ºC results in dissociation of small voids accompanying with large void growth. The second phase precipitates are fractionally dissolved under annealing and their volume ratio is decreased.

Temperature Gradient Influence on Voids Distribution in Irradiated Polycrystals

V. V. Slezov1, O. A. Osmaev1,2, R. V. Shapovalov1

1Institute of Theoretical Physics, NSC Kharkov Institute of Technical Physics, Kharkov, Ukraine (oleg_osmayev@kipt.kharkov.ua)

2Ukraine State Academy of Railway Transport,  Kharkov, Ukraine

In an irradiated polycrystalline is known to arise additional point and macroscopic defects: vacancies and interstitial atoms, voids and dislocations. These defects influence substantially the most important polycrystalline properties such as conductivity, strength etc.

Diffusion – dislocation current of an unlimited isotropic irradiated material has been studied in [1]. Gas atoms generation and temperature gradient absence has been taken into account too. Swelling and plastically flow velocity of the material were received in the different cases.

Ensemble voids movement in isotropic irradiated material, which is limited on temperature gradient direction, is studied in the present work. There sources of vacancies, interstitial atoms and gas atoms in the material. Several void movements under temperature gradient forces mechanisms were examined. It was formulated a supposition that in practically important cases voids are moved on the strength of matrix atoms void surface diffusion.

As full equations system described void moving is too complex, two limit cases were studied. A “big” voids case is observed if a characteristic time of a void volume changing is much more than a characteristic time of a void filled up with gas. A “small” voids case is observed in the reverse characteristic times correlation. The bulbs distributions function in sizes continuum, a bulb size and gas density in a bulb and in the material dependence on space location is found in the extreme case of “big” or “small” bulbs. Criteria define the material plastic deformation initial are received. These criteria confine the gas atom sources power and gas density in a bulb

References

- V.V. Slezov, UFG, 13,  No. 9, 1968.

Influence of Composition and Treatment on Iron and Tin Atoms States and Irradiation-Induced Growth of Model Zirconium Alloy Samples

Yu. A. Shikanova*, V. P. Filippov *, V. I. Petrov*, A. E. Novoselov**, G. P. Kobylyansky **

*Moscow Engineering - Physics Institute (State University), Moscow, Russia (filippov@d108.mephi.ru)

** Research Institute of Atomic Reactors, Dimitrovgrad, Russia

The model samples of zirconium alloys in systems Zr-Nb-Sn-Fe and Zr-Sn-Fe-Ni, containing iron and tin atoms enriched with isotopes 119Sn and 57Fe have been investigated. The composition of alloys is close to industrial alloys. Alloys were prepared in laboratory conditions, then they were rolled in plates 0.8 mm thick for studying their irradiating growth and a foil £150 microns thick for Mössbauer investigations of iron and tin atoms states. Three variants or thermomechanical treatment are used: recrystallized annealing, cold deformation (20 and 50 %) and quenching out of the b-phase states. Mössbauer investigations were made with the use of scintillation and resonant detectors.

The analysis of parameters of the received spectra has allowed finding out five states of iron atoms in practically all investigated samples. The following iron phases and compounds are found: Zr3Fe, Zr2Fe, (Zr1-xNbx)2Fe, two compound parameters similar to those of (ZrxNb1-x)Fe2 and a solid solution of Fe atoms in αZr. Relative content of these phases in samples depends on an initial sample state. Annealing, as a rule, increases the content of compound (ZrxNb1-x)Fe2 and in small limits of compound Zr3Fe, Zr2Fe. This increase is followed by reduction of (ZrxNb1-x)Fe2 compound content. Also it was revealed, that tin in the investigated samples of alloys is present in a solid solution as αZr.

The irradiation tests of model samples were carried out in reactor the BOR-60 at ~320 ºС to fast neutrons fluence of (2,2-11)×1025 m-2 (E > 1 MeV).  After  irradiation the increase in length of flat samples was defined. The dependence of irradiation growth strain on neutron fluence for alloy samples of system Zr-Nb-Sn-Fe in recrystallized and coldworked states is weaker, than for system Zr-Sn-Fe-Ni, and the magnitude of irradiation growth strain after irradiation to maximum fluence is much lower. The irradiation growth strain of the quenched samples of these alloys is less, than for recrystallized and coldworked  states.

Structural State of Fe0.61Ni0.36Ti0.03 Before and After

Irradiation with Fast Neutrons

V. I. Voronin, I. F. Berger, V. V. Sagaradze, B. N. Goshchitskii.

IMP UB RAS, Ekaterinburg, Russia (voronin@imp.uran.ru)

Using the methods of X-ray (on thin foils) and neutron (on massive samples) diffraction, a study was carried out of real crystal structure of intermetallic compounds of the same composition but subjected to different kinds of pretreatment. First all samples were annealed at 1100 ºC during 30 minutes. Then all three foils (F1, F2, F3) and one massive sample (M1) were quenched in water. Further, foil F1 was subjected to plastic deformation, and F2 was aged at 650 ºC during 30 min. The second  massive sample (M2) was quenched in oil and then, similar to F2, was aged at 650 ºC during 30 minutes.

An element of X-ray diffraction patterns of foils, reflection (331), is shown in Fig. 1. Reflection (331) broadening is the largest in F1, which points to the presents of significant lattice distortions (defects and stresses). Reflections F2 and F3 are also broadened, but to a lesser degree. Neutron diffraction study showed that distortions are even less noticeable in massive samples, and the widths of lines in the neutron diffraction patterns are close to standard.

Further all samples were irradiated with fast neutrons at 80 ºC to fluences 5, 10 and 50×1019 cm–2.

Study of the irradiated samples showed changes in the structural state with fluence increase. At that, the greatest changes were observed in the sample subjected to plastic deformation (F1). Figure 2 shows the reflection (331) from F1 before and after irradiation to a maximum fluence of 50×1019 cm-2. It may be seen that after irradiation the reflection width has decreased 1.35 times. This testifies to a radiation-stimulated annealing of the defects caused by deformation. The paper gives a detailed analysis of structural changes taking place in samples with different initial states after their irradiation with fast neutrons. To exclude the influence of surface effects, which are likely to occur in thin foils and may be observed with the help of X-ray diffraction study, analysis of the structural state in the bulk of massive samples was made using the neutron diffraction study method.

Work supported by the Program of Basic Research of the Department of Physical Sciences of RAS "Neutron diffraction study of materials structure and fundamental properties of matter” (Project No. 14 UB RAS/Contract No. 26/04), the Program "Neutron diffraction study of condensed matter" (State Contract No. 40.012.1.1.1150), the RFBR Project No. 04-02-1653 and Grant of the RF President for support to leading scientific schools of RF No. NSh-639.2003.2.

# Time Evolution of Microstructure in Materials Under Irradiation

V. V. Slezov1, A. V. Subbotin, O. A. Osmaev3, 1

1Institute of Theoretical Physics, NSC Kharkov Institute of Technical Physics, Kharkov, Ukraine (oleg_osmayev@kipt.kharkov.ua)

2FSUE N. A. Dollezhal Research and Development Institute of Power Engineering, Moscow, Russia

3Ukraine State Academy of Railway Transport, Kharkov, Ukraine