- Implanted and

Transmutated Gaseous

Impurities Behavior

in Irradiated Metals

and Alloys

Mechanisms of Gaseous Porosity Evolution in BCC and FCC Materials

during Post-Irradiation Annealings and High-Temperature

Implantation of Helium

S. Yu. Binyukova, I. I. Chernov, B. A. Kalin, Than Swe

Moscow Engineering Physics Institute (State University)

(binu@phm.mephi.ru)

Accumulation and/or implantation of significant helium concentrations negatively influences the radiation damage of nuclear and thermonuclear reactors structural materials. In this connection a great attention was paid to the problem of helium behavior and gaseous porosity evolution in various materials.

Generally two types of experiments are used to investigate the regularities of bubble formation and their growth mechanisms:

- irradiation immediately at high temperature;

- post-irradiation isochronous annealing of samples irradiated at low temperature.

In case of continuous helium implantation at high temperature, it is possible to find the information about peculiarities of bubble formation, but it is difficult to precisely determine the dose of their nucleation as the bubbles attain the sizes and density necessary for experimental detection already at higher doses. In the second case the information about the initial state of helium-vacancy complexes is insignificant and it is impossible to make definite conclusions about bubble nucleation processes. However, the bubble growth kinetics makes it possible to get some information about mechanisms of their growth, migration or dissociation of gas from the bubbles. The experiments testify that these conditions of microstructure evolution are nonequivalent with respect to formation of defects. Differences of the results obtained in these two experiments are due to various mechanisms of gaseous porosity evolution under post-irradiation annealings or during high-temperature irradiation by helium ions.

On use of post-irradiation annealings of samples irradiated at low temperature, different helium-vacancy complexes forming under irradiation play the main role in porosity evolution. For example, the complexes of HemVn, VnCk, InCk, HemCkVn and HemMekVn types (He, С, Ме, I and V  atoms of helium, carbon, substitution alloying element, own matrix atom and vacancy respectively) in dependence on materials, at that only simple complexes of HemVn type are formed in pure metals. The complexes have various bonding energies. Correspondingly, thermally less stable complexes dissociate and helium bubbles are formed on more stable complexes during post-irradiation heating.

Under high temperature irradiation the role of helium-vacancy complexes is not great as their dissociation temperature is often lower than that of irradiation. Moreover, in condition of continuous injection of helium the bubbles begin to form on the most thermally stable complexes on an early stage of irradiation. Thus, at high-temperature irradiation the regulative processes for gaseous porosity evolution are diffusive processes.

Besides, in both types of experiments various energies of point defects, an ambiguous affect of alloying elements on the self-diffusion coefficient of matrix atoms, as well as the initial structural-phase state of materials significantly influence the regularities of helium porosity formation in BCC and FCC materials.

The experimental data on gaseous porosity formation in BCC and FCC materials after           40-keV helium-ion irradiation up to a dose of 51020 m-2 are presented in the paper:

- irradiation at temperatures of 650 and 750 ОС;

- irradiation at room temperature followed by post-irradiation annealings at 650 and 750 ОС.

The model binary alloys of Ni-X systems (where Х is a substitution element), alloys of Ni-C and Fe-C systems, as well as structural BCC and FCC materials are investigated in the paper.

In the experiments on post-irradiation annealing of these materials, the role of helium-vacancy complexes in bubble formation is shown, as well as the fact that higher bonding energy of helium-vacancy complexes in BCC materials (various ferritic and ferritic-martensitic steels, Fe and Fe-C alloys) than in FCC materials (various austenitic steels and alloys, Ni, alloys of        Ni-C and Ni-X systems) suppresses the gaseous porosity formation: dissociation of the type HemVn complexes up to 650 ОС results in formation of large bubbles and high gaseous swelling of FCC materials while helium remains connected with complexes in the BCC lattice.

It was demonstrated with an example of the same materials that under high-temperature helium-ion irradiation at the same temperature larger bubbles, on the contrary, are formed in BCC materials than in FCC materials. The higher mobility of helium atoms and point defects in BCC metals promotes quick growth of bubbles in ferritic materials and higher gaseous swelling at high-temperature injection of helium than that in FCC materials. Besides, rapid bubble growth in BCC materials is also possible owing to their coalescence as lower self-diffusion activation energy assists higher speed migration of bubbles than in FCC metals.

Thermodesorption Peculiarities of Helium and Hydrogen

in BCC and FCC Materials

I. I. Chernov, S. Yu. Binyukova, B. A. Kalin, Than Swe

Moscow Engineering Physics Institute (State University)

(chernov@phm.mephi.ru)

Significant concentrations of transmutation and injected helium and hydrogen will be accumulated in structural materials of nuclear and, especially, controlled thermonuclear reactors. Helium and hydrogen negatively influence the radiation resistance of materials and can be a reason for catastrophic degradation of their properties and a decrease of the reactors constructional elements life time. Therefore, it is of great interest to investigate the helium and hydrogen behavior in the materials of different crystalline systems (BCC and FCC).

The peculiarities of trapping and gas release from BCC (model Fe and alloy Fe+0.4wt.%С; ferritic-martensitic steel of Cr13 type) and FCC (model Ni and alloy Ni+0.1wt.%С; austenitic steel of Cr16Ni15 type) materials were investigated by thermodesorption spectrometry (TDS). The samples were irradiated: 1) by 15-keV D2+ ions at 100 K and 290 up to a fluence of 51022 m-2; 2) by 40-keV Не+ ions at 290-900 К up to a fluence of 51020 m-2 and, consecutively, by 25-keV Н2+ ions at 290 K up to a fluence of 51020 m-2.

It is found that the quantity of trapped hydrogen increases in the presence of carbon in metals. For low fluences of D2+ ( 1021 m-2) the re-emission coefficients  significantly differ for pure metals and alloys:  for alloys of Fe-C and Ni-C systems is lower by 20% and for steels it is lower by 30% than that for pure metals. At high fluences ( 1021 m-2)  is close to one for both types of model materials and independent of carbon content NC. Re-emission coefficients is significantly lower for steels than that for model materials and reaches its saturation only after high fluences (about 1022 m-2).

The TDS spectra peculiarities are the following: 1) at 100 K, carbon shifts the TDS peaks to the area of higher temperatures, but the quantity of trapped particles is almost invariable in dependence on NC; 2) at 280 K, the influence of carbon on the quantity of trapped hydrogen significantly increases and the maximum quantity of gas is trapped by structural steels; 3) at 280 K for FCC materials, the carbon affect on TDS peaks positions is slight, the spectra are simple; whereas for BCC materials the TDS spectra have a great number of peaks and high-temperature gas release peaks show up at high fluences. In Ni, the addition of carbon increases the activation energy of gas desorption Еа from 0.45 up to 0.55 eV; in Fe, carbon does not change the gas release activation energy (Еа  0.68 eV), but results in a decrease of the pre-exponential factor that becomes apparent in a shift of a dependence between ln(Tm-2) and (1/Tm) under an invariable inclination of a line ( is the rate of uniform heating).

Hydrogen having a very high mobility in metals can be trapped only by crystal lattice defects, which can be impurity atoms that strongly distort the lattice, boundaries between the matrix and different particles of second phases et al. The fact that the influence of carbon on trapping and releasing of hydrogen in alloys is significant only for low fluences and such the influence is almost absent for high fluences testifies to saturability of traps at high concentrations of implanted hydrogen. Besides, the fact that the TDS peaks for Fe-C and Ni-C alloys irradiated at low-temperature (100 К) shift to a high-temperature area with an increase of NC, while at 280 K there is only an increase of the intensity of gas release peaks under invariable location of peaks temperature, gives rise the argument to assert that the carbon atoms as traps for hydrogen are active at low temperatures. Along with this, the increase of Еа in the alloys of a Ni-C system testifies that carbon atoms in solid solution of Ni-C alloys are more effective traps for implanted hydrogen than in Fe as Еа does not change in the presence of carbon in Fe, although its absolute value (0.7 eV) is higher than that for Ni-C alloys (0.45-0.55 eV).

The distinction of the alloys of a Fe-C system from those of a Ni-C system is the fact that the first alloys contain second phase particles (cementite F3C). During heating the irradiated samples, deuterium releases outside through the external surface of samples, as well as onto the second phases’ boundaries from which it can release after an excess of some critical pressure (the reverse solution in the matrix and diffusion to the sample surface). The last processes need higher temperatures. Apparently these factors are the reasons for a shift of the gas release temperature to higher temperatures in the Fe-C alloys with a high carbon content as well as they are the reasons for formation of more complicated TDS spectra.

Under Не+ ion irradiation, TDS spectra for BCC materials are more complicated than for FCC materials as in case of hydrogen implantation. At that, the temperature range of helium release widens with an increase of the irradiation temperature. It is shown that at a fluence of 51020 m-2 the release of helium in the main TDS peak is the result of growth, migration, coalescence during migration and outlet by formation on the surface of a distinctive pin-hole structure. In contrast to austenitic steel with one intensive TDS peak at temperature about 1380 К, the TDS spectra of ferritic-martensitic steel have two intense peaks at temperatures about 1180 and 1300 К. The temperature of 1180 К corresponds to that of    transformation for steel of Cr13 type during the heating. Therefore it can be supposed that the light-weight migration of bubbles through the BCC lattice results in their partial outlet onto the surface and the first peak is appeared. At higher temperature the straitened migration of bubbles through the FCC lattice initiates bubbles-out already from austenite at the temperature of 1300 К.

Features of Heavy Hydrogen Isotopes Interaction with Austenitic Class Steels

Yu. N. Dolinsky, Yu. N. Zouev, I. A. Lyasota, I. V. Saprykin 
RFNC – All-Russia Research Institute of Technical Physics, Snezhinsk, Russia (dep5@vniitf.ru)

Investigation of Reactor Irradiation Effect on

Hydrogen Isotopes Release from Vanadium

T. V. Kulsartov*, V. P. Shestakov*, E. A. Kenzhin**
*Research Institute of Experimental and Theoretical Physics at Kazakh State University,

Almaty, Kazakhstan (kulsartov@physics.kz)
**Institute of Atomic Energy NNC RK, Semipalatinsk-21, Kazakhstan

Vanadium-based alloys are most perspective materials for lithium breeder blankets of future fusion reactors due to their combination of good mechanical and radiative properties. Under fusion reactor operation conditions interaction of vanadium alloys and hydrogen isotopes under neutron and gamma irradiation is of great interest. In this paper we present results of first experimental stage on reactor irradiation effect on hydrogen isotopes release parameters from vanadium alloys. Particularly, parameters of gas release and characteristics of vanadium hydride phase transformations under various values of reactor irradiation are presented.

Preliminary saturation of vanadium samples was performed from gas phase. All experiments were carried out with thermal desorption spectroscopy method. Irradiation was performed on IVG1.M reactor. Investigations were made for various values of irradiation and this helped to find reactor irradiation influence on processes of hydrogen release from vanadium.

Preliminary Results on Tritium Release from Li2TiO3 Ceramics under Long-Term Reactor Irradiation

T. V. Kulsartov*, I. L. Tazhibaeva*, V. P. Shestakov*, M. A. Makukov*, S. E. Afanasyev*,

H.  Kawamura**
*Research Institute of Experimental and Theoretical Physics at Kazakh State University,

Almaty, Kazakhstan (makukov@physics.kz)
** Blanket Irradiation and Analysis Laboratory at JAERI, Orai-machi, Japan

Lithium-containing ceramics, for example Li2O, Li2TiO3, Li2Zr03 and Li2SiO4, are perspective materials for tritium breeding in blankets of thermonuclear power plants. Li2TiO3 ceramics is one of most interesting due to easy recovery of tritium generated in this ceramics under relatively low temperatures, chemical stability and so on.

In this paper we present description of part of the experiments on investigation of Li2TiO3 95% 6Li-enriched ceramics. Objective of long-term reactor irradiation of Li2TiO3 was to obtain burn-out of 20% 6Li. Also during experiment in situ registration of released tritium was performed under various ceramics temperatures.

In this paper preliminary results on tritium release from Li2TiO3 ceramics under long-term irradiation are presented.

Radiation-Induced Segregation of Deuterium in Two-Phase Cr16Ni9Mo3 Steel

G. A. Raspopova*, V. L. Arbuzov*, V. V. Sagaradze*, N. L. Pecherkina*,

K. V. Shalnov*, Yu. N. Zouev**

*Institute of Metal Physics, Ural Branch RAS, Ekaterinburg, Russia (raspopova@imp.uran.ru)

**Russian Federal Nuclear Center – All-Russian Research Institute of Technical Physics, Snezhinsk, Chelyabinsk Oblast, Russia

Implantation of hydrogen in metal materials is generally accompanied by formation of regions with a more or less stable segregation of the implant (radiation-induced segregation (RIS) of hydrogen). If mobility of hydrogen atoms is high, the RIS stability is determined by characteristics of the interaction between hydrogen and structural traps, which are represented by crystal lattice defects. It was shown earlier that efficient traps of hydrogen in austenitic steels are vacancy clusters, interfaces and large-angle grain boundaries.

It is difficult to separate the contribution of each type of traps to the aggregate accumulation of hydrogen in irradiated regions in steels, because new radiation-induced traps appear in addition to the initial traps and /or the initial traps are modified under irradiation. Therefore, the analysis of the behavior of implanted deuterium in a two-phase steel, whose structure and the phase ratio can be changed by thermal treatment, presents a special interest.

The hydrogen RIS was studied in a two-phase austenitic-martensitic steel of the formula Cr16Ni9Mo3 having different phase ratios. It is known that the deuterium RIS in this steel is unstable after the dispersal type unlike in the austenitic steel (where the segregation is enhanced after irradiation is removed) and the Fe-Cr BCC alloy (where the segregation is stable).

The effect of the structural state of the Cr16Ni9Mo3 steel on the deuterium RIS was studied using the nuclear reactions method. The steel microstructure was certified by the methods of transmission, scanning and tunneling electron microscopy.

It was shown that the accumulation of implanted deuterium in the steel samples under ion irradiation depended on the martensite/austenite ratio and the extent and the structure of interfaces in the steel studied. It was found that structural and phase transformations, which favored the capture of the implant and facilitated the segregation, took place in the steel under irradiation. Possible mechanisms, by which structural elements influence the capture of implanted deuterium, were analyzed and a model of the deuterium RIS in the steel under study was proposed.

The present study was supported financially by the RFBR (Project No. 04-02-16053).

Theoretical and Experimental Study of Hydrides in

Zirconium Components of Nuclear Reactors

A. A. Shmakov*,  R. L. Eadie**,  D. Yan**

*Moscow Engineering Physics Institute, Moscow, Russia  (shmakov@phm.mephi.ru)

**University of Alberta, Edmonton, Canada

Delayed hydride cracking in structural materials is generally accepted as a repeated process which involves stress-induced hydrogen diffusion, precipitation of brittle hydride platelets normal to the applied tensile stress, their growth up to some critical size and fracturing of the embrittled region. The first incidents connected with delayed hydride cracking in zirconium components of nuclear reactors were observed in the 1970’s. After that an extensive study of delayed hydride cracking has been conducted for zirconium-based reactor alloys. Only in the last decade a number of theoretical models was developed to predict the basic parameters of delayed hydride cracking such as the stable velocity and threshold stress intensity factor. Unfortunately, the most of the known models ignores a doubtless dependence of the crack-tip hydrides on temperature and stress intensity factors. Such admission essentially reduces a reliability of theoretical results.

In this paper we present the experimentally verified theoretical model allowing to predict the critical length and thickness of the crack-tip hydride platelets forming during delayed hydride cracking in the industrial zirconium alloys. The model is based on the careful analysis of the tensile stresses near the crack tip [1]. The experimental study of hydrides during delayed hydride cracking in Zr2.5%Nb pressure tubes of CANDU (Canadian Deuterium Uranium) nuclear reactors was performed for 1500C and stress intensity factors in the range from 5,9 to 20  MPam [2, 3]. It is shown that the theoretical predictions are in excellent agreement with the obtained experimental data.

References

- Shmakov A.A., Atomic Energy. 2004, in press.

- Yan D., Eadie R. L., Intern. J. Pressure Vessels & Piping. 77, 167 (2000).

- Yan D., Eadie R. L., J. Mater. Science. 35, 5667 (2000).

Influence of Irradiation Regimes on Retention of Gaseous Products of Nuclear Reaction into Structural Materials

## A.G.Zaluzhnyi, A.L.Suvorov

SSC RF Institute of Theoretical and Experimental Physics

117218, Russia, Moscow, B. Cheremushkinskaya Str., 25 (zaluzhnyi@vitep5.itep.ru)

Materials are known to change their physical and mechanical properties under the influence of irradiation. The main factors limiting material life are radiation swelling, high-temperature and low-temperature radiation blistering, radiation creep and others. Gaseous products of nuclear reactions, including helium, play the main part in these unwanted effects.

Direct irradiation of investigated materials in reactor takes much time and material costs therefore different express methods are used now to imitate helium accumulation: irradiation by helium ions of different energies, high-energy electrons and γ-quanta irradiation, saturation from plasma and others. The essential question here is how adequately each of these methods can simulate reactor irradiation.

In the present work we tried to compare helium desorption kinetics under linear heating of samples saturated by means of different methods (irradiation on cyclotron and magnetic mass-separating plant, on IRT-2000 and BOR-60 reactors and helium saturation by the “tritium trick” method), and estimate the influence of dislocations on helium retention in materials.

The results of investigations, which studied the influence of conditions of helium introduction into the lattice of material on gas release kinetics, showed that in case of helium behavior in structural materials the simulating experiments reproduce reactor irradiation quite adequately. These simulating experiments provided simultaneous introduction of helium and radiation defects into the lattice of material (in a wide range of helium concentration and radiation damageability). In all probability, it is caused by helium atoms stabilization of certain configurations of radiation defects. For zero-defects methods of helium introduction it is necessary to consider the peculiarities of its retention and mobility in every case. Neglecting these peculiarities can cause incorrect interpretation of the received results. The fact, that helium release at heating the irradiated samples starts with the temperatures, which are higher than temperature of irradiation, could be used to define the temperature of irradiation.

Investigations of kinetics of helium release from 0X16H15M3B steel samples after their preliminary deformation and during deformation showed that during heating helium atoms can migrate along the dislocation tubes and strongly influence helium release and redistribution in the bulk of material. The activation energy of helium atoms diffusion along the dislocation tubes for austenitic steel 0X16H15M3B is about 0.7 eV. Moving dislocations can promote helium release to the surface of material, to grain boundaries, to interfaces.