- Materials for Nuclear

and Thermonuclear

Power Engineering

Interrelationship of Changes in Microstructure and

Mechanical Properties of Fe-18Cr-10Ni-Ti Stainless Steel

Irradiated at Low Temperatures in Power Reactors

Е. V. Boyev, V. S. Neustroev and Z. E. Ostrovsky

FSUE “SSC RF RIAR”, Dimitrovgrad, , Russia (fae@niiar.ru)

In spite of a long-term operation period of power reactors such as VVER, the data on radiation stability of Fe–18Cr-10Ni-Ti austenitic stainless steel used as material for reactor internal components (former, basket etc.) exposed to direct irradiation in the VVER reactors have not been obtained yet. In the last years investigation of guide tube made from Fe–18Cr-10Ni-Ti stainless steel irradiated in the VVER-1000 reactor of the Rovenskaya NPP was carried out at the FSUE “SSC RF RIAR”. The present paper is devoted to analysis of these results and a new investigation of guide tubes from the VVER-1000 fuel assembly of Balakovskaya NPP.

The evolution of dislocation loops, voids, radiation-induced formation of the second phases results in significant changes of the material mechanical properties [1-2]. This work aims at studying the dose changes of microstructure and mechanical properties of Fe–18Cr10NiTi stainless steel after irradiation in the VVER-1000 reactors and their interrelationship.

TEM-examination of the Fe–18Cr10NiTi still microstructure parameters before and after irradiation was carried out. damage dose was plotted as a function of microstructure parameters (dislocation loops size and density) for the irradiated Fe–18Cr10NiTi stainless steel.

It is evident that sharp hardening of Fe-0.06C-18Cr-10Ni-Ti steel takes place at the initial irradiation period of 4-5 dpa with further saturation at about 500 МPа and higher damage doses and sharp reduction in plastic properties (uniform elongation) down to 1-3 %.

A good correlation between hardening calculated on the basis of the microstructures parameters and experimental data was found.

# Reference

- V. S. Neustroev, V. K. Shamardin, G. A. Shimansky, E. V. Boyev, A. V. Zaharov. Hardening of Fe-18Cr-10Ni-Ti austenitic steel irradiated at temperatures about 300 C in VVER-1000 reactors, Proceedings of the XIV International meeting on Radiation physics of solids (Sevastopol, July 5-10, 2004), M., P. 329-334.

- V. S. Neustroev, V. G. Dvoretsky, Z. E. Ostrovsky, V. K. Shamardin, G. A. Shimansky. Investigations of a microstructure and mechanical properties of Fe-18Cr-10Ni-Ti stainless steel after irradiation in the core of VVER-1000 reactor. Voprosy atomnoy nauki i tehniki. Ser.: Fizika radiacionnih povrezhdeniy i radiacionnoe materialovedenie. No. 3(83) (2003) P. 73-78. (in Russian).

Comparative Examination of Changes in Structure and

Mechanical Characteristics of Austenitic 16Cr15Ni2MoMn and

Ferritic-Martensitic 13Cr2MoNbVB Steels at High-Dose

Neutron Irradiation

S. V. Brushkova, Е. А. Kinev, А. V. Kozlov, S. А. Averin, V. L. Panchenko,

I. А.Portnykh, V. N. Shemyakin

FSUE «INM», Zarechny, Sverdlovsk Oblast, Russia (sfti@uraltc.ru )

The austenitic steel 16Cr15Ni2MoMn is used as structural material for devices of fast nuclear reactor core. Steel swelling deteriorates its performance. The ferritic-martensitic steel 13Cr2MoNbVB is considered as a promising material for use in fast reactor fuel cladding.

Examinations after high dose irradiation up to 70 dpa in a fast reactor at temperatures from 380 up to 600 C were carried out for comparison of irradiation effect on 16Cr15Ni2MoMn and 13Cr2MoNbVB steels. Structural changes and mechanical characteristics data are given.

Plasticity characteristics of the 13Cr2MoNbVB steel are reduced at test temperature of 400 C after irradiation at 380-420 C. A lot of '-phase precipitations in the steel and crystalline matrix depletion in chrome are displayed by structural examinations. The steel does not practically swell during irradiation up to a maximum damage dose at ~500 C. Under such conditions mainly - phase is precipitated.

The worst plasticity and strength properties of the austenitic steel are observed after irradiation at 470-500 C. The structural analysis shows that a great population of radiation pores is formed and swelling reaches ~10 %. It is the basic reason of the material embrittlement.

Verification results of mechanical properties have shown that the ferritic-martensitic 13Cr2MoNbVB steel is more preferable than the austenitic 16Cr15Ni2MoMn steel after their neutron irradiation at temperatures and damage dose mentioned above.

Features of Behaviour of Structural Materials in

Neutrons Spectrum of High-Power Fast Reactor

V. V. Chuev

Affiliate of Concern Rosenergoatom Beloyarskaya NPP, Zarechny, Russia

Beloyarskaya NPP power unit with BN600 reactor is successfully operated at the power levels near to nominal, generating commercial electricity and heat. Simultaneously the tasks on testing and checking new scientific and technical developments are solved. Throughout the years of BN600 operation a unique experience on different problems of fast neutron reactors has been accumulated, which will be undoubtedly realized when constructing power units with new generation reactors.

One of the most important components of the power unit is the core that defines reactor’s safety and economical operation. The design characteristics of the first generation core for burnup were not reached at the beginning of operation. As a result of two upgrades the stable core operation was achieved with the peak fuel burnup of 10 % of h.a.

Since 1995 standard fuel assemblies have been tested at BN600 to increase burnup with accumulated ~560 effective days for most fuel assemblies and up to ~720 effective days for peripheral fuel assemblies of high enrichment zone. The final aim of these activities is to introduce into standard operation the third generation core with the core components of traditional structural materials and standard pelletized uranium fuel with peak burnup of ~11 % of h.a. Resulting from it the reactor’s technical-and-economic index will improve; the cycles of fuel assemblies will extend from 480 to 560 effective days; the burnup will increase from ~60 to ~70 MW·day/kg UO2 with material damaging dose increase of ~ 10 % and the maximum of up to 82 dpa; the average structure irradiation temperatures and fuel assembly unit loads will decrease; fresh fuel annual consumption will drop 1418 % and so will the corresponding volume of the irradiated fuel sent for reprocessing; four-step core refuelling will be realized and more optimal reactor operating mode with different intervals between refuellings in summer (110 effective days) and winter (170 effective days) operating periods will be provided.

Fuel assembly life extension up to 584 effective days [1] and corresponding burnup increase up to ~11.5 % of h.a. is the most optimal for power-and-heat supply from BN600 power unit and maximum use of fuel with four-step core refuelling. According to the results of the work [1], for BN600 power unit operating under a seasonal limitation with the planned availability factor of ~80 % the duration of the next optimal fuel cycle should be 876 effective days with six-step core refuelling (peak burnup ~17 % of h.a.). The intermediate non-optimal variant with five-step core refuelling is the cycle of 730 effective days (peak burnup ~ 14 % of h.a.) [1].

In connection with the political decision on warhead plutonium utilization the task is set to develop a hybrid core for BN600 where a part of standard uranium fuel assemblies should be replaced by MOX assemblies, and the amount of radial blanket fuel assemblies may be reduced by replacement of a part of plutonium producing fuel assemblies by steel rods and/or isotope producing assemblies.

The given work, purposed to review the sufficiency of experimental grounding and reveal the problems with realization of the set tasks, presents the main results of systematic after-reactor research on serviceability of fuel elements and assemblies, tested in the first and second generations of BN600 cores.

References

- N. N. Oshkanov. Fuel cycle planning under NPP fixed operating cycle. – Nuclear power, Volume 91, Issue 6, December 2001, p. 488-489.

## Synergistic Effect of Temperature, DPA Rate and Stress to

## Determine Swelling of AISI 304 Stainless Steel in

## Hexagonal Wrappers and Fuel Pin Cladding

F. A. Garner1 and B. J. Makenas2

1Pacific Northwest National Laboratory, Richland WA, USA

2Fluor Hanford Company, Richland, WA, USA

After the discovery in Britain of the void swelling phenomenon there was a strong focus in the USA on swelling in annealed AISI 304 stainless steel, since it was the primary construction material of the EBR-II fast reactor.  This steel was indeed found to be swelling to rather large levels.  After a period of rather intense examination this steel was discarded as a construction candidate for other reactors such as FFTF.  Further investigation of this steel was not performed, and ongoing EBR-II experiments directed toward the use of AISI 304 for FFTF fuel cladding were terminated without analysis or publication.

Recently, interest in the swelling behavior of this steel has been resurrected due to the realization that austenitic internal components of pressurized water reactors are slowly developing swelling. The majority of the internals are constructed from annealed AISI 304 stainless steel, sometimes fastened with cold-worked 304 bolts. Prediction of swelling of these PWR components is rather difficult given the significant difference in neutron flux-spectra, temperature history and coolant environment between PWRs and fast reactors.

This paper examines both previously published data and a large amount of unpublished swelling data of AISI 304 in light of the recently discovered strong influence of neutron flux or dpa rate to affect the duration of the transient regime of swelling, not only in AISI 304 but in austenitic steels in general.  It is shown that the combined effect of dpa rate and temperature distribution along any given structural component produces a “swelling loop” that allows estimation of the separate dependencies of swelling on temperature and dpa rate. In components operating under stress the loop is modified, moving to lower dpa levels. It is also shown that over a wide range of irradiation conditions the terminal steady-state swelling rate of AISI 304 is consistent with the ~1 %/dpa characteristic of austenitic stainless steels. At first observation components which span a wide range of temperature and dpa rate can give a misleading impression that the 1 %/dpa swelling rate has not been reached, however. When flux and temperature effects are properly taken into account, the 1 %/dpa is observed.

These insights provide some guidance in the extrapolation of swelling data from PWR and VVER components at relatively low exposures to higher neutron exposure.

Structure and Properties of Steel 08Cr16Ni11Mo3

Irradiated to High Damaging Doses in BN-350 Reactor

O. P. Maksimkin*, M. N. Gusev*, K. V. Tsai*, O. V. Tivanova*

Institute of Nuclear Physics, Almaty, Kazakhstan Republic (gusev.maxim@inp.kz)

A subject of studies is austenitic stainless steel 08Cr16Ni11Mo3, material of the hexagonal shroud of a fuel assembly (of the BN-350) reactor irradiated up to maximal damaging dose comprising 15.6 dpa. Structure parameters (porosity, defect distribution pattern) were studied by techniques of transmission electron microscopy (TEM) and metallography. As a result of mechanical unaxial tensile test, characteristics of the strength and plasticity were determined. Also the peculiarities of the material behavior under deformation and failure were researched.

The correlation relation between the dose variations in the yield stress, s02, and the microhardness, Нm,, was obtained and compared with similar published data referring to other materials and irradiation conditions.

The performed electron-microscopy studies justify that character of  void formation, in particular, a value of the threshold fluence, depends strongly on a rate of increase in the damaging dose. Void formation is revealed already at 1.27-dpa damaging dose, 0.39×10-8  dpa/s irradiation rate and irradiation temperature 281°C.

It is shown that deformation in irradiated stainless steel is inhomogeneous, and local deformations at low values of plasticity may reach the values compared with those related to unirradiated steel.

By the optical deformation extensometry technique, character of interaction between the values of true strains and local deformations is established in the developing neck of high-dose irradiated samples.

With the deformation magnetometry and TEM techniques, the character and peculiarities in direct (under deformation) and reverse (under post-deformation annealing) martensitic  g↔a transformation are studied.

Characteristics of strength, plasticity and structure parameters versus fluence, irradiation temperature and rate of damaging dose increase are analyzed.

Development of a Structure and Creation of a Database

on Physics of Radiation Damages of Reactor Materials

B. A. Kalin1, G. A. Birzhevoy2, G. N. Elmanov1, V. V. Svetukhin3,

E. A. Smirnov1, S. I. Chausova1

1Moscow Engineering Physics Institute (State University), Russia (kalin@phm.mephi.ru)

2FSUE “SSC RF – IPPE”, Obninsk, Russia

3FSUE “SSC RF – RIAR”, Dimitrovgrad, Russia

The first stage of works was devoted to the development of a computer database structure on diffusion characteristics of materials, state diagrams of metal systems, and threshold displacement energies and characteristics of point defects.

The developed data access system provides a remote access to data through the Internet, and makes possible remotely administrationof the database on the basis of a client-server technology.

The interface of the program enables one to search and sort data using various criteria, to approximate the temperature dependences by various equations and make their graphic representation, as well as to determine the main diffusion characteristics of materials for a specified temperature range.

A search has been made and scientific and technical information on the coefficients of self-diffusion, impurity diffusion and the diffusion of components in alloys of - and -Zr has been selected.

According to the developed structure, materials have been prepared for filling the database’s sections with the necessary information concerning the purity of the used materials and isotopes, measurement techniques, as well as temperatures and diffusion coefficients corresponding to these temperatures. As a part of the data available in the literature is presented in the form of dependence diagrams of diffusion coefficients from temperature, computer processing of these diagrams has been carried out with the purpose to present experimental points in the form of tables with an estimation of an error of this processing.

A computer processing of the most reliable data has been made with consideration for an expert estimation with the purpose to receive linear and nonlinear dependences between the diffusion coefficients and the temperature. Dependences that can be recommended to consumers for an estimation of diffusion coefficients have been received. An analysis of the influence of impurities and alloying on the coefficients of self-diffusion, impurity diffusion and diffusion of components in zirconium alloys has been made. Methods for estimation and recommended values of stimulated diffusion in zirconium are presented.

Software to manage the database using state diagrams and their representation has been developed. State diagrams of various systems of zirconium alloys are included into the database.

Mean threshold displacement energies for various materials, including those of zirconium alloys, have been presented. The presented values are based, for the most part, on the results of computer simulation of low-energy cascades.

The characteristics of point defects for metals, as well as a variant of the database for averaged characteristics of point defects for FCC metals are presented.

Low-Temperature Hardening of Austenitic Steel Cr18Ni10Ti

Irradiated in Different Reactors

V. S. Neustroev, V. V. Svetukhin, V. K. Shamardin, E. V. Boyev

FSUE “SSC RF RIAR”, Dimitrovgrad, Ulyanovsk Oblast, Russia (fae@niiar.ru)

Low-Temperature High-Dose Neutron Irradiation Influence on

Swelling, Mechanical Properties and Microstructure

of Promising Beryllium Grades

V. P. Chakin, A. O. Posevin

SSC-RIAR, Research Institute of Atomic Reactors, 433510, Dimitrovgrad, Ulyanovsk Region, Russian Federation (chakin@niiar.ru)

In this work, investigation results of neutron irradiation influence in the SM reactor at temperature 70 oC within a wide fluence range (0.6-11.1)1022 cm-2 (E  0.1 MeV) on swelling, mechanical properties and microstructure of the four beryllium grades manufactured in Russia are presented. The recently obtained data at the maximum neutron doses are of particular interest.

Accumulation of helium and tritium atoms occurs in beryllium under neutron irradiation in a nuclear reactor. Since, irradiation occurs under low temperatures, diffusion mobility introduced gas atoms is not great [1]. So, gas atoms stay in places of its formation practically. Calculation show that for irradiation time only small part of gas atoms, basing in a grain body, leaves on distances of order 1-10 m.  This leads to accumulation of helium and tritium atoms on different sinks and, as effect, to increasing of swelling and essential degradation of mechanical properties of beryllium [2, 3].

A study was made for four beryllium grades manufactured by hot extrusion (HE) and hot isostatic pressing (HIP) methods. The obtained results do not provide evidence of the advantage of one beryllium grade over another in terms of resistance to radiation damage in the fission reactor.

Microstructure examination of beryllium samples in initial state shows the presence of voids with significant sizes (1-5 m), distributed on grain boundaries mainly. Neutron irradiation of beryllium leads to filling this voids of transmutated helium and tritium atoms, that leads to growing pressure into voids and, as a result, to increasing of strength on the grain boundaries.

# References

- Dalle Donne M., Scaffidi-Argentina F., Ferreco C., Ronchi C., Modelling of swelling and tritium release in irradiated beryllium, Journal of Nuclear Materials, 1994, vol. 212-215, p. 954-960.

- V. P. Chakin et al., High dose neutron irradiation damage in beryllium as blanket material, Fus. Eng. Des. 58&59 (2001) 535

- V. P. Chakin, Radiation Damage of Beryllium Blocks of an SM Reactor, The Physics of Metals and Metallography, Vol. 88, No. 2, pp. 200-204.

Nanooxide-Strengthened Reactor Steels

V. V. Sagaradze, V. A. Shabashov, A. V. Litvinov, N. F. Vildanova,

B. N. Goschitskii, V. L. Arbuzov

Institute of Metal Physics, Ural Branch RAS,

Ekaterinburg, Russia (vsagaradze@imp.uran.ru)

The subjects of study were oxide dispersion strengthened (ODS) steels types K2 (13Cr-2Mo-2Ti), K5 (13Cr-1Mo-1Ti) and K7 (13Cr-2W-1Ti) (China), which contained ~0.4 mass % Y2O3 powder each. The production process of reactor ODS steels includes mechanical alloying of powders in ball mills and sintering. A very important factor, which has a fundamental effect on properties of ODS steels, is the deformation dissolution of relatively "coarse" yttrium oxides 40 to 100 nm in size in the steel matrix (during long-time grinding of powders in mills at 300 K) and their subsequent precipitation (during high-temperature sintering) in the form of nanooxides that efficiently strengthen the steel. The average size of Y2O3-TiO2 complex oxides precipitating in the K2, K5 and K7 steels was 3, 2.5 and 3.3 nm respectively, while the concentration of the oxides was 0.4, 2.0 and 1.61017 cm3, which corresponded to 0.06, 0.16 and 0.30 vol. %. Strength characteristics of the steels were improved sharply as the number of dispersed oxides increased. Specifically, the yield stress of the K5 steel, which was annealed at 1373 K, was 1272 MPa. This value is almost one order of magnitude larger than the yield stress of the "oxide-free" ferritic steel type Cr13, which is prepared by the standard metallurgical smelting. The creep rate in the K5 and K7 steels at temperatures of 923 and 973 K and loads from 150 to 450 MPa was much smaller than the creep rate in standard reactor steels having FCC and BCC lattices.

Neutron irradiation of the ODS steels at 77-683 K caused their strengthening and a considerable impairment of their plasticity characteristics. The vacancy migration began from 220 K, "vacancyinterstitial atom" complexes dissociated at 350 K, and vacancy clusters decomposed at 450 K in the ODS steels. The thermal diffusion became appreciable over 650 K.

We have proposed a new approach to production of ODS steels involving deformation-induced implantation of oxygen from feebly stable iron oxides into yttrium- and titanium-doped ferritic stainless steels so as to form thermally stable yttrium-titanium nanooxides during annealing.

This study was financed in part by the Presidium of the Russian Academy of Sciences (nanomaterials, Project 7 and Contract 34/04), the Russian Foundation for Fundamental Research (Project No. 04-02-16053), and the MMC-Aucfer-Intels Foundation (Grant No. 12-03-03).

Evaluation of Graphite-Like Material Resistance to

Electron Irradiation by X-Ray Diffraction Method

A. E. Shestakov,  V. V. Plokhoi, I. L. Svyatov 
RFNC VNIITF, Snezhinsk, Russia   (btk@five.ch70.chel.su)

Influence of Temperature and Duration of Aging on Change in Structure and Physical and Mechanical Properties of 13Cr2MoNbVB Steel

E. N. Shcherbakov, A. B. Kozlov, V. N. Shemyakin, M. V. Evseev, V. S. Shikhalev,
 J. V. Ershova, P. I. Yagovitin, A. P. Isakov

FSUE «INM», Zarechny, Sverdlovsk Oblast, Russia (sfti@uraltc.ru )

Cladding material of fuel elements of 13Cr2MoNbVB steel (EP-450) is subjected to complex influence of both higher temperatures 400-600 °C and neutron flux, the intensity of which varies over the core height under reactor conditions. One can see a marked difference in structural and phase state of the material in various cladding sections after its operation in  the reactor. It is followed by change in strength and elasticity properties. The steel having good resistance to radiation swelling has shown loss of elasticity in sections with temperature of 400-500 °C.

Measurements of electrical resistivity and Young’s modulus performed at 400 and 500 °C during duration aging were studded in order to make clear an influence of temperature on change physical and mechanical properties of the steel. Electrical resistivity of unirradiated specimens cut from cladding tubes has decreased on 4 % after their aging within 500 hours at 400 °C. This value gradually has increased to the initial one at following aging of specimens within 500 hours and increasing of temperature to 500 °C. Young’s modulus did not vary at 400 °C and it had sharp growth during temperature increasing to 500 °C.

Additional examination of specimen structure was performed in order to explain observing phenomenon.

Influence of Structural-Phase State of Nb-Containing

Zr Alloys on Irradiation-Induced Growth

V. N. Shishov1, M. M. Peregud1, A. V. Nikulina1, Yu. V. Pimenov,2  G. P. Kobylyansky3, A. E. Novoselov3, Z. E. Ostrovsky3, A. V. Obukhov3

1FSUE A. A. Bochvar All-Russia Research Institute of Inorganic   Materials,

Moscow, Russia (gor@bochvar.ru)

2FSS «TVEL», Moscow, Russia

3FSUE «SSC of Russian Federation. Research Institute of Atomic Reactors»,

Dimitrograd, Russia

On account of the search for optimal composition and structure-phase state of Zr alloys much attention is paid to upgrade E110(Zr-1%Nb) and E635(Zr-1%Nb-0.35%Fe-1.2%Sn) alloys that proved well in terms of irradiation-induced creep and growth, high strength characteristics, corrosion. The difference between the alloy properties is determined by their states related to their compositions.

The structure-phase state of the Zr-Nb and  Zr-Nb-Fe-Sn  systems has been studied after heat treatment in the α-- and  α + β- regions and the influence was investigated that is produced by this state on the irradiation-induced growth (IIG) during BOR-60 irradiation at T =315-350 oC. A substantial difference has been revealed in the deformation effected by IIG of those alloys, it is less for Zr-Nb-Fe-Sn  alloy in dissimilar structure-phase states. The incubation period of the accelerated growth stage is determined by the α-matrix composition, the phase state and the initial dislocation structure. Neutron irradiation leads to a redistribution of alloying elements between the matrix and the precipitates, to changes in the α-solid solution composition and affect accumulation and mobility of irradiation defects, anisotropy and formation of vacancy c-component dislocation loops. The appearance of c-loops usually correlates with an axial direction acceleration of the IIG of tubes conforming to their texture.

The basic regularities of the phase transformation have been established:

- β-Nb precipitates in Zr-Nb alloys alter their composition to reduce the Nb content from  85-90 % to ~ 50 %, fine precipitates likely enriched in Nb are formed;

- β-Zr precipitates are subject to irradiation –stimulated decomposition;

- Laves phase precipitates change the composition (the content of Fe decreases) and the crystal structure, HCP to BCC (β-Nb);

- (Zr, Nb)2Fe precipitates having the FCC lattice  retain the composition and crystal structure;

- no amorphization of secondary phase precipitates is observable under the given conditions of irradiation (T = 315 - 350 oC).

Based  on the  dpa  the results were compared pertaining to Zr-alloy IIG deformation vs fluence in various reactors at different energies of fast neutrons. The presented  graphs enable comparison between the results of numerous experiments and prediction of Zr-material behaviour in long-term operation and at high burn-up in commercial reactors.