- Physical Properties and Self-Irradiation Effects in Actinides and Their Alloys

Change in Flow Stress and Ductility of -Phase

Pu-Ga Alloys due to Self-Irradiation Damage

A. Arsenlis, W. G. Wolfer, and A. J. Schwartz

Materials Science and Technology Division, Lawrence Livermore National Laboratory,

P.O. Box 808, L-371, Livermore, CA 94550, USA (arsenlis@llnl.gov)

An internal state variable model for the mechanical behavior of aged Pu-Ga alloys is developed and used to predict the change of the material with accumulated self-irradiation damage or age.  The material model incorporates microstructural data such as the primary irradiation-induced defect density from cascades, the density and average size of helium bubbles, the initial dislocation density, and the initial average segment length of the dislocation density as input parameters, and then evaluates the stress-strain response of a representative volume element of the material.  Given this response at a single material point, the deformation behavior of tensile specimens is predicted, and it forecasts increased strength, decreased strain hardening, and more strain localization with aging.  Although the material point behavior showed some slight strain softening, this strain softening is expected to be masked by statistical variations of different volume elements and by the strain rate sensitivity of the material.  Hence, it is not expected to appear in the stress-strain response of macroscopic tensile specimens, and only the increase in flow stress will be measured.

This work was performed under the auspices of the U.S. Department of Energy by University of California Lawrence Livermore National Laboratory under contract No. W 7405-Eng-48.

Magnetic Properties of Radiation Damage in Pu

M. J. Fluss, S. McCall, B. W. Chung, M. McElfresh, D. Jackson, and G. Chapline

Lawrence Livermore National Laboratory, Livermore, California 94550, USA

Plutonium’s unusual position in the actinide series places it directly between the light actinides with f-electron delocalization, and the heavy actinides with f-electron localization.  Point- and extended-defects are expected to, and do exhibit extraordinary properties as a consequence of the unusual nature of plutonium’s electronic structure.  Recently, we observed and reported1 that vacancies and vacancy clusters in Pu( 3.3 at% Ga) fcc delta-phase behave in an anomalous manner with respect to their specific resistance.  The vacancy defect resistance was seen to follow a –ln(T) behavior from 250 to 10K, suggesting the possibility of local moments with a low critical temperature.  Unfortunately no magnetic studies were possible at the time.

Here we report in alpha-Pu, a preliminary study of our discovery of the magnetic susceptibility from radiation damage, as a function of time and temperature.  First, using isochronal annealing, we observed annealing stages associated with the accumulated damage, in the form of an excess magnetic susceptibility.  The first annealing stage begins above 30K, meaning that below that temperature the displacement damage from self-irradiation of the Pu alpha particle emission and the U recoil are 'frozen' in.  These results are comparable and similar to resistivity data on alpha-Pu taken almost 40 years ago by Wigley.2  A detailed study was made of this excess magnetic susceptibility below the first annealing stage of alpha-Pu as a function of time (<45d) and temperature (<30K), at a field of 2 Tesla.  It revealed, at early times, a Curie-Weiss behavior with a small negative Weiss temperature that evolves into a power-law behavior with increasing time.  Additionally, we will report annealing experiments that appear to differentiate between the magnetic properties of interstitials and vacancies in alpha-Pu.

We will discuss all these results in terms of the complex nature of plutonium’s electronic structure and discuss the notion that the properties of local disorder may provide information about the organizing principles of plutonium itself.

This work was performed under the auspices of the U. S. DOE by Lawrence Livermore National Laboratory, under contract W-7405-Eng-48.

References

- M. J. Fluss et. al, Journal of Alloys and Compounds 368 (2004) 62–74

- D. A. Wigley, Proc. R. Soc. A 284 (1964) 344

Nonmagnetic State of δ and α Phases of Plutonium

M. A. Korotin*, A. O. Shorikov*, A. V. Lukoyanov** and V. I. Anisimov*
*Institute of Metal Physics, Ekaterinburg, Russia (mkorotin@optics.imp.uran.ru)
**Ural State Technical University-UPI, Ekaterinburg, Russia

Magnetic state and electronic structure of Pu in δ and α phases have been investigated with the use of calculation method LDA+U [1] with spin-orbit coupling considered in the matrix form (LDA+U+SO). The value of Hund exchange interaction parameter JH = 0.48 eV for 5f shell was calculated by constrain LDA method. For this value of JH and value of Coulomb interaction parameter U = 2.5 eV, the calculated equilibrium volume of Pu in δ phase coincides with the experimental one. For plutonium in both phases a nonmagnetic ground state was found with Pu ions in f 6 configuration with zero values of spin S, orbital L and total J moments. Thus, a pure jj coupling scheme was found to be valid for metallic Pu. Recently published experimental data support the calculated results — the absence of magnetic moments in metallic plutonium [2].

The Fermi level is on the low-energy slope of a pseudogap between the fully occupied f 5/2 and empty f 7/2 subbands. Even without taking into account of correlations (the LDA+SO approach), the pseudogap is preformed by spin-orbit splitting.

A small increase (less than 10 %) of exchange interaction parameter for Pu in δ phase would result in magnetic ground state, whereas for Pu in α phase the nonmagnetic state is more stable (corresponding increase is about 17 %).

For Pu compounds investigated in the present work, predominantly f 6 configuration with nonzero magnetic moments was found in PuCoGa5, PuSi2 and PuTe, while PuN, PuRh2 and PuSb have f 5 configuration with sizeable magnetic moment values. In contrast to metallic plutonium, an intermediate coupling scheme is needed to describe 5f shell in Pu compounds.

A nonmagnetic state of metallic Pu obtained in the present theoretical investigation is a consequence of correct consideration within the LDA+U+SO scheme of a delicate balance between competing spin-orbit coupling and exchange interaction. Our results show that both aforementioned interaction terms in the Hamiltonian must be treated in a general matrix form for Pu and its compounds.

## References

- Anisimov V. I., Aryasetiawan F., and Lichtenstein A. I., J. Phys.: Condens. Matter 9, 767 (1997).

- Lashley J. C., Lawson A. C., McQueeney R. J., and Lander G. H., preprint cond-mat/0410634.

Solubility of Actinide / Lanthanide Trifluorides in Molten Mixtures

of LiF, BeF2 and NaF

##### M. Vologin, V. Menchenin, A. Panov,  V.  Subbotin

RFNC – All-Russia RI of Technical Physics, Snezhinsk, Russia (bkv@vniitf.ru)

The main objective of our activity is to obtain the key physical & chemical properties information necessary for the design of MOSART system. MOSART concept represents single fluid design fuelled only by TRU trifluorides without UF4 or ThF4 support. Due to the solubility limit, main concern for MOSART concept is to be expected with TRU and rare earths dissolved as trifluorides. In MOSART study main emphasis is placed on new Na,Li,Be/F salt composition with decreased BeF2 and LiF content.

The solubility of PuF3 in molten 2LiF-BeF2, 58NaF-15LiF-27BeF2 and 58NaF-17LiF-25BeF2 mixtures was determined over the temperature range of 525 – 675 oC. In our experiments method of isothermal saturation in molten phase with permanent measurement of PuF3 distribution in system by -spectrometry was used. Note, that time at temperature before sampling (needed to reach equilibrium in the system) in our studies changed from 20 to 32 hours with temperature increase from 550 to 675 oC.

Our experimental data on solubility of PuF3 for molten 2LiF-BeF2 salt system are in good agreement with previous ORNL data. For considered NaF-LiF-BeF2 - containing systems, decrease of BeF2 from 34 mole % down to 25 mole % provide about 5 times increase of PuF3 solubility.

The results are expressed as a function of temperature. For molten 58NaF-15LiF-27BeF2 and 58NaF-17LiF-25BeF2 mixtures (in mole %), the following solubility of PuF3 was obtained in our study: 1.33 and 1.94 mole % at 550 oC and 1.94 and 3.00 mole % at 600 oC. The results of measurements on actinide plus lanthanide trifluorides (difluorides) solubility in Na,Li,Be/F system are also summarized in this paper. The measured solubility of PuF3 truly satisfy the requirements for Na,Li,Be/F MOSART concept.

Experiments were carried out with ISTC support (Project #1606).

Structural Features of Non-Doped Uranium after Shock-Wave Loading, Comparison of Light and Transmission Electron Microscopy

Yu.. N. Zouev*, E. A. Kozlov*, I. V. Podgornova*, V. V. Sagaradze** 
 *RFNC – All-Russia Research Centre of Technical Physics, Snezhinsk, Russia (dep5@vniitf.ru)

**IMP UB RAS, Ekaterinburg, Russia

Structure of Uranium Samples after Shock Wave Treatment

Yu. N. Zouev*, V. V. Sagaradze**, N. V. Podgornova*, N. L. Pecherkina**, M. L. Mukhin**,

S. A. Lekomtsev*, A. V. Petrovtsev*, E. A. Kozlov*

*RFNC – All-Russia Research Institute of Technical Physics, Snezhinsk, Russia

**Institute of Metal Physics, Ural B RAS, Ekaterinburg, Russia (vsagaradze@imp.uran.ru)

Foils, which were prepared from preserved flat samples of uranium exposed to explosion loading with different intensities, were examined in an electron microscope. The material had a deformation banded structure, which comprised alternating twins, intertwin matrix regions and dislocations. It is known that twinning planes in uranium may be {172}, {130}, {112}, {121}, and {176} planes. The calculations, which were made using the arrangement of the main network of reflections in the electron diffraction pattern, showed that the foil plane was the (100) plane of -uranium with the parameters a = 2.836, b = 5.867 and c = 4.936 Å. The twin trace coincided with the [014] direction, a fact which pointed to the (172) or (121) twinning plane. Grains had serrate boundaries. The denticles on some boundaries were as high as 20-30 m. Uranium carbides up to 2-3 m in size were observed. Pores, which sometimes joined to cracks, were formed after the explosion.

Structures of the samples 1 and 2, which experienced a smaller and larger explosion load respectively, differed little. Long crystals of the twin orientation in the sample 1 were 0.05-0.25 m wide. The dislocation structure was chaotic and corresponded to a cold deformation structure. The number of twins increased in the lower part of the sample 1 and they often crossed one another. A dislocation structure, which corresponded to a higher heating temperature and a more intensive load than those used for the sample 1, was observed in twins and the neighboring matrix regions in the sample 2. Dislocation pileups with a cellular structure inside (cells ~25 nm in size) were formed at band boundaries. Also, subgrains with boundary dislocation walls and networks were observed. The selected-area diffraction pattern of this structure in the region of a twin or matrix band was similar to the pattern of a single crystal. This observation pointed to the absence of recrystallization and polygonization processes in the sample exposed to a larger load. The absence of recrystallization suggested that the heating temperature of the explosion-loaded sample 2 was not over 300-350 C. The density of dislocations in the foil ~70 nm thick was (cm2) 71018 to 1.11011 for the sample 1 and 3.31010 to 11011 for the sample 2. The density of dislocations in the wall at the subgrain boundary was 3.71011 cm2.

This study was supported financially by All-Russian Research Institute of Technical Physics,  (Agreement No. 7/04), Russian Foundation for Fundamental Research (Project No. 04-02-16053) and the Program for support of scientific schools (Project NSh-639.2003.2).

Characterization of Aging Phenomena in Pu-Alloys

Adam J. Schwartz

Chemistry and Materials Science Directorate

Lawrence Livermore National Laboratory

Livermore, CA 94550, USA (schwartz6@llnl.gov)

The time-dependence of the properties of aging plutonium has been the focus of investigation for the past five years.  The origin of these aging phenomena is the α-decay process, which produces a 5 MeV α particle and an 85 keV uranium recoil.  The U recoil produces significant short-term lattice damage that may lead to volume swelling and the potential for void swelling.  The α particle loses energy to electronic excitations before coming to rest as a helium atom.  Our first-principles modeling indicates that Pu should be highly resistant to void swelling and in situ dilatometry experiments are underway to evaluate the time dependent behavior of old material.  Transmission electron microscopy characterization of new and old material reveals the presence of helium bubbles in line with predictions using rate equations.

An experimental and modeling effort is underway to evaluate the effects of radioactive decay on the equation of state.  Two independent methods have been applied to predict the effects of helium on the equation of state: first principles and classical.  Both methods predict insignificant changes in the equation of state over time frames of interest.  We have also conducted diamond anvil cell experiments to compare the compressibility of new and old material.  The preliminary experiments indicate insignificant changes as a function of age.

This work was performed under the auspices of the U.S. Department of Energy by the University of California, Lawrence Livermore National Laboratory under contract No. W-7405-Eng-48.

Investigating the δ/α' Phase Transformation in Pu-Ga Alloys

K. J. M. Blobaum, C. R. Krenn, M. A. Wall, and A. J. Schwartz

Chemistry and Materials Science Directorate

Lawrence Livermore National Laboratory

Livermore, CA 94550, USA

(schwartz6@llnl.gov)

The δ to α' phase transformation in Pu-Ga alloys is intriguing for both scientific and technological reasons.  On cooling, the ductile FCC δ-phase transforms martensitically to the brittle monoclinic α'-phase at ~160 K (depending on composition).  This exothermic transformation involves a 20 % volume contraction and a significant increase in resistivity.

Complete transformation to the α' phase is not observed; typically a maximum of 30 % is formed. Furthermore, time-temperature-transformation diagrams found in the literature indicate that the kinetics of this transformation involve “double-C-curve” behavior, and the two maximum rates of transformation are a function of composition.  The reversion of α' to δ involves a large temperature hysteresis; reversion begins at ~310 K.  In an attempt to better understand the underlying thermodynamics and kinetics responsible for these unusual features, we examined  the  α'/δ  transformations  in  a  0.6 wt% Pu-Ga  alloy  using  optical  microscopy, transmission electron microscopy, resistometry, and differential scanning calorimetry as shown in Figs 1-4.

At this composition, the martensite start temperature is ~154 K and the austenite start temperature is ~310 K.  Differential scanning calorimetry shows evidence of α' formation and reversion to δ. The feature corresponding to the reversion contains a series of “oscillations” which  are  the  subject  of  much  investigation.   These  “oscillations”  are  periodic,  and  their periodicity with respect to temperature does not vary with heating rate.  Thermal cycling of a single sample shows highly reproducible transformation and reversion behavior, provided that the sample is alloyed to “rest” at room temperature after a high temperature anneal. Possible reasons for these observations will be discussed.  Elucidating the thermodynamics and kinetics of the δ/α' phase transformation are important for understanding how Pu-Ga alloys can change over time and under a variety of thermal conditions.

This work was performed under the auspices of the U.S. Department of Energy by the University of California, Lawrence Livermore National Laboratory under Contract No. W–7405–Eng-48.

The Effect of Self-Irradiation on Diffusion Process Enhancement in Actinides

E. A. Smirnov.

Moscow Engineering Physics Institute, 115409 Moscow, Kashirskoe sh., 31 (smirnov@phm.mephi.ru)

In view of the need for predicting the effect of self-irradiation on diffusion processes enhancement in actinides, analysis of the possibility of radiation-enhanced diffusion (RED) on an example of Pu -phase was carried out with the known rate of radiation defects generation total for all isotopes of Pu, K0=0,1056 dpa/yr, as per Ref. [1].

In evaluation of the characteristics of RED in -Pu under natural self-irradiation, an earlier suggested method [2] was used, which consisted in use of acceleration coefficient R evaluated on the basis of the RED experimental data. For the estimates proposed in the present work, coefficient R was determined by processing the statistical data on the effect of -radiation on diffusion in Ag, Au, Ni and Pb. With account for the obtained weak correlation of R on K0, the temperature dependence of R under self-irradiation with -particles takes the form (for Tплα−Pu=567 K):

RREDα−Pu=(4.12−2.29+5.14)⋅10−13exp[(14.30±0.41)⋅Tплα−PuT]

The temperature dependence DRED in -Pu calculated with the use of this expression has the form: DRED=(1.12−0,67+1.84)⋅10−16exp[−0.175±0.024eVk⋅T], сm2/s, the evaluated value Evm=0.35±0.05 eV is in agreement with the earlier obtained values [3]. Using the methods taking into account the retardation effect of the RED admixture and the grain boundaries, the

respective approximate estimates are given [3-5].

#### References

- W. Wolfer. Radiation Damage in Pu, CMS Workshop, LANL, 1998

- E. A. Smirnov, A. A. Shmakov. Defect and Diffusion Forum, 2001, v.194-199, p.1451

- E. A. Smirnov. Transact. of Internat. Seminar “Basic Properties of Plutonium, Sarov, 2004, p. 86

- E. A. Smirnov, A. A. Shmakov. Transact. of Fifth Internat. Ural Seminar “Radiation Damage Physics of Metals and Alloys”. Snezhinsk, 2003, p. 63

- E. E. Smirnov. Transact. Of Russian Scientific Conf. MAYAT-TEMEK, Agoi, 2003, p. 95

### An Atomistic View of Radiation Damage in Plutonium Metal and Alloys

S. M. Valone*, M. I. Baskes*, M. Stan*, and B. P. Uberuaga*
*Los Alamos National Laboratory, Los Alamos, New Mexico, USA (smv@lanl.gov)

Using basic thermodynamic and mechanical properties of plutonium (Pu) metal and its gallium (Ga)-stabilized alloys, an atomistic model is generated from the Modified Embedded Atom Method (MEAM) of Baskes.  The essential features of MEAM are that it uses a “universal binding energy relation” (UBER) to calibrate the energetics of the model, includes angular dependencies in the background density function, and uses an analytic, information-theoretic form (“x ln x”) for the embedding energy.  The angular-dependence of the background density permits crystal of different symmetries, but the same number of nearest neighbors (e. g. FCC vs HCP), to have different energies.  It is this feature that permits MEAM to achieve correct phase ordering in crystalline materials using just first nearest neighbor interactions.

In MEAM, each type of pairwise interaction must possess its own parameter set.  Thus one set of parameters is needed for each combination:  Pu-Pu, Ga-Ga, and Pu-Ga.  In all three cases, a cubic structure is used as the basis for the UBER.  For Pu and Ga, the FCC structure is used, while for Pu-Ga, the L12 structure, without tetragonal distortions, is used.  The cohesive energy, bulk modulus, and atomic volume are the main properties needed to determine the UBER.  For Pu-Pu and Ga-Ga, the pressure derivative of the bulk modulus is also included, resulting in a higher-order UBER.

The background density parameters are determined from other sources of information.  The primary sources are the shear modulus for Ga-stabilized δ-Pu, the atomic volume of α-Pu, and the formation energy between the α and δ phases of Pu metal.

Once these interactions are determined, a phase diagram for the complete Pu-Ga composition range is calculated without any further modification to the parameters.  The free energy of a candidate phase is calculated using the Einstein oscillator as an ideal reference.

Most of the “f-electron” physics and how Ga effects the f electrons are contained in the background density, and in particular the symmetry properties of the background density.  The model mimics Ga stabilization through the mixing of the Ga and Pu background density parameters.  The most critical aspect of the mixing elements concerns how the presence or absence of inversion symmetry in the lattice affects the energy of a particular phase.  By controlling sensitivity of the model to the loss of inversion symmetry, we can control the stability of the FCC structure relative to the monoclinic structure.  In pure Pu metal at 0 K, the lack of inversion symmetry in the monoclinic structure makes it energetically more favorable.  The addition of Ga reduces the relative stability of monoclinic over FCC structures and introduces a barrier to the reversion of Ga-stabilized δ -Pu to α -Pu.

Radiation damage and defects in plutonium (Pu) metal and its gallium (Ga)-stabilized alloys are modeled at an atomistic level using the Modified Embedded Atom Method (MEAM).  For radiation damage modeling, we are concerned with the minimum displacement threshold energy in different crystallographic directions of FCC Pu, the damage production as a function of primary knock-on atom (PKA) energy, and the migration rates and energies of formation of small vacancy and interstitial clusters.  We attempt to relate radiation damage properties to properties of the Pu-Ga phase diagram.  The minimum displacement threshold is determined as a function of Ga concentration.  In an earlier model of Pu metal, that threshold was no greater than 10 eV, which might be compared to 14 eV in lead (Pb).  The migration rates of mono-vacancies and di-vacancies are estimated from accelerated molecular dynamics simulations.  The acceleration technique that was used for Pu is called Parallel Replica Dynamics.  This method takes advantage to the special nature of first-order rate processes.  Multiple processors (CPUs) perform a dynamical simulation of a migration event on copies of the same cell of atoms assigned to different processors.  The migration time is estimated from the cumulative time in all of the processors rather than from the simulation time on a single processor.  The geometry and migration rates of an interstitial defect are also estimated from traditional molecular dynamics simulations.

The behavior of small helium (He) filled cavities in pure Pu metal is explored with respect to the effects of cavity size, He-Pu vacancy ratio, low hydrostatic compress (< 15 kbar), bubble density, and temperature (300 – 500 K).  In the cavity size range from the 1 – 10 Å diameter, He over-pressure is adsorbed through interstitial emission.  This relaxation mechanism results in local strain fields.  Varying the He-Pu vacancy ratio between 2:1 and 6:1 constructed from monovacancies does not cause a change in this mechanism.  When 2-Å bubbles at a 2:1 He-Pu ratio are compressed by 15 vol.%, long-range strain fields become apparent.  The equivalent simulation for a cell with no He bubble shows no strain fields.  When the bubble density is increased from 6 × 10+17/cm3 to 3 · 10+19/cm3 with 2-Å diameter bubbles, the strain fields become sufficiently close to provide a transformation pathway between δ -Pu and α-Pu.  10-Å diameter bubbles at 300 K increase the stability of the FCC lattice.  The increased stability is such that these simulations can be performed at constant pressure boundary conditions, where as the radiation damage studies on pure Pu metal are conducted at constant volume.  The presence of the bubble provides a pressurized free surface that can alleviate the tension in the pure metal lattice that otherwise would lead to a collapse to α -Pu.  Finally, when a 10-Å diameter bubble is heated to 500 K, the strain fields almost completely disappear, resulting in a nearly pristine FCC structure.  These results are consistent with (1) the 500 K temperature being above the stage V annealing temperature, and (2) the increased stability of the FCC phase at higher temperatures.

References

- M. I. Baskes, Phys. Rev. B 46, 2727 (1992).

- M. I. Baskes, Mater. Sci. Eng., A 261, 165 (1999).

- M. I. Baskes, Phys. Rev. B 62, 15532 (2000).

- M. I. Baskes, S. P. Chen, and F. J. Cherne, Phys. Rev. B 66, 104 (2002).

- M. I. Baskes, K. Muralidharan, M. Stan, S. M. Valone, and F. J. Cherne, J. Metals 55, 41 (2003).

- S. M. Valone, M. I. Baskes, M. Stan, T. E. Mitchell, A. C. Lawson, and K. E. Sickafus, J. Nucl. Mater. 324, 41 (2003).

- B. P. Uberuaga, S. M. Valone, and M. I. Baskes, preprint, LA-UR-04-6201.

Spin Susceptibility of Ga-Stabilized δ-Pu Probed by 69,71Ga NMR

S. Verkhovskii*, Yu. Piskunov*, K. Mikhalev*, V. Arkhipov*, Yu. Zouev**, I. Svyatov**, S. Lekomtsev**,  A. Gerashenko, A. Pogudin, V. Ogloblichev, A. Tankeyev

* Institute  of Metal Physics, Ural Branch of RAS, Ekaterinburg, Russia (verkhovskii@imp.uran.ru) **RFNC – Research Institute of Technical Physics, Snezhinsk, Russia

The rich phase diagram of plutonium [1] presents six polymorphous transitions. The unique structural, transport and magnetic properties are determined by the degree of itinerancy for 5f-electrons in each of the Pu allotropes. Many efforts are undertaken at present to elucidate the ground state of the f-electron system in δ-Pu and in stabilized δ phase Pu-Ga, Pu-Al alloys.

Spin susceptibility of stabilized δ phase in the Pu-Ga alloy with nominal Ga concentration of 1.5 wt% was studied by measuring 69,71Ga NMR spectra and nuclear spin-lattice relaxation rate (69Т1-1) in the temperature range 5-350 K [2]. The shift (69K) of the 69,71Ga NMR central transition line (-1/2 ↔ +1/2) and 69Т1-1 are controlled correspondingly by the static and time-fluctuating parts of local magnetic field arisen at nonmagnetic gallium due to transferred hyperfine coupling with the nearest f-electron environment of more magnetic Pu. The nonmonotonic behavior of 69K(T) ~ χs,5f(T) with a maximum around 150 K is attributed to the temperature dependence peculiarities of the f-electron spin susceptibility χs,5f(T) in δ phase of plutonium. The temperature reversibility being observed in 69K(T) data provides strong evidence for an electronic instability developed with T in f-electron bands near the Fermi energy and accompanied with a pseudogap-like decrease of χs,5f at Т < 150 K. Such kind of instability may be considered as a driving force for martensitic δ-α transformation observed recently in Pu1-xGax (x <  0.04) alloys at low Т < 150 K. Similar decrease of 69K with T was revealed below 100 K in the δ-stabilized Pu0.983Ga0.017 [3]. According to NMR data the 5f-electrons of Pu  demonstrate a mainly localized character in δ phase at high temperature T > 200 K. With temperature decrease the growth of short wave contributions to χs,5f occurs. However, no NMR evidences favoring formation of  a static magnetic order in δ-Pu were revealed at down to 5 K.

References

- S. S. Hecker and L. F. Timofeeva, Los Alamos Sci. 26, 244 (2000).

- Yu. Piskunov et al. cond-mat/0404460, submitted to Phys. Rev. B

- N. J. Curro and L. Morales, Mat. Res. Soc. 802, DD2.4.1 (2004).